Development of JPCP Design Catalog for New York State

Shad Sargand, Jianfeng Qin, and Issam Khoury

for

Engineering and Software Consultants, Inc.

and the

New York Department of Transportation

and the

United States Department of Transportation

Federal Highway Administration

Contract No. DTFH61-05-D-00017

May 2012

| 1. Report No. FHWA/ | 2. Government Accession No. | 3. Recipient’s Catalog No. |
| --- | --- | --- |
| 4. Title and Subtitle Development of JPCP Design Catalog for New York State | 5. Report Date |
|  | 6. Performing Organization Code |
| 7. Author(s) | 8. Performing Organization Report No. |
| 9. Performing Organization Name and Address Ohio Research Institute for Transportation and the Environment (ORITE) 141 Stocker Center Ohio University Athens OH 45701-2979 | 10. Work Unit No. (TRAIS) |
|  | 11. Contract or Grant No. Contract No. DTFH61-05-D-00017 |
| 12. Sponsoring Agency Name and Address Engineering and Software Consultants, Inc. 14123 Robert Paris Court. Chantilly VA 20151 |  |
|  | 13. Type of Report and Period Covered Technical Report |
|  | 14. Sponsoring Agency Code |
| 15. Supplementary Notes Prepared in cooperation with Engineering and Software Consultants, Inc., the New York Department of Transportation (NYDOT), and the U.S. Department of Transportation, Federal Highway Administration |
| 16. Abstract For this project data were collected for calibration and development of a design catalogue for PCC pavements for the State of New York. A literature review was conducted to identify the most important input parameters for the design of PCC pavements used in the MEPDG and Darwin-ME programs. PCC pavement material properties were determined based on laboratory testing of samples collected from three projects on Interstates 86, 90, and 490 in New York. Base material properties were also determined from laboratory testing of samples collected from various test sections in the state including I90. In addition a survey questionnaire was sent to the New York Department of Transportation Region Offices to collect additional material properties and pavement performance data for pavement sections in each region. Traffic, climatic, and subgrade material data were collected and analyzed by Dr. Stefan Romanoschi of the University of Texas, Arlington. These data will also be used to conduct a local calibration of the MEPDG. Pavement performance data from three test sections on Interstates 86, 90 and 490 is also included in this report and will be used to conduct the local calibration and to build a catalog for pavement design in the State of New York. |
| 17. Key Words MEPDG, PCC, base material, performance data, laboratory testing, pavement performance | 18. Distribution Statement No Restrictions. This document is available to the public through the National Technical Information Service, Springfield, Virginia 22161 |
| 19. Security Classif. (of this report) Unclassified | 20. Security Classif. (of this page) Unclassified | 21. No. of Pages 184 | 22. Price |

Development of JPCP Design Catalog for New York State

Prepared in cooperation with

Engineering and Software Consultants, Inc.,

the

New York Department of Transportation,

and the

U.S. Department of Transportation, Federal Highway Administration

Prepared by

Shad Sargand, Jianfeng Qin, and Issam Khoury

Ohio Research Institute for Transportation and the Environment

Russ College of Engineering and Technology

Ohio University

Athens, Ohio 45701-2979

The contents of this report reflect the views of the authors who are responsible for the facts and the accuracy of the data presented herein. The contents do not necessarily reflect the official views or policies of the Ohio Department of Transportation or the Federal Highway Administration. This report does not constitute a standard, specification or regulation.

Final Report

May 2012

Table of Contents

Background	1

Problem Statement	2

Objectives	2

Literature Review	3

PCC durability and performance	3

PCC strength and stiffness and mechanistic properties	5

PCC temperature gradients and deformations; temperature dependence of modulus	5

PCC Coefficient of Thermal Expansion	6

Performance of Base materials	8

Resilient modulus of base materials	8

MEPDG based pavement design catalog for states and local calibration	9

Survey of Pavement Design Practice in NYDOT Regional Offices	10

Available MEPDG Models	10

Distress Prediction Equations for Rigid Pavements and PCC Overlays	13

Mean Joint Faulting and Joint Load Transfer Efficiency	13

Transverse Slab Cracking	15

Smoothness	16

Data from New York JPCP experimental pavements	18

Coefficient of thermal expansion of PCC	18

Summary of test methods used for unbound materials and soils	19

Sieve Analysis	19

Proctor Compaction Test	20

Resilient Modulus and Permanent Deformation Test	22

Resilient Modulus Parameters	24

Permanent Deformation Parameters	25

Performance Data from I490 Victor	26

Project Location and Background	26

Initial Falling Weight Deflectometer Test Results	30

October 2006 FWD testing results	38

September 2007 testing results	40

September 2008 testing results	40

August 2009 testing results	44

June 2011 testing results	47

Summary of FWD results	47

Performance Data from I86 Hinsdale	51

Project Overview and Description	51

Compressive & Flexural Strength Results	52

FWD Testing Results	53

FWD Deflections, Load Transfer Efficiency, Joint Support Ratio and Spreadability	53

Forensic Investigations	59

Performance Data from I90 Weedsport	60

Project Overview and Description	60

Properties of Materials	61

Field Forensic Observations	65

Falling Weight Deflectometer Testing	66

Review of MEPDG Data Requirements	69

Calibration of MEPDG Software for New York	70

Development of JPCP Design Catalog	70

References	71

Bibliography	76

Appendix A:   Survey form sent to NYDOT regions	81

Appendix B:  Resilient Modulus Results	87

Appendix C:  Permanent Deformation Test Results	91

Appendix D:  FWD Data from I490 October 11-12, 2006	95

Appendix E:  FWD Data from I490 September 24-25, 2008	110

Appendix F:  FWD data from I490 East, August 19, 2009.	123

Appendix G:  I490 Eastbound FWD data collected June 21, 2011	133

Appendix H: Supplemental falling weight testing data from I86 Hinsdale	142

Appendix I:  Supplemental FWD Response Data from I90, Weedsport	167

List of Tables

Table 1.  PCC Performance Predictors	13

Table 2.  Equation parameters used in the MEPDG	14

Table 3.  Variables and Description used for Equation 8 through Equation 11	16

Table 4.  Variable and descriptions used in equations 13 through 16 for IRI measurement.	17

Table 5.  Coefficient of thermal expansion for PCC samples from New York.	19

Table 6.  Test Protocols and Standards for Unbound Materials and Soils.	19

Table 7.  Aggregate gradations (percent passing).	20

Table 8. Optimal Moisture Content and Maximum Dry Density fo New York soils	20

Table 9. Testing Sequences of Resilient Modulus and Permanent Deformation Test.	23

Table 10.  Collected Data Points for Permanent Deformation Test.	24

Table 11.  Material Constants and MR Values Calculated for Stress State, σ1 = 7.4 psi and σ3 = 2 psi.	25

Table 12.  Permanent deformation parameters.	25

Table 13 PCC Mix Design	26

Table 14 I-490 Eastbound Tie Bar Spacing	27

Table 15 I-490 East Cross-Sectional Area of Steel	28

Table 16 I-490 East Dowel Bar Spacing	29

Table 17  Cross-sectional dowel bar areas for the three dowel bar arrangements on I490 East.	30

Table 18  I-490 East 37.4 kN (8.4 kip) FWD, Slabs 1-25, October 26, 2004, from Sargand and Morrison [2007]	31

Table 19  I-490 East 50.3 kN (11.3 kip) FWD, Slabs 1-25, October 26, 2004, from Sargand and Morrison [2007]	32

Table 20  I-490 East 37.4 kN (8.4 kip) FWD, Slabs 26-55, October 26, 2004, from Sargand and Morrison [2007]	33

Table 21  I-490 East 50.3 kN (11.3 kip) FWD, Slabs 26-55, October 26, 2004, from Sargand and Morrison [2007]	34

Table 22 I-490 East 37.4 kN (8.4 kip) FWD, Slabs 56-84, October 26, 2004, from Sargand and Morrison [2007]	36

Table 23 I-490 East 50.3 kN (11.3 kip) FWD, Slabs 56-84, October 26, 2004, from Sargand and Morrison [2007]	37

Table 24.  FWD data averages and standard deviations for I-490 West, Monroe, Rochester on morning and afternoon of Oct. 11, 2006.	38

Table 25.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on October 12, 2006 for different dowel bar configurations.	39

Table 26.  FWD data averages and standard deviations for I-490 West, Monroe, Rochester on September 24, 2008.	41

Table 27.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on September 25, 2008 for different dowel bar configurations.	42

Table 28.  Distress Survey, I 490 Westbound September 2008	43

Table 29.  Distress survey, I490 eastbound September 2008	44

Table 30.  I490W Distress survey, August 2009	44

Table 31.  I490E Distress survey, August 2009	44

Table 32.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on Aug. 19, 2009 for different dowel bar configurations.	46

Table 33.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on June 21, 2011 for different dowel bar configurations.	48

Table 34.  Summary of average approach LTEs by date, with  standard deviation and standard deviation of the mean.	49

Table 35.  Summary of average leave LTEs by date, with  standard deviation and standard deviation of the mean.	50

Table 36.  Mechanical properties of PCC overlay material on I86.	53

Table 37.  Summary 3rd drop FWD data averages and standard deviations for C&S section (1 µm/kN = 0.17526 mil/kip).	58

Table 38.  Summary of 3rd drop FWD data averages and standard deviations for rubblized section (1 µm/kN = 0.17526 mil/kip).	58

Table 39.  Summary of 3rd drop FWD data averages and standard deviations for untreated section (1 µm/kN = 0.17526 mil/kip).	59

Table 40.  Percentage of cracked slabs observed in distress survey of November 2009.	60

Table 41  Subgrade sieve analysis	61

Table 42  Atterberg limits	61

Table 43  CTPB mix design for I90	63

Table 44  CTPB Mechanical Properties for I90	65

Table 45  Concrete Mix Design for I90	65

Table 46  Concrete Test Results for I90	65

Table 47  Summary of FWD results September 29 2009	68

Table 48 Summary of FWD results November 15 2011	68

Table 49.  Input levels required for MEPDG recalibration	70

List of Figures

Figure 1.  MEPDG Flow Chart	12

Figure 2. Measured Aggregate Gradations (25.4 mm = 1 in).	20

Figure 3.  NY15 Type 4 Compaction Curve (1kg/m3 = 0.0624 pcf).	21

Figure 4.  NY I-90 Type 4 Compaction Curve (1kg/m3 = 0.0624 pcf).	21

Figure 5.  NY I-90 Type 3 Compaction Curve (1kg/m3 = 0.0624 pcf).	22

Figure 6.  SR 219 Type 4 Compaction Curve (1kg/m3 = 0.0624 pcf).	22

Figure 7.  Tie Bar Detail (350 mm = 13.8 in, 400 mm = 15.7 in, 700 mm = 27.6 in)	27

Figure 8. Tie Bar Configuration	28

Figure 9. I-490 East Test Sections Overview	29

Figure 10. I-490 East Dowel Bar Arrangement Detail	29

Figure 11.  Corner cracks identified on I490W distress survey, August 2009.	45

Figure 12.  I-86 Project Location near Hinsdale and Cuba. [Google Maps, 2011].	52

Figure 13.  I86 PCC Material Strength: (a) Compressive Strength, (b) Flexural Strength.	52

Figure 14.  Normalized deflection (a) and load transfer efficiency (b) averaged for all sections (1 µm/kN = 0.17526 mil/kip).	56

Figure 15.  Joint support ratio (a) and mid-slab spreadability (b) averaged for all sections.	57

Figure 16.  Hairline cracks at tie-bar locations in the untreated section.	60

Figure 17.  Construction schedule of I-90 thruway rehabilitation (NYSTA) (5.1 mi = 8.2 km, 5.2 mi = 8.4 km, 4.9 mi = 7.9 km).	60

Figure 18.  Grain-size distribution for NYSDOT Type 3 and Type 4 DGAB (1 mm = 39.4 mil; 25.4 mm = 1 in)	62

Figure 19.  Static modulus and Poisson’s ratio test setup for CTPB specimen	63

Figure 20.  Split-cylinder tensile test setup on CTPB sample	64

Figure 21.  Failure of specimen during split-cylinder tensile test	64

Figure 22.  Bonded CTPB and PCC slab in refuse pile at I90 construction site	66

Figure 23.  Average normalized D0 deflections on CTPB and DGAB prior to paving (5.714 µm/kN = 1 mil/kip)	67

# Background

Pavement design concepts and practices change as technologies advance.  The new Mechanistic-Empirical Pavement Design Guide (MEPDG) reflects the current consensus on pavement design, as developed and released under NCHRP Projects 1-37A and 1-40D.   The MEPDG includes methods for analyzing and designing most types of new and rehabilitated flexible, rigid, and composite pavements.  It emphasizes the use of sound principles of engineering mechanics as well as existing models and databases.  With the high percentage of pavement projects in the US that involve the rehabilitation of existing pavements, the MEPDG specifically emphasizes rehabilitation design.

The MEPDG is accompanied by a Windows software package used to expedite the determination of suitable prescribed alternatives. The consistency between the rigid and flexible pavement modules allows for the same inputs and interfaces, whenever possible, giving the user the ability to examine either rigid or flexible pavement alternatives. The software is easily interfaced with any open database connectivity (ODBC)-compliant database. There are provisions to enable the use of other advanced database management systems.

The MEPDG performance was calibrated based on Long Term Pavement Performance (LTPP) database field pavement performance data.  The LTPP database compiles measurements from thousands of flexible and rigid pavement projects nationwide, including data on design, material properties, climate, traffic, and performance data from.  Despite its nationwide orientation, the LTPP does not include extensive results from all states; some states did not participate, and others submitted data for only limited sites.  The LTPP database does not yet include all materials used in highway construction.  Also, when the MEPDG software was previously used to predict performance of pavements on local projects, the results did not correlate well with actual performance data.  This shows the importance of local calibration.

The state of New York is very large and contains a great variety of climates, locally accessible materials, and traffic conditions.  This diversity of conditions has led to a diversity of pavement designs, which the MEPDG may not accurately model, and which makes implementation of the MEPDG in New York state a challenge.

In addition, the existing MEPDG documentation is quite complex and oriented toward the advanced user.  The documentation will need to be remade into a form usable by NYSDOT Region Office engineering personnel using the state calibration.  Software orientation and/or training of pavement designers may also be required.

LTPP jointed plain concrete pavement (JPCP) performance indicators relevant to MEPDG models include:

- Mean transverse joint faulting

- Transverse slab cracking under load

- Smoothness or IRI

# Problem Statement

The New York State Department of Transportation (NYSDOT) wants to implement the MEPDG within the state.   NYSDOT has been constructing JPCP experimental sections as part of the work conducted for the Pooled Fund Study TPF-5(121), “Monitoring and Modeling of Pavement response and Performance”.  The pavements were instrumented, their materials tested, and their performance monitored. Traffic and climate monitoring devices were also installed.   Data from the project as well as other LTPP data pertinent to New York can be used to calibrate the MEPDG software to conditions in the state.

Additional data can be found in various sources, including the report entitled Seasonal Variations of In Situ Materials Properties in New York State [Orr and Irwin, 2006].  Additionally, there is a need for a new set of design charts and an update to the New York State DOT Comprehensive Pavement Design Manual (CPDM).

# Objectives

The objectives of this task order are:

- Evaluate various aspects of the MEPDG in relation to New York State’s current practice and past pavement performance

- Provide recommended input parameters appropriate to New York

- Develop the database for JPCP data that will include all parameters used in MEPDG

- Develop/automate a pavement design procedure for JPCP based on the MEPDG that fits New York’s environment, materials, construction practices, soils and maintenance needs.

To meet these objectives, the project work was divided into the following tasks:

- Task 1. Collect and review relevant literature, current practices, and other information relative to adopting/calibrating MEPDG to local conditions.

- Task 2. Survey of the Pavement Design Practice in the Regional Offices – In this task, a questionnaire will be sent to the 11 regional offices.

- Task 3. Identify, discuss, and evaluate the performance models currently available in the MEPDG for estimating faulting, fatigue cracking and IRI.

- Task 4. Collect available data for NYSDOT JPCP experimental pavements and develop a database.  These data include traffic data, climate data, response data, design features, and material properties.  For sections where required material data are not available, obtain materials and conduct laboratory testing.

- Task 5. Review MEPDG data requirements and determine availability of all data required in addition to those compiled in Task 3.

- Task 6. Calibrate MEPDG design guide software for those regions in New York where sufficient data are available.

- Task 7. Develop the JPCP catalogs with a step by step Pavement Design Procedure.  Update standards sheets for rural and urban JPCP.

- Task 8. Prepare a final report summarizing results from each task and documenting the research effort.

# Literature Review

For literature published up through 2007, see (1), which contains a review of MEPDG references conducted for the state of Ohio.  This review focuses on more recent publications relevant to PCC pavement, aggregate base materials, and modeling and local calibration of MEPDG software for PCC pavement systems, and includes a few articles cited in (1).

## PCC durability and performance

Schwartz, et al (2), in a paper entitled “Effect of concrete strength and stiffness characterization on predictions of mechanistic-empirical performance for rigid pavements”, includes a comparison of results predicted using Level 1, 2, and 3 models and a sensitivity analysis and examined eight PCC mixes in a variety of design scenarios.  As for the output parameters, transverse cracking, was extremely sensitive to input parameters (strength and stiffness), while international roughness index (IRI) was moderately sensitive, and faulting was not sensitive.  It was also determined that 28-day modulus of rupture and 28-day modulus of elasticity values were the most important parameters.

Won (3) examined continuously reinforced concrete pavement (CRCP) for the Texas DOT to create a database for MPDG use, based on data collected from 27 sections, each 300 m (1000 ft) long, from throughout the state.  A falling weight deflectometer (FWD) was used to collect load transfer efficiency (LTE) data at small, medium, and large cracks during summer and winter. Crack spacings and slab deflections were also measured.  LTEs were consistently higher than 90%.  Primary distresses were caused by imperfections in design details or problems with construction or material quality.  The major cause of distress is horizontal cracking apparently resulting from the interactions between longitudinal steel and concrete in response to wheel loads.  A mechanistic-empirical design procedure for CRCP was developed and will probably require further refinement of the transfer function.

Elfino et al (4), also looked at CRCP, this time on I-64 Battlefield Blvd in Chesapeake, Virginia Virginia.  At this site, a full set of Level 1 MEPDG data was collected.  MEPDG software was used to compare predicted performance using Level 1 and Level 3 inputs, assuming the original design thickness, as determined using the original design following the 1993 AASHTO Design Guide.

Schram and Abdelrahman (5) examined how to correlate data in Nebraska’s existing pavement management system (PMS), which is based on an index derived from visual distress surveys, with the distresses used in the MEPDG.  The authors intended the Nebraska approach as a model for other locales.  The MEPDG analysis can be expanded to include fund allocation, estimations of need, remaining service life, etc.  Also, failure criteria can be selected and made more meaningful to local designers.  Detailed guidance for local calibration is also presented.

Chatti et al (6) examined “The effect of different axle configurations on the fatigue life of plain cement concrete” pavement.   In Michigan, the state is experimenting with various heavy truck axle configurations, with up to 11 axles per vehicle and 8 axles in one axle group.  There is a considerable need to determine whether these novel axle configurations have an effect on pavement life.  In this experiment, cyclic four-point beam tests were conducted with load pulses equivalent to the passing of an axle group, with S-N curves generated to determine the expected fatigue life.  In general, an increased number of axles within an axle group at the same stress ratio caused increased damage, though the damage per axle for multiple axles is less than for a single axle.  Also, the axle factors for multiple axles tend to increase as the stress ratio decreases.

Snyder (7) discussed how Mn/ROAD results from 1992 to 2007 were used to improve low-volume concrete pavement design. Since construction in 1993, the five original low-volume road test sections have each been subjected to over 300,000 80 kN (18 kip) equivalent single-axle loads (ESALs).  The design differences between the sections include slab length, joint design, base design, and drainage.  Current distress summaries, maintenance records, deflection data, and ride histories were examined.  Performance life was projected based on IRI data and compared with projections from common design procedures; on this basis, the effectiveness of the design procedures are evaluated.  The MEPDG provided the best match to the IRI observations, but predicted performance was still about 23% short.

McCracken et al (8) compared different sets or levels of input into the MEPDG on predicted performance of a jointed plain concrete pavement (JPCP).  First the 1993 AASHTO Design Guide was compared to the MEPDG, and considerably different design thicknesses were computed.  Then different levels of design inputs were selected for different parameters of the pavement.  The study indicated that different input levels can change the design thickness for a given pavement by up to 51 mm (2 inches).

Ker, et al (9) examined the prediction of transverse cracking of jointed concrete pavements using data gleaned from the Long-Term Pavement Performance database.  The accuracy of prediction models used with the MEPDG were found to be inadequate.  In part, the assumption of the normal distribution of random errors and constant variance may not be warranted.  Thus more modern regression techniques, such as generalized linear regression and generalized additive model were adopted along with the assumption of a Possion distribution.  The agreement of the MEPDG with these new predictive models was improved, but further investigation is warranted.

Haider and Harichandran (10) correlated rigid pavement performance with axle load distribution.  The MEPDG uses axle load spectra customized to a particular site, which are typically a bimodal shape that can be modeled as a mixture of two continuous distributions in a closed-form solution, with the details depending on local data.  Observed axle load spectra from eleven sites in several states were used to correlate the load distributions to the predicted rigid pavement performance.  Cracking was found to be a function of the 85th percentile load, faulting strongly related to the mean load, and IRI with the 4th moment of the axle load spectrum.  Heavier loads thus appear to be the predominant cause of cracking and IRI deterioration, while faulting depends on the average load.

Hiller (11) looked at the sensitivity of predicted performance measures and fatigue failure mechanisms on input parameters, including joint spacing, shoulder type, traffic level, climate, and built-in curl.  Wider lanes were found to have different predicted failure mechanisms depending on the assumptions of the method employed.  It was also found that the design thickness was minimized with a built-in curling level of about -6°C (-11°F).

Sargand, Figueroa, and Romanello (12) used MEPDG v. 0.992 to analyze a long-lived JPCP pavement and a perpetual AC pavement built on the US Route 30 bypass of Wooster, Ohio, known as the WAY-30 project.  The analysis was conducted using Level 3 inputs and the extra thick/durable design being tested on that pavement.  For the AC pavement, most measures of deterioration were very low at the 20 year mark, with IRI and total rutting at about half the failure criterion.  For the PCC pavement, the percentage of cracked slabs was negligible after 20 years, while faulting just met the failure criterion of 0.12 in (3.0 mm), minimum LTE declined to 80% at 8 years and leveled out at around 55% at 15 years, while IRI approached 80% of the design limit.

In a subsequent project report, Sargand and Figueroa (13) revisited the WAY-30 simulation, this time using MEPDG v. 1.100 software and with site-specific material properties from Sargand et al (14).  The AC results were generally comparable to the earlier simulation and confirmed the perpetual pavement’s designed longevity.  The PCC simulation showed much improved performance of the pavement, with faulting remaining well under 10% of the design criterion at the 20 year mark, and with IRI rising from 37% of the design limit to 46%, remaining well below the design limit. The minimum LTE was 93.7% after 20 years.  The percentage of cracked slabs increased from a negligible amount to 1.2%, which was still well below design limit of 15%.

Khanum et al. (15) in 2006 used the MEPDG to predicted performance of typical Kansas JPCP and determined the effect on the current Kansas Department of Transportation (KDOT) QA/QC specifications and identified the acceptable levels of PCC strength. The current KDOT percent within limits (PWL) specifications were shown to be more sensitive to the PCC strength than to the slab thickness. Distresses predicted by MEPDG strongly depended on both factors as well as truck traffic, and their interactions were also significant. Each JPCP project would have an optimal combination of PCC strength and slab thickness to create the most economical design, which was determined to be 9.5 to 10 inches (24.1 to 25.4 cm) for 3,000 psi (20.7 MPa) concrete and 8.5 to 9.0 inches (21.6 to 22.9 cm) for 5,000 psi (34.5 MPa) concrete, independent of traffic levels. The authors recommend that KDOT specify an upper limit for the concrete strength in their PWL specifications.

## PCC strength and stiffness and mechanistic properties

Hu, Wang, and Gi (16) studied the mechanical properties of typical PCC in Iowa for use in MEPDG.  Using a database of over 20,000 items, typical input values for 28-day compressive strength, elastic modulus, modulus of rupture,and splitting tensile strength were obtained and compared to MEPDG defaults.  A nonlinear regression was used to determine the relationships between different properties.  While the Iowa database had good documentation of compressive strength, there was a severe lack of complete sets of data, which needs to be remedied going forward.

## PCC temperature gradients and deformations; temperature dependence of modulus

Asbahan and Vandenbossche (17) studied the effects of temperature and moisture gradients on slab deformation in JPCP, collecting data from a newly built instrumented JPCP over two years.  Slab temperature, moisture, static strains, and pavement surface measurements were combined to compute and/or predict slab curvature.  The presence of dowel and tie bars did little to restrain slab curvature due to daily temperature fluctuations or reversible drying shrinkage, but did reduce curvature attributed to long-term drying shrinkage.  The MEPDG default value was close to the measured value in this study, but is apparently not appropriate for undoweled slabs.

Gedafa et al (18) studied six typical JPCP pavements in Kansas, modeling them with the MEPDG software and looking at performance parameters as a function of alternative inputs of PCC strength development, shrinkage, and “zero-stress” temperature.  IRI and faulting were found to be insensitive to PCC strength, but slab cracking decreases as strength increases.  Long-term cracking and IRI are insensitive to shrinkage strain, but higher shrinkage strain does lead to more faulting.  Slab cracking and IRI are insensitive to the zero-stress temperature, but faulting is highly affected, unless the lane is widened and tied to a PCC shoulder.  April and October are determined to be the optimal months for JPCP paving in Kansas.

## PCC Coefficient of Thermal Expansion

The most common topic to appear in the literature review was the thermal expansion of concrete, with ten references, including two cited in (1).

Buch and Jahangimejad (19) looked at the coefficient of thermal expansion (CTE) of concrete.  The authors examined the change on CTE depending on test variables such as aggregate geology, sample age, and number of heating and cooling cycles.  The impact of CTE variables on MEPDG predictions, particularly of transverse cracking, was also investigated.

The same authors (20) documented measurements of CTE for typical PCC paving mixtures made using aggregate sourced from eight locations in the state of Michigan, including the classes limestone, dolomite, slag, gravel, and trap rock. Triplicate test specimens were moist cured for 3, 7, 14, 28, 90, 180, and 365 days before testing using the provisional AASHTO TP60 protocol and a revision devised at the University of Texas.  The measured CTE values were then compared using statistical analyses, and the resulting distributions used to determine the impact on transverse cracking performance of JPCP using the MEPDG software.

Naik, Kraus, and Kumar (21) looked more closely at the impact of aggregate type on CTE of PCC.  Aggregates belonging to the six basic classes of aggregate – glacial gravel, quartzite, granite, diabase, basalt, and dolomite – were used to make PCC samples in 15 typical mixtures.  At 28 days, the following parameters were measured:  CTE, compressive strength, and splitting tensile strength, the first and last of these being basic inputs in MEPDG.  CTE was found to vary with the type of aggregate, which ran highest to lowest with quartzite, dolomite, glacial gravel, granite, diabase, and basalt.  The splitting tensile strength recommended for Level 2 MEPDG input was found to be about 17-31% lower than experimental values.

Crawford, Gudimettla, and Tanesi (22) state that the CTE is one of the most sensitive MEPDG input values.  The most common method to measure CTE is the AASHTO TP60 method, which may be measured using automated equipment.  These researchers had one 410 stainless steel specimen, a low CTE PCC specimen, and a high CTE PCC specimen tested in 18 laboratory units including 11 custom-built automated systems and 7 commercial automated devices.  A statistical analysis was conducted to determine the overall variability of the measurements, including a comparison of custom-built to commercial units, and the AASHTO TP60 versus the Texas modification.  Accuracy of the CTE measurement of steel was compared to a measurement with a push-rod dilatometer following ASTM E228-06.

Smith and Tighe (23) examined the CTE of recycled concrete aggregate.  Sixteen cores containing 0%, 15%, 30%, and 50% recycled crushed aggregate were prepared and tested using a simplified method.  PCC performance was seen to improve, i.e. reduced CTE, as recycled aggregate content increased, from 7.28µε/°C (4.04µε/°F) at 0% to 4.10µε/°C (2.28µε/°F) at 50%.  Pavement performance in MEPDG simulations was also found to improve as recycled aggregate content increased and CTE decreased.

Yeon, Choi, and Won (24) looked at the effect of relative humidity on CTE.  In the standard AASHTO TP60 method, the PCC sample is saturated before and during testing.  Previous studies indicated that the maximum CTE was observed at 70% relative humidity (RH), which was almost twice the value at 100% RH.  In this test, RH sensors were installed in specimens which were cured at 50% RH at 23°C (73°F) for six weeks, then the specimens were tested at RH target values of 45%, 60%, 70%, 80%, and 100%.  Testing was conducted in an environmental chamber with the specimen RH set to the target value by measuring displacement with change in temperature.  Maximum CTE was observed at 70% to 80% RH, with a much larger effect on cement paste than on concrete.  The researchers conclude that because the effect on concrete is lower than on paste, the AASHTO TP60 method remains adequate for MEPDG usage.

Kohler and Karmekanti (25) looked at the influence of CTE on cracking in over 100 sections of jointed PCC pavements in California, including multiple lanes and crack histories.  CTE values were measured, and ranged from 4.8 µε/°F (8.6 µε/°C) to 6.7 µε/°F (12.1 µε/°C), and correlated with cracking data obtained from the Caltrans pavement management database.  CTE does affect crack development on PCC pavements, but the effect was limited by the subjective nature of the cracking data.  Still, it was clear that pavements with CTE over 5.7 µε/°F (10.2 µε/°C) showed more cracking than the other pavements.

Tran, Hall, and James (26) studied CTE  inputs for the MEPDG.  24 PCC and cement paste mixtures were tested in triplicate at 7 and 28 days of aging, and were found to be comparable to literature values.  The type of aggregate used significantly influenced the CTE and pavement performance predictions.  Since this experiment was limited to mixtures containing limestones and sandstones, it was recommended that further studies be made of CTEs for PCCs with other classes of aggregate, and that the MEPDG allow for more classes of aggregate in its input menu.

Tanesi et al. (27) in 2007 analyzed CTE tests data from 1800 PCC samples representing a variety of mixtures representative of pavements from across the United States. The analysis reported no correlation between CTE variability and CTE. For a typical JPCP design, higher CTE led to higher effect of CTE variability on predicted distresses and smoothness.  The CTE variability could make for a significant changes or discrepancies in predicted performance in terms of predicted IRI, slabs cracked, and faulting.  High testing standards and proper quality assurance/quality control (QA/QC) are essential to minimizing CTE test variability.

Hossain et al. (28) in 2006 reviewed CTE results from Long Term Pavement Performance (LTPP) projects in Iowa, Kansas, and Missouri.  Kansas had a wide variety of CTE values in PCC, due partly to variations in aggregates and mixes.  Calculating a PCC CTE value as a weighted average of CTE of paste and aggregate always yielded a higher value than did direct measurement.  The deleterious effects of high PCC CTE can be tempered by increasing slab thickness, increasing dowel bar thickness, and/or increasing lane width and using a tied concrete shoulder.

## Performance of Base materials

Khoury, Naji, and Banks (29) looked at the performance of a stabilized aggregate base subjected to different freeze-thaw durability procedures.  Cylindrical specimens were formed and stabilized with 10% Class C fly ash and cured.  They were then subjected to 24 hours at -25°C (-13°F) followed by 24 hours at 21.7°C (71.1°F) at high RH, either with or without a membrane.  Resilient modulus and unconfined compressive strength were determined as a function of the number of freeze-thaw cycles.   Resilient modulus values of 28-day cured specimens increased up to 12 freeze-thaw cycles with no membrane; 13 or more cycles led to decreased modulus.  For three-day cured specimens, the resilient modulus increased up to 30 freeze thaw cycles with no membrane. Unconfined compressive strengths showed similar behavior as a function of freeze-thaw cycles.  Freeze-thaw testing with a membrane led to faster deterioration of performance.  These results suggest that the resilient modulus stress model recommended in the MEPDG could be a reliable predictor.

## Resilient modulus of base materials

Schuettpelz, Fratta, and Edil (30) looked at mechanistic corrections to elastic wave determinations of resilient modulus of base course materials.  Standard tests are expensive and cannot be applied to materials with large (> 25 mm (>1 inch)) aggregate particles in 125 mm (5 inch) diameter specimens.  The authors recommend measuring the propagation of elastic waves.  P-wave velocity can be used to determine modulus, and corrections made for stress, void ratio, and Poisson’s ratio effects.  This approach can be applied when large aggregate particles are present.

Siripun, Nikraz, and Jitsangiam (31) examined the mechanical properties of hydrated cement treated crushed rock base subjected to repeated cyclic loads on triaxial tests with various stress paths.  A “shakedown concept” was applied to describe the mechanical response of unbound granular materials under traffic load, utilizing macro-mechanical observation of the unbound granular material response and the distribution of vertical plastic strain in the base material.  Compacted specimens of the hydrated  cement treated crushed rock base were subject to triaxial testing with ratios of vertical major stress to horizontal minor stress (σ1/σ3) of 11 achieved a stable state with a large number of load cycles.  Mechanical responses and limit ranges for using the hydrated cement treated crushed rock base in pavements were determined.

Khogali and Mohamed (32) in 2007 evaluated the reasonableness of the default resilient modulus values for unbound base materials and subgrade soils, and found that MEPDG defaults tended to be higher than in the field.  Furthermore, AASHTO soil class and mechanical properties do not correlate well, suggesting a different approach to estimating resilient modulus is needed.

Kim (33) in 2007 reviewed the MEPDG subgrade soil characterization procedure.  The MEPDG assumes that the subgrade is compacted to optimum moisture content; an average resilient modulus would create a more conservative design.  Wetter than optimum resilient modulus values can be used to characterize subgrades during thawing; however, MEPDG values for frozen soils tend to be greater than lab values, and must be used with caution.

## MEPDG based pavement design catalog for states and local calibration

Li, Xiao, and Hall (34) discussed the creation of an MEPDG-based design catalog for low-volume roads in Arkansas.  Traditional design approaches, based on a standard section applying a double surface treatment over a specified thickness of granular base, were often inadequate.  Thus the Arkansas State Highway and Transportation Department decided to consider applying MEPDG methods generally targeted at high-volume roads on low-volume designs as well, resulting in the catalog under discussion.  In essence, a variety or catalog of feasible design alternatives were generated and tested for a comprehensive array of site conditions.  The five geographical regions in Arkansas are accounted for.  The traffic design considers three levels of volume with a typical load spectrum, three types of subgrade, and six potential types of aggregate that can be used in base and surface layers.  All input data come from previous MEPDG implementation research in Arkansas.  This represents a simplified and rational design process for low volume roads in the state.

Li et al (35) discuss efforts to update the pavement thickness design catalog for the state of Washington.  The revisions utilized the MEPDG, 1993 AASHTO guide, and Washington State Department of Transportation (WSDOT) historical pavement performance data.  The design process begins by selecting the ESAL levels and performance criteria, then using the 1993 AASHTO guide and/or MEPDG to devise the thickness choices in the catalog.  In addition to the historical performance data, other inputs included properties of new pavement materials, regional practices, and construction variability.

Siraj et al (36) conducted a verification of an MEPDG for the state of New Jersey. Nine LTPP and 16 non-LTPP sections in New Jersey were evaluated by applying Level 3 material data and Level 2 traffic data into MEPDG and computing predicted values for rutting, alligator cracking, longitudinal cracking, thermal cracking, and IRI.  These were compared to field measurements and were generally found to be statistically similar to predicted values.  The difference between measured and observed alligator cracking was considered reasonable given the errors in the field data and prediction error from Level 3 inputs.

Khazanovich et al (37) looked at adapting the MEPDG for designing low-volume PCC roads in Minnesota.  The faulting model produced acceptable results, but the cracking model had to be adjusted using performance data from 65 sections located in Minnesota, Iowa, Wisconsin, and Illinois.  A prototype design catalog was generated using MEPDG Version 0.910, subject to revision when the MEPDG software is finalized.

Haider et al (38) looked at calibrating the MEPDG for JPCP in Michigan.  The sensitivity analysis included both single variable studies, which identified the most significant variables, and a detailed full factorial analysis, which highlighted the major effects and interaction effects on performance predictions.  The list of most significant variables, once identified, was further refined using engineering judgment and/or local practices.  The interaction effects are expected to be important when interpreting the pavement performance from the perspective of the designer.

Schram and Abdelrahman (39) in 2006 used pavement management data from Nebraska to calibrate two MEPDG smoothness models at the local project level. The dataset was categorized by surface layer thickness and annual daily truck traffic. This calibration reduced the default model prediction error to nearly half the previous network-level calibration value.

Swan et al (40) examined the characterization of regional traffic data for the MEPDG, specifically by determining default traffic data for northern and southern regions in Ontario, Canada.  The sensitivity of the results to changes in traffic inputs was explored.  Discussions of the differences between the default loads and the regional spectra are noted.  For example, in Ontario there are fewer heavily overloaded axles, and the peaks between loaded and unloaded axles are more pronounced.  In the north, axle load spectra are heavier and have a higher proportion of fully loaded axles.  The number and type of trucks is found to be the major influence on predicted performance, followed by the axle load spectra.  Some of the traffic parameters, including hourly volume adjustment factors and axle spacing, were not found to have any significant influence on predicted performance.

# Survey of Pavement Design Practice in NYDOT Regional Offices

A survey questionnaire about design practices and local material properties was drafted in cooperation with NYDOT personnel and Dr. Stefan Romanoschi of the University of Texas, Arlington. The four-page form and instructions are reproduced in Appendix A.  The form was sent to all the NYDOT Region Offices.  Completed responses have not been received to date, and thus there were no results to process.

# Available MEPDG Models

The Mechanistic Empirical Design Guide (MEPDG) (41) is described as an iterative process for pavement design.  The software system does not produce a specific recommendation for a pavement system consisting of layer types and thickness giving design parameters such as traffic loading, weather conditions and available local aggregates and resources, instead, the software system outputs pavement distresses and smoothness, given certain design criteria.  It is up to the engineer to enter a specific pavement design based on either experience or current convention, and then using specific site conditions such as traffic loading and local weather conditions, the MEPDG will provide a measure on which the design engineer can decide whether the design criteria used is adequate or needs modifications.  A conceptual flow chart adapted from the MEPG design guide is shown in Figure 1 (adapted from (41)).  The design/analysis process consists of three steps; Evaluation, Analysis, and Strategy Selection.  In the Evaluation Stage, the design engineer uses tools available to him such as soil testing in the field and laboratory, availability and type of local paving materials, local climatic conditions, traffic analysis and local and state wide design criteria to create a pavement section that would need to be analyzed.  This pavement section is then inputted into the Analysis Stage of the MEPDG process and the software calculates expected distresses and the timeline on which these distresses will occur.  The engineer then decides whether the expected distresses and associated timeline are within the design criteria and period for this pavement or not.  The design engineer will then decide whether to adopt his particular design or adjust it and rerun the analysis.  Once a certain set of appropriate pavement design sections have been created then the third stage is the selection strategy.  This stage is not guided by the MEPDG software but is left to the particular department of transportation to explore costs, constructability and other political decisions and decide on a final pavement design.

To this end, it is apparently important that the performance models used by the MEPDG for estimating the criteria on which pavement design decision are based be studied and explained as part of the calibration to local conditions (42).  The applicability of these models to the State of New York will also be discussed.  The performance indicators predicted by the MEPDG for Portland Cement Concrete pavements (PCC) and PCC overlays are shown in Table 1.  Prior to explaining the methodology used for the performance indicators, it also noteworthy to discuss someperformamce parameters that are not accounted for in the MEPDG.  The MEPDG does not show friction/skid resistance numbers and does not output any noise attenuation from a particular pavement design.   State DOTs usually use skid resistance as a performance criteria to decide when to rehabilitate a particular pavement section, but in this case will not have these numbers as predictors.  Noise attenuation levels are usually used to decide whether to place noise barriers and/or to use different texturing techniques for the finished pavements.  At certain times this will also influence the type of pavement use (HMA or PCC).  Again in this case the DOT designers will need to use historical numbers and criteria to decide whether a particular pavement design will meet these requirements or not.  The MEPDG does not have the capability to predict durability of particular mix design and in the case of concrete pavement their susceptibility to alkali silica reactivity or D-cracking.  Again the design engineers should use historical data and material testing to verify that these would not be issues that need to deal with.  Other criteria that are not accounted for in the MEPDG and not necessarily related to performance parameters include the use of Single Truck Tires, volume changes in soils, Geogrids used as a reinforcing material, ultra-thin PCC overlays, Jointed Reinforced Concrete Pavement, early-age PCC opening to traffic.  The design engineers are instructed to use other resources to account for these factors.

The MEPDG uses an accumulation of damage as a function of time and truck traffic to provide a distress estimate for the desired analysis period.  The minimum analysis period used is one month except during freeze/thaw conditions when the time period become half a month. The performance indicator equations and explanation follows.

Figure 1.  MEPDG Flow Chart

Table 1.  PCC Performance Predictors

| Pavement Type | Performance Indicator |
| --- | --- |
| Jointed Plain Concrete Pavement (JPCP) | Mean Joint Faulting |
| JPCP | Joint Load Transfer Efficiency (LTE) |
| JPCP | Load-Related Transverse Slab Cracking (bottom and surface initiated cracks) |
| JPCP | Joint Spalling (embedded into IRI prediction model) |
| Continuously Reinforced Concrete Pavement (CRCP) | Crack Spacing and Crack Width |
| CRCP | LTE |
| CRCP | Punch outs |
| JPCP and CRCP | Smoothness (IRI) |

## Distress Prediction Equations for Rigid Pavements and PCC Overlays

Table 1 will be used as a list guide for the performance predictors discussed in this section.  It should be noted that the State of New York does not specify as standard practice the use of continuously reinforced concrete pavements (CRCP), so performance measures that are particular to CRCP will not be discussed as these are not applicable to the state of New York at this time.  CRJCP are also not specified in the State of New York standards at this point in time and these types of pavements are not supported in the current version of the MEPDG program.

### Mean Joint Faulting and Joint Load Transfer Efficiency

As discussed above the MEPDG uses a month by month incremental approach to predict mean transvers joint faulting.  These increments are accumulated over the entire desired design period and reported in graph or data format.  The equations used for determining this faulting are listed below, with Table 2 showing the parameters used in these equations and a description of these parameters.

(1)

(2)

(3)
		(4)

According to the MEPDG guide, the faulting analysis is only carried out during the occurrence of maximum differential density energy on the subgrade, again defined as the maximum faulting occurring during the nighttime between the hours of 8:00 PM and 8:00 AM.  In addition, the equivalent linear temperature difference for nighttime is determined for each calendar month using Equation 5 below.

(5)

The MEPDG calculates the PCC slab temperature using 11 evenly spaced points through the depth of the slab, hourly, and these temperatures are converted into equivalent temperature differentials.  Using the effective temperature differentials and the corresponding effective k-value and base modulus, the corner deflections is determined using neural network finite element software within the guide, and the initial maximum faulting is determined.  This number is further adjusted for traffic damage.

The magnitude of the corner deflection is not only controlled by the temperature differentials and the base conditions but also by the joint Load Transfer Efficiencies (LTE).  This is depended on both the type and size and amount of dowel bars used as well as possible aggregate interlock.  Equation 6 is used to calculate LTEs.

(6)

The MEPDG assumes a 20% LTE for aggregate bases, 30% LTE for Asphalt Treated or Concrete Treated bases and 40% LTE for Lean concrete bases.

Table 2.  Equation parameters used in the MEPDG

| Parameter | Description |
| --- | --- |
| Faultm | Mean joint faulting at the end of period m (in.) |
| ΔFaulti | Incremental change in mean transverse joint faulting during time period (in.) |
| FAULTMAXi | Maximum mean transverse joint faulting (in.) |
| FAULTMAX0 | Initial maximum mean transverse faulting (in.) |
| EROD | Base and Subbase erodibility factor |
| DEi | Differential density of energy subgrade deformation accumulated during time period i |
| δcurling | Maximum mean monthly PCC slab corner upward deflection due to temperature curling and moisture warping |
| Ps | Subgrade overburden (lb) |
| P200 | Percent Subgrade material passing #200 sieve |
| WetDays | Average annual number of days with precipitation greater than 0.1 in. |
| C1,2,3,4,5,6,7,12,34 | Global calibration constants |
| C12 | C1+C2*FR0.25 |
| C34 | C3+C4*FR0.25 |
| FR | Freezing Index; Percentage of time the top of base temperature is below 32 ºF |
| ΔTm | Effective temperature differential for time period m |
| ΔTt,m | Mean PCC top-surface nighttime temperature for time period m |
| ΔTb,m | Mean PCC bottom-surface nighttime temperature for time period m |
| ΔTsh,m | Equivalent temperature differential due to reversible shrinkage for time period m, for old concrete |
| ΔTPCW | Equivalent temperature differential due to permanent curl/warp |
| LTEjoint | Total transverse joint LTE (%) |
| LTEdowel | Joint LTE if dowels are the only available mechanism (%) |
| LTEbase | Joint LTE if base is the only available mechanism (%) |
| LTEagg | Joint LTE id aggregate interlock is the only available mechanism (%) |

The maximum faulting of Equation 3 is adjusted for traffic damage using the accumulated differential energy (DE).  Using the deflections, the differential energy, shear stress at the corner and maximum dowel bearing capacity (if present) are calculated.  In addition the equations used also calculate the loss of shear capacity due to wheel load repetition, this is characterized in terms of the width of the transverse joint base on functions derived from the analysis of load transfer test data developed by the Portland Cement Association (PCA), and is calculated for a time period of m equal to one month.  Dowel damage is also calculated, to account for the damage that occurs at the dowel-concrete interface due to repeated loadings.  Equation 4 above is then used to calculate the faulting increment for each month period, and using equation 1 the faulting at the end of the current month is determined.  These steps are repeated in the program for the life of the pavement.  Using the global calibration factors, the MEPDG estimates that the standard error for transverse joint faulting is given by equation 7, where FAULT is the predicted mean transverse joint faulting at any given time period m in inches ad described in Table 2.

(7)

The MEPDG was calibrated using test road data from the LTPP program and other national test roads, but as extensive as this data is it still does not account for local conditions in each state.  The implication for the state of New York, is that a local calibration would be necessary to reduce these error values for joint faulting and LTEs.  Local numbers from the test sites around the state of New York would be used to determine the local calibration factors and adjust the C calibration constants in order to reduce the error associated with just using the global calibration factors.

### Transverse Slab Cracking

The MEPDG considers both bottom-up and top-down cracking for PCC pavement.  The guide also specifies that the likelihood of both types of cracking occurring at the same time in a slab is not possible due to its limited potential and thus only one or the other is considered possible at one time.  The percentage of slabs with transverse cracks is used as a measure of the durability of the pavement sections under the given traffic loading conditions.  The following equations are used for predicting the transverse cracking of the slabs.

(8)

(9)

(10)

(11)

Table 3 lists the parameters used in equations 8 through 11 and provide a description for each variable.

It should be noted that factor I from the above equations accounts for change in the PCC modulus of rupture, elasticity and slab/base contact friction as well as deterioration of the shoulder load transfer efficiency over time.  Factor j, accounts for change in the base modulus of elasticity and change in effective dynamic modulus of subgrade reaction.  Factor k accounts for axle type difference, between single tandem and tridem axles for bottom-up cracking and the truck wheel-base dimensions for top-down cracking.

The calculations in the MEPDG for the transverse cracking combines the base and the slab are combined into an equivalent section based on equivalent stresses.  Again the MEPDG was calibrated using the test road data available and the using the global calibration factor the standard error reported is given by equation 12 where CRACK is the predicted transverse cracking based on mean inputs in percent.

(12)

Table 3.  Variables and Description used for Equation 8 through Equation 11

| Variable | Description |
| --- | --- |
| CRK | Predicted amount of bottom-up or top-down cracking |
| DIF | Calculated total fatigue damage |
| ni,j,k,l,m,n,o | Applied number of load applications under given conditions |
| Ni,j,k,l,m,n,o | Allowable number of load applications under given conditions |
| i | Age |
| j | Month |
| k | Axle type |
| l | Load level |
| m | Equivalent temperature difference between top and bottom |
| n | Traffic offset |
| o | Hourly truck traffic fraction |
| MRi | PCC Modulus of rupture at age I,(psi) |
| σi,j,k,l,m,n,o | Applied stress under the given conditions |
| C1 | Calibration Constant (2.0) |
| C2 | Calibration Constant (1.22) |
| TCRACK | Total transverse cracking (%) |
| CRKbottom-up | Predicted amount of bottom-up transverse cracking (fraction) |
| CRKtop-down | Predicted amount of top-down transverse cracking (fraction |

As previously discussed, in order for the transverse cracking equation to predict the cracking in the State of New York with better reliability, local calibration parameters need to be used and the calibration constants in the equations above need to be adjusted for local conditions.  These equations account for changes in temperature as well as traffic condition in addition to the local materials used.  Local calibration would greatly enhance the output of these equations.

### Smoothness

The MEPDG predicts the pavement longitudinal smoothness as a function of the initial as-constructed profile of the pavement and any changes over time due to traffic distress and foundation movement.  This model was calibrated using the LTPP field data base and was calibrated under various weather conditions. Equation 13 through Equation 16 are used for predicting the pavement smoothness.

(13)

(14)

(15)

(16)

Table 4 lists the variables used in equations 13 through 16 and a description of these variables.

Table 4.  Variable and descriptions used in equations 13 through 16 for IRI measurement.

| Variable | Description |
| --- | --- |
| IRI | Predicted IRI, (in./mi) |
| IRI1 | Initial smoothness measured as IRI (in./mi) |
| CRK | Percent slabs with transverse cracks |
| SPALL | Percentage of joints with spalling (medium to high severity) |
| TFAULT | Total joint faulting accumulated per mile (in.) |
| C1 | 0.8203 |
| C2 | 0.4417 |
| C3 | 0.4929 |
| C4 | 25.24 |
| SF | Site Factor |
| AGE | Pavement age (years) |
| FI | Freezing Index (ºF-days) |
| P200 | Percent subgrade material passing No.200 sieve |
| SCF | Scaling factor based on site, design and climate |
| ACPCC | PCC air content (%) |
| PREFORM | =1 if preformed sealant is used, =0 otherwise |
| f’c | PCC compressive strength |
| FTcycles | Average annual freeze-thaw cycles |
| HPCC | PCC slab thickness (in) |
| WCPCC | w/c ratio in PCC slab |

The standard error of the predicted IRI versus the measured IRI in the global calibration is given in the MEPDG and is show in Equation 17 below.  The factors in the this equation are the variance in initial IRI, cracking, spalling, faulting and an overall model error Se2 = 745.3 (in./mi)

(17)

For the purpose of this research these values will be checked against IRI values from the State of New York and a statistical variation will be calculated.  This variation will determine if this equation is adequate for use in New York, or if further adjustment of the local factors will be conducted in order to achieve better correlation between the predicted IRI using the MEPDG and the actual IRI numbers measured in New York.

The calibration of the MEPDG requires materials property data on all pavement structure components, including PCC, base materials, and subgrade soils.  Also required are climatic data and traffic data.  For generation of the JPCP database for New York, the material data on PCC and base materials is being collected by this research team, while the traffic, climatic, and subgrade material data were collected and analyzed by Dr. Stefan Romanoschi of the University of Texas, Arlington.  All these data will also be used to conduct a local calibration of the MEPDG.

# Data from New York JPCP experimental pavements

## Coefficient of thermal expansion of PCC

Measuring the coefficient of thermal expansion (CTE) for concrete pavement is a simple procedure which involves measuring the change in length of a concrete specimen due to the change in temperature.  AASHTO TP60-00 “The Standard Method of Test for Coefficient of Thermal Expansion of Hydraulic Cement Concrete” was used.

Specimen preparation and conditioning

Concrete samples are cored out of the pavement of interest. The core is 4 inches (10 cm) in diameter. The ends of the specimen are sawed to create a smooth surface and to meet the desired thickness of 7 inches (18 cm).  The specimens then must be saturated in water mixed with lime at room temperature. The specimens must be in the bath for at least 48 hours and then weighed until the difference in the weight is less than 0.5%.

Testing

A water bath is prepared that will allow the specimen to fully be submerged in the bath. The specimen thickness is measured and placed in a specially designed stand that holds the core in place. A linear variable displacement transducer (LVDT) is placed above the specimen and the tip is placed in the middle of the core to measure the specimen’s displacement.   The temperature of the water bath is lowered to 10°C (50°F) and maintained at that temperature. The LVDT stand with the core is then lowered into the bath. The specimen must be in the water at that temperature for at least 30 minutes; then the displacement is read. When an “equilibrium” displacement is apparent, record that value as well as the temperature; this will serve as the initial reading.

The temperature of the water is then raised to 50°C (122°F). The same measuring procedure is performed with displacement and temperature.  The CTE value is the difference in displacement readings divided by the initial length and by the difference in temperature (40°C (72°F)).

The temperature of the water is then lowered back down to 10°C (50°F) and the displacement measured one more time. The final reading will result in the second CTE value.

The two CTE values must be within 0.3×10-6 °C-1 (0.17×10-6 °F-1) of one another for the test to be valid. If they meet that standard then the two CTE values are averaged to compute the CTE for that specimen.   Typical CTE values stay near 10×10-6 °C-1 (6×10-6 °F-1) for concrete pavements.

Results

Specimens collected from experimental PCC pavements on I90 near Syracuse, I490 near Rochester and I86 at Hinsdale were tested via the AASHTO TP60-00 method.  The I86 pavement experiment involved placing the PCC over three different sections of an existing JRCP pavement, on each of which the existing pavement was subjected to a different treatment:  rubblization, cracking and seating, or no treatment.  The PCC mix applied on all three sections was the same, but included different batches; the four specimens tested included one from each section plus a second core taken from the untreated section.  Table 5 lists the measured CTEs from the New York specimens.

Table 5.  Coefficient of thermal expansion for PCC samples from New York.

| Specimen | CTE (10-6°C-1) | CTE (10-6°F-1) |
| --- | --- | --- |
| I90 Syracuse | 11.51 | 6.39 |
| I490 Rochester | 12.06 | 6.70 |
| I86 crack and seat | 10.06 | 5.59 |
| I86 untreated #1 | 10.52 | 5.84 |
| I86 untreated #2 | 10.92 | 6.07 |
| I86 rubblized | 8.58 | 4.77 |
| I86 average | 10.02 | 5.57 |
| I86 standard deviation | 1.02 | 0.57 |

## Summary of test methods used for unbound materials and soils

In this research, four types of material were tested (NY I-90 Type 3, NY I-90 Type 4, NY 15 Type 4 and SR 219 Type 4). Sieve analysis, proctor compaction test, resilient modulus, and permanent deformation tests were conducted for each type of material. The following properties and parameters were obtained: gradation; optimum water content and maximum dry density; resilient modulus value and the parameters k1, k2, and k3; and permanent deformation parameters α and µ. Test protocols and standards used in this research are summarized in Table 6.

Table 6.  Test Protocols and Standards for Unbound Materials and Soils.

| AASHTO T 88 | Particle Size Analysis of Soils |
| --- | --- |
| AASHTO T 99 | Moisture-Density Relations of Soils Using a 2.5-kg (5.5-lb) Rammer and a 305-mm (12-in) Drop |
| AASHTO T 100 | Specific Gravity of Soils |
| AASHTO T 265 | Laboratory Determination of Moisture Content of Soils |
| AASHTO T 307 | Determining the Resilient Modulus of Soils and Aggregate Materials |
| ASTM C 136-06 | Standard Test Method for Sieve Analysis of Fine and Coarse Aggregates |
| ASTM D 698 | Test Methods for Moisture-Density Relations of Soils and Soil-Aggregate Mixtures, Using 5.5 lb (2.5 kg) Rammer and 12 inch (305 mm) Drop |
| ASTM D 2487 | Classification of Soils for Engineering Purposes |

## Sieve Analysis

ASTM C136 – 06, “Standard Test Method for Sieve Analysis of Fine and Coarse Aggregates” was used. A representative sample of 20 kg (44 lb) for each type of material was sieved. Materials were oven-dried for 24 hours before testing. After completing the sieve process, the material on each sieve was weighed, and the gradation was produced. The aggregate gradations are summarized in Table 7. Measured aggregate graduations for different types of materials are shown in Figure 2.

Table 7.  Aggregate gradations (percent passing).

| Sieve Size (English) | 2" | 1.5" | 1" | 3/4" | 3/8" | 1/4" | No. 4 | No. 10 | No. 40 | No. 60 | No. 200 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Sieve Size (mm) | 50.8 | 38.1 | 25.4 | 19.05 | 12.7 | 9.525 | 4.76 | 2 | 0.42 | 0.25 | 0.074 |
| NY I-90 Type 3 | 96% | 93% | 84% | 75% | 61% | 53% | 36% | 24% | 8% | 5% | 3% |
| NY I-90 Type 4 | 99% | 97% | 78% | 61% | 45% | 35% | 21% | 13% | 6% | 4% | 2% |
| SR 219 Type 4 | 100% | 98% | 93% | 88% | 80% | 74% | 54% | 36% | 6% | 3% | 2% |
| NY 15 Type 4 | 100% | 92% | 81% | 72% | 62% | 55% | 42% | 35% | 9% | 6% | 4% |

Figure 2. Measured Aggregate Gradations (25.4 mm = 1 in).

## Proctor Compaction Test

The proctor compaction test was conducted according to ASTM D698 -91 Test Method using Procedure C. Water was added to the soil type at a predetermined moisture content percentage. A six-inch (15 cm) mold was used, three layers of soils were compacted with 56 blows using a standard proctor hammer. The weights of the specimen and mold were recorded, a representative portion of the specimen was used to determine the water content.  The optimal moisture content and maximum dry density for each type of soil are listed in Table 8. The compaction curves for each type of material are shown in Figure 3 through Figure 6.

Table 8. Optimal Moisture Content and Maximum Dry Density fo New York soils

| Soil Type | NY I90 Type 4 | NY I90 Type 3 | SR219 Type 4 | NY15 Type 4 |
| --- | --- | --- | --- | --- |
| Optimal water content, w% | 10.4% | 6.1% | 6.9% | 7.3% |
| Maximum Dry Density (pcf) | 125.3 | 145.4 | 138.5 | 137.0 |
| Maximum Dry Density (kg/m3) | 2007 | 2329 | 2219 | 2195 |

Figure 3.  NY15 Type 4 Compaction Curve (1kg/m3 = 0.0624 pcf).

Figure 4.  NY I-90 Type 4 Compaction Curve (1kg/m3 = 0.0624 pcf).

Figure 5.  NY I-90 Type 3 Compaction Curve (1kg/m3 = 0.0624 pcf).

Figure 6.  SR 219 Type 4 Compaction Curve (1kg/m3 = 0.0624 pcf).

## Resilient Modulus and Permanent Deformation Test

In resilient modulus and permanent deformation tests, the samples were prepared according to the standard method of sample preparation given in AASHTO T307. The required amount of material was calculated use the optimum water content and maximum dry density. The specimen dimension used in this research was 6 inches (15 cm) diameter and 12 inches (30 cm) height. The specimen was compacted in a compaction mold. After compaction, a rubber membrane was placed around the specimen with the top and bottom sealed. Two Linear Variable Displacement Transducers (LVDT) were mounted to measure the axial displacement. After completion of the test specimen, the repeated triaxial testing was conducted. The test sequences of resilient modulus and permanent deformation test are shown in Table 9. Three stages are included in the test sequences: Conditioning, Resilient modulus test, and Permanent deformation test.

Table 9. Testing Sequences of Resilient Modulus and Permanent Deformation Test.

| Sequence | Confining Pressure | Cyclic Stress | Contact Stress | Max. Axial Stress | Load Cycles |
| --- | --- | --- | --- | --- | --- |
|  | kPa | psi | kPa | psi | kPa | psi | kPa | psi |  |
| Conditioning |
| 0 | 103.4 | 15.0 | 93.1 | 13.5 | 10.3 | 1.5 | 103.4 | 15.0 | 500 |
| Resilient Modulus |
| 1 | 20.7 | 3.0 | 18.6 | 2.7 | 2.1 | 0.3 | 20.7 | 3.0 | 100 |
| 2 | 20.7 | 3.0 | 37.3 | 5.4 | 4.1 | 0.6 | 41.4 | 6.0 | 100 |
| 3 | 20.7 | 3.0 | 55.9 | 8.1 | 6.2 | 0.9 | 62.1 | 9.0 | 100 |
| 4 | 34.5 | 5.0 | 31.0 | 4.5 | 3.5 | 0.5 | 34.5 | 5.0 | 100 |
| 5 | 34.5 | 5.0 | 62.0 | 9.0 | 6.9 | 1.0 | 68.9 | 10.0 | 100 |
| 6 | 34.5 | 5.0 | 93.1 | 13.5 | 10.3 | 1.5 | 103.4 | 15.0 | 100 |
| 7 | 68.9 | 10.0 | 62.0 | 9.0 | 6.9 | 1.0 | 68.9 | 10.0 | 100 |
| 8 | 68.9 | 10.0 | 124.1 | 18.0 | 13.8 | 2.0 | 137.9 | 20.0 | 100 |
| 9 | 68.9 | 10.0 | 186.1 | 27.0 | 20.7 | 3.0 | 206.8 | 30.0 | 100 |
| 10 | 103.4 | 15.0 | 62.0 | 9.0 | 6.9 | 1.0 | 68.9 | 10.0 | 100 |
| 11 | 103.4 | 15.0 | 93.1 | 13.5 | 10.3 | 1.5 | 103.4 | 15.0 | 100 |
| 12 | 103.4 | 15.0 | 186.1 | 27.0 | 20.7 | 3.0 | 206.8 | 30.0 | 100 |
| 13 | 137.9 | 20.0 | 93.1 | 13.5 | 10.3 | 1.5 | 103.4 | 15.0 | 100 |
| 14 | 137.9 | 20.0 | 124.1 | 18.0 | 13.8 | 2.0 | 137.9 | 20.0 | 100 |
| 15 | 137.9 | 20.0 | 248.2 | 36.0 | 27.6 | 4.0 | 275.8 | 40.0 | 100 |
| Permanent Deformation |
|  | 20.7 | 3 | 206.8 | 30 | 20.7 | 3 | 227.5 | 33 | 10000 |

A conditioning process is used to establish steady-state behavior. The specimen needs to be preconditioned by applying 500 repetitions of a load using a haversine-shaped 0.1 second load pulse followed by a 0.9 second rest period. The maximum axial stress of 15 psi (103.4 kPa) and corresponding cyclic axial stress of 13.5 psi (93.1 kPa) are used in conditioning process. Confining pressure is set to be 15 psi (103.4 kPa).

The resilient modulus test starts after the completion of conditioning process. The test is performed following the 15 loading sequences with different combinations of confining pressures and cyclic stresses (as shown in Table 9). The cycles are repeated 100 times for each loading sequence using a haversine-shaped load pulse. The results of resilient modulus test for different types of material are presented in Appendix B.

The same specimen was used to conduct the permanent deformation test. The confining pressure was set to be 3 psi (21 kPa), a haversine load with a 0.1 second load pulse followed by a 0.9 second rest period was applied up to 10,000 load applications. The maximum axial stress was 33 psi (227.7 kPa) and the corresponding cyclic stress was 30 psi (207 kPa). The axial deformation and the applied load were measured from two LVDTs and a load cell. The data were automatically recorded by the data acquisition system. During data acquisition, data was collected at specified time intervals to save storage space. The selected data points for permanent deformation test are presented in Table 10. Additional results of the permanent deformation test are shown in Appendix C.

Table 10.  Collected Data Points for Permanent Deformation Test.

| 1 - 20 | 100 | 500 | 900 | 1600 | 2800 | 6500 |
| --- | --- | --- | --- | --- | --- | --- |
| 30 | 150 | 550 | 950 | 1700 | 3000 | 7000 |
| 40 | 200 | 600 | 1000 | 1800 | 3500 | 7500 |
| 50 | 250 | 650 | 1100 | 1900 | 4000 | 8000 |
| 60 | 300 | 700 | 1200 | 2000 | 4500 | 8500 |
| 70 | 350 | 750 | 1300 | 2200 | 5000 | 9000 |
| 80 | 400 | 800 | 1400 | 2400 | 5500 | 9500 |
| 90 | 450 | 850 | 1500 | 2600 | 6000 | 10000 |

## Resilient Modulus Parameters

The resilient modulus model used in this research was NCHRP model or MEPDG model. This model was proposed by NCHRP project 1-28A. The relationship is as follows:

where:

= Resilient Modulus in psi.

= 14.696 psi (101.33 kPa = Atmospheric pressure).

Regression constants

The resilient modulus of unbound materials can be calculated based on the stress analyses by KENLAYER. In a simplified procedure for determination of MR, σ1= 7.4 psi (51 kPa) and σ2 = σ3 = 2 psi (14 kPa), are suggested to be used, subsequently, θ = 11.4 psi (79 kPa) and τoct= 2.55 psi (17.6 kPa). Material constants and MR calculated for stress state σ1= 7.4 psi (51 kPa) and σ2 = σ3 = 2 psi (14 kPa) for each sample are shown in Table 11.

Table 11.  Material Constants and MR Values Calculated for Stress State, σ1 = 7.4 psi and σ3 = 2 psi.

| Material Type and Sample # | k1 | k2 | k3 | Predicted MR (psi) | Predicted MR (MPa) | Average MR (psi) | Average MR (MPa) |
| --- | --- | --- | --- | --- | --- | --- | --- |
| NY I90 Type 3 #1 | 1572.17 | 0.72 | -0.24 | 18520 | 127.7 | 16123 | 111.2 |
| NY I90 Type 3 #2 | 1207.04 | 0.84 | -0.27 | 13726 | 94.6 |  |  |
| NY I90 Type 4 #1 | 1035.50 | 0.85 | -0.33 | 11626 | 80.2 | 15420 | 106.3 |
| NY I90 Type 4 #2 | 1715.36 | 0.78 | -0.46 | 19214 | 132.5 |  |  |
| NY 15 Type 4 #1 | 1112.75 | 0.75 | -0.28 | 12926 | 89.1 | 12750 | 87.9 |
| NY 15 Type 4 #2 | 1081.84 | 0.76 | -0.26 | 12575 | 86.7 |  |  |
| SR 219 Type 4 #1 | 1132.12 | 0.73 | -0.47 | 12822 | 88.4 | 12833 | 88.5 |
| SR 219 Type 4 #2 | 1102.53 | 0.72 | -0.31 | 12843 | 88.5 |  |  |

## Permanent Deformation Parameters

The relationship between the permanent deformation and load cycles can be expressed as follows:

The permanent deformation parameter  and  can be determined by the following equations:

;

where:  = resilient strain,

= permanent strain,

N = Number of load cycles

,  = permanent deformation parameters.

A summary of the test results of the permanent deformation parameters is shown in Table 12.

Table 12.  Permanent deformation parameters.

| Material Type | Sample # | εr at 500th load cycle | a | b | Rutting Parameter µ | Rutting Parameter α |
| --- | --- | --- | --- | --- | --- | --- |
| NY I90 Type 3 | 1 | 0.001252 | 0.00099 | 0.26532 | 0.210 | 0.735 |
|  | 2 | 0.001621 | 0.00072 | 0.27268 | 0.121 | 0.727 |
| NY I90 Type 4 | 1 | 0.001831 | 0.00027 | 0.35476 | 0.053 | 0.645 |
|  | 2 | 0.001132 | 0.00025 | 0.38631 | 0.085 | 0.614 |
| NY 15 Type 4 | 1 | 0.001664 | 0.00043 | 0.42621 | 0.110 | 0.574 |
|  | 2 | 0.001724 | 0.00123 | 0.28434 | 0.202 | 0.716 |
| SR 219 Type 4 | 1 | 0.002928 | 0.00085 | 0.47209 | 0.138 | 0.528 |
|  | 2 | 0.002589 | 0.00198 | 0.32321 | 0.247 | 0.677 |

## Performance Data from I490 Victor

### Project Location and Background

The I-490 project site is approximately 16 km (10 mi) south-east of Rochester, New York close to Victor NY, as part of a two year reconstruction project of both the east and west bound lanes of I-490.  The pavement was placed two lanes at a time by a slip form paver.  The jointed plain concrete pavement (JPCP) slab dimensions are 5 meters (16.4 feet) long, 4.27 meters (14 feet) wide, and 250 millimeters (9.84 inches) thick.  The two driving lanes were constructed first, with the 3.6 meter (11.8 feet) passing lane and 3.0 meter (9.8 feet) concrete shoulders installed later.  Typical dowel bar spacing is 305 mm (12 inches) on center, with a dowel bar diameter of 32 mm (1.25 inches).  The typical tie bar spacing is 714 mm (28.1 inches) on center with a diameter of 19 mm (0.75 inches).  The eastbound lanes were constructed in 1999.  Five slabs were studied to determine the effects of varying tie bar spacing.  Additionally, nine sections of ten slabs each were studied to investigate the effect of transverse dowel bar spacing and diameter.  Details on the project beyond what is contained in this report may be found in the Modeling and Monitoring of Pavement Response and Performance Task B report, Volume 1 (43).

The westbound lanes were constructed in 2002.  Two slabs were instrumented in the driving lane to study the environmental effects on the pavement.  Both the eastbound and westbound test sections were paved with NYDOT Class C mix as detailed in Table 13.  The desired 28 day strength of this mix is 31.5 MPa (4.57 ksi).  The concrete has a coefficient of thermal expansion of 12×10-6/°C (6.7×10-6/°F) and elastic modulus of 29,000 MPa (4200 ksi).  The slabs are supported by a 100 mm (4 in) thick cement treated permeable base placed on a 150 mm (6in) thick dense graded aggregate base.

Table 13. PCC Mix Design

| Material | kg/m3 | pcf |
| --- | --- | --- |
| Water | 158 | 9.87 |
| Cement | 287 | 17.9 |
| Fly Ash | 72 | 4.5 |
| Fine Aggregates | 634 | 39.6 |
| Coarse Aggregates (#1 Stone, 40% Split) | 454 | 28.3 |
| Coarse Aggregates (#2 Stone) | 682 | 42.6 |
| Water-Cement Ratio | 0.44 |

#### Westbound Lanes

In the westbound driving lanes, two adjacent slabs were instrumented to monitor the environmental strain on the slabs as well the vertical deflection.  The concrete strength, base type, base thickness, and drainage conditions were consistent for these two slabs.  The slabs were monitored during construction so that the actual strains and deflections the slab experienced during the curing process could be recorded.  Additional periods of monitoring occurred after the pavement cured.

#### Eastbound Lanes

The first five PCC slabs in the eastbound test section were constructed to study the effect of varying longitudinal tie bar spacing.  The tie bar diameter and length were held constant at 19 mm (0.75 in) and 700 mm (27.6 in) respectively.  Joint A, between Lane 1 and Lane 2, was constructed during the concrete placement and subsequently saw-cut.  Lane 3 was later constructed; resulting in a cold construction joint, joint B, between Lane 2 and Lane 3.  As illustrated in Figure 7, for joint A, the tie bar is centered between Lane 1 and Lane 2.  For joint B the tie bar is installed with the epoxy joint method, and is slightly offset from center.  The epoxy joint method allows for tie bar installation during shoulder placement and after the placement of the driving lane.  The side of the previously poured driving lane is drilled at the desired tie bar locations.  The tie bars are then inserted and secured with epoxy grout.  The shoulder is then placed around the tie bars.  The tie bar configuration for each slab is listed in Table 14 and depicted in Figure 8.  The cross sectional area of the three dowel bar configurations for both the entire slab width as well as one-third of the slab surrounding the right wheel path is listed in Table 15.

Also installed in the eastbound test section of I-490 is a series of slabs with three variations in transverse dowel bar diameters and spacing.  This pavement section includes nine sections consisting of ten slabs each as shown in Figure 9.  The dowel bar length is 450 mm (17.7 inches) with the diameter and spacing as varying as shown in Table 16 and depicted in Figure 10.  The total cross sectional area of steel from the three dowel bar arrangements is given in Table 17.

Figure 7.  Tie Bar Detail (350 mm = 13.8 in, 400 mm = 15.7 in, 700 mm = 27.6 in)

Table 14. I-490 Eastbound Tie Bar Spacing

| Slab Number | Number of Tie Bars | Tie Bar Spacing (mm) | Tie Bar Spacing (in) |
| --- | --- | --- | --- |
| 1 | 5 | 1075 | 42.3 |
| 2 | 7 | 717 | 28.2 |
| 3 | 9 | 538 | 21.2 |
| 4 | 11 | 430 | 16.9 |
| 5 | 13 | 358 | 14.1 |

Table 15. I-490 East Cross-Sectional Area of Steel

| Section | Slab | 1/3 Slab |
| --- | --- | --- |
|  | (mm2) | (in2) | (mm2) | (in2) |
| STD | 11,259 | 17.45 | 4,021 | 6.23 |
| E1 | 10,468 | 16.23 | 3,695 | 5.73 |
| E2 | 10,800 | 16.74 | 3,436 | 5.33 |

Figure 8. Tie Bar Configuration

Figure 9. I-490 East Test Sections Overview

Table 16. I-490 East Dowel Bar Spacing

| Type | Bar Diameter | Dowel Bar Spacing |
| --- | --- | --- |
|  |  |  | A | B | C | D |
|  | (mm) | (in) | (mm) | (in) | (mm) | (in) | (mm) | (in) | (mm) | (in) |
| STD | 32 | 1.26 | 150 | 5.9 | 300 | 11.8 | 150 | 5.9 | 300 | 11.8 |
| E1 | 28 | 1.10 | 180 | 7.1 | 240 | 9.4 | 120 | 4.7 | 240 | 9.4 |
| E2 | 25 | 0.98 | 105 | 4.1 | 190 | 7.5 | 90 | 3.5 | 190 | 7.5 |

Figure 10. I-490 East Dowel Bar Arrangement Detail

Table 17.  Cross-sectional dowel bar areas for the three dowel bar arrangements on I490 East.

|  | Bar cross section | Number of dowel bars in lane | Total bar cross section |
| --- | --- | --- | --- |
|  |  |  | driving | passing |
| Type | (mm2) | (in2) | driving | passing | (mm2) | (in2) | (mm2) | (in2) |
| STD | 804.2 | 1.247 | 14 | 12 | 11259 | 17.46 | 9651 | 14.96 |
| E1 | 615.8 | 0.950 | 17 | 15 | 10468 | 16.16 | 9236 | 14.25 |
| E2 | 490.9 | 0.754 | 22 | 18 | 10799 | 16.59 | 8836 | 13.58 |

### Initial Falling Weight Deflectometer Test Results

FWD testing was conducted on the joints of 84 of the 85 slabs in the test section beginning at 10:30 am and continuing until 2:00 pm.  Not all of the collected data is thought to be accurate because some of the calculated load transfer efficiencies (LTE) are significantly greater than the maximum possible LTE of 100%.  These discrepancies most likely result from faulty FWD testing equipment.  For analysis purposes, all LTE values greater than 105% are considered inaccurate and are eliminated from the calculations.  The LTE, deflection in μm/kN and mils/kip, and Joint Support Ratio (JSR) of the different dowel bar test sections for both the 37.4 kN (8.4 kip) and the 50.3 kN (11.3 kip) test loads are compared in Table 18 through Table 23.  These results indicate that as the test progressed the LTE generally increased, corresponding to the flattening of the slabs as the temperature increased.  Additionally, the changes in LTE from sections with different dowel bar arrangements tested in a close timeframe are can be compared in Table 18 through Table 23.

The STD, E1 and E2 sections from Slab 1 to Slab 25 are tabulated in Table 18 and Table 19.  The E2 sections deflected the least while the STD sections deflected the most in both the approach and leave positions for both test weights.  This corresponds to the average slab curl, with the STD slabs curled 0.5 mm (0.02 in or 20 mil) more than the E2 sections.  The JSR for these sections also follows this trend, with the E2 sections having the highest JSR, E1 sections in the middle and STD sections the lowest JSR.  When the LTE data is examined for these sections, the previously established trend is not followed as closely.

For the 37.4 kN (8.4 kip) test weight, the E1 approach LTE is an average of 0.4% higher that the E2 approach LTE, with the STD section approach LTE over 10% less than either E1 or E2.  However, in leave position, the LTE for the E2 section is about 4% less than either the STD or E1 LTE.  For the 50.3 kN (11.3 kip) test weight the E2 section did perform better than either the STD or E1 sections, with both the approach and leave LTE over 2% higher than either the STD or E1 efficiencies.

Upon examining the data for the joints from Slab 26 to Slab 55 in Table 20 and Table 21, it can be seen that the E2 sections once again deflected the least.  However, the E1 sections deflected slightly more that the STD sections in this group.  The JSR results for the 50.3 kN (11.3 kip) test correspond to this data with the E2 and STD slabs having higher JSR’s than the E1 slabs.  The JSR results for the 37.4 kN (8.4 kip) loading was opposite of those expected based on the deflection data, with the E1 slabs having the highest JSR while the E2 slabs had the lowest JSR.

Table 18.  I-490 East 37.4 kN (8.4 kip) FWD, Slabs 1-25, October 26, 2004.

| Joint Number | Joint Approach | Joint Leave | JSR |
| --- | --- | --- | --- |
|  | Deflection | LTE (%) | Deflection | LTE (%) |  |
|  | (μm/kN) | (mil/kip) |  | (μm/kN) | (mil/kip) |  |  |
| STD Dowel Bar Arrangement |
| 1 | 0.623 | 0.109 | 83.8 | 0.470 | 0.082 | 96.1 | 0.75 |
| 2 | 0.530 | 0.093 | 64.6 | 0.548 | 0.096 | 83.6 | 1.03 |
| 3 | 0.507 | 0.089 | 97.9 | 0.502 | 0.088 | 89.7 | 0.99 |
| 4 | 0.484 | 0.085 | 83.6 | 0.432 | 0.076 | 88.3 | 0.89 |
| 5 | 0.434 | 0.076 | 107 | 0.440 | 0.077 | 95.1 | 1.01 |
| μ | 0.536 | 0.094 | 82.5 | 0.488 | 0.085 | 89.4 | 0.92 |
| σ | 0.061 | 0.011 | 13.7 | 0.049 | 0.009 | 5.2 | 0.12 |
| E1 Dowel Bar Arrangement |
| 6 | 0.444 | 0.078 | 91.8 | 0.414 | 0.073 | 86.0 | 0.93 |
| 7 | 0.432 | 0.076 | 97.9 | 0.432 | 0.076 | 93.6 | 1.00 |
| 8 | 0.446 | 0.078 | 90.8 | 0.432 | 0.076 | 90.8 | 0.97 |
| 9 | 0.398 | 0.070 | 106.9 | 0.460 | 0.081 | 86.4 | 1.15 |
| 10 | 0.432 | 0.076 | 95.8 | 0.395 | 0.069 | 91.9 | 0.92 |
| 11 | 0.382 | 0.067 | 95.2 | 0.368 | 0.064 | 88.8 | 0.96 |
| 12 | 0.392 | 0.069 | 92.2 | 0.426 | 0.075 | 97.5 | 1.09 |
| 13 | 0.345 | 0.060 | 110.2 | 0.392 | 0.069 | 270.4 | 1.14 |
| 14 | 0.411 | 0.072 | 94.8 | 0.379 | 0.066 | 85.9 | 0.92 |
| 15 | 0.426 | 0.075 | 88.9 | 0.415 | 0.073 | 147.8 | 0.97 |
| μ | 0.421 | 0.074 | 93.4 | 0.413 | 0.072 | 90.1 | 0.97 |
| σ | 0.024 | 0.004 | 3.0 | 0.031 | 0.005 | 4.2 | 0.06 |
| E2 Dowel Bar Arrangement |
| 16 | 0.357 | 0.063 | 97.9 | 0.380 | 0.067 | 147.4 | 1.06 |
| 17 | 0.369 | 0.065 | 95.5 | 0.437 | 0.077 | 72.7 | 1.18 |
| 18 | 0.374 | 0.065 | 95.5 | 0.359 | 0.063 | 90.2 | 0.96 |
| 19 | 0.275 | 0.048 | 115.6 | 0.333 | 0.058 | 230.7 | 1.21 |
| 20 | 0.366 | 0.064 | 92.1 | 0.374 | 0.065 | 79.6 | 1.02 |
| 21 | 0.333 | 0.058 | 89.0 | 0.350 | 0.061 | 86.0 | 1.05 |
| 22 | 0.316 | 0.055 | 91.8 | 0.270 | 0.047 | 106.8 | 0.86 |
| 23 | 0.278 | 0.049 | 115.9 | 0.369 | 0.065 | 85.5 | 1.33 |
| 24 | 0.350 | 0.061 | 91.3 | 0.301 | 0.053 | 97.5 | 0.86 |
| 25 | 0.337 | 0.059 | 91.0 | 0.330 | 0.058 | 93.1 | 0.98 |
| μ | 0.350 | 0.061 | 93.0 | 0.360 | 0.063 | 86.4 | 1.01 |
| σ | 0.020 | 0.004 | 3.0 | 0.042 | 0.007 | 8.3 | 0.11 |
| LTE=Load Transfer Efficiency |
| JSR=Joint Support Ratio |
| Averages (μ) and standard deviations (σ) include only slabs with LTE less than 105% |

Table 19.  I-490 East 50.3 kN (11.3 kip) FWD, Slabs 1-25, October 26, 2004.

| Joint Number | Joint Approach | Joint Leave | JSR |
| --- | --- | --- | --- |
|  | Deflection | LTE | Deflection | LTE |  |
|  | (μm/kN) | (mil/kip) | (%) | (μm/kN) | (mil/kip) | (%) |  |
| STD Dowel Bar Arrangement |
| 1 | 0.619 | 0.108 | 85.1 | 0.610 | 0.107 | 87.3 | 0.99 |
| 2 | 0.601 | 0.105 | 86.0 | 0.581 | 0.102 | 85.7 | 0.97 |
| 3 | 0.626 | 0.110 | 82.0 | 0.610 | 0.107 | 80.4 | 0.97 |
| 4 | 0.553 | 0.097 | 83.2 | 0.552 | 0.097 | 81.5 | 1.00 |
| 5 | 0.555 | 0.097 | 87.3 | 0.561 | 0.098 | 81.6 | 1.01 |
| μ | 0.591 | 0.103 | 84.7 | 0.583 | 0.102 | 83.3 | 0.99 |
| σ | 0.035 | 0.006 | 2.1 | 0.027 | 0.005 | 3.0 | 0.02 |
| E1 Dowel Bar Arrangement |
| 6 | 0.505 | 0.088 | 86.3 | 0.482 | 0.084 | 81.6 | 0.96 |
| 7 | 0.498 | 0.087 | 89.3 | 0.528 | 0.092 | 83.0 | 1.06 |
| 8 | 0.504 | 0.088 | 81.8 | 0.509 | 0.089 | 81.0 | 1.01 |
| 9 | 0.502 | 0.088 | 88.2 | 0.504 | 0.088 | 84.5 | 1 |
| 10 | 0.512 | 0.090 | 88.0 | 0.505 | 0.088 | 80.2 | 0.99 |
| 11 | 0.472 | 0.083 | 79.6 | 0.478 | 0.084 | 78.4 | 1.01 |
| 12 | 0.518 | 0.091 | 74.6 | 0.480 | 0.084 | 198.8 | 0.93 |
| 13 | 0.481 | 0.084 | 85.8 | 0.495 | 0.087 | 181.9 | 1.03 |
| 14 | 0.515 | 0.090 | 81.7 | 0.492 | 0.086 | 139.0 | 0.95 |
| 15 | 0.506 | 0.089 | 82.1 | 0.489 | 0.086 | 105.8 | 0.97 |
| μ | 0.501 | 0.088 | 83.7 | 0.501 | 0.088 | 81.5 | 1 |
| σ | 0.014 | 0.002 | 4.6 | 0.018 | 0.003 | 2.1 | 0.03 |
| E2 Dowel Bar Arrangement |
| 16 | 0.472 | 0.083 | 81.7 | 0.455 | 0.080 | 143.1 | 0.96 |
| 17 | 0.439 | 0.077 | 89.9 | 0.464 | 0.081 | 91.9 | 1.06 |
| 18 | 0.444 | 0.078 | 87.0 | 0.459 | 0.080 | 85.1 | 1.03 |
| 19 | 0.380 | 0.067 | 89.6 | 0.392 | 0.069 | 291.3 | 1.03 |
| 20 | 0.433 | 0.076 | 82.9 | 0.420 | 0.074 | 79.2 | 0.97 |
| 21 | 0.378 | 0.066 | 89.8 | 0.385 | 0.067 | 86.1 | 1.02 |
| 22 | 0.338 | 0.059 | 98.3 | 0.395 | 0.069 | 81.9 | 1.17 |
| 23 | 0.434 | 0.076 | 82.5 | 0.400 | 0.070 | 85.5 | 0.92 |
| 24 | 0.383 | 0.067 | 89.3 | 0.371 | 0.065 | 88.4 | 0.97 |
| 25 | 0.418 | 0.073 | 82.9 | 0.404 | 0.071 | 83.4 | 0.97 |
| μ | 0.412 | 0.072 | 87.4 | 0.412 | 0.072 | 85.2 | 1.01 |
| σ | 0.041 | 0.007 | 5.1 | 0.034 | 0.006 | 3.9 | 0.08 |
| LTE=Load Transfer Efficiency |
| JSR=Joint Support Ratio |
| Averages (μ) and standard deviations (σ) include only slabs with LTE less than 105% |

Table 20.  I-490 East 37.4 kN (8.4 kip) FWD, Slabs 26-55, October 26, 2004.

| Joint Number | Joint Approach | Joint Leave | JSR |
| --- | --- | --- | --- |
|  | Deflection | LTE | Deflection | LTE |  |
|  | (μm/kN) | (mil/kip) | (%) | (μm/kN) | (mil/kip) | (%) |  |
| STD Dowel Bar Arrangement |
| 26 | 0.331 | 0.058 | 98.6 | 0.345 | 0.060 | 89.8 | 1.04 |
| 27 | 0.308 | 0.054 | 100.0 | 0.336 | 0.059 | 85.5 | 1.09 |
| 28 | 0.414 | 0.073 | 70.8 | 0.339 | 0.059 | 81.1 | 0.82 |
| 29 | 0.339 | 0.059 | 97.3 | 0.334 | 0.058 | 100.5 | 0.99 |
| 30 | 0.334 | 0.058 | 94.5 | 0.316 | 0.055 | 92.8 | 0.95 |
| 31 | 0.313 | 0.055 | 86.8 | 0.307 | 0.054 | 85.6 | 0.98 |
| 32 | 0.322 | 0.056 | 88.2 | 0.269 | 0.047 | 106.3 | 0.83 |
| 33 | 0.325 | 0.057 | 83.1 | 0.284 | 0.050 | 87.1 | 0.87 |
| 34 | 0.278 | 0.049 | 84.1 | 0.232 | 0.041 | 100.0 | 0.84 |
| 35 | 0.243 | 0.043 | 101.9 | 0.302 | 0.053 | 78.8 | 1.25 |
| μ | 0.321 | 0.056 | 90.5 | 0.311 | 0.054 | 89.0 | 0.98 |
| σ | 0.044 | 0.008 | 9.7 | 0.036 | 0.006 | 7.6 | 0.13 |
| E1 Dowel Bar Arrangement |
| 36 | 0.405 | 0.071 | 53.6 | 0.377 | 0.066 | 65.2 | 0.93 |
| 37 | 0.328 | 0.057 | 91.6 | 0.356 | 0.062 | 82.0 | 1.08 |
| 38 | 0.365 | 0.064 | 87.0 | 0.261 | 0.046 | 117.0 | 0.72 |
| 39 | 0.289 | 0.051 | 106.9 | 0.302 | 0.053 | 101.5 | 1.05 |
| 40 | 0.276 | 0.048 | 114.9 | 0.275 | 0.048 | 111.7 | 0.99 |
| 41 | 0.330 | 0.058 | 97.2 | 0.385 | 0.067 | 77.4 | 1.17 |
| 42 | 0.290 | 0.051 | 96.8 | 0.282 | 0.049 | 101.6 | 0.97 |
| 43 | 0.298 | 0.052 | 94.4 | 0.290 | 0.051 | 96.8 | 0.97 |
| 44 | 0.278 | 0.049 | 98.9 | 0.276 | 0.048 | 92.3 | 0.99 |
| 45 | 0.246 | 0.043 | 113.7 | 0.316 | 0.055 | 85.0 | 1.29 |
| μ | 0.328 | 0.057 | 88.5 | 0.323 | 0.057 | 87.7 | 1.02 |
| σ | 0.045 | 0.008 | 15.9 | 0.043 | 0.008 | 12.8 | 0.09 |
| E2 Dowel Bar Arrangement |
| 46 | 0.286 | 0.050 | 91.4 | 0.275 | 0.048 | 98.3 | 0.96 |
| 47 | 0.263 | 0.046 | 107.6 | 0.247 | 0.043 | 119.8 | 0.94 |
| 48 | 0.273 | 0.048 | 117.3 | 0.301 | 0.053 | 102.0 | 1.10 |
| 49 | 0.256 | 0.045 | 116.1 | 0.240 | 0.042 | 117.2 | 0.93 |
| 50 | 0.249 | 0.044 | 122.1 | 0.261 | 0.046 | 113.5 | 1.05 |
| 51 | 0.270 | 0.047 | 119.8 | 0.292 | 0.051 | 107.9 | 1.08 |
| 52 | 0.255 | 0.045 | 122.2 | 0.324 | 0.057 | 99.5 | 1.27 |
| 53 | 0.289 | 0.051 | 107.4 | 0.340 | 0.060 | 88.8 | 1.18 |
| 54 | 0.235 | 0.041 | 133.8 | 0.205 | 0.036 | 147.0 | 0.87 |
| 55 | 0.331 | 0.058 | 94.0 | 0.299 | 0.052 | 108.2 | 0.90 |
| μ | 0.308 | 0.054 | 92.7 | 0.310 | 0.054 | 97.2 | 0.96 |
| σ | 0.032 | 0.006 | 1.8 | 0.029 | 0.005 | 5.8 | - |
| LTE=Load Transfer Efficiency |
| JSR=Joint Support Ratio |
| Averages (μ) and standard deviations (σ) include only slabs with LTE less than 105% |

Table 21.  I-490 East 50.3 kN (11.3 kip) FWD, Slabs 26-55, October 26, 2004.

| Joint Number | Joint Approach | Joint Leave | JSR |
| --- | --- | --- | --- |
|  | Deflection | LTE | Deflection | LTE |  |
|  | (μm/kN) | (mil/kip) | (%) | (μm/kN) | (mil/kip) | (%) |  |
| STD Dowel Bar Arrangement |
| 26 | 0.394 | 0.069 | 91.1 | 0.397 | 0.070 | 85.1 | 1.01 |
| 27 | 0.381 | 0.067 | 88.4 | 0.394 | 0.069 | 80.1 | 1.03 |
| 28 | 0.385 | 0.067 | 82.3 | 0.383 | 0.067 | 78.9 | 0.99 |
| 29 | 0.386 | 0.068 | 92.9 | 0.427 | 0.075 | 82.7 | 1.11 |
| 30 | 0.396 | 0.069 | 86.5 | 0.383 | 0.067 | 86.9 | 0.97 |
| 31 | 0.334 | 0.058 | 89.1 | 0.364 | 0.064 | 79.8 | 1.09 |
| 32 | 0.362 | 0.063 | 86.8 | 0.359 | 0.063 | 85.1 | 0.99 |
| 33 | 0.333 | 0.058 | 87.4 | 0.356 | 0.062 | 76.8 | 1.07 |
| 34 | 0.342 | 0.060 | 80.1 | 0.354 | 0.062 | 74.0 | 1.04 |
| 35 | 0.336 | 0.059 | 80.1 | 0.346 | 0.061 | 75.4 | 1.03 |
| μ | 0.365 | 0.064 | 86.5 | 0.376 | 0.066 | 80.5 | 1.03 |
| σ | 0.027 | 0.005 | 4.4 | 0.025 | 0.004 | 4.4 | 0.05 |
| E1 Dowel Bar Arrangement |
| 36 | 0.463 | 0.081 | 52.9 | 0.435 | 0.076 | 60.3 | 0.94 |
| 37 | 0.386 | 0.068 | 85.3 | 0.371 | 0.065 | 84.7 | 0.96 |
| 38 | 0.401 | 0.070 | 85.8 | 0.426 | 0.075 | 78.1 | 1.06 |
| 39 | 0.396 | 0.069 | 86.5 | 0.415 | 0.073 | 80.3 | 1.05 |
| 40 | 0.381 | 0.067 | 90.8 | 0.395 | 0.069 | 83.6 | 1.04 |
| 41 | 0.384 | 0.067 | 87.3 | 0.400 | 0.070 | 83.5 | 1.04 |
| 42 | 0.370 | 0.065 | 82.5 | 0.373 | 0.065 | 82.1 | 1.01 |
| 43 | 0.367 | 0.064 | 86.7 | 0.360 | 0.063 | 83.9 | 0.98 |
| 44 | 0.337 | 0.059 | 87.2 | 0.341 | 0.060 | 84.0 | 1.01 |
| 45 | 0.336 | 0.059 | 90.2 | 0.342 | 0.060 | 87.0 | 1.02 |
| μ | 0.382 | 0.067 | 83.5 | 0.386 | 0.068 | 80.8 | 1.01 |
| σ | 0.036 | 0.006 | 11.0 | 0.034 | 0.006 | 7.6 | 0.04 |
| E2 Dowel Bar Arrangement |
| 46 | 0.328 | 0.057 | 89.6 | 0.337 | 0.059 | 85.5 | 1.03 |
| 47 | 0.349 | 0.061 | 92.8 | 0.352 | 0.062 | 91.3 | 1.01 |
| 48 | 0.369 | 0.065 | 94.2 | 0.385 | 0.067 | 87.3 | 1.04 |
| 49 | 0.347 | 0.061 | 91.5 | 0.352 | 0.062 | 87.1 | 1.01 |
| 50 | 0.318 | 0.056 | 102.9 | 0.339 | 0.059 | 93.3 | 1.07 |
| 51 | 0.364 | 0.064 | 94.1 | 0.369 | 0.065 | 90.2 | 1.01 |
| 52 | 0.351 | 0.061 | 97.7 | 0.366 | 0.064 | 92.5 | 1.04 |
| 53 | 0.370 | 0.065 | 89.0 | 0.378 | 0.066 | 84.4 | 1.02 |
| 54 | 0.356 | 0.062 | 93.6 | 0.350 | 0.061 | 91.9 | 0.98 |
| 55 | 0.334 | 0.058 | 101.4 | 0.358 | 0.063 | 94.9 | 1.07 |
| μ | 0.349 | 0.061 | 94.7 | 0.359 | 0.063 | 89.8 | 1.03 |
| σ | 0.018 | 0.003 | 4.6 | 0.016 | 0.003 | 3.6 | 0.03 |
| LTE=Load Transfer Efficiency |
| JSR=Joint Support Ratio |
| Averages (μ) and standard deviations (σ) include only slabs with LTE less than 105% |

When comparing the LTE’s for this group, the E2 slabs consistently had the highest efficiency.  Upon comparison of the STD and E1 sections, the STD sections generally had a higher LTE.  While this corresponds to the deflection data as well as the JSR results, it conflicts with the curling data gathered with the profilometer.  The profiles show the STD slabs with an average curling 1 mm (0.04 in or 40 mil) greater than the E1 sections and 1.2 mm (0.047 in or 47 mil) greater than the E2 sections.  To follow the trend established from Slabs 1 through 25, the STD slabs should experience more deflection and have lower LTE’s and JSR’s than the E1 slabs.  This discrepancy may be due to the fact that there was a slight difference between the time the profile surveys were collected and the FWD testing was conducted.  The FWD testing was conducted about 25 minutes after the profile was collected.  These data collections took place between 11:00 am and 12:00 pm while the air temperature was rising.  The rising air temperature may have caused the pavement gradient to rise significantly between the time of the profile and FWD, which would have resulted in the pavement flattening between the collections.  Therefore, the results from the slab warp and the LTE may not correspond directly.

The deflection data from the joints between slabs 56 to 84 displayed in Table 22 and Table 23 consistently show the E1 slabs deflecting the least.  During the 37.4 kN (8.4 kip) test weight the STD slabs deflected slightly less than the E2 sections while during the 50.3 kN (11.3 kip) test weight the E2 slabs deflected slightly less than the STD slabs.  This is not what is expected from the slab shapes; the E1 section had an average warp of 2.1 mm (0.083 in or 83 mil) while both the STD and E2 sections had an average warp of 1.9 mm (0.075 in or 75 mil) so the E1 section would be expected to deflect the most.

However, when these curling measurements are compared with the original warping of the slabs of up to 3.6 mm (0.14 in or 140 mil), the difference of 0.2 mm (0.008 in or 8 mil) between all three slab types becomes negligible.  Therefore since the slab curl is nearly the same for the three dowel bar arrangements, the differences in slab performance during this testing time is based primarily on the differences in dowel bar arrangement.

Upon comparing the LTE’s for the 37.4 kN (8.4 kip) testing, the E1 sections were most efficient for both the approach and leave tests.  The STD sections averaged slightly higher LTE’s than the E2 sections.  For the 50.3 kN (11.3 kip) testing, the E2 sections were most efficient followed closely by the STD sections then the E1 sections.  Within both approach and leave efficiencies test categories for both test weights, the difference between the three dowel bar arrangements never exceeded 4.6%.  In contrast, the LTE difference in some other test sections approached 11%.  The relatively close efficiencies of the 56 to 84 slab sections reinforces that the relaxation of the slabs due to temperature gradient increase resulted in similar slab reactions.

Table 22. I-490 East 37.4 kN (8.4 kip) FWD, Slabs 56-84, October 26, 2004.

| Joint Number | Joint Approach | Joint Leave | JSR |
| --- | --- | --- | --- |
|  | Deflection | LTE | Deflection | LTE |  |
|  | (μm/kN) | (mil/kip) | (%) | (μm/kN) | (mil/kip) | (%) |  |
| STD Dowel Bar Arrangement |
| 56 | 0.311 | 0.054 | 97.5 | 0.272 | 0.048 | 109.6 | 0.87 |
| 57 | 0.299 | 0.052 | 110.2 | 0.301 | 0.053 | 109.1 | 1.01 |
| 58 | 0.331 | 0.058 | 97.2 | 0.304 | 0.053 | 99.5 | 0.92 |
| 59 | 0.319 | 0.056 | 91.4 | 0.218 | 0.038 | 132.9 | 0.68 |
| 60 | 0.25 | 0.044 | 107.3 | 0.231 | 0.040 | 118.5 | 0.92 |
| 61 | 0.293 | 0.051 | 89.1 | 0.266 | 0.047 | 97.1 | 0.91 |
| 62 | 0.197 | 0.034 | 118.6 | 0.226 | 0.040 | 113.5 | 1.15 |
| 63 | 0.279 | 0.049 | 92.9 | 0.304 | 0.053 | 85.4 | 1.09 |
| 64 | 0.229 | 0.040 | 102.7 | 0.209 | 0.037 | 116.1 | 0.91 |
| 65 | 0.269 | 0.047 | 95.5 | 0.229 | 0.040 | 122.7 | 0.85 |
| μ | 0.290 | 0.051 | 95.2 | 0.291 | 0.051 | 94.0 | 0.97 |
| σ | 0.035 | 0.006 | 4.5 | 0.022 | 0.004 | 7.5 | 0.10 |
| E1 Dowel Bar Arrangement |
| 66 | 0.269 | 0.047 | 105.7 | 0.249 | 0.044 | 102.5 | 0.93 |
| 67 | 0.224 | 0.039 | 109.5 | 0.217 | 0.038 | 110.6 | 0.97 |
| 68 | 0.261 | 0.046 | 99.4 | 0.273 | 0.048 | 90.5 | 1.05 |
| 69 | 0.253 | 0.044 | 92.8 | 0.231 | 0.040 | 101.3 | 0.91 |
| 70 | 0.235 | 0.041 | 98.7 | 0.218 | 0.038 | 103.5 | 0.93 |
| 71 | 0.221 | 0.039 | 116.6 | 0.246 | 0.043 | 87.6 | 1.11 |
| 72 | 0.208 | 0.036 | 101.5 | 0.202 | 0.035 | 105.3 | 0.97 |
| 73 | 0.189 | 0.033 | 122.6 | 0.226 | 0.040 | 89.2 | 1.19 |
| 74 | 0.223 | 0.039 | 104.8 | 0.214 | 0.037 | 112.9 | 0.96 |
| 75 | 0.235 | 0.041 | 96.8 | 0.234 | 0.041 | 98.0 | 0.99 |
| μ | 0.236 | 0.041 | 99.0 | 0.239 | 0.042 | 96.1 | 0.97 |
| σ | 0.020 | 0.004 | 4.1 | 0.018 | 0.003 | 6.8 | 0.06 |
| E2 Dowel Bar Arrangement |
| 76 | 0.191 | 0.033 | 111.2 | 0.197 | 0.034 | 113.2 | 1.03 |
| 77 | 0.198 | 0.035 | 133.1 | 0.202 | 0.035 | 128.0 | 1.02 |
| 78 | 0.266 | 0.047 | 108.6 | 0.29 | 0.051 | 103.7 | 1.09 |
| 79 | 0.296 | 0.052 | 111.3 | 0.319 | 0.056 | 97.1 | 1.08 |
| 80 | 0.325 | 0.057 | 98.6 | 0.263 | 0.046 | 112.8 | 0.81 |
| 81 | 0.266 | 0.047 | 108.0 | 0.305 | 0.053 | 93.0 | 1.15 |
| 82 | 0.295 | 0.052 | 88.1 | 0.223 | 0.039 | 115.8 | 0.76 |
| 83 | 0.238 | 0.042 | 100.6 | 0.275 | 0.048 | 85.6 | 1.15 |
| 84 | 0.304 | 0.053 | 96.5 | 0.328 | 0.057 | 87.9 | 1.08 |
| μ | 0.290 | 0.051 | 96.0 | 0.304 | 0.053 | 93.5 | 1.12 |
| σ | 0.037 | 0.006 | 5.5 | 0.022 | 0.004 | 7.3 | 0.05 |
| LTE=Load Transfer Efficiency |
| JSR=Joint Support Ratio |
| Averages (μ) and standard deviations (σ) include only slabs with LTE less than 105% |

Table 23. I-490 East 50.3 kN (11.3 kip) FWD, Slabs 56-84, October 26, 2004.

| Joint Number | Joint Approach | Joint Leave | JSR |
| --- | --- | --- | --- |
|  | Deflection | LTE | Deflection | LTE |  |
|  | (μm/kN) | (mil/kip) | (%) | (μm/kN) | (mil/kip) | (%) |  |
| STD Dowel Bar Arrangement |
| 56 | 0.354 | 0.062 | 94.6 | 0.356 | 0.062 | 92.4 | 1.01 |
| 57 | 0.367 | 0.064 | 97.8 | 0.368 | 0.064 | 94.8 | 1.00 |
| 58 | 0.397 | 0.070 | 84.9 | 0.378 | 0.066 | 87.1 | 0.95 |
| 59 | 0.361 | 0.063 | 88.1 | 0.376 | 0.066 | 84.3 | 1.04 |
| 60 | 0.354 | 0.062 | 85.6 | 0.356 | 0.062 | 81.5 | 1.01 |
| 61 | 0.337 | 0.059 | 85.2 | 0.338 | 0.059 | 83.9 | 1.00 |
| 62 | 0.320 | 0.056 | 83.3 | 0.342 | 0.060 | 80.4 | 1.07 |
| 63 | 0.342 | 0.060 | 83.1 | 0.335 | 0.059 | 81.0 | 0.98 |
| 64 | 0.321 | 0.056 | 82.3 | 0.334 | 0.058 | 78.9 | 1.04 |
| 65 | 0.372 | 0.065 | 78.7 | 0.389 | 0.068 | 74.3 | 1.05 |
| μ | 0.353 | 0.062 | 86.3 | 0.357 | 0.063 | 83.9 | 1.01 |
| σ | 0.024 | 0.004 | 5.8 | 0.020 | 0.004 | 6.2 | 0.03 |
| E1 Dowel Bar Arrangement |
| 66 | 0.328 | 0.057 | 94.8 | 0.358 | 0.063 | 76.2 | 1.09 |
| 67 | 0.317 | 0.056 | 84.2 | 0.329 | 0.058 | 80.3 | 1.04 |
| 68 | 0.343 | 0.060 | 82.5 | 0.346 | 0.061 | 79.3 | 1.01 |
| 69 | 0.317 | 0.056 | 82.1 | 0.319 | 0.056 | 80.4 | 1.01 |
| 70 | 0.338 | 0.059 | 76.5 | 0.313 | 0.055 | 79.7 | 0.93 |
| 71 | 0.301 | 0.053 | 97.7 | 0.301 | 0.053 | 78.5 | 1.00 |
| 72 | 0.307 | 0.054 | 76.7 | 0.309 | 0.054 | 76.8 | 1.01 |
| 73 | 0.283 | 0.050 | 94.0 | 0.274 | 0.048 | 85.1 | 0.97 |
| 74 | 0.336 | 0.059 | 91.2 | 0.286 | 0.050 | 88.5 | 0.85 |
| 75 | 0.303 | 0.053 | 83.1 | 0.300 | 0.053 | 84.8 | 0.99 |
| μ | 0.317 | 0.056 | 86.3 | 0.313 | 0.055 | 81.0 | 0.99 |
| σ | 0.019 | 0.003 | 7.6 | 0.026 | 0.005 | 3.9 | 0.06 |
| E2 Dowel Bar Arrangement |
| 76 | 0.297 | 0.052 | 81.7 | 0.299 | 0.052 | 80.2 | 1.00 |
| 77 | 0.296 | 0.052 | 100.0 | 0.317 | 0.056 | 84.9 | 1.07 |
| 78 | 0.366 | 0.064 | 91.3 | 0.391 | 0.068 | 83.7 | 1.07 |
| 79 | 0.394 | 0.069 | 89.9 | 0.384 | 0.067 | 88.5 | 0.97 |
| 80 | 0.396 | 0.069 | 84.2 | 0.373 | 0.065 | 87.2 | 0.94 |
| 81 | 0.351 | 0.061 | 89.0 | 0.366 | 0.064 | 84.5 | 1.04 |
| 82 | 0.341 | 0.060 | 85.0 | 0.335 | 0.059 | 83.7 | 0.98 |
| 83 | 0.330 | 0.058 | 83.5 | 0.328 | 0.057 | 83.4 | 0.99 |
| 84 | 0.375 | 0.066 | 87.0 | 0.371 | 0.065 | 87.2 | 0.99 |
| μ | 0.350 | 0.061 | 88.0 | 0.351 | 0.061 | 84.8 | 1.01 |
| σ | 0.037 | 0.006 | 5.5 | 0.033 | 0.006 | 2.5 | 0.04 |
| LTE=Load Transfer Efficiency |
| JSR=Joint Support Ratio |
| Averages (μ) and standard deviations (σ) include only slabs with LTE less than 105% |

### October 2006 FWD testing results

Testing on the west bound lanes was conducted on October 11, 2006; the weather was windy and raining which did not allow us to collect any dipstick data.  Falling weight deflectometer tests were conducted both in the morning and afternoon according to the previously illustrated pattern, but due to traffic control limits, the outer wheel path could not be collected.  No distress was observed in the 1.6 km (1 mi) traffic control zone that was provided. A summary of the data from the westbound lanes is in Table 24.  The full set of data is provided in Appendix D.

Testing on the eastbound lanes was conducted on October 12, 2006; the weather conditions were clear but cold.  Falling weight load transfer measurements as well as mid-panel drops on the dowel bar test sections were conducted.  Due to traffic control limitations, the FWD vehicle could not be positioned safely to collect any meaningful data from the tie bar sections.  A summary of the results is provided in Table 25.

The test section was inspected for distresses but none were observed.

Table 24.  FWD data averages and standard deviations for I-490 West, Monroe, Rochester on morning and afternoon of Oct. 11, 2006.

|  | Load | DO L | DO M | LTE L | SPR | D3/D0 M |
| --- | --- | --- | --- | --- | --- | --- |
| Morning | (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |
| Average | 10 | 44 | 0.9208 | 5.2581 | 0.6029 | 3.4426 | 82.96% | 84.58% | 0.9388 |
| Std. Dev. | 0 | 0 | 0.3010 | 1.7189 | 0.2693 | 1.5377 | 1.09% | 7.36% | 0.0352 |
| Average | 13 | 58 | 0.9208 | 5.2581 | 0.6029 | 3.4426 | 82.96% | 84.58% | 0.9388 |
| Std. Dev. | 0 | 0 | 0.3010 | 1.7189 | 0.2693 | 1.5377 | 1.09% | 7.36% | 0.0352 |
| Average | 16 | 71 | 0.8604 | 4.9129 | 0.5731 | 3.2725 | 82.65% | 84.43% | 0.9327 |
| Std. Dev. | 0 | 0 | 0.2495 | 1.4245 | 0.2402 | 1.3718 | 1.04% | 7.05% | 0.0346 |
| Afternoon |
| Average | 10 | 44 | 0.9698 | 5.5375 | 0.6192 | 3.5358 | 83.77% | 83.77% | 0.9432 |
| Std. Dev. | 0 | 0 | 0.2986 | 1.7048 | 0.2939 | 1.6782 | 1.81% | 7.20% | 0.0496 |
| Average | 13 | 58 | 0.9451 | 5.3966 | 0.6114 | 3.4913 | 83.44% | 83.66% | 0.9343 |
| Std. Dev. | 0 | 0 | 0.2763 | 1.5780 | 0.2800 | 1.5989 | 1.77% | 6.98% | 0.0494 |
| Average | 16 | 71 | 0.9069 | 5.1785 | 0.5919 | 3.3799 | 83.35% | 83.73% | 0.9366 |
| Std. Dev. | 0 | 0 | 0.2553 | 1.4575 | 0.2651 | 1.5136 | 1.79% | 6.72% | 0.0487 |

Table 25.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on October 12, 2006 for different dowel bar configurations.

| Standard dowels | Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| Average | 10 | 44 | 0.5888 | 3.3619 | 0.5657 | 3.2305 | 0.2471 | 1.4109 | 82.39% | 80.25% | 86.26% | 0.9286 | 0.9817 |
| Std. Dev. | 0 | 0 | 0.1530 | 0.8735 | 0.1823 | 1.0411 | 0.0347 | 0.1979 | 0.88% | 0.85% | 7.40% | 0.0269 | 0.0971 |
| Average | 13 | 58 | 0.5820 | 3.3233 | 0.5641 | 3.2210 | 0.2523 | 1.4406 | 82.10% | 80.05% | 86.07% | 0.9218 | 0.9818 |
| Std. Dev. | 0 | 0 | 0.1415 | 0.8079 | 0.1721 | 0.9829 | 0.0336 | 0.1918 | 1.00% | 1.04% | 7.01% | 0.0291 | 0.0906 |
| Average | 16 | 71 | 0.5694 | 3.2513 | 0.5534 | 3.1601 | 0.2535 | 1.4475 | 81.92% | 80.04% | 86.03% | 0.9186 | 0.9825 |
| Std. Dev. | 0 | 0 | 0.1324 | 0.7561 | 0.1567 | 0.8947 | 0.0328 | 0.1871 | 0.81% | 0.79% | 6.83% | 0.0259 | 0.0792 |
| E1 dowel bar configuration |
| Average | 10 | 44 | 0.5646 | 3.2238 | 0.5600 | 3.1974 | 0.2533 | 1.4464 | 82.22% | 80.06% | 84.26% | 0.9261 | 0.9581 |
| Std. Dev. | 0 | 0 | 0.1297 | 0.5523 | 0.1197 | 0.6833 | 0.0256 | 0.1462 | 1.11% | 1.29% | 1.99% | 0.0148 | 0.0641 |
| Average | 13 | 58 | 0.5581 | 3.1868 | 0.5533 | 3.1595 | 0.2571 | 1.4681 | 82.02% | 80.18% | 83.80% | 0.9203 | 0.9591 |
| Std. Dev. | 0 | 0 | 0.1188 | 0.5109 | 0.1106 | 0.6313 | 0.0248 | 0.1417 | 0.92% | 1.25% | 1.81% | 0.0139 | 0.0603 |
| Average | 16 | 71 | 0.5440 | 3.1065 | 0.5426 | 3.0981 | 0.2574 | 1.4699 | 81.89% | 80.09% | 83.65% | 0.9227 | 0.9608 |
| Std. Dev. | 0 | 0 | 0.1060 | 0.4593 | 0.1010 | 0.5770 | 0.0241 | 0.1378 | 0.92% | 1.13% | 1.75% | 0.0116 | 0.0561 |
| E2 dowel bar configuration |
| Average | 10 | 44 | 0.4914 | 2.8058 | 0.4709 | 2.6888 | 0.2411 | 1.3766 | 82.37% | 80.21% | 84.19% | 0.9220 | 0.9939 |
| Std. Dev. | 0 | 0 | 0.0809 | 0.2001 | 0.0366 | 0.2088 | 0.0123 | 0.0701 | 0.59% | 1.00% | 1.06% | 0.0094 | 0.0834 |
| Average | 13 | 58 | 0.4884 | 2.7887 | 0.4678 | 2.6714 | 0.2446 | 1.3970 | 82.15% | 80.38% | 83.78% | 0.9197 | 0.9926 |
| Std. Dev. | 0 | 0 | 0.0753 | 0.1957 | 0.0343 | 0.1958 | 0.0134 | 0.0765 | 0.82% | 1.10% | 0.98% | 0.0082 | 0.0764 |
| Average | 16 | 71 | 0.4803 | 2.7427 | 0.4639 | 2.6490 | 0.2447 | 1.3973 | 82.02% | 79.94% | 83.81% | 0.9165 | 0.9914 |
| Std. Dev. | 0 | 0 | 0.0684 | 0.1837 | 0.0320 | 0.1829 | 0.0159 | 0.0909 | 0.55% | 0.88% | 1.11% | 0.0109 | 0.0740 |

### September 2007 testing results

Testing on the westbound lanes was conducted on September 11, 2007.  No visible distress was recorded on the instrumented slabs, but in the traffic control zone, east of the instrumentation section, three slabs had corner breaks.  No faulting was recorded.  Testing on the eastbound lanes was conducted on September 12, 2007.  FWD testing was conducted on the dowel bar test sections.  Faultmeter readings were conducted on the tie bar sections but no faulting was recorded.

### September 2008 testing results

Testing on the westbound lanes was conducted on September 24, 2008.  Falling weight deflectometer testing was conducted on the sections, with the falling weight applying loads on the approach and leave of each joint as well as mid panel drops.  A summary of the data from the westbound lanes is in Table 26.  The full set of data is provided in Appendix E.   Testing on the eastbound lanes was conducted on September 25, 2008; the weather conditions were clear but cold.  Falling weight load transfer measurements as well as mid-panel drops on the dowel bar test sections were conducted.  Due to traffic control limitations, the FWD vehicle could not be positioned safely to collect any meaningful data from the tie bar sections.  A summary of the results is provided in Table 27.

A comprehensive distress survey was also conducted on September 24, 2008 starting at westbound station 36.4 to include all visible lanes of traffic.  The distress summary is presented in Table 28.  A comprehensive distress survey of the eastbound lanes was conducted on the following day and the results are given in Table 29.  Multiple slabs had “pop outs” but these were noted as minor and not affecting the overall quality of the pavement.

Table 26.  FWD data averages and standard deviations for I-490 West, Monroe, Rochester on September 24, 2008.

|  | Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| Average | 10 | 44 | 0.6701 | 3.8263 | 0.6198 | 3.5389 | 0.2268 | 1.2951 | 80.77% | 83.11% | 88.18% | 0.9325 | 1.0002 |
| Std. Dev. | 0 | 0 | 0.1082 | 0.6178 | 0.1013 | 0.5785 | 0.0296 | 0.1693 | 1.41% | 1.66% | 4.27% | 0.0301 | 0.1299 |
| Average | 13 | 58 | 0.6583 | 3.7592 | 0.6128 | 3.4995 | 0.2291 | 1.3084 | 80.90% | 82.90% | 88.53% | 0.9302 | 0.9991 |
| Std. Dev. | 0 | 0 | 0.1053 | 0.6011 | 0.0943 | 0.5387 | 0.0294 | 0.1677 | 1.26% | 1.30% | 4.40% | 0.0231 | 0.1192 |
| Average | 16 | 71 | 0.6280 | 3.5862 | 0.5867 | 3.3503 | 0.2244 | 1.2815 | 83.14% | 69.73% | 87.87% | 0.9338 | 0.9983 |
| Std. Dev. | 0 | 0 | 0.0959 | 0.5474 | 0.0874 | 0.4988 | 0.0274 | 0.1565 | 1.16% | 31.10% | 4.86% | 0.0247 | 0.1133 |

Table 27.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on September 25, 2008 for different dowel bar configurations.

| Standard dowels | Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| Average | 10 | 44 | 0.4118 | 2.3515 | 0.3797 | 2.1680 | 0.1960 | 1.1193 | 80.84% | 83.79% | 80.52% | 0.9232 | 1.0712 |
| Std. Dev. | 0 | 0 | 0.2327 | 1.3286 | 0.2075 | 1.1849 | 0.0560 | 0.3196 | 1.25% | 2.77% | 13.16% | 0.0437 | 0.3995 |
| Average | 13 | 58 | 0.4087 | 2.3337 | 0.3843 | 2.1945 | 0.2019 | 1.1527 | 80.94% | 83.44% | 80.20% | 0.9392 | 1.0550 |
| Std. Dev. | 0 | 0 | 0.2285 | 1.3050 | 0.2022 | 1.1547 | 0.0553 | 0.3158 | 2.42% | 3.86% | 12.85% | 0.0235 | 0.3732 |
| Average | 16 | 71 | 0.3204 | 1.8297 | 0.2934 | 1.6755 | 0.1273 | 0.7269 | 81.46% | 83.64% | 46.68% | 0.4824 | 0.7247 |
| Std. Dev. | 0 | 0 | 0.1037 | 0.5923 | 0.1023 | 0.5842 | 0.0828 | 0.4726 | 2.33% | 1.86% | 38.89% | 0.5183 | 0.3909 |
| E1 dowel bar configuration |
| Average | 10 | 44 | 0.3539 | 2.0209 | 0.3249 | 1.8554 | 0.2010 | 1.1479 | 80.54% | 82.94% | 78.24% | 0.8905 | 0.9454 |
| Std. Dev. | 0 | 0 | 0.1572 | 0.8976 | 0.1393 | 0.7956 | 0.0431 | 0.2462 | 1.98% | 2.04% | 10.51% | 0.1804 | 0.1422 |
| Average | 13 | 58 | 0.3506 | 2.0017 | 0.3222 | 1.8398 | 0.1982 | 1.1318 | 81.02% | 83.21% | 80.29% | 0.9284 | 0.9566 |
| Std. Dev. | 0 | 0 | 0.1527 | 0.8718 | 0.1319 | 0.7533 | 0.0588 | 0.3356 | 1.64% | 1.58% | 8.21% | 0.0254 | 0.1445 |
| Average | 16 | 71 | 0.3406 | 1.9450 | 0.3007 | 1.7171 | 0.1982 | 1.1318 | 80.90% | 83.42% | 80.29% | 0.9284 | 0.9587 |
| Std. Dev. | 0 | 0 | 0.1372 | 0.7836 | 0.1323 | 0.7556 | 0.0588 | 0.3356 | 1.85% | 1.70% | 8.21% | 0.0254 | 0.1255 |
| E2 dowel bar configuration |
| Average | 10 | 44 | 0.2316 | 1.3227 | 0.1883 | 1.0750 | 0.1555 | 0.8880 | 82.45% | 85.13% | 77.57% | 0.9238 | 1.0652 |
| Std. Dev. | 0 | 0 | 0.0914 | 0.5218 | 0.0521 | 0.2976 | 0.0517 | 0.2952 | 2.52% | 8.21% | 10.13% | 0.0284 | 0.3037 |
| Average | 13 | 58 | 0.2338 | 1.3353 | 0.2064 | 1.1786 | 0.1611 | 0.9199 | 82.60% | 84.31% | 79.85% | 0.9247 | 1.0363 |
| Std. Dev. | 0 | 0 | 0.0914 | 0.5217 | 0.0354 | 0.2019 | 0.0409 | 0.2337 | 2.37% | 2.13% | 6.85% | 0.0334 | 0.1680 |
| Average | 16 | 71 | 0.2405 | 1.3733 | 0.2162 | 1.2344 | 0.1701 | 0.9715 | 82.71% | 84.67% | 81.54% | 0.9180 | 1.0230 |
| Std. Dev. | 0 | 0 | 0.0816 | 0.4660 | 0.0346 | 0.1976 | 0.0282 | 0.1609 | 1.87% | 2.05% | 4.49% | 0.0226 | 0.1285 |

Table 28.  Distress Survey, I 490 Westbound September 2008

| Slab No. | Distress Type |
| --- | --- |
| 0 | Start Station W 36.4 |
| 1 | North west corner crack in center lane |
| 7 | Transverse mark in inner lane (Crack or finish error) |
| 8 | Small crack on the north edge |
| 10 | South East corner minor crack in center lane |
| 15 | South West corner, 1 foot minor edge crack in the center lane |
| 16 | 4901 4403 1106 Sign - Slab 0 |
| 4 | Outer lane center spalling |
| 9 | Inner lane finish problem |
| 11 | Inner lane finish problem |
| 12 | North East corner center lane corner crack 600 mm (2 ft) length x 150 mm (6 in) |
| 15 | North East corner center lane corner crack 300 m (1ft) length x 75 mm (3 in) |
| 16 | Station W 36.3 |
| 1 | North West corner crack in center lane w/ missing concrete 75 mm (3 in) x 50 mm (2 in) |
| 2 | Inner lane finish problem |
| 3 | Inner lane, polished aggregate slab |
| 4 | Inner lane, polished aggregate slab |
| 5 | Inner lane, polished aggregate slab |
| 6 | Inner lane, polished aggregate slab |
| 7 | Inner lane, polished aggregate slab |
| 8 | inner lane, polished aggregate slab (25%) |
| 14 | 4901 4403 1005 sign -Slab 0 |
| 6 | Center lane spalling in center |
| 10 | Inner lane finish problem |
| 16 | Inner lane finish problem |
| 18 | Station W 36.2 |
| 1 | Inner lane, polished aggregate |
| 2 | Inner lane, polished aggregate |
| 3 | Inner lane, polished aggregate |
| 4 | Inner lane, polished aggregate |
| 5 | Inner lane, polished aggregate |
| 6 | Inner lane, polished aggregate |
| 7 | Inner lane, polished aggregate |
| 8 | Inner lane, polished aggregate |
| 9 | Inner lane, polished aggregate |
| 10 | Inner lane, polished aggregate |
| 11 | Inner lane, polished aggregate |
| 12 | Inner lane, polished aggregate |

Table 29.  Distress survey, I490 eastbound September 2008

| Slab No. | Distress Type |
| --- | --- |
| 0 | Station E 36.3 |
| 6 | Joint inner lane, minor crack |
| 15 | Joint installation problem |
| 21 | South East Corner crack outer lane 200 mm (8 in) x 150 mm (6 in) |
| 32 | Station E 36.2 |
| 15 | Edge joint blow up (Due to truck accident) 300 mm (1 ft) x 75 mm (3 in) |
| 31 | Station E 36.1 |
| 5 | Small blowup (25 mm (1 in) x 75 mm (3 in)) |
| 7 | Longitudinal crack inner lane |
| 8 | Longitudinal crack inner lane |
| 10 | Longitudinal crack inner lane |
| 13 | Longitudinal crack inner lane |
| 48 | Edge joint 50 mm (2 in) x 25 mm (1 in) Center lane South West Corner |
| 64 | Station E 35.9 |

### August 2009 testing results

The westbound sections were tested on August 18th; the distress survey results are tabulated in Table 30.  Pictures of the corner cracks are in Figure 11.  Average pavement temperature during this test was 88ºF (31ºC).  During this site visit the sensors were checked but were still non-responsive.

Table 30.  I490W Distress survey, August 2009

| Slab No. | Distress Type |
| --- | --- |
| 0 | Station W 36.4 |
| 1 | Corner crack - 2nd lane |
| 2 | Corner crack - 3rd lane |
| 10 | Corner crack - 3rd lane |
| 29 | Corner crack - 2nd lane |
| 32 | Corner crack - 2nd lane |
| 33 | Corner crack - 2nd lane |
| 34 | Corner crack - 2nd lane |
| 36 | Corner crack - 2nd lane |
| 116 | Edge of Rest Area , Past Station W 36.1 |

The eastbound lanes on I490 were tested on August 19, 2009.  The distress is documented in Table 31.  Falling weight deflectometer readings were conducted on the dowel bar test sections.   The FWD data averages and standard deviations by dowel bar configuration are presented in Table 32.  The full set of data is provided in Appendix F.

Table 31.  I490E Distress survey, August 2009

| Slab No. | Distress Type |
| --- | --- |
| 0 | Station W 36.2 |
| W 35.6 | 2 slabs, center lane, concrete missing |
| General | Some construction pop outs, polished aggregates, minor surface cracks |

Figure 11.  Corner cracks identified on I490W distress survey, August 2009.

Table 32.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on Aug. 19, 2009 for different dowel bar configurations.

| Standard dowels | Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| Average | 10 | 44 | 0.2547 | 1.4545 | 0.2596 | 1.4825 | 0.1558 | 0.8899 | 82.86% | 83.16% | 82.29% | 0.9298 | 0.9884 |
| Std. Dev. | 0 | 0 | 0.0527 | 0.3007 | 0.0551 | 0.3147 | 0.0186 | 0.1063 | 3.08% | 6.78% | 6.43% | 0.0532 | 0.1230 |
| Average | 13 | 58 | 0.2569 | 1.4671 | 0.2588 | 1.4777 | 0.1582 | 0.9036 | 83.16% | 82.94% | 78.99% | 0.8679 | 0.9920 |
| Std. Dev. | 0 | 0 | 0.0538 | 0.3072 | 0.0564 | 0.3220 | 0.0176 | 0.1008 | 2.54% | 5.68% | 6.96% | 0.2330 | 0.1301 |
| Average | 18 | 80 | 0.2506 | 1.4307 | 0.2532 | 1.4456 | 0.1547 | 0.8836 | 83.16% | 82.61% | 84.35% | 0.9052 | 0.9864 |
| Std. Dev. | 0 | 0 | 0.0484 | 0.2762 | 0.0493 | 0.2817 | 0.0167 | 0.0954 | 1.17% | 3.87% | 5.83% | 0.0175 | 0.1091 |
| E1 dowel bar configuration |
| Average | 10 | 44 | 0.2923 | 1.6689 | 0.2913 | 1.6632 | 0.1787 | 1.0204 | 83.03% | 79.25% | 83.89% | 0.9053 | 1.0090 |
| Std. Dev. | 0 | 0 | 0.0704 | 0.4019 | 0.0687 | 0.3921 | 0.0104 | 0.0593 | 2.79% | 6.31% | 4.53% | 0.0336 | 0.1825 |
| Average | 13 | 58 | 0.2955 | 1.6874 | 0.2918 | 1.6665 | 0.1796 | 1.0254 | 83.50% | 82.36% | 83.77% | 0.9223 | 1.0101 |
| Std. Dev. | 0 | 0 | 0.0689 | 0.3934 | 0.0686 | 0.3920 | 0.0105 | 0.0597 | 2.48% | 6.26% | 8.50% | 0.0255 | 0.1673 |
| Average | 18 | 80 | 0.2860 | 1.6332 | 0.2832 | 1.6170 | 0.1766 | 1.0084 | 83.54% | 83.98% | 82.19% | 0.9196 | 1.0057 |
| Std. Dev. | 0 | 0 | 0.0642 | 0.3665 | 0.0613 | 0.3500 | 0.0086 | 0.0493 | 1.44% | 5.51% | 5.60% | 0.0222 | 0.1619 |
| E2 dowel bar configuration |
| Average | 10 | 44 | 0.2641 | 1.5083 | 0.2617 | 1.4941 | 0.1756 | 1.0028 | 84.17% | 80.56% | 83.37% | 0.9083 | 0.9867 |
| Std. Dev. | 0 | 0 | 0.0577 | 0.3296 | 0.0588 | 0.3360 | 0.0166 | 0.0948 | 2.00% | 8.79% | 8.05% | 0.0309 | 0.1507 |
| Average | 13 | 58 | 0.2655 | 1.5163 | 0.2626 | 1.4994 | 0.1775 | 1.0133 | 84.60% | 83.39% | 82.36% | 0.9127 | 0.9896 |
| Std. Dev. | 0 | 0 | 0.0590 | 0.3368 | 0.0577 | 0.3297 | 0.0129 | 0.0739 | 1.33% | 5.37% | 9.31% | 0.0158 | 0.1545 |
| Average | 18 | 80 | 0.2568 | 1.4662 | 0.2580 | 1.4731 | 0.1722 | 0.9831 | 85.43% | 82.79% | 85.24% | 0.9184 | 0.9876 |
| Std. Dev. | 0 | 0 | 0.0523 | 0.2988 | 0.0530 | 0.3029 | 0.0114 | 0.0648 | 2.74% | 4.91% | 5.58% | 0.0166 | 0.1467 |

### June 2011 testing results

The eastbound lanes were tested on June 21, 2011.  Falling weight deflectometer testing as well as faulting and distress survey were conducted on these sections.  Due to delays in traffic control implementation, the section testing did not start until 11:00 AM.  The traffic control configuration also excluded the standard dowel bar configuration sections from testing.  The surface temperature at that time was 40.6°C (105ºF).  Distress survey did not show any additional distress beyond what was documented in the previous visits.  Faulting survey did not indicate any faulting at any of the joints.  At mid-day, the falling weight machine suffered an electrical failure and testing was stopped for the day.

The westbound sections were scheduled to be tested on June 22, 2011.  Traffic control closed the lanes, but the FWD machine was not available for testing.  Distress survey did not show any additional distress beyond what was documented previously.  Prior to starting faultmeter readings, a severe thunderstorm went through the area and the traffic control operation had to be discontinued.  Further testing was not able to be scheduled due to time and effort conflicts with the NYDOT office in Rochester.

FWD data summary from the eastbound lanes is shown in Table 33.  As can be seen from this table the load transfer efficiencies are on average around 80% after more than 11 years of service.  The full set of data is given in Appendix G.

### Summary of FWD results

Table 34 and Table 35 respectively summarize the approach and leave data collected using the FWD over the course of the project.  For each treatment on each date, the data include the load, the average load transfer efficiency, the standard deviation, and the standard deviation of the mean (the standard deviation divided by the square root of the number of measurements made). While the last data points, taken in June 2011, appear to show that the E2 configuration has the highest LTE, it should be noted that only two measurements of E2 LTEs (compared to 25 or more of the other configurations) were conducted before the FWD malfunctioned.  On earlier dates the LTEs of the three configurations are comparable.  In all cases, the LTEs are at or above the 80% criterion, within error limits, except for E1 in June 2011, which was about 76% at all loads.

Table 33.  FWD data averages and standard deviations for I-490 East, Monroe, Rochester on June 21, 2011 for different dowel bar configurations.

| E1 dowels | Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| Average | 10 | 44 | 0.3786 | 2.1621 | 0.3589 | 2.0491 | 0.1676 | 0.9571 | 82.92% | 80.12% | 90.74% | 0.9193 | 1.0571 |
| Std. Dev. | 0 | 0 | 0.0597 | 0.3412 | 0.0595 | 0.3396 | 0.0122 | 0.0696 | 1.28% | 1.63% | 3.85% | 0.0124 | 0.0378 |
| Average | 13 | 58 | 0.3774 | 2.1548 | 0.3573 | 2.0400 | 0.1684 | 0.9617 | 82.63% | 80.92% | 89.30% | 0.9232 | 1.0597 |
| Std. Dev. | 0 | 0 | 0.0558 | 0.3188 | 0.0582 | 0.3324 | 0.0114 | 0.0654 | 0.94% | 1.30% | 3.25% | 0.0138 | 0.0390 |
| Average | 18 | 80 | 0.3618 | 2.0660 | 0.3442 | 1.9657 | 0.1657 | 0.9463 | 81.86% | 80.17% | 89.31% | 0.9088 | 1.0549 |
| Std. Dev. | 0 | 0 | 0.0510 | 0.2913 | 0.0534 | 0.3049 | 0.0098 | 0.0562 | 1.04% | 1.09% | 2.85% | 0.0134 | 0.0375 |
| E2 dowel bar configuration |
| Average | 10 | 44 | 0.2601 | 1.4853 | 0.2481 | 1.4164 | 0.1687 | 0.9631 | 79.66% | 75.66% | 81.88% | 0.8896 | 1.0490 |
| Std. Dev. | 0 | 0 | 0.0197 | 0.1123 | 0.0183 | 0.1046 | 0.0093 | 0.0531 | 1.32% | 1.90% | 2.29% | 0.0108 | 0.0350 |
| Average | 13 | 58 | 0.2633 | 1.5032 | 0.2484 | 1.4186 | 0.1706 | 0.9741 | 79.45% | 76.56% | 80.76% | 0.8954 | 1.0600 |
| Std. Dev. | 0 | 0 | 0.0186 | 0.1065 | 0.0180 | 0.1026 | 0.0084 | 0.0479 | 1.10% | 1.37% | 1.58% | 0.0115 | 0.0267 |
| Average | 18 | 80 | 0.2618 | 1.4947 | 0.2485 | 1.4190 | 0.1728 | 0.9870 | 78.76% | 76.00% | 80.66% | 0.8831 | 1.0540 |
| Std. Dev. | 0 | 0 | 0.0169 | 0.0964 | 0.0168 | 0.0962 | 0.0086 | 0.0490 | 0.80% | 1.14% | 1.17% | 0.0095 | 0.0296 |
| E1 dowel bar configuration |
| Average | 10 | 44 | 0.2268 | 1.2953 | 0.2343 | 1.3382 | 0.1832 | 1.0459 | 89.89% | 86.39% | 86.37% | 0.9075 | 0.9658 |
| Std. Dev. | 0 | 0 | 0.0368 | 0.2102 | 0.0299 | 0.1710 | 0.0091 | 0.0522 | 2.81% | 0.48% | 6.42% | 0.0169 | 0.0337 |
| Average | 13 | 58 | 0.2308 | 1.3180 | 0.2359 | 1.3468 | 0.1852 | 1.0575 | 90.32% | 87.61% | 85.14% | 0.9159 | 0.9766 |
| Std. Dev. | 0 | 0 | 0.0374 | 0.2134 | 0.0311 | 0.1774 | 0.0119 | 0.0680 | 2.03% | 2.03% | 5.88% | 0.0158 | 0.0298 |
| Average | 18 | 80 | 0.2200 | 1.2563 | 0.2269 | 1.2954 | 0.1814 | 1.0359 | 89.66% | 86.67% | 84.81% | 0.1814 | 0.9670 |
| Std. Dev. | 0 | 0 | 0.0365 | 0.2086 | 0.0265 | 0.1511 | 0.0092 | 0.0523 | 3.50% | 0.74% | 5.76% | 0.0092 | 0.0482 |

Table 34.  Summary of average approach LTEs by date, with  standard deviation and standard deviation of the mean.

| Standard dowels | Load (kip) | Load (kN) | Direction | Average | Std. Dev. | SD of M | Load (kip) | Load (kN) | Average | Std. Dev. | SD of M | Load (kip) | Load (kN) | Average | Std. Dev. | SD of M |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 26-Oct-04 | 8.4 | 37.4 | A | 90.55% | 9.86% | 2.15% | 11.3 | 50.3 | 86.08% | 4.58% | 0.92% |  |  |  |  |  |
| 12-Oct-06 | 10 | 44 | A | 80.25% | 0.85% | 0.20% | 13 | 58 | 80.05% | 1.04% | 0.25% | 16 | 71 | 80.04% | 0.79% | 0.19% |
| 25-Sep-08 | 10 | 44 | A | 83.79% | 2.77% | 0.55% | 13 | 58 | 83.44% | 3.86% | 0.77% | 16 | 71 | 83.64% | 1.86% | 0.37% |
| 19-Aug-09 | 10 | 44 | A | 83.16% | 6.78% | 1.70% | 13 | 58 | 82.94% | 5.68% | 1.42% | 18 | 80 | 82.61% | 3.87% | 0.97% |
| 21-Jun-11 | 10 | 44 | A | 80.11% | 1.67% | 0.33% | 13 | 58 | 80.89% | 1.27% | 0.25% | 18 | 80 | 80.23% | 1.16% | 0.23% |
| E1 dowel bar configuration |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 26-Oct-04 | 8.4 | 37.4 | A | 93.38% | 10.05% | 2.19% | 11.3 | 50.3 | 84.51% | 7.99% | 1.46% |  |  |  |  |  |
| 12-Oct-06 | 10 | 44 | A | 80.06% | 1.29% | 0.26% | 13 | 58 | 80.18% | 1.25% | 0.25% | 16 | 71 | 80.09% | 1.13% | 0.23% |
| 25-Sep-08 | 10 | 44 | A | 80.54% | 1.98% | 0.39% | 13 | 58 | 81.02% | 1.64% | 0.32% | 16 | 71 | 83.42% | 1.70% | 0.33% |
| 19-Aug-09 | 10 | 44 | A | 79.25% | 6.31% | 1.45% | 13 | 58 | 82.36% | 6.26% | 1.40% | 18 | 80 | 83.98% | 5.51% | 1.23% |
| 21-Jun-11 | 10 | 44 | A | 75.58% | 1.84% | 0.36% | 13 | 58 | 76.45% | 1.32% | 0.26% | 18 | 80 | 75.98% | 1.22% | 0.24% |
| E2 dowel bar configuration |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 26-Oct-04 | 8.4 | 37.4 | A | 93.81% | 3.74% | 1.00% | 11.3 | 50.3 | 90.08% | 5.98% | 1.11% |  |  |  |  |  |
| 12-Oct-06 | 10 | 44 | A | 80.21% | 1.00% | 0.20% | 13 | 58 | 80.38% | 1.10% | 0.22% | 16 | 71 | 79.94% | 0.88% | 0.18% |
| 25-Sep-08 | 10 | 44 | A | 85.13% | 8.21% | 1.52% | 13 | 58 | 84.31% | 2.13% | 0.40% | 16 | 71 | 84.67% | 2.05% | 0.38% |
| 19-Aug-09 | 10 | 44 | A | 80.56% | 8.79% | 1.97% | 13 | 58 | 83.39% | 5.37% | 1.20% | 18 | 80 | 82.79% | 4.91% | 1.10% |
| 21-Jun-11 | 10 | 44 | A | 86.39% | 0.48% | 0.34% | 13 | 58 | 87.61% | 2.03% | 1.44% | 18 | 80 | 86.67% | 0.74% | 0.52% |

Table 35.  Summary of average leave LTEs by date, with  standard deviation and standard deviation of the mean.

| Standard dowels | Load (kip) | Load (kN) | Direction | Average | Std. Dev. | SD of M | Load (kip) | Load (kN) | Average | Std. Dev. | SD of M | Load (kip) | Load (kN) | Average | Std. Dev. | SD of M |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 26-Oct-04 | 8.4 | 37.4 | L | 90.35% | 6.79% | 1.65% | 11.3 | 50.3 | 82.40% | 5.07% | 1.01% |  |  |  |  |  |
| 12-Oct-06 | 10 | 44 | L | 82.39% | 0.88% | 0.21% | 13 | 58 | 82.10% | 1.00% | 0.24% | 16 | 71 | 81.92% | 0.81% | 0.19% |
| 25-Sep-08 | 10 | 44 | L | 80.84% | 1.25% | 0.25% | 13 | 58 | 80.94% | 2.42% | 0.48% | 16 | 71 | 81.46% | 2.33% | 0.47% |
| 19-Aug-09 | 10 | 44 | L | 82.86% | 3.08% | 0.80% | 13 | 58 | 83.16% | 2.54% | 0.66% | 18 | 80 | 83.16% | 1.17% | 0.30% |
| 21-Jun-11 | 10 | 44 | L | 83.16% | 1.10% | 0.22% | 13 | 58 | 82.87% | 0.95% | 0.19% | 18 | 80 | 82.15% | 0.98% | 0.19% |
| E1 dowel bar configuration |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 26-Oct-04 | 8.4 | 37.4 | L | 91.10% | 9.07% | 1.89% | 11.3 | 50.3 | 80.99% | 5.23% | 1.02% |  |  |  |  |  |
| 12-Oct-06 | 10 | 44 | L | 82.22% | 1.11% | 0.23% | 13 | 58 | 82.02% | 0.92% | 0.19% | 16 | 71 | 81.89% | 0.92% | 0.19% |
| 25-Sep-08 | 10 | 44 | L | 80.54% | 1.98% | 0.38% | 13 | 58 | 81.02% | 1.64% | 0.32% | 16 | 71 | 80.90% | 1.85% | 0.36% |
| 19-Aug-09 | 10 | 44 | L | 83.03% | 2.79% | 0.62% | 13 | 58 | 83.50% | 2.48% | 0.55% | 18 | 80 | 83.54% | 1.44% | 0.32% |
| 21-Jun-11 | 10 | 44 | L | 79.75% | 1.48% | 0.29% | 13 | 58 | 79.44% | 1.24% | 0.24% | 18 | 80 | 78.75% | 0.91% | 0.18% |
| E2 dowel bar configuration |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |  |
| 26-Oct-04 | 8.4 | 37.4 | L | 91.28% | 8.40% | 2.10% | 11.3 | 50.3 | 86.79% | 4.02% | 0.77% |  |  |  |  |  |
| 12-Oct-06 | 10 | 44 | L | 82.37% | 0.59% | 0.12% | 13 | 58 | 82.15% | 0.82% | 0.16% | 16 | 71 | 82.02% | 0.55% | 0.11% |
| 25-Sep-08 | 10 | 44 | L | 82.45% | 2.52% | 0.47% | 13 | 58 | 82.60% | 2.37% | 0.44% | 16 | 71 | 82.71% | 1.87% | 0.35% |
| 19-Aug-09 | 10 | 44 | L | 84.17% | 2.00% | 0.45% | 13 | 58 | 84.60% | 1.33% | 0.30% | 18 | 80 | 85.43% | 2.74% | 0.61% |
| 21-Jun-11 | 10 | 44 | L | 89.89% | 2.81% | 1.99% | 13 | 58 | 90.32% | 2.03% | 1.44% | 18 | 80 | 89.66% | 3.50% | 2.47% |

## Performance Data from I86 Hinsdale

### Project Overview and Description

Interstate 86 in Cattaraugus County, New York comprises four lanes of jointed reinforced concrete pavement (JRCP) running in the east-west direction near the town of Hinsdale. When first built in 1972, the pavement structure consisted of 229mm (9 in) JRCP with slabs 18.3m (60ft) long and 3.65m (12ft) wide; the pavement also included dowels at the joints and longitudinal tie-bars [Swart, 2006]. After 34 years of service, NYSDOT decided to rehabilitate the road, which at the time presented severe distresses and a high percentage of cracked slabs. A complete forensic study was carried on in 2006 before rehabilitation started, which found the pavement was in poor serviceability condition, which justified its rehabilitation. The rehabilitation consisted of rubblization of the existing pavement and a 225mm (8.86 in) thick hot mix asphalt (HMA) overlay. Details on the project beyond what is contained in this report may be found in the Modeling and Monitoring of Pavement Response and Performance Task B report, Volume 2 (44).

The rehabilitation project also included the construction of a 2.54 km (1.58 mi) stretch of unbonded concrete overlay divided in three experimental sections, one 820 m (2690 ft) long and the other two 860 m (2822 ft) long. The main purpose of these is to evaluate two fracturing techniques widely used in New York State for the rehabilitation of concrete pavements using unbonded JPCP overlays and compare to not using any fracturing method [Bendaña, Ambrosino & Sargand, 2008]. The sections are located along the southbound lanes of the southern tier expressway between Exit 27 close to Hinsdale and exit 28 close to Cuba in Western New York, shown in the map in Figure 12. In the first section, the existing pavement was cracked and seated before overlaying and it is referred herein as the C&S Section. In the second section, the existing pavement was rubblized before placing the JPCP overlay and it is referred herein as the Rubblized Section. Finally, in the third section or Untreated Section, the existing pavement was not treated prior to overlaying.

The cross sectional build-up consists of a 225 mm (8.86 in) JPCP overlay resting on either untreated, rubblized, or cracked & seated JRCP with a 75 mm (3 in) asphalt-treated permeable base (ATPB) acting as bond-breaker interlayer between the existing and the new concrete pavement layers. Joints every 4.75 m (15.58 ft) with dowel bars spaced every 305 mm (1 ft) and tie bars along the longitudinal joint were provided. Each experimental section included four instrumented slabs with sensors and gauges to allow measuring of mechanical responses and temperatures of the pavement as described below.

Figure 12.  I-86 Project Location near Hinsdale and Cuba. [Google Maps, 2011].

### Compressive & Flexural Strength Results

SJB Services Inc. of Hamburg carried out the compressive strength (fc) and flexural strength  (fr) testing of field-cured concrete cylinders and beams.  Figure 13(a) shows the results of the compressive strength for all the cylinders tested. The f’c after 28 days averaged 30.50MPa (4.42ksi) and after 90 days the average increased to 32.98MPa (4.78ksi). These values are visibly higher than the design value of 27.58MPa (4.0ksi).  Ambrosino [2007] reported values of compressive strength, elastic modulus and Poisson ratio for three cylinders tested at Ohio University after 30 days of pouring. The values for each of the mentioned properties are summarized in Table 36. Observe that the value of the compressive strength obtained by SJB Services is slightly higher than the value obtained at Ohio University.

Figure 13.  I86 PCC Material Strength: (a) Compressive Strength, (b) Flexural Strength.

The flexural strength values obtained by SJB Services, Inc. are shown in Figure 13(b). The average modulus of rupture reached its maximum at 28 days with a value of 3.91MPa (567psi) and decreased for the test at 90 days. Ambrosino [2007] suggested that the decrement could be the result of inappropriate consolidation of the specimens and suggested as well that a reason for this could have been that the better-compacted specimens were tested in the first place. Using the measured average compressive strength at 28 days and the expression proposed by ACI 325.12R (2002),  fr = 0.0135[wf’c]0.5 (in MPa) to approximate the flexural strength gives fr = 3.59MPa (521 psi). This value is only 8.2% less than the average  fr obtained by SJB; therefore, the flexural strength values from testing meet the ACI 2002 specification.

Table 36.  Mechanical properties of PCC overlay material on I86.

| Property | Value | Measured by |
| --- | --- | --- |
| Compressive Strength (28-days) |  | 30.50MPa (4.42ksi) | SJB Services, Inc. |
|  |  | 27.94MPa (4.05ksi) | Ohio University |
| Modulus of Rupture |  | 3.91MPa (0.567ksi) | SJB Services, Inc. |
| Elastic Modulus |  | 23235.33MPa (3370ksi) | Ohio University |
| Poisson Ratio |  | 0.181 | Ohio University |
| Unit Weight |  | 2315kg/m3 (144.5lb/ft3) | Ohio University |

### FWD Testing Results

As mentioned above the deflections were measured at the center of the slabs and load transfer testing was performed at the joints along the centerline of the slabs. The data collected was plotted to identify trends or inconsistency within the data. Subsequently, values corresponding to the third drop of the normalized deflection measured by seismometer zero (i.e. at the loading location), the joint load transfer efficiencies (LTE), joint support ratio and spreadability were averaged. The averages and standard deviations for each measurement data are listed in Table 37, Table 38, and Table 39 respectively for crack and seat, rubblized, and untreated experimental sections. In addition, FWD testing was performed also at the sensor locations with the purpose of establishing relationships between these and the strain and displacement responses discussed above.  The FWD data corresponding to the first and second drops are provided in Appendix H.

### FWD Deflections, Load Transfer Efficiency, Joint Support Ratio and Spreadability

Figure 14(a) shows the average of the normalized deflection measured under the loading plate for each of the dates where FWD testing was performed. It can be seen that the NDf0 values at the approach and leave positions are close together with differences no more than 7%. In addition, the normalized deflection varied between 0.89 (m/kN (0.156 mil/kip) and 2.34 (m/kN (0.410 mil/kip) showing the maximum values for the winter 2007 and fall testing sessions which are the coldest periods. In the case of the C&S section, the maximum normalized deflection occurred during the winter 2007 and fall 2008 and the minimum occurred for the fall 2006 period. The rubblized section on the other hand, experienced more steady averages of NDf0 showing the maximum values for the summer 2006 and winter 2007 sessions while the minimum values were observed for the fall 2006 and 2007 tests. Finally, the untreated section showed highest normalized deflections for the fall 2007 and 2008 periods while the minimum NDf0 was observed for the summer 2006 test. In general, the rubblized section showed the highest normalized deflections, which is the expected trend since it has the most flexible base among the three sections. The normalized deflection average at the center of the slab showed a higher variability than those at the joints specially in the C&S section which experienced the highest values reaching an average NDf0 of 4.77 (m/kN (0.836 mil/kip) for the winter 2007 test. Moreover, the highest NDf0 averages in each section were observed for the testing sessions of winter 2007, spring 2008 and spring 2009. This coincides with a lower compressive stiffness of the base and subgrade due to the thawing process of the subgrade and/or base materials. The lowest values on the other hand, were observed in general for the fall testing sessions. Notice that the March 2007 periods correspond to late winter periods or early spring period, which will explain the similar averages measured in this period compared to those for the spring 2008 and 2009 values.

The load transfer efficiency averages for each section is plotted in Figure 14(b). It can be seen that for the three sections, the LTE values were in general higher compared to the adjacent points for the warmer seasons (i.e. summer and spring periods) which is the expected behavior. Moreover, a direct relationship can be inferred when comparing the LTE values to the corresponding values of the normalized deflections at the joints where an increment in the load transfer efficiency is associated to a decrement in the NDf0 values. However, a decreasing tendency of the LTE values since soon after paving is observed for the three sections. The LTE values observed for the summer 2006 test were above 80% and dropped to averages of about 75% for the C&S section, and 70% for the rubblized and untreated sections. According to Sargand et al. [2002], these values are considering to be in the fair range (50% to 80%), but notice that a decrement of about 10% in the LTE values in three years is a higher than average rate of deterioration of the load transfer mechanism with time.

The average of the joint support ratio was calculated for each section and shown in Figure 15(a). It can be seen that the variance of the average JSR values is small despite the tendency of JSR values higher than one for most of the testing sessions in the three sections. The JSR ratio values were between 0.9 and 1.1, a range that is considered acceptable according to Sargand et al. [2002]. However, notice that C&S section showed JSR values higher than one for the majority of the testing sessions which indicates unequal support conditions (i.e. weaker) at the leave location for some of the slabs. Likewise, the rubblized section showed JSR values higher than one, but closer to the unit than those observed in the C&S and untreated section. The untreated section on the other hand, showed the most variations from test to test with JSR values between those showed by the other two sections.

Average spreadability at the mid-slab was plotted for each section in Figure 15(b). It can be seen that the average SPR was between 60% and 70% where the C&S section tended to show highest values. Moreover, the average SPR in the C&S section showed less variation between testing sessions than the other two sections followed by the rubblized section. Lower values of the spreadability compared to the adjacent values were observed during the fall 2006 and spring 2009 testing sessions for all three sections. In addition, SPR values decreased in the rubblized and untreated sections for the spring 2008 and fall 2007 sessions respectively. It seems from the SPR values that the C&S section showed the highest values for the majority of testing session with the exception of the winter 2007 and spring 2009 sessions.

Figure 14.  Normalized deflection (a) and load transfer efficiency (b) averaged for all sections (1 µm/kN = 0.17526 mil/kip).

Figure 15.  Joint support ratio (a) and mid-slab spreadability (b) averaged for all sections.

Table 37.  Summary 3rd drop FWD data averages and standard deviations for C&S section (1 µm/kN = 0.17526 mil/kip).

| Section 1: Crack & Seated |
| --- |
| Load Transfer Averages |
| Date | NDf-0 | LTE | JSR | MidSlab SPR |
|  | (μm/kN) | (%) |  |  |
|  | Approach | Leave | MidSlab | Approach | Leave |  | (%) |
| Jun-2006 | 1.671 | 1.772 | - | 84.3 | 82.0 | 1.054 | - |
| Nov-2006 | 1.518 | 1.613 | 1.348 | 84.5 | 78.3 | 1.066 | 66.9 |
| Mar-2007 | 2.219 | 2.291 | 4.768 | 77.9 | 74.4 | 1.038 | 74.4 |
| Oct-2007 | 1.607 | 1.648 | 3.120 | 77.0 | 74.3 | 1.027 | 69.9 |
| May-2008 (1) | 1.709 | 1.764 | 3.622 | 86.2 | 84.8 | 1.019 | 70.5 |
| May-2008 (2) | 1.662 | 1.726 | - | 69.0 | 71.2 | 1.048 | - |
| Oct-2008 | 2.128 | 2.231 | 1.213 | 68.4 | 70.5 | 1.051 | 70.5 |
| May-2009 | 1.760 | 1.803 | 3.294 | 75.3 | 74.5 | 1.017 | 62.4 |
| Load Transfer Standard Deviation |
| Jun-2006 | 0.174 | 0.205 | - | 4.0 | 5.9 | 0.034 | - |
| Nov-2006 | 0.176 | 0.194 | 0.169 | 6.4 | 6.7 | 0.081 | 4.2 |
| Mar-2007 | 0.367 | 0.317 | 1.091 | 4.4 | 3.9 | 0.070 | 4.0 |
| Oct-2007 | 0.149 | 0.151 | 0.520 | 4.5 | 3.4 | 0.047 | 3.2 |
| May-2008 (1) | 0.094 | 0.086 | 0.457 | 5.3 | 2.4 | 0.040 | 3.1 |
| May-2008 (2) | 0.218 | 0.159 | - | 9.7 | 4.2 | 0.108 | - |
| Oct-2008 | 0.254 | 0.230 | 0.179 | 5.9 | 4.6 | 0.046 | 3.2 |
| May-2009 | 0.184 | 0.215 | 0.585 | 3.9 | 4.6 | 0.054 | 1.2 |

Table 38.  Summary of 3rd drop FWD data averages and standard deviations for rubblized section (1 µm/kN = 0.17526 mil/kip).

| Section 2: Rubblized |
| --- |
| Load Transfer Averages |
| Date | NDf-0 | LTE | JSR | MidSlab SPR |
|  | (μm/kN) | (%) |  |  |
|  | Approach | Leave | MidSlab | Approach | Leave |  | (%) |
| Jun-2006 | 2.148 | 2.244 | - | 84.7 | 87.1 | 1.038 | - |
| Nov-2006 | 1.703 | 1.756 | 1.637 | 78.7 | 74.6 | 1.036 | 63.7 |
| Mar-2007 | 2.340 | 2.309 | 2.979 | 75.8 | 74.7 | 0.999 | 70.7 |
| Oct-2007 | 1.731 | 1.737 | 2.412 | 68.5 | 64.7 | 1.012 | 66.9 |
| May-2008 (1) | 1.808 | 1.849 | 3.361 | 80.4 | 80.4 | 1.001 | 68.5 |
| May-2008 (2) | 1.904 | 1.927 | - | 66.7 | 73.4 | 1.014 | - |
| Oct-2008 | 2.009 | 2.079 | 1.117 | 68.8 | 69.4 | 1.039 | 65.5 |
| May-2009 | 1.974 | 1.981 | 3.768 | 68.4 | 69.7 | 0.996 | 63.3 |
| Load Transfer Standard Deviation |
| Jun-2006 | 0.130 | 0.103 | - | 5.9 | 5.2 | 0.020 | - |
| Nov-2006 | 0.160 | 0.137 | 0.138 | 4.0 | 2.8 | 0.025 | 1.5 |
| Mar-2007 | 0.432 | 0.368 | 1.154 | 6.8 | 4.9 | 0.086 | 5.7 |
| Oct-2007 | 0.130 | 0.134 | 0.601 | 6.3 | 4.7 | 0.036 | 2.9 |
| May-2008 (1) | 0.143 | 0.141 | 0.695 | 4.7 | 2.8 | 0.052 | 5.8 |
| May-2008 (2) | 0.224 | 0.153 | - | 8.6 | 7.6 | 0.038 | - |
| Oct-2008 | 0.348 | 0.324 | 0.088 | 8.3 | 5.7 | 0.047 | 1.1 |
| May-2009 | 0.166 | 0.166 | 0.781 | 5.4 | 4.9 | 0.036 | 2.4 |

Table 39.  Summary of 3rd drop FWD data averages and standard deviations for untreated section (1 µm/kN = 0.17526 mil/kip).

| Section 3: Untreated |
| --- |
| Load Transfer Averages |
| Date | NDf-0 | LTE | JSR | MidSlab SPR |
|  | (μm/kN) | (%) |  |  |
|  | Approach | Leave | MidSlab | Approach | Leave |  | (%) |
| Jun-2006 | 0.886 | 0.918 | - | 101.2 | 84.7 | 1.021 | - |
| Nov-2006 | 1.306 | 1.297 | 1.106 | 76.6 | 77.1 | 0.995 | 64.9 |
| Mar-2007 | 1.389 | 1.415 | 2.566 | 75.1 | 71.8 | 1.026 | 67.4 |
| Oct-2007 | 1.962 | 1.833 | 1.109 | 60.5 | 63.8 | 0.938 | 68.0 |
| May-2008 (1) | 1.335 | 1.363 | 2.503 | 73.3 | 73.1 | 1.017 | 63.6 |
| May-2008 (2) | 1.457 | 1.395 | - | 70.2 | 79.7 | 0.973 | - |
| Oct-2008 | 1.990 | 2.080 | 0.980 | 68.0 | 68.6 | 1.050 | 71.8 |
| May-2009 | 1.331 | 1.360 | 2.297 | 70.2 | 69.9 | 1.027 | 61.7 |
| Load Transfer Standard Deviation |
| Jun-2006 | 0.071 | 0.115 | - | 16.6 | 7.9 | 0.043 | - |
| Nov-2006 | 0.155 | 0.134 | 0.078 | 6.1 | 11.9 | 0.045 | 2.1 |
| Mar-2007 | 0.246 | 0.201 | 1.658 | 8.7 | 5.9 | 0.081 | 4.3 |
| Oct-2007 | 0.502 | 0.426 | 0.085 | 15.4 | 14.1 | 0.050 | 2.6 |
| May-2008 (1) | 0.126 | 0.120 | 1.128 | 6.6 | 3.3 | 0.048 | 3.4 |
| May-2008 (2) | 0.155 | 0.119 | - | 6.7 | 3.3 | 0.032 | - |
| Oct-2008 | 0.236 | 0.202 | 0.089 | 6.5 | 6.1 | 0.058 | 2.3 |
| May-2009 | 0.171 | 0.173 | 0.951 | 6.6 | 5.7 | 0.076 | 4.6 |

### Forensic Investigations

During distress surveys completed during November 2009 mid-panel top-down cracks were observed in the 90% of the slabs of the untreated section. Mid-panel cracks also were observed in the rubblized and C&S sections but these were considered localized cases given the percentage of cracked slabs. The percentages of cracks observed for each section are listed in Table 40. Additionally, hairline cracks like those in Figure 16 were observed at the tie-bar locations in all three sections.  These top-down cracks, however, are believed to be a consequence of the tie-bar installation procedure used during paving. The tie-bar holes were drilled in the concrete slabs of the passing lane, which was constructed first, and then these were glued with epoxy into the holes before paving the driving lane. The results presented support the initial expectations about the performance of the untreated section and the early conclusions drawn by Bendaña et al. [2008].  Additional surveys conducted in 2010 and 2011 did not show any increase in the number of cracks found in November 2009.  Minor faulting between the asphalt shoulder and the concrete pavement was apparent in limited areas and this was due to the asphalt shoulder paving process.

These test sections also included some experimental joint treatments.  These joints exhibited signs of distress but were not be considered as part of the overall performance of these concrete sections, since they were localized.

Table 40.  Percentage of cracked slabs observed in distress survey of November 2009.

| Section | Mid-Panel | Hairline |
| --- | --- | --- |
|  | % Slabs Cracked | % Slabs Cracked | Cracks per Slab |
| Cracked and seated | 5% | 40% | 0 – 2 |
| Rubblized | 5% | 50% | 1 – 3 |
| Untreated | 90% | 90% | 3 – 6 |

Figure 16.  Hairline cracks at tie-bar locations in the untreated section.

## Performance Data from I90 Weedsport

### Project Overview and Description

The New State York Thruway Authority (NYSTA) has undertaken a 15-mile (24 km) reconstruction project on Interstate 90 (I-90) in upstate New York at Weedsport, near Syracuse.  The project was a full-depth reconstruction of the pavement structure, and included new Portland cement concrete (PCC) pavement, base and sub-base.  The two test sections were constructed at the end of construction phase A (Figure 17, reproduced from NYSTA, www.thruway.ny.gov).  Details on the project beyond what is contained in this report may be found in the Modeling and Monitoring of Pavement Response and Performance Task B report, Volume 3 (45).

Figure 17.  Construction schedule of I-90 thruway rehabilitation (NYSTA) (5.1 mi = 8.2 km, 5.2 mi = 8.4 km, 4.9 mi = 7.9 km).

The reconstruction of the I-90 Thruway was based upon the NYSDOT Highway Design Manual (HDM).  The roadway is a principle arterial interstate in an urban region, with an AADT of 34,320 vehicles and experienced less than 1% growth between 2006 and 2009 (NYSDOT, 2011).  The CTPB and DGAB thicknesses were based on the standard design used in the HDM, with an expected design life of 50 years (NYSDOT HDM, 2002).

### Properties of Materials

In order to characterize the material properties found at each test section, subgrade, DGAB, CTPB and PCC test specimens were collected.  ORITE researchers and graduate research assistants recovered subgrade material during TDR and LVDT instrumentation from various depths at each section.  We then combined this material in the laboratory to obtain a composite sample for the entire site.  The DGAB sample was collected from the contractor’s material stockpile in September 2010.  CTPB specimen were cast in cylinders on-site and transported to Ohio University for testing.  FHWA technicians cast concrete beams and cylinders during construction, which were then cured and tested on-site.

#### Subgrade Properties

In the lab, we processed and tested the subgrade soil samples for classification.  The sample was and dried and broken down to separate collated material.  Next, the soil was wet-washed to determine the quantity passing the No. 200 sieve.  A sieve analysis was then conducted on the remaining dried sample, shown in Table 41.  Finally, the Atterberg limits were determined to classify the soil, as summarized in Table 42.

Table 41.  Subgrade sieve analysis

| Sieve No. | Diameter | Retained | Passed |
| --- | --- | --- | --- |
|  | (mm) | (mil) | (g) | (oz) | (%) | (g) | (oz) | (%) |
| 4 | 4.75 | 187 | 63 | 2.2 | 9.30% | 616.5 | 21.7 | 90.70% |
| 10 | 2 | 79 | 55 | 1.9 | 8.10% | 561.5 | 19.8 | 82.60% |
| 20 | 0.84 | 33 | 47 | 1.7 | 6.90% | 514.5 | 18.1 | 75.70% |
| 40 | 0.425 | 16.7 | 37 | 1.3 | 5.40% | 477.5 | 16.8 | 70.30% |
| 60 | 0.25 | 9.8 | 38 | 1.3 | 5.60% | 439.5 | 15.5 | 64.70% |
| 100 | 0.15 | 5.9 | 39.5 | 1.4 | 5.80% | 400 | 14.1 | 58.90% |
| 200 | 0.075 | 2.95 | 46 | 1.6 | 6.80% | 354 | 12.5 | 52.10% |
| pan | - | - | 354 | 12.5 | 52.10% | - | - | - |

Table 42.  Atterberg limits

| Property | Value |
| --- | --- |
| Liquid Limit (LL) | 24.6% |
| Plastic Limit (PL) | 13.4% |
| Plasticity Index (Ip) | 11.2% |
| Group Index (GI) | 2.53 |

Using the AASHTO and Unified Soil Classification (USC) systems, the soil was classified respectively as A-6 and CL.  Under the USC, the soil was further characterized by the group name sandy lean clay.

#### DGAB Properties

The DGAB was placed in two layers with different gradations, classified as NYSDOT Type 3 and Type 4.  Both materials were crushed reclaimed concrete pavement (RCP); however, Type 3 was a finer material used as the upper DGAB layer.  The grain-size distribution of both materials is shown in Figure 18.  ORITE researchers and graduate research assistants performed the resilient modulus tests on both material types.  Deviator stress was varied for different confining stresses to test each sample at different stress levels.  The resilient modulus at a confining stress of 20 kPa (2.9 psi) and a deviator stress of 59 kPa (8.6 psi), chosen as the expected pavement stress state, resulted in a resilient modulus of 142.0 MPa (20.60 ksi) and 134.7 MPa (19.54 ksi) for Type 3 and Type 4, respectively.

Figure 18.  Grain-size distribution for NYSDOT Type 3 and Type 4 DGAB (1 mm = 39.4 mil; 25.4 mm = 1 in)

#### CTPB Properties

The CTPB mix, shown in Table 43, was also tested for mechanical properties.  Test cylinders were cast in September 2009, and additional cylinders were cast for further testing in September 2010.  The contractor verified that the mix design and material sources had not changed over that period, making the samples collected at both times representative of the project.

Table 43.  CTPB mix design for I90

| Material | kg/m3 | pcf |
| --- | --- | --- |
| Cement | 143 | 8.93 |
| Fine Aggregate | 193 | 12.05 |
| Coarse Aggregate (#1) | 736 | 45.95 |
| Coarse Aggregate (#2) | 673 | 42.01 |
| Water (max.) | 53 | 3.31 |
| Water/cement Ratio (max) | 0.37 |

The static modulus of elasticity and Poisson’s ratio were found according to the American Society for Testing and Materials (ASTM) C469/C469M using a ring-compressometer, since strain gauges would be difficult to adhere to the material’s irregular surface.  Dial gauges on the ring-compressometer measure strain in both transverse and longitudinal directions.  During loading, strains measurements were taken at a strain of 50µε and at 40% of ultimate compressive strength (ASTM C469/C469M, 2010).  Using these two data points, the static elastic modulus and Poisson’s ratio were calculated.  Figure 19 shows the test setup for the static modulus and Poisson’s ratio test.  After the static modulus test, the ring compressometer device was removed and the specimen was loaded to capacity to determine the ultimate compressive strength of the CTPB sample.

Figure 19.  Static modulus and Poisson’s ratio test setup for CTPB specimen

Split-cylinder tensile tests were also performed to determine the tensile strength of the CTPB.  For this test, a 15.2 cm (6 in) diameter cylinder was cut into two 15.2 cm (6 in) long specimens.  Each specimen was loaded along its length with two wood shims positioned horizontally along the specimen length to distribute the compressive force during the test (Figure 20).  The specimen was loaded until failure, which occurred along the vertical plane as tensile stresses formed perpendicular to the load direction, shown in Figure 21.

Figure 20.  Split-cylinder tensile test setup on CTPB sample

Figure 21.  Failure of specimen during split-cylinder tensile test

Results for the CTPB compressive strength, elastic modulus, and tensile strength are summarized in Table 44.  The range of results indicates the material properties were quite variable.  The variability of the CTPB was related to concrete coverage and specimen unit weight.  The samples with higher strengths were observed to have more cement coverage and greater unit weights.

Table 44.  CTPB Mechanical Properties for I90

| Age (day) | Sample No. | Compressive Strength | Tensile Strength | Elastic Modulus | Poisson's Ratio | Unit Weight |
| --- | --- | --- | --- | --- | --- | --- |
|  |  | (kPa) | (psi) | (kPa) | (psi) | (MPa) | (ksi) |  | (kN/m3) | (pcf) |
| 14 | 1 | 3,375 | 490 | - | - | 9,299 | 1,349 | 0.167 | 18.03 | 0.1148 |
|  | 2 | 7,501 | 1,088 | - | - | 13,975 | 2,027 | 0.303 | 19.13 | 0.1218 |
| 28 | 1 | 5,506 | 799 | - | - | 15,883 | 2,304 | 0.012 | 19.34 | 0.1231 |
|  | 2 | - | - | 1,169 | 170 | - | - | - | 19.42 | 0.1236 |
| Average | 5,461 | 792 | 1,169 | 170 | 13,052 | 1,893 | 0.161 | 18.83 | 0.1199 |
| Std. Dev. | 2,063 | 299 | - | - | 3,388 | 491 | 0.146 | 0.64 | 0.0041 |

#### Concrete Properties

The specified mix design for the concrete pavement was NYSDOT Class C Modified, as summarized in Table 45.  During paving, test cylinders and beams were cast by FHWA technicians.  The specimen were cured on-site and tested in the mobile FHWA testing laboratory.  Tests conducted on the samples at various curing ages are summarized in Table 46.

Table 45.  Concrete Mix Design for I90

| Material | Quantity/m3 | Quantity/ft3 |
| --- | --- | --- |
| Cement | 287 kg | 17.9 lb |
| Fly Ash | 72 kg | 4.5 lb |
| Fine Aggregate | 703 kg | 43.9 lb |
| Coarse Aggregate | 1083 kg | 67.6 lb |
| Water Reducing Agent | 1172 mL | 112.2 fl oz |
| Air Entraining Agent | 96.7 mL | 9.26 fl oz |
| Water | 148 kg | 9.2 lb |
| Slump | 5.1 ± 1.25cm | 2.0 ± 0.5 in |
| Air Content | 6.5 ± 1.5% |
| Water/cement Ratio (max.) | 0.44 |

Table 46.  Concrete Test Results for I90

| Age (days) | Compressive Strength | Modulus of Rupture | Compressive Strength | Modulus of Rupture | Elastic Modulus | Poisson's Ratio |
| --- | --- | --- | --- | --- | --- | --- |
|  | (MPa) | (ksi) | (MPa) | (ksi) | (MPa) | (ksi) | (MPa) | (ksi) | (MPa) | (ksi) |  |
| 7 | 24.57 | 3.56 | 2.87 | 0.42 | 24.44 | 3.54 | 3.06 | 0.44 | - | - | - |
| 14 | 31.20 | 4.53 | 3.85 | 0.56 | 29.77 | 4.32 | 3.74 | 0.54 | 22431.70 | 3253.44 | 0.252 |
| 28 | 37.44 | 5.43 | 4.22 | 0.61 | 37.30 | 5.41 | 4.27 | 0.62 | 23843.50 | 3458.21 | 0.240 |

### Field Forensic Observations

During construction operations, the contractor reported bonding between the CTPB and PCC slab shortly after construction.  When paving was halted at the end of each day, a portion of unfinished pavement was left, which was cut and removed at the beginning of the next day.  When the pavement was removed, the CTPB was adhered to the PCC slab, and was removed with the slab.  During a data collection trip, we visited the material refuse area where used material was stored on site prior to recycling.  As reported by the contractor, the CTPB was bonded to the PCC slabs (Figure 22).  This verifies the claim that the PCC mortar penetrates the porous CTPB structure and forms a bond as the concrete slab cures.

Figure 22.  Bonded CTPB and PCC slab in refuse pile at I90 construction site

### Falling Weight Deflectometer Testing

In this section, the FWD testing results on the base and pavement are presented and discussed.  For the base material test, only deflections at the load center are discussed; however, for the PCC pavement tests, several parameters for pavement stiffness and joint performance are presented for discussion.  Additional results and figures are provided in Appendix I.

FWD testing reveals stiffness and joint performance characteristics of pavements and base materials.  The device produces a pulse-load by dropping a 250-kg (551 lb) weight onto a 15-cm (6 in) radius plate.  For the base testing, eight geophones were used, configured at 0 cm (0 in), 20.3 cm (8 in), 30.5 cm (12 in), 45.7 cm (18 in), 61 cm (24 in), 91.4 cm (36 in), 122 cm (48 in), 152.4 cm (60 in), and 182.9 cm (72 in) from the load center.  For testing on PCC pavement, the geophones were spaced at 0 cm (0 in), 30.5 cm (12 in), 45.7 cm (18 in), 61 cm (24 in), 91.4 cm (36 in), 122 cm (48 in), 152.4 cm (60 in), and 182.9 cm (72 in) behind the load plate center, with one geophone 30.5 cm (12 in) in front of the load plate.  The loads were applied at 26.7 kN (6.0 kip), 40.0 kN (9.0 kip) and 53.4 kN (12.0 kip) on the base and 40.0 kN (9.0 kip), 53.4 kN (12.0 kip), and 71.2 kN (16 kip) on the pavement.  All readings were normalized to 1 kN (0.22 kip, or to 1 kip (4.45 kN)) prior to the analysis to make comparisons between the different loads.  The geophone readings at the point of loading (D0) are representative of the overall pavement stiffness, while readings at 152.4 cm (60 in) from the load (D60) are representative of the subgrade stiffness.

#### Base Testing

FWD testing was done on the CTPB and DGAB layers in both lanes on October 1 2009, prior to PCC paving.  The average normalized D0 deflections are shown in Figure 23.  The separation line between base types shown on this plot is in accordance to site plan dimensions.  The CTPB response was less variable than the DGAB, which typically had greater deflections.  DGAB deflections increased in the region past station 17+350, which can also be seen in the pavement tests on this region.  It is important to note again the location of Section 1 and 2 are between stations 17+331.5 to 17+345 and 17+120 to 17+133.5, respectively.

Figure 23.  Average normalized D0 deflections on CTPB and DGAB prior to paving (5.714 µm/kN = 1 mil/kip)

#### PCC Testing

Early-age FWD tests were performed on the right lane at 21-day curing strength.  The thermocouples embedded in the test sections were not recording temperature data during this time due to a power failure.  Therefore, the results discussed in terms of the ambient and pavement surface temperatures as recorded by the FWD testing machine.  During the test, ambient air temperatures were an average of 12.1°C (53.8°F), and PCC surface temperatures were an average of 12.0°C (53.6°F).  The temperatures were nearly constant, indicating slab shape should be constant throughout the test.  These results are summarized in Table 47.  After two years in service, additional tests were conducted in November 2011.  The results from these tests are shown in Table 48.  During the test, ambient air temperatures were an average of 13.6°C (56.5°F), and PCC surface temperatures were an average of 14.2°C (57.6°F).  Tests were done in three positions on each slab: at the joint approach, mid-slab, and joint leave positions.  The mid-slab test indicates pavement stiffness, while the joint tests indicate joint performance and support conditions.  Additional figures for these results can be found in Appendix I.

Table 47.  Summary of FWD results September 29 2009

|  | Date: | 10/29/2009 |
| --- | --- | --- |
|  | Load | D0 (m/kN) | D0 (mil/kip) | LTE (%) | JSR | SPR (%) | D3/D0 |
|  | (kN) | (kip) | M | JA | JL | M | JA | JL | A | L | M | M | M |
| Section 1 | 40 | 9.0 | 0.963 | 1.373 | 1.412 | 0.169 | 0.240 | 0.247 | 84.25% | 81.06% | 1.062 | 67.97% | 0.879 |
|  | 53 | 11.9 | 0.978 | 1.405 | 1.428 | 0.171 | 0.246 | 0.250 | 82.96% | 81.96% | 1.038 | 68.54% | 0.876 |
|  | 71 | 16.0 | 0.972 | 1.393 | 1.407 | 0.170 | 0.244 | 0.246 | 83.47% | 81.79% | 1.038 | 68.25% | 0.878 |
| Section 2 | 40 | 9.0 | 0.75 | 1.44 | 1.461 | 0.131 | 0.252 | 0.256 | 82.70% | 82.18% | 1.057 | 72.90% | 0.885 |
|  | 53 | 11.9 | 0.768 | 1.464 | 1.477 | 0.134 | 0.256 | 0.258 | 83.60% | 83.02% | 1.066 | 73.77% | 0.88 |
|  | 71 | 16.0 | 0.764 | 1.441 | 1.455 | 0.134 | 0.252 | 0.255 | 84.07% | 83.43% | 1.069 | 73.51% | 0.889 |
|  | Note: JA=Joint approach; JL=Joint leave; M=Mid-slab |

Table 48.  Summary of FWD results November 15 2011

|  | Date: | 11/15/2011 |
| --- | --- | --- |
|  | Load | D0 (m/kN) | D0 (mil/kip) | LTE (%) | JSR | SPR (%) | D3/D0 |
|  | (kN) | (kip) | M | JA | JL | M | JA | JL | A | L | M | M | M |
| Section 1 | 44 | 9.9 | 0.963 | 1.416 | 1.485 | 0.169 | 0.248 | 0.260 | 87.11% | 79.96% | 1.049 | 70.15% | 0.89 |
|  | 58 | 13.0 | 0.974 | 1.419 | 1.503 | 0.170 | 0.248 | 0.263 | 87.43% | 80.18% | 1.060 | 70.73% | 0.895 |
|  | 80 | 18.0 | 0.987 | 1.419 | 1.495 | 0.173 | 0.248 | 0.262 | 86.64% | 79.40% | 1.054 | 69.84% | 0.883 |
| Section 2 | 44 | 9.9 | 0.958 | 1.997 | 2.111 | 0.168 | 0.349 | 0.369 | 95.75% | 90.24% | 1.057 | 80.49% | 0.916 |
|  | 58 | 13.0 | 0.958 | 2.002 | 2.104 | 0.168 | 0.350 | 0.368 | 96.48% | 90.16% | 1.052 | 80.46% | 0.922 |
|  | 80 | 18.0 | 0.937 | 1.908 | 1.997 | 0.164 | 0.334 | 0.349 | 95.57% | 89.48% | 1.048 | 80.00% | 0.909 |
|  | Note: JA=Joint approach; JL=Joint leave; M=Mid-slab |

#### Distress Surveys

As of November of 2011, no distress or faulting has been recorded on the I90 project.  Further observations and tests will be conducted.

# Review of MEPDG Data Requirements

The MEPDG program allows three different types of input levels (Level 1 through Level 3).  These levels allow users with varying information on the design project to use either of these levels.  Level 1 is primarily used on pavement designs that have unusual features, materials or traffic conditions and allows the designer the maximum number of inputs that are project specific.  This level is also designed for the most advanced users with intimate knowledge of the particular project under consideration.  This level requires the most input and assumes that the user has access to extensive library of laboratory and in-situ test results.  Level 2 inputs use built-in equations and regression analysis to calculate material properties, traffic and climatic conditions using data from other sites that are similar to the proposed design.  Level 2 inputs in general represent regional information and data.  Level 3 inputs are numbers usually based on the global calibration numbers and are best estimates of what would be expected.  Level 3 inputs allow for the least amount of project specific knowledge, and the predictions would not be calibrated for the specific sites.  This level of input should only be used when no other data is available or possible.

This hierarchical input procedure offers the design engineer the maximum flexibility when entering data into the guide, allowing the mixed use of Levels 1 through Level 3.  But it should be noted, as previously discussed, the error associated with the pavement performance predictors’ increases with the increase in use of Levels 2 and Level 3 inputs and reduction in Level 1 input.  The increase in Level 1 input in addition to local calibration would increase the reliability of the MEPDG and decrease the error associated with the pavement performance predictors.

Table 49 is adapted from the MEPDG and shows the input groups associated with the program, a brief description of each group and the required recalibration input level for better predictability.  As shown in Chapter 4 above, data was collected and laboratory tests conducted to allow for these input levels in order to proceed with the local calibration of the model.  The table excludes HMA and subgrade materials as they are beyond the scope of this report and in addition requirements for CRCP are excluded since CRCP is not used in the State of New York.

Table 49.  Input levels required for MEPDG recalibration

| Input Group | Input Parameter | Recalibration Input level Used |
| --- | --- | --- |
| Truck Traffic | Axle-load Distributions (Single, Tandem, Tridem), Truck Volume Distribution | Level 1 |
|  | Lane and Directional Truck Distribution | Level 1 |
|  | Tire Pressure | Level 3 |
|  | Axle Configuration, tire Spacing | Level 3 |
|  | Truck Wander | Level 3 |
| Climate | Temperature, Wind Speed, Cloud Cover, Precipitation, Relative Humidity | Level 1 weather stations |
| All Materials | Unit Weight | Level 1 |
|  | Poisson’s Ratio | Level 1 & 3 |
|  | Thermal properties: Conductivity, heat capacity, surface absorptivity | Level 3 |
| Material Properties | PCC | Elastic Modulus | Level 1 |
|  |  | Flexural Strength | Level 1 |
|  |  | PCC Coefficient of thermal Expansion | Level 1 |
|  | Unbound Layers | Resilient Modulus | Level 1 |
|  |  | Classification and Volumetric properties | Level 1 |
|  |  | Soil-Water Characteristic Relationships | Level 3 |
|  |  | Saturated Hydraulic Conductivity | Level 3 |
| Existing Pavement | Condition of existing layers | Levels 1 and 2 |

# Calibration of MEPDG Software for New York

The local calibration of the MEPDG was initially started using the MEPDG software version 1.1, which was then the latest version.  Nationally, some problems were identified and reported with this version of the software and its calibration with PCC data.  The New York liaison recommended that the research team wait for the upcoming version of the MEPG (Darwin-ME) before conducting the local calibration.  The research team is presently awaiting delivery of the software to complete the calibration.

# Development of JPCP Design Catalog

Development of the JPCP design catalog is dependent on completion of the local calibration of the MEPDG.  Once the Darwin-ME software is received, the local calibration of the software and the compilation of the JPCP design catalog will be undertaken.

# References

- Mallela, Jagannath; Glover, Leslie Titus; Liang, Robert; and Chou, Eddie; 2009, Guidelines for Implementing NCHRP1-37A M-E Design Procedures in Ohio:  Volume 2 – Literature Review, Technical Report No. FHWA/OH-2009/9B for the Ohio Department of Transportation, State Job No.  134300, November 2009.

- Schwartz, Charles; Li, Rui; Kim, Sunghwan); Ceylan, Halil; Gopalakrishnan, Kasthurirangan; 2011, “Effect of concrete strength and stiffness characterization on predictions of mechanistic-empirical performance for rigid pavements”, Transportation Research Record 2226, December 1, 2011, p. 41-50.

- Won, Moon; 2011, “Continuously reinforced concrete pavement”, Transportation Research Record 2226, December 1, 2011, p. 51-59.

- Elfino, Mohamed; Nair, Harikrishnan; Crawford, Gary; Gudimettla, Jagan; 2011, “Comparison of predicted distresses between different input levels using M-E PDG for CRC pavement”, T and DI Congress 2011: Integrated Transportation and Development for a Better Tomorrow - Proceedings of the 1st Congress of the Transportation and Development Institute of ASCE, Chicago, IL, March 13, 2011 - March 16, American Society of Civil Engineers (ASCE), Reston, VA, 2011, p. 558-575.

- Schram, Scott A.; Abdelrahman, Magdy; 2010, “Integration of mechanistic-empirical pavement design guide distresses with local performance indices”, Transportation Research Record 2153, January 12, 2010, p. 13-23.

- Chatti, K.; Brake, N.A.; Haider, S.W.; Salama, H.; 2008, “The effect of different axle configurations on the fatigue life of plain cement concrete”, Pavement Cracking: Mechanisms, Modeling, Detection, Testing and Case Histories, Proceedings of the 6th RILEM International Conference on Cracking in Pavements, Chicago  IL, June 16, 2008 - June 18, 2008, CRC Press, Netherlands, p. 155-165.

- Snyder, Mark B.; 2008, “Lessons learned from Mn/ROAD (1992-2007): Low-volume road concrete pavement design and performance”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 364-383.

- McCracken, Jennifer K.; Vandenbossche, Julie M.; Asbahan, Rania E.; 2008, “Effect of the MEPDG hierarchal levels on the predicted performance of a jointed plain concrete pavement”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 153-170.

- Ker, Hsiang-Wei; Lee, Ying-Haur; Lin, Chia-Huei; 2008, “Prediction models for transverse cracking of jointed concrete pavements: Development with long-term pavement performance database”, Transportation Research Record 2068, 2008, p. 20-31.

- Haider, Syed Waqar; Harichandran, Ronald S.; 2008, “Correlation between properties of axle load distribution and rigid pavement performance measures”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 659-672.

- Hiller, Jacob E.; Roesler, Jeffery R.; 2008, “Comparison of mechanistic-empirical thickness design methods and predicted critical fatigue locations”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 171-188.

- Sargand, Shad; Figueroa, J. Ludwig; and Romanello, Michael; 2008, Instrumentation of the Way-30 Test Pavements, Technical Report No. FHWA/OH-2008/7 for the Ohio Department of Transportation, State Job No.  14815, June 2008.

- Sargand, Shad; and Figueroa, J. Ludwig; 2010, Monitoring and Modeling of Pavement Response and Performance Task A:  Ohio, Technical Report No. FHWA/OH-2010/03A for the Ohio Department of Transportation, Pooled Fund Project TPF-5(121), State Job No.  134287, June 2010.

- Sargand, Shad; Masada, Teruhisa; Hernandez, Jaime; and Kim, Sang-Soo; 2010, Determination of Mechanical Properties of Materials Used in Way-30 Test Pavements, Technical Report No. FHWA/OH-2010/9 for the Ohio Department of Transportation, State Job No.  437046, May 2010.

- Khanum, T.; Hossain, M.; Barezinsky, R.; and Romanaschi, S.A.; 2006, “Influence of Selected Design and Construction Features on JPCP Performance," Proceedings of the 85th Annual Meeting of the Transportation Research Board, Washington,D.C., January 2006.

- Hu, Jiong; Wang, Kejin; Ge, Zhi; 2010, “Study of the mechanical properties of Iowa concrete pavement for use in the Mechanistic-Empirical Pavement Design Guide (MEPDG)”, Geotechnical Special Publication:  Paving Materials and Pavement Analysis - Proceedings of the 2010 GeoShanghai International Conference, June 3, 2010 - June 5, 2010, Shanghai, China, American Society of Civil Engineers (ASCE), Reston, VA, 2010, p. 169-175.

- Asbahan, Rania E.; Vandenbossche, Julie M.; 2011, “Effects of temperature and moisture gradients on slab deformation for jointed plain concrete pavements”, Journal of Transportation Engineering, Vol. 137 Issue 8, August 3, 2011, p. 563-570.

- Gedafa, Daba S.; Khanum, Taslima; Hossain, Mustaque; Schieber, Gregg; 2011, “Effect of construction environment on JPCP performance”, T and DI Congress 2011: Integrated Transportation and Development for a Better Tomorrow - Proceedings of the 1st Congress of the Transportation and Development Institute of ASCE, Chicago, IL, March 13, 2011 - March 16, American Society of Civil Engineers (ASCE), Reston, VA, 2011, p. 834-843.

- Buch, Neeraj; Jahangimejad, Shervin, 2011, “Impact of portland cement concrete coefficient of thermal expansion on the performance of jointed concrete pavements”, International Conference on Concrete Pavement Design, Construction and Rehabilitation, Xi'an, China, April 19, 2011 - April 20, 2011, Society for Concrete Pavements, Inc.

- Jahangimejad, Shervin; Buch, Neeraj; 2010, “Comparison of Portland cement concrete CTE calculation protocols”, Geotechnical Special Publication:  Paving Materials and Pavement Analysis - Proceedings of the 2010 GeoShanghai International Conference, June 3, 2010 - June 5, 2010, Shanghai, China, American Society of Civil Engineers (ASCE), Reston, VA, 2010, p. 176-183.

- Naik, Tarun R.; Kraus, Rudolph N.; Kumar, Rakesh; 2011, “Influence of types of coarse aggregates on the coefficient of thermal expansion of concrete”, Journal of Materials in Civil Engineering, Vol. 23, Issue 4, April 8, 2011, p. 467-472.

- Crawford, Gary L.; Gudimettla, Jagan M.; Tanesi, Jussara; 2010, “Interlaboratory study on measuring coefficient of thermal expansion of concrete”, Transportation Research Record 2164, January 12, 2010, p. 58-65.

- Smith, James T.; Tighe, Susan L.; 2009, “Recycled concrete aggregate coefficient of thermal expansion: Characterization, variability, and impacts on pavement performance”, Transportation Research Record 2113, 2009, p. 53-61.

- Yeon, Jung Heum; Choi, Seongcheol; Won, Moon C.; 2009, “Effect of relative humidity on coefficient of thermal expansion of hardened cement paste and concrete”, Transportation Research Record 2113, 2009, p. 83-91.

- Kohler, E.; Karmekanti, V.; 2008; “Influence of the coefficient of thermal expansion on the cracking of jointed concrete pavements”, Pavement Cracking: Mechanisms, Modeling, Detection, Testing and Case Histories, Proceedings of the 6th RILEM International Conference on Cracking in Pavements, Chicago  IL, June 16, 2008 - June 18, 2008, CRC Press, Netherlands, p. 69-77.

- Tran, Nam H.; Hall, Kevin D.; James, Mainey; 2008, “Coefficient of thermal expansion of concrete materials characterization to support implementation of the mechanistic-empirical pavement design guide”, Transportation Research Record 2087, 2008, p. 51-56.

- Tanesi, J.; Kutay, M.E.; Abbas, A. R.; and Meininger, R.C.; 2007, "Effect of Coefficient of Thermal Expansion Test Variability on Concrete Pavement Performance as Predicted by Mechanistic-Empirical Pavement Design Guide," Transportation Research Record 2020, 2007.

- Hossain, M.; Khanum, T.; Tanesi, J.; Schieber, G.; and Montney, R.A.; 2006, "Portland Cement Concrete Coefficient of Thermal Expansion Input for Mechanistic-Empirical Pavement Design Guide," Proceedings of the 85th Annual Meeting of the Transportation Research Board, Washington, D.C., January 2006.

- Khoury, Naji N.; Brooks, Robert; 2010, “Performance of a stabilized aggregate base subject to different durability procedures”, Journal of Materials in Civil Engineering, Vol. 22, Issue 5, May 2010, p. 506-514.

- Schuettpelz, C.C.; Fratta, D.; Edil, T.B.; 2010, “Mechanistic corrections for determining the resilient modulus of base course materials based on elastic wave measurements”, Journal of Geotechnical and Geoenvironmental Engineering, Vol. 136, Issue 8, August 2010, p. 1086-1094.

- Siripun, K.; Nikraz, H.; Jitsangiam, P.; 2009, “Mechanical behaviour of hydrated cement treated crushed rock base (HCTCRB) under repeated cyclic loads”, Australian Geomechanics Journal, Vol. 44, Issue 4, December 2009, p. 53-64.

- Khogali, W.E.I.; and Mohamed, E.H.H.; 2007, “Mechanistic Classification of Unbound Materials,” Transportation Research Record 2016, 2007.

- Kim, H. B.; 2007, “Development of Reliability-Based Safety Factors for the Mechanistic-Empirical Flexible Pavement Design.” Proceedings of the 86th Annual Meeting of the Transportation Research Board, Washington, D.C., January 2007.

- Li, Qiang; Xiao, Danny; Hall, Kevin; 2011, “Mechanistic-empirical pavement design guide-based pavement design catalog for low-volume roads in Arkansas”, Transportation Research Record 2203, December 1, 2011, p. 169-177.

- Li, Jianhua; Uhlmeyer, Jeff; Mahoney, Joe; Muench, Stephen; 2010, “Updating the pavement design catalog for the Washington State department of transportation”, Transportation Research Record 2154, January 12, 2010, p. 124-129.

- Siraj, N.; Mehta, Y.A.; Muriel, K.M.; Sauber, R.W.; 2009, “Verification of Mechanistic-Empirical pavement design guide for the state of New Jersey”, Bearing Capacity of Roads, Railways and Airfields - Proceedings of the 8th International Conference on the Bearing Capacity of Roads, Railways and Airfields, Champaign  IL, June 29, 2009 - July 2, 2009, CRC Press, Netherlands, p. 921-930.

- Khazanovich, Lev; Yut, Iliya; Husein, Shariq; Turgeon, Carly; Burnham, Tom; 2008, “Adaptation of mechanistic-empirical pavement design guide for design of minnesota low-volume portland cement concrete pavements”, Transportation Research Record 2087, 2008, p. 57-67.

- Haider, Syed Waqar; Buch, Neeraj; Chatti, Karim; 2008, “Evaluation of M-E PDG for rigid pavements - Incorporating the state-of-the-practice in Michigan”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 111-133.

- Schram, S.; and Abdelrahman, M.; 2006, “Improving Prediction Accuracy in the Mechanistic-Empirical Pavement Design Guide.” Transportation Research Record 1947, 2006.

- Swan, D.J.; Tardif, Robert; Hajek, Jerry J.; Hein, David K.; 2008, “Development of regional traffic data for the Mechanistic-Empirical Pavement Design Guide”, Transportation Research Record 2049, 2008, p. 54-62.

- American Association of State Highway and Transportation Officials (AASHTO); 2008, Mechanistic-Empirical Pavement Design Guide, A Manual of Practice, July 2008 Interim Edition, ASSHTO, ISBN:  978-1-56051-423-7.

- American Association of State Highway and Transportation Officials (AASHTO); 2010, Guide for the Local Calibration of the Mechanistic-Empirical Pavement Design Guide, November 2010, ASSHTO, ISBN:  978-1-56051-449-7.

- Sargand, Shad; Khoury, Issam; and Morrison, Jill; 2012, Monitoring and Modeling of Pavement Response and Performance Task B:  New York:  Volume 1:  I490, RT9A, and I86 Perpetual Pavement, Technical Report No. FHWA/OH-2012/08A for the Ohio Department of Transportation, State Job No.  134287, May 2012.

- Sargand, Shad; Khoury, Issam; and Padilla-Llano, David; 2012, Monitoring and Modeling of Pavement Response and Performance Task B:  New York:  Volume 2:  I86 PCC, Technical Report No. FHWA/OH-2012/08B for the Ohio Department of Transportation, State Job No.  134287, May 2012.

- Sargand, Shad; Khoury, Issam; and Hatton, Drew; 2012, Monitoring and Modeling of Pavement Response and Performance Task B:  New York:  Volume 3:  I90, Technical Report No. FHWA/OH-2012/08C for the Ohio Department of Transportation, State Job No.  134287, May 2012.

# Bibliography

American Association of State Highway and Transportation Officials (AASHTO); 2008, Mechanistic-Empirical Pavement Design Guide, A Manual of Practice, July 2008 Interim Edition, ASSHTO, ISBN:  978-1-56051-423-7.

American Association of State Highway and Transportation Officials (AASHTO); 2010, Guide for the Local Calibration of the Mechanistic-Empirical Pavement Design Guide, November 2010, ASSHTO, ISBN:  978-1-56051-449-7.

Asbahan, Rania E.; Vandenbossche, Julie M.; 2011, “Effects of temperature and moisture gradients on slab deformation for jointed plain concrete pavements”, Journal of Transportation Engineering, Vol. 137 Issue 8, August 3, 2011, p. 563-570.

Buch, Neeraj; Jahangimejad, Shervin, 2011, “Impact of portland cement concrete coefficient of thermal expansion on the performance of jointed concrete pavements”, International Conference on Concrete Pavement Design, Construction and Rehabilitation, Xi'an, China, April 19, 2011 - April 20, 2011, Society for Concrete Pavements, Inc.

Chatti, K.; Brake, N.A.; Haider, S.W.; Salama, H.; 2008, “The effect of different axle configurations on the fatigue life of plain cement concrete”, Pavement Cracking: Mechanisms, Modeling, Detection, Testing and Case Histories, Proceedings of the 6th RILEM International Conference on Cracking in Pavements, Chicago  IL, June 16, 2008 - June 18, 2008, CRC Press, Netherlands, p. 155-165.

Crawford, Gary L.; Gudimettla, Jagan M.; Tanesi, Jussara; 2010, “Interlaboratory study on measuring coefficient of thermal expansion of concrete”, Transportation Research Record 2164, January 12, 2010, p. 58-65.

Elfino, Mohamed; Nair, Harikrishnan; Crawford, Gary; Gudimettla, Jagan; 2011, “Comparison of predicted distresses between different input levels using M-E PDG for CRC pavement”, T and DI Congress 2011: Integrated Transportation and Development for a Better Tomorrow - Proceedings of the 1st Congress of the Transportation and Development Institute of ASCE, Chicago, IL, March 13, 2011 - March 16, American Society of Civil Engineers (ASCE), Reston, VA, 2011, p. 558-575.

Gedafa, Daba S.; Khanum, Taslima; Hossain, Mustaque; Schieber, Gregg; 2011, “Effect of construction environment on JPCP performance”, T and DI Congress 2011: Integrated Transportation and Development for a Better Tomorrow - Proceedings of the 1st Congress of the Transportation and Development Institute of ASCE, Chicago, IL, March 13, 2011 - March 16, American Society of Civil Engineers (ASCE), Reston, VA, 2011, p. 834-843.

Haider, Syed Waqar; Buch, Neeraj; Chatti, Karim; 2008, “Evaluation of M-E PDG for rigid pavements - Incorporating the state-of-the-practice in Michigan”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 111-133.

Haider, Syed Waqar; Harichandran, Ronald S.; 2008, “Correlation between properties of axle load distribution and rigid pavement performance measures”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 659-672.

Hiller, Jacob E.; Roesler, Jeffery R.; 2008, “Comparison of mechanistic-empirical thickness design methods and predicted critical fatigue locations”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 171-188.

Hossain, M.; Khanum, T.; Tanesi, J.; Schieber, G.; and Montney, R.A.; 2006, "Portland Cement Concrete Coefficient of Thermal Expansion Input for Mechanistic-Empirical Pavement Design Guide," Proceedings of the 85th Annual Meeting of the Transportation Research Board, Washington, D.C., January 2006.

Hu, Jiong; Wang, Kejin; Ge, Zhi; 2010, “Study of the mechanical properties of Iowa concrete pavement for use in the Mechanistic-Empirical Pavement Design Guide (MEPDG)”, Geotechnical Special Publication:  Paving Materials and Pavement Analysis - Proceedings of the 2010 GeoShanghai International Conference, June 3, 2010 - June 5, 2010, Shanghai, China, American Society of Civil Engineers (ASCE), Reston, VA, 2010, p. 169-175.

Jahangimejad, Shervin; Buch, Neeraj; 2010, “Comparison of Portland cement concrete CTE calculation protocols”, Geotechnical Special Publication:  Paving Materials and Pavement Analysis - Proceedings of the 2010 GeoShanghai International Conference, June 3, 2010 - June 5, 2010, Shanghai, China, American Society of Civil Engineers (ASCE), Reston, VA, 2010, p. 176-183.

Ker, H. W.; Lee, Y. H.; and Wu, P. H.; 2007, “Development of Fatigue Cracking Performance Prediction Models for Flexible Pavements Using LTPP Database.” Proceedings of the 86th Annual Meeting of the Transportation Research Board, Washington, D.C., 2007.

Ker, Hsiang-Wei; Lee, Ying-Haur; Lin, Chia-Huei; 2008, “Prediction models for transverse cracking of jointed concrete pavements: Development with long-term pavement performance database”, Transportation Research Record 2068, 2008, p. 20-31.

Khanum, T.; Hossain, M.; Barezinsky, R.; and Romanaschi, S.A.; 2006, “Influence of Selected Design and Construction Features on JPCP Performance," Proceedings of the 85th Annual Meeting of the Transportation Research Board, Washington,D.C., January 2006.

Khazanovich, Lev; Yut, Iliya; Husein, Shariq; Turgeon, Carly; Burnham, Tom; 2008, “Adaptation of mechanistic-empirical pavement design guide for design of minnesota low-volume portland cement concrete pavements”, Transportation Research Record 2087, 2008, p. 57-67.

Khogali, W.E.I.; and Mohamed, E.H.H.; 2007, “Mechanistic Classification of Unbound Materials,” Transportation Research Record 2016, 2007.

Khoury, Naji N.; Brooks, Robert; 2010, “Performance of a stabilized aggregate base subject to different durability procedures”, Journal of Materials in Civil Engineering, Vol. 22, Issue 5, May 2010, p. 506-514.

Kim, H. B.; 2007, “Development of Reliability-Based Safety Factors for the Mechanistic-Empirical Flexible Pavement Design.” Proceedings of the 86th Annual Meeting of the Transportation Research Board, Washington, D.C., January 2007.

Kohler, E.; Karmekanti, V.; 2008; “Influence of the coefficient of thermal expansion on the cracking of jointed concrete pavements”, Pavement Cracking: Mechanisms, Modeling, Detection, Testing and Case Histories, Proceedings of the 6th RILEM International Conference on Cracking in Pavements, Chicago  IL, June 16, 2008 - June 18, 2008, CRC Press, Netherlands, p. 69-77.

Li, Jianhua; Uhlmeyer, Jeff; Mahoney, Joe; Muench, Stephen; 2010, “Updating the pavement design catalog for the Washington State department of transportation”, Transportation Research Record 2154, January 12, 2010, p. 124-129.

Li, Qiang; Xiao, Danny; Hall, Kevin; 2011, “Mechanistic-empirical pavement design guide-based pavement design catalog for low-volume roads in Arkansas”, Transportation Research Record 2203, December 1, 2011, p. 169-177.

Mallela, Jagannath; Glover, Leslie Titus; Liang, Robert; and Chou, Eddie; 2009, Guidelines for Implementing NCHRP1-37A M-E Design Procedures in Ohio:  Volume 2 – Literature Review, Technical Report No. FHWA/OH-2009/9B for the Ohio Department of Transportation, State Job No.  134300, November 2009.

McCracken, Jennifer K.; Vandenbossche, Julie M.; Asbahan, Rania E.; 2008, “Effect of the MEPDG hierarchal levels on the predicted performance of a jointed plain concrete pavement”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 153-170.

Naik, Tarun R.; Kraus, Rudolph N.; Kumar, Rakesh; 2011, “Influence of types of coarse aggregates on the coefficient of thermal expansion of concrete”, Journal of Materials in Civil Engineering, Vol. 23, Issue 4, April 8, 2011, p. 467-472.

Sargand, Shad; Figueroa, J. Ludwig; and Romanello, Michael; 2008, Instrumentation of the Way-30 Test Pavements, Technical Report No. FHWA/OH-2008/7 for the Ohio Department of Transportation, State Job No.  14815, June 2008.

Sargand, Shad; Masada, Teruhisa; Hernandez, Jaime; and Kim, Sang-Soo; 2010, Determination of Mechanical Properties of Materials Used in Way-30 Test Pavements, Technical Report No. FHWA/OH-2010/9 for the Ohio Department of Transportation, State Job No.  437046, May 2010.

Sargand, Shad; and Figueroa, J. Ludwig; 2010, Monitoring and Modeling of Pavement Response and Performance Task A:  Ohio, Technical Report No. FHWA/OH-2010/03A for the Ohio Department of Transportation, Pooled Fund Project TPF-5(121), State Job No.  134287, June 2010.

Sargand, Shad; Khoury, Issam; and Morrison, Jill; 2012, Monitoring and Modeling of Pavement Response and Performance Task B:  New York:  Volume 1:  I490, RT9A, and I86 Perpetual Pavement, Technical Report No. FHWA/OH-2012/08A for the Ohio Department of Transportation, State Job No.  134287, May 2012.

Sargand, Shad; Khoury, Issam; and Padilla-Llano, David; 2012, Monitoring and Modeling of Pavement Response and Performance Task B:  New York:  Volume 2:  I86 PCC, Technical Report No. FHWA/OH-2012/08B for the Ohio Department of Transportation, State Job No.  134287, May 2012.

Sargand, Shad; Khoury, Issam; and Hatton, Drew; 2012, Monitoring and Modeling of Pavement Response and Performance Task B:  New York:  Volume 3:  I90, Technical Report No. FHWA/OH-2012/08C for the Ohio Department of Transportation, State Job No.  134287, May 2012.

Schram, S.; and Abdelrahman, M.; 2006, “Improving Prediction Accuracy in the Mechanistic-Empirical Pavement Design Guide.” Transportation Research Record 1947, 2006.

Schram, Scott A.; Abdelrahman, Magdy; 2010, “Integration of mechanistic-empirical pavement design guide distresses with local performance indices”, Transportation Research Record 2153, January 12, 2010, p. 13-23.

Schuettpelz, C.C.; Fratta, D.; Edil, T.B.; 2010, “Mechanistic corrections for determining the resilient modulus of base course materials based on elastic wave measurements”, Journal of Geotechnical and Geoenvironmental Engineering, Vol. 136, Issue 8, August 2010, p. 1086-1094.

Schwartz, Charles; Li, Rui; Kim, Sunghwan); Ceylan, Halil; Gopalakrishnan, Kasthurirangan; 2011, “Effect of concrete strength and stiffness characterization on predictions of mechanistic-empirical performance for rigid pavements”, Transportation Research Record 2226, December 1, 2011, p. 41-50.

Siraj, N.; Mehta, Y.A.; Muriel, K.M.; Sauber, R.W.; 2009, “Verification of Mechanistic-Empirical pavement design guide for the state of New Jersey”, Bearing Capacity of Roads, Railways and Airfields - Proceedings of the 8th International Conference on the Bearing Capacity of Roads, Railways and Airfields, Champaign  IL, June 29, 2009 - July 2, 2009, CRC Press, Netherlands, p. 921-930.

Siripun, K.; Nikraz, H.; Jitsangiam, P.; 2009, “Mechanical behaviour of hydrated cement treated crushed rock base (HCTCRB) under repeated cyclic loads”, Australian Geomechanics Journal, Vol. 44, Issue 4, December 2009, p. 53-64.

Smith, James T.; Tighe, Susan L.; 2009, “Recycled concrete aggregate coefficient of thermal expansion: Characterization, variability, and impacts on pavement performance”, Transportation Research Record 2113, 2009, p. 53-61.

Snyder, Mark B.; 2008, “Lessons learned from Mn/ROAD (1992-2007): Low-volume road concrete pavement design and performance”, 9th International Conference on Concrete Pavements: The Golden Gate to Tomorrow's Concrete Pavements, San Francisco, CA, August 17, 2008 - August 21, 2008, p. 364-383.

Swan, D.J.; Tardif, Robert; Hajek, Jerry J.; Hein, David K.; 2008, “Development of regional traffic data for the Mechanistic-Empirical Pavement Design Guide”, Transportation Research Record 2049, 2008, p. 54-62.

Tanesi, J.; Kutay, M.E.; Abbas, A. R.; and Meininger, R.C.; 2007, "Effect of Coefficient of Thermal Expansion Test Variability on Concrete Pavement Performance as Predicted by Mechanistic-Empirical Pavement Design Guide," Transportation Research Record 2020, 2007.

Tran, Nam H.; Hall, Kevin D.; James, Mainey; 2008, “Coefficient of thermal expansion of concrete materials characterization to support implementation of the mechanistic-empirical pavement design guide”, Transportation Research Record 2087, 2008, p. 51-56.

Won, Moon; 2011, “Continuously reinforced concrete pavement”, Transportation Research Record 2226, December 1, 2011, p. 51-59.

Yeon, Jung Heum; Choi, Seongcheol; Won, Moon C.; 2009, “Effect of relative humidity on coefficient of thermal expansion of hardened cement paste and concrete”, Transportation Research Record 2113, 2009, p. 83-91.

Appendix A:   Survey form sent to NYDOT regions

Appendix B:  Resilient Modulus Results

Resilient Modulus Results for NY I-90 Type 3 Sample # 1 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.91 | 2.89 | 21573.66 | 1.34E-04 | 4.31E-06 |
| 2 | 2.91 | 5.74 | 22114.53 | 2.61E-04 | 8.46E-04 |
| 3 | 2.91 | 8.54 | 23774.64 | 3.61E-04 | 2.17E-03 |
| 4 | 4.88 | 4.80 | 26449.12 | 1.83E-04 | 2.77E-03 |
| 5 | 4.88 | 9.44 | 29724.52 | 3.19E-04 | 3.66E-03 |
| 6 | 4.88 | 13.88 | 32649.95 | 4.29E-04 | 5.60E-03 |
| 7 | 9.81 | 9.43 | 43413.86 | 2.22E-04 | 7.14E-03 |
| 8 | 9.81 | 18.61 | 48707.22 | 3.88E-04 | 9.36E-03 |
| 9 | 9.81 | 27.72 | 50743.93 | 5.66E-04 | 1.51E-02 |
| 10 | 14.74 | 9.45 | 53446.81 | 1.77E-04 | 1.54E-02 |
| 11 | 14.74 | 14.06 | 55853.02 | 2.52E-04 | 1.57E-02 |
| 12 | 14.74 | 27.46 | 63373.35 | 4.39E-04 | 1.81E-02 |
| 13 | 19.67 | 14.08 | 67939.47 | 2.08E-04 | 1.85E-02 |
| 14 | 19.67 | 18.46 | 71719.27 | 2.58E-04 | 1.89E-02 |
| 15 | 19.67 | 39.05 | 75794.13 | 5.34E-04 | 2.42E-02 |

Resilient Modulus Results for NY I-90 Type 3 Sample # 2 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.91 | 2.76 | 16640.57 | 1.66E-04 | 6.92E-06 |
| 2 | 2.91 | 5.61 | 16288.56 | 3.50E-04 | 2.17E-03 |
| 3 | 2.91 | 8.54 | 17414.88 | 4.96E-04 | 4.66E-03 |
| 4 | 4.88 | 4.79 | 21178.61 | 2.32E-04 | 6.49E-03 |
| 5 | 4.88 | 9.46 | 25270.69 | 3.78E-04 | 8.17E-03 |
| 6 | 4.88 | 13.90 | 27002.61 | 5.22E-04 | 1.12E-02 |
| 7 | 9.81 | 9.41 | 39818.43 | 2.48E-04 | 1.42E-02 |
| 8 | 9.81 | 18.60 | 43673.99 | 4.36E-04 | 1.74E-02 |
| 9 | 9.81 | 27.87 | 44428.12 | 6.51E-04 | 2.42E-02 |
| 10 | 14.74 | 9.43 | 46040.70 | 2.07E-04 | 2.52E-02 |
| 11 | 14.74 | 14.05 | 50035.97 | 2.81E-04 | 2.57E-02 |
| 12 | 14.74 | 27.78 | 58197.66 | 4.85E-04 | 2.87E-02 |
| 13 | 19.66 | 14.12 | 61966.43 | 2.30E-04 | 2.97E-02 |
| 14 | 19.67 | 18.68 | 67314.51 | 2.78E-04 | 3.01E-02 |
| 15 | 19.67 | 38.49 | 73336.80 | 5.48E-04 | 3.61E-02 |

Resilient Modulus Results for NY I-90 Type 4 Sample # 1 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.91 | 2.72 | 14754.13 | 1.85E-04 | -5.02E-07 |
| 2 | 2.91 | 5.59 | 15198.79 | 3.69E-04 | 9.57E-04 |
| 3 | 2.91 | 8.42 | 15425.41 | 5.49E-04 | 2.76E-03 |
| 4 | 4.88 | 4.71 | 17756.23 | 2.68E-04 | 3.91E-03 |
| 5 | 4.88 | 9.49 | 19832.82 | 4.81E-04 | 5.25E-03 |
| 6 | 4.88 | 14.21 | 21181.10 | 6.81E-04 | 9.42E-03 |
| 7 | 9.81 | 9.45 | 31041.57 | 3.13E-04 | 1.22E-02 |
| 8 | 9.81 | 18.52 | 35601.38 | 5.33E-04 | 1.63E-02 |
| 9 | 9.81 | 27.71 | 37483.04 | 7.83E-04 | 2.69E-02 |
| 10 | 14.74 | 9.47 | 40951.78 | 2.31E-04 | 2.73E-02 |
| 11 | 14.74 | 14.07 | 42871.17 | 3.29E-04 | 2.77E-02 |
| 12 | 14.74 | 27.73 | 49928.10 | 5.65E-04 | 3.13E-02 |
| 13 | 19.67 | 14.15 | 54833.93 | 2.58E-04 | 3.18E-02 |
| 14 | 19.67 | 18.57 | 58429.59 | 3.18E-04 | 3.23E-02 |
| 15 | 19.67 | 38.97 | 62732.63 | 6.47E-04 | 3.91E-02 |

Resilient Modulus Results for NY I-90 Type 4 Sample # 2 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.91 | 2.86 | 23012.75 | 1.24E-04 | -3.85E-06 |
| 2 | 2.91 | 5.69 | 23282.58 | 2.45E-04 | 5.71E-04 |
| 3 | 2.91 | 8.47 | 24631.71 | 3.46E-04 | 1.70E-03 |
| 4 | 4.88 | 4.79 | 29167.26 | 1.65E-04 | 2.38E-03 |
| 5 | 4.88 | 9.39 | 31898.59 | 2.95E-04 | 3.04E-03 |
| 6 | 4.88 | 13.90 | 33042.90 | 4.26E-04 | 5.19E-03 |
| 7 | 9.81 | 9.41 | 47309.52 | 2.03E-04 | 6.67E-03 |
| 8 | 9.81 | 18.51 | 50443.05 | 3.73E-04 | 9.04E-03 |
| 9 | 9.81 | 27.60 | 51261.40 | 5.66E-04 | 1.59E-02 |
| 10 | 14.74 | 9.45 | 59098.85 | 1.60E-04 | 1.61E-02 |
| 11 | 14.74 | 14.02 | 60657.21 | 2.31E-04 | 1.64E-02 |
| 12 | 14.74 | 27.44 | 66399.41 | 4.19E-04 | 1.88E-02 |
| 13 | 19.67 | 14.04 | 75037.80 | 1.88E-04 | 1.92E-02 |
| 14 | 19.67 | 18.46 | 78933.82 | 2.34E-04 | 1.96E-02 |
| 15 | 19.67 | 39.08 | 80389.30 | 5.06E-04 | 2.48E-02 |

Resilient Modulus Results for NY 15 Type 4 Sample # 1 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.90 | 2.76 | 14927.13 | 1.85E-04 | 2.61E-08 |
| 2 | 2.90 | 5.60 | 15635.12 | 3.61E-04 | 1.43E-03 |
| 3 | 2.90 | 8.44 | 16715.11 | 5.13E-04 | 4.59E-03 |
| 4 | 4.87 | 4.71 | 19124.76 | 2.47E-04 | 4.92E-03 |
| 5 | 4.87 | 9.38 | 21545.74 | 4.38E-04 | 6.49E-03 |
| 6 | 4.87 | 13.90 | 22586.57 | 6.32E-04 | 1.18E-02 |
| 7 | 9.80 | 9.39 | 30996.64 | 3.05E-04 | 1.31E-02 |
| 8 | 9.80 | 18.48 | 34506.10 | 5.48E-04 | 1.73E-02 |
| 9 | 9.80 | 27.57 | 35764.29 | 8.27E-04 | 2.97E-02 |
| 10 | 14.72 | 9.40 | 39663.16 | 2.38E-04 | 2.95E-02 |
| 11 | 14.72 | 14.00 | 40493.51 | 3.46E-04 | 2.99E-02 |
| 12 | 14.72 | 27.62 | 46596.39 | 6.02E-04 | 3.37E-02 |
| 13 | 19.65 | 14.06 | 50303.08 | 2.79E-04 | 3.39E-02 |
| 14 | 19.65 | 18.58 | 52991.11 | 3.51E-04 | 3.43E-02 |
| 15 | 19.65 | 38.66 | 58196.65 | 6.92E-04 | 4.16E-02 |

Resilient Modulus Results for NY 15 Type 4 Sample # 1 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.91 | 2.79 | 14554.40 | 1.91E-04 | 8.67E-07 |
| 2 | 2.91 | 5.61 | 15352.81 | 3.68E-04 | 1.27E-03 |
| 3 | 2.91 | 8.44 | 16408.31 | 5.21E-04 | 3.98E-03 |
| 4 | 4.88 | 4.72 | 18380.97 | 2.57E-04 | 4.57E-03 |
| 5 | 4.88 | 9.38 | 21190.29 | 4.45E-04 | 6.09E-03 |
| 6 | 4.88 | 13.92 | 22279.51 | 6.39E-04 | 1.09E-02 |
| 7 | 9.81 | 9.39 | 30759.20 | 3.10E-04 | 1.28E-02 |
| 8 | 9.81 | 18.48 | 34504.72 | 5.49E-04 | 1.71E-02 |
| 9 | 9.81 | 27.56 | 35759.17 | 8.26E-04 | 2.95E-02 |
| 10 | 14.74 | 9.41 | 38849.72 | 2.42E-04 | 2.96E-02 |
| 11 | 14.74 | 14.00 | 40620.17 | 3.45E-04 | 3.00E-02 |
| 12 | 14.74 | 27.62 | 46373.70 | 6.06E-04 | 3.39E-02 |
| 13 | 19.67 | 14.02 | 49752.32 | 2.82E-04 | 3.43E-02 |
| 14 | 19.67 | 18.54 | 52712.36 | 3.52E-04 | 3.47E-02 |
| 15 | 19.67 | 38.87 | 57751.88 | 7.05E-04 | 4.29E-02 |

Resilient Modulus Results for SR 219 Type 4 Sample # 1 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.91 | 2.70 | 15470.64 | 1.75E-04 | -2.62E-06 |
| 2 | 2.91 | 5.48 | 15184.90 | 3.63E-04 | 1.26E-03 |
| 3 | 2.91 | 8.31 | 15806.22 | 5.33E-04 | 4.10E-03 |
| 4 | 4.88 | 4.65 | 18843.92 | 2.47E-04 | 4.77E-03 |
| 5 | 4.88 | 9.32 | 20651.75 | 4.54E-04 | 6.36E-03 |
| 6 | 4.88 | 13.88 | 21153.12 | 6.77E-04 | 1.25E-02 |
| 7 | 9.81 | 9.36 | 29778.23 | 3.19E-04 | 1.44E-02 |
| 8 | 9.81 | 18.43 | 31403.57 | 6.06E-04 | 2.01E-02 |
| 9 | 9.81 | 27.37 | 31281.49 | 9.65E-04 | 3.81E-02 |
| 10 | 14.74 | 9.38 | 37154.20 | 2.52E-04 | 3.83E-02 |
| 11 | 14.74 | 13.97 | 37513.06 | 3.73E-04 | 3.88E-02 |
| 12 | 14.74 | 27.53 | 40796.75 | 6.90E-04 | 4.39E-02 |
| 13 | 19.67 | 14.02 | 45498.86 | 3.08E-04 | 4.44E-02 |
| 14 | 19.67 | 18.55 | 47300.95 | 3.93E-04 | 4.49E-02 |
| 15 | 19.67 | 38.84 | 48843.65 | 8.44E-04 | 5.63E-02 |

Resilient Modulus Results for SR 219 Type 4 Sample # 2 (1 psi = 6.89 kPa, 1 in = 25.4 mm).

| Level | Confining Stress (psi) | Deviatoric Stress (psi) | MR (psi) | Resilient Strain | Permanent Deformation (in) |
| --- | --- | --- | --- | --- | --- |
| 1 | 2.88 | 2.73 | 15054.45 | 1.82E-04 | -3.72E-06 |
| 2 | 2.88 | 5.52 | 15267.20 | 3.63E-04 | 9.82E-04 |
| 3 | 2.88 | 8.32 | 16154.39 | 5.18E-04 | 2.77E-03 |
| 4 | 4.84 | 4.67 | 18387.01 | 2.56E-04 | 3.69E-03 |
| 5 | 4.88 | 9.35 | 20872.15 | 4.51E-04 | 5.44E-03 |
| 6 | 3.97 | 13.97 | 20304.50 | 6.97E-04 | 9.17E-03 |
| 7 | 9.78 | 9.39 | 29546.48 | 3.28E-04 | 1.22E-02 |
| 8 | 9.79 | 18.48 | 33004.57 | 5.69E-04 | 1.56E-02 |
| 9 | 9.79 | 27.45 | 33841.42 | 8.42E-04 | 2.42E-02 |
| 10 | 14.72 | 9.40 | 37163.37 | 2.53E-04 | 2.46E-02 |
| 11 | 14.72 | 14.00 | 38621.91 | 3.63E-04 | 2.51E-02 |
| 12 | 14.72 | 27.52 | 43302.23 | 6.42E-04 | 2.81E-02 |
| 13 | 19.65 | 14.02 | 46580.18 | 3.02E-04 | 2.88E-02 |
| 14 | 19.65 | 18.51 | 49180.45 | 3.77E-04 | 2.92E-02 |
| 15 | 19.66 | 38.83 | 52011.93 | 7.71E-04 | 3.63E-02 |

Appendix C:  Permanent Deformation Test Results

Permanent Deformation Results for NY I-90 Type 3 Sample #1 (1 in = 25.4 mm).

Permanent Deformation Results for NY I-90 Type 3 Sample #2 (1 in = 25.4 mm).

Permanent Deformation Results for NY I-90 Type 4 Sample #1 (1 in = 25.4 mm).

Permanent Deformation Results for NY I-90 Type 4 Sample #2 (1 in = 25.4 mm).

Permanent Deformation Results for NY 15 Type 4 Sample #1 (1 in = 25.4 mm).

Permanent Deformation Results for NY 15 Type 4 Sample #2 (1 in = 25.4 mm).

Permanent Deformation Results for SR 219 Type 4 Sample #1 (1 in = 25.4 mm).

Permanent Deformation Results for SR 219 Type 4 Sample #1 (1 in = 25.4 mm).

Appendix D:  FWD Data from I490 October 11-12, 2006

FWD data for I-490 West, Monroe, Rochester on morning of Oct. 11, 2006, with nominal load 44 kN (10 kip).

| Load | DO L | DO M | LTE L | SPR | D3/D0 M |
| --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |
| 10 | 44 | 1.3433 | 7.6706 | 0.7862 | 4.4896 | 84.40% | 75.30% | 0.9112 |
| 10 | 44 | 1.4196 | 8.1059 | 0.6765 | 3.8628 | 84.34% | 83.87% | 0.9316 |
| 10 | 44 | 1.2614 | 7.2029 | 0.7490 | 4.2767 | 83.89% | 93.16% | 0.9831 |
| 10 | 44 | 1.2374 | 7.0658 | 1.2153 | 6.9396 | 84.42% | 79.21% | 0.8784 |
| 10 | 44 | 0.7824 | 4.4678 | 0.7587 | 4.3323 | 83.63% | 75.10% | 0.9125 |
| 10 | 44 | 0.8045 | 4.5940 | 0.6352 | 3.6269 | 82.61% | 81.65% | 0.9339 |
| 10 | 44 | 0.7190 | 4.1054 | 0.6544 | 3.7368 | 81.91% | 92.94% | 0.9806 |
| 10 | 44 | 0.8244 | 4.7073 | 1.0761 | 6.1446 | 82.17% | 80.70% | 0.9295 |
| 10 | 44 | 0.6630 | 3.7858 | 0.7379 | 4.2135 | 82.59% | 78.26% | 0.9379 |
| 10 | 44 | 0.6879 | 3.9282 | 0.6940 | 3.9626 | 82.23% | 80.73% | 0.9101 |
| 10 | 44 | 0.5944 | 3.3942 | 0.7005 | 4.0001 | 81.61% | 91.36% | 0.9804 |
| 10 | 44 | 0.7126 | 4.0691 | 1.1520 | 6.5778 | 81.79% | 79.14% | 0.8757 |
| 10 | 44 |  |  | 0.3016 | 1.7224 |  | 83.42% | 0.9271 |
| 10 | 44 |  |  | 0.3378 | 1.9289 |  | 101.87% | 0.9814 |
| 10 | 44 |  |  | 0.7097 | 4.0524 |  | 86.11% | 0.9807 |
| 10 | 44 |  |  | 0.3547 | 2.0254 |  | 71.79% | 0.8902 |
| 10 | 44 |  |  | 0.3122 | 1.7825 |  | 83.00% | 0.9392 |
| 10 | 44 |  |  | 0.3150 | 1.7985 |  | 94.00% | 0.9633 |
| 10 | 44 |  |  | 0.6096 | 3.4808 |  | 86.00% | 0.9810 |
| 10 | 44 |  |  | 0.3336 | 1.9050 |  | 80.50% | 0.9340 |
| 10 | 44 |  |  | 0.3682 | 2.1026 |  | 101.52% | 0.9857 |
| 10 | 44 |  |  | 0.7222 | 4.1241 |  | 86.70% | 0.9956 |
| 10 | 44 |  |  | 0.2599 | 1.4839 |  | 83.60% | 0.9150 |
| 10 | 44 |  |  | 0.6650 | 3.7975 |  | 83.02% | 0.9329 |
| 10 | 44 |  |  | 0.2770 | 1.5815 |  | 80.96% | 0.8977 |
| 10 | 44 |  |  | 0.5703 | 3.2564 |  | 81.57% | 0.9182 |
| 10 | 44 |  |  | 0.3054 | 1.7441 |  | 88.08% | 0.9410 |
| Average | 0.9208 | 5.2581 | 0.6029 | 3.4426 | 82.96% | 84.58% | 0.9388 |
| Std. Dev. | 0.3010 | 1.7189 | 0.2693 | 1.5377 | 1.09% | 7.36% | 0.0352 |

FWD data for I-490 West, Monroe, Rochester on morning of Oct. 11, 2006, with nominal load 58 kN (13 kip).

| Load | DO L | DO M | LTE L | SPR | D3/D0 M |
| --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |
| 13 | 58 | 1.3056 | 7.4550 | 0.7753 | 4.4273 | 83.84% | 75.73% | 0.9059 |
| 13 | 58 | 1.3271 | 7.5781 | 0.6650 | 3.7974 | 84.32% | 83.88% | 0.9341 |
| 13 | 58 | 1.2026 | 6.8673 | 0.7328 | 4.1844 | 83.48% | 92.91% | 0.9771 |
| 13 | 58 | 1.1962 | 6.8307 | 1.1703 | 6.6826 | 84.24% | 78.76% | 0.8693 |
| 13 | 58 | 0.7799 | 4.4534 | 0.7525 | 4.2968 | 83.11% | 74.59% | 0.9011 |
| 13 | 58 | 0.7922 | 4.5238 | 0.6282 | 3.5874 | 82.33% | 81.35% | 0.9276 |
| 13 | 58 | 0.7143 | 4.0787 | 0.6442 | 3.6787 | 81.63% | 92.44% | 0.9727 |
| 13 | 58 | 0.8158 | 4.6583 | 1.0281 | 5.8706 | 82.01% | 80.62% | 0.9201 |
| 13 | 58 | 0.6603 | 3.7703 | 0.7081 | 4.0434 | 82.37% | 78.22% | 0.9321 |
| 13 | 58 | 0.6705 | 3.8285 | 0.6770 | 3.8656 | 82.13% | 81.66% | 0.9059 |
| 13 | 58 | 0.5926 | 3.3840 | 0.6832 | 3.9012 | 81.50% | 91.55% | 0.9742 |
| 13 | 58 | 0.7094 | 4.0509 | 1.1168 | 6.3773 | 81.40% | 78.70% | 0.8668 |
| 13 | 58 |  |  | 0.3078 | 1.7577 |  | 84.27% | 0.9154 |
| 13 | 58 |  |  | 0.3424 | 1.9552 |  | 99.76% | 0.9469 |
| 13 | 58 |  |  | 0.7061 | 4.0319 |  | 86.57% | 0.9763 |
| 13 | 58 |  |  | 0.3558 | 2.0320 |  | 72.15% | 0.8894 |
| 13 | 58 |  |  | 0.3210 | 1.8331 |  | 83.33% | 0.9238 |
| 13 | 58 |  |  | 0.3203 | 1.8292 |  | 93.91% | 0.9578 |
| 13 | 58 |  |  | 0.6052 | 3.4559 |  | 86.11% | 0.9725 |
| 13 | 58 |  |  | 0.3390 | 1.9359 |  | 81.39% | 0.9209 |
| 13 | 58 |  |  | 0.3706 | 2.1160 |  | 100.53% | 0.9787 |
| 13 | 58 |  |  | 0.7147 | 4.0813 |  | 86.87% | 0.9878 |
| 13 | 58 |  |  | 0.2657 | 1.5172 |  | 83.64% | 0.9050 |
| 13 | 58 |  |  | 0.6589 | 3.7625 |  | 83.21% | 0.9262 |
| 13 | 58 |  |  | 0.2865 | 1.6357 |  | 81.30% | 0.8984 |
| 13 | 58 |  |  | 0.5608 | 3.2022 |  | 82.08% | 0.9137 |
| 13 | 58 |  |  | 0.2913 | 1.6634 |  | 84.66% | 0.9133 |
| Average |  | 0.8972 | 5.1233 | 0.5936 | 3.3897 | 82.70% | 84.45% | 0.9301 |
| Std. Dev. | 0.2755 | 1.5730 | 0.2557 | 1.4604 | 1.06% | 6.99% | 0.0344 |

FWD data for I-490 West, Monroe, Rochester on morning of Oct. 11, 2006, with nominal load 71 kN (16 kip).

| Load | DO L | DO M | LTE L | SPR | D3/D0 M |
| --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |
| 16 | 71 | 1.2243 | 6.9908 | 0.7346 | 4.1948 | 83.99% | 75.93% | 0.9101 |
| 16 | 71 | 1.2494 | 7.1342 | 0.6410 | 3.6600 | 84.05% | 83.73% | 0.9338 |
| 16 | 71 | 1.1309 | 6.4575 | 0.7024 | 4.0109 | 83.51% | 93.01% | 0.9757 |
| 16 | 71 | 1.1423 | 6.5227 | 1.1192 | 6.3908 | 84.08% | 78.49% | 0.8595 |
| 16 | 71 | 0.7606 | 4.3430 | 0.7190 | 4.1056 | 82.97% | 75.19% | 0.9090 |
| 16 | 71 | 0.7680 | 4.3855 | 0.6042 | 3.4501 | 82.11% | 81.18% | 0.9364 |
| 16 | 71 | 0.6934 | 3.9592 | 0.6202 | 3.5414 | 81.48% | 92.36% | 0.9733 |
| 16 | 71 | 0.7876 | 4.4974 | 0.9730 | 5.5562 | 81.95% | 80.74% | 0.9152 |
| 16 | 71 | 0.6471 | 3.6948 | 0.6764 | 3.8621 | 82.63% | 78.44% | 0.9347 |
| 16 | 71 | 0.6567 | 3.7501 | 0.6460 | 3.6886 | 81.95% | 81.49% | 0.9078 |
| 16 | 71 | 0.5804 | 3.3144 | 0.6562 | 3.7469 | 81.62% | 91.94% | 0.9767 |
| 16 | 71 | 0.6839 | 3.9051 | 1.0778 | 6.1541 | 81.42% | 78.31% | 0.8607 |
| 16 | 71 |  |  | 0.3069 | 1.7524 |  | 84.54% | 0.9214 |
| 16 | 71 |  |  | 0.3325 | 1.8985 |  | 100.70% | 0.9657 |
| 16 | 71 |  |  | 0.6729 | 3.8426 |  | 86.20% | 0.9775 |
| 16 | 71 |  |  | 0.3506 | 2.0018 |  | 72.88% | 0.8940 |
| 16 | 71 |  |  | 0.3176 | 1.8133 |  | 82.96% | 0.9302 |
| 16 | 71 |  |  | 0.3166 | 1.8078 |  | 93.83% | 0.9617 |
| 16 | 71 |  |  | 0.5859 | 3.3454 |  | 85.81% | 0.9703 |
| 16 | 71 |  |  | 0.3356 | 1.9165 |  | 81.07% | 0.9267 |
| 16 | 71 |  |  | 0.3643 | 2.0801 |  | 100.77% | 0.9786 |
| 16 | 71 |  |  | 0.6909 | 3.9454 |  | 86.71% | 0.9825 |
| 16 | 71 |  |  | 0.2685 | 1.5332 |  | 83.24% | 0.9170 |
| 16 | 71 |  |  | 0.6361 | 3.6321 |  | 82.86% | 0.9242 |
| 16 | 71 |  |  | 0.2876 | 1.6425 |  | 81.00% | 0.9083 |
| 16 | 71 |  |  | 0.5490 | 3.1347 |  | 81.81% | 0.9102 |
| 16 | 71 |  |  | 0.2888 | 1.6492 |  | 84.53% | 0.9215 |
| Average |  | 0.8604 | 4.9129 | 0.5731 | 3.2725 | 82.65% | 84.43% | 0.9327 |
| Std. Dev. |  | 0.2495 | 1.4245 | 0.2402 | 1.3718 | 1.04% | 7.05% | 0.0346 |

FWD data for I-490 West, Monroe, Rochester on afternoon of Oct. 11, 2006, with nominal load 44 kN (10 kip).

| Load | DO L | DO M | LTE L | SPR | D3/D0 M |
| --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |
| 10 | 44 | 1.2730 | 7.2689 | 0.7868 | 4.4926 | 85.47% | 74.66% | 0.9170 |
| 10 | 44 | 1.2979 | 7.4115 | 0.6811 | 3.8891 | 85.76% | 85.67% | 0.9468 |
| 10 | 44 | 1.4240 | 8.1311 | 1.1953 | 6.8251 | 86.07% | 84.99% | 1.0767 |
| 10 | 44 | 1.2592 | 7.1903 | 0.8222 | 4.6951 | 86.84% | 77.20% | 0.9210 |
| 10 | 44 | 1.3505 | 7.7113 | 0.6876 | 3.9262 | 84.77% | 83.77% | 0.9495 |
| 10 | 44 | 0.8382 | 4.7860 | 0.7640 | 4.3625 | 83.02% | 92.19% | 0.9794 |
| 10 | 44 | 0.7948 | 4.5387 | 1.1905 | 6.7981 | 83.24% | 78.26% | 0.8712 |
| 10 | 44 | 0.7365 | 4.2053 | 0.8872 | 5.0661 | 82.01% | 77.74% | 0.9277 |
| 10 | 44 | 0.8659 | 4.9445 | 0.8224 | 4.6957 | 82.53% | 87.85% | 0.9564 |
| 10 | 44 | 0.6886 | 3.9317 | 1.2475 | 7.1232 | 83.75% | 76.87% | 0.8458 |
| 10 | 44 | 0.7285 | 4.1600 | 0.3837 | 2.1909 | 81.76% | 70.89% | 0.8932 |
| 10 | 44 | 0.6018 | 3.4366 | 0.3113 | 1.7777 | 82.01% | 83.55% | 0.9327 |
| 10 | 44 | 0.7480 | 4.2713 | 0.3481 | 1.9880 | 81.71% | 104.37% | 0.9939 |
| 10 | 44 |  |  | 0.7356 | 4.2003 |  | 86.13% | 0.9885 |
| 10 | 44 |  |  | 0.3682 | 2.1026 |  | 72.78% | 0.8971 |
| 10 | 44 |  |  | 0.3338 | 1.9062 |  | 84.60% | 0.9272 |
| 10 | 44 |  |  | 0.3393 | 1.9375 |  | 98.02% | 0.9534 |
| 10 | 44 |  |  | 0.6537 | 3.7328 |  | 85.24% | 0.9725 |
| 10 | 44 |  |  | 0.3434 | 1.9609 |  | 78.93% | 0.9264 |
| 10 | 44 |  |  | 0.3348 | 1.9120 |  | 81.68% | 0.9214 |
| 10 | 44 |  |  | 0.7205 | 4.1143 |  | 87.30% | 1.0030 |
| 10 | 44 |  |  | 0.2559 | 1.4610 |  | 82.98% | 0.9174 |
| 10 | 44 |  |  | 0.6503 | 3.7134 |  | 88.46% | 1.0148 |
| 10 | 44 |  |  | 0.2855 | 1.6304 |  | 82.90% | 0.9033 |
| 10 | 44 |  |  | 0.6048 | 3.4533 |  | 81.71% | 0.8989 |
| 10 | 44 |  |  | 0.2947 | 1.6827 |  | 84.12% | 0.9245 |
| 10 | 44 |  |  | 0.6707 | 3.8296 |  | 88.80% | 1.0064 |
| Average | 0.9698 | 5.5375 | 0.6192 | 3.5358 | 83.77% | 83.77% | 0.9432 |
| Std. Dev. | 0.2986 | 1.7048 | 0.2939 | 1.6782 | 1.81% | 7.20% | 0.0496 |

FWD data for I-490 West, Monroe, Rochester on afternoon of Oct. 11, 2006, with nominal load 58 kN (13 kip).

| Load | DO L | DO M | LTE L | SPR | D3/D0 M |
| --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |
| 13 | 58 | 1.2197 | 6.9648 | 0.7682 | 4.3868 | 85.03% | 75.06% | 0.9182 |
| 13 | 58 | 1.2549 | 7.1654 | 0.6679 | 3.8138 | 85.12% | 85.16% | 0.9448 |
| 13 | 58 | 1.3598 | 7.7646 | 1.1595 | 6.6209 | 86.09% | 85.02% | 1.0734 |
| 13 | 58 | 1.2134 | 6.9287 | 0.7986 | 4.5601 | 86.50% | 77.22% | 0.9187 |
| 13 | 58 | 1.2985 | 7.4148 | 0.6900 | 3.9403 | 84.37% | 83.24% | 0.9498 |
| 13 | 58 | 0.8361 | 4.7740 | 0.7521 | 4.2948 | 82.86% | 92.18% | 0.9734 |
| 13 | 58 | 0.7948 | 4.5386 | 1.1553 | 6.5969 | 82.67% | 77.80% | 0.8634 |
| 13 | 58 | 0.7338 | 4.1902 | 0.8514 | 4.8613 | 82.18% | 77.16% | 0.9206 |
| 13 | 58 | 0.8464 | 4.8332 | 0.7965 | 4.5479 | 82.09% | 87.79% | 0.9510 |
| 13 | 58 | 0.6670 | 3.8086 | 1.2150 | 6.9376 | 82.94% | 76.73% | 0.8387 |
| 13 | 58 | 0.7203 | 4.1130 | 0.3884 | 2.2179 | 82.33% | 71.90% | 0.8841 |
| 13 | 58 | 0.6040 | 3.4487 | 0.3214 | 1.8354 | 81.16% | 84.38% | 0.9238 |
| 13 | 58 | 0.7376 | 4.2118 | 0.3580 | 2.0440 | 81.39% | 103.54% | 0.9756 |
| 13 | 58 |  |  | 0.7281 | 4.1578 |  | 86.50% | 0.9738 |
| 13 | 58 |  |  | 0.3675 | 2.0983 |  | 72.82% | 0.8925 |
| 13 | 58 |  |  | 0.3380 | 1.9302 |  | 83.51% | 0.9021 |
| 13 | 58 |  |  | 0.3399 | 1.9410 |  | 97.32% | 0.9509 |
| 13 | 58 |  |  | 0.6358 | 3.6302 |  | 85.35% | 0.9701 |
| 13 | 58 |  |  | 0.3473 | 1.9830 |  | 79.48% | 0.9159 |
| 13 | 58 |  |  | 0.3356 | 1.9166 |  | 81.77% | 0.9106 |
| 13 | 58 |  |  | 0.7226 | 4.1259 |  | 87.32% | 1.0000 |
| 13 | 58 |  |  | 0.2712 | 1.5485 |  | 84.23% | 0.9035 |
| 13 | 58 |  |  | 0.6307 | 3.6011 |  | 88.14% | 1.0089 |
| 13 | 58 |  |  | 0.2955 | 1.6875 |  | 82.16% | 0.8952 |
| 13 | 58 |  |  | 0.5983 | 3.4165 |  | 81.61% | 0.8973 |
| 13 | 58 |  |  | 0.2976 | 1.6995 |  | 83.15% | 0.9019 |
| 13 | 58 |  |  | 0.6778 | 3.8703 |  | 88.36% | 0.9667 |
| Average |  | 0.9451 | 5.3966 | 0.6114 | 3.4913 | 83.44% | 83.66% | 0.9343 |
| Std. Dev. | 0.2763 | 1.5780 | 0.2800 | 1.5989 | 1.77% | 6.98% | 0.0494 |

FWD data for I-490 West, Monroe, Rochester on afternoon of Oct. 11, 2006, with nominal load 71 kN (16 kip).

| Load | DO L | DO M | LTE L | SPR | D3/D0 M |
| --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |
| 16 | 71 | 1.1581 | 6.6128 | 0.7256 | 4.1433 | 84.90% | 76.06% | 0.9189 |
| 16 | 71 | 1.1850 | 6.7666 | 0.6404 | 3.6567 | 85.01% | 85.24% | 0.9459 |
| 16 | 71 | 1.2880 | 7.3549 | 1.1030 | 6.2984 | 86.11% | 84.84% | 1.0760 |
| 16 | 71 | 1.1507 | 6.5707 | 0.7619 | 4.3506 | 86.55% | 77.60% | 0.9195 |
| 16 | 71 | 1.2466 | 7.1185 | 0.6647 | 3.7954 | 84.36% | 83.20% | 0.9452 |
| 16 | 71 | 0.8169 | 4.6645 | 0.7277 | 4.1555 | 82.70% | 91.98% | 0.9772 |
| 16 | 71 | 0.7700 | 4.3970 | 1.1150 | 6.3670 | 82.26% | 77.78% | 0.8625 |
| 16 | 71 | 0.7100 | 4.0543 | 0.8179 | 4.6704 | 81.80% | 77.16% | 0.9211 |
| 16 | 71 | 0.8147 | 4.6523 | 0.7749 | 4.4246 | 81.99% | 88.84% | 0.9511 |
| 16 | 71 | 0.6579 | 3.7566 | 1.1754 | 6.7119 | 82.76% | 76.87% | 0.8348 |
| 16 | 71 | 0.6963 | 3.9758 | 0.3862 | 2.2050 | 82.10% | 71.95% | 0.8932 |
| 16 | 71 | 0.5910 | 3.3745 | 0.3197 | 1.8255 | 81.22% | 84.76% | 0.9168 |
| 16 | 71 | 0.7044 | 4.0223 | 0.3448 | 1.9687 | 81.84% | 102.20% | 0.9755 |
| 16 | 71 |  |  | 0.7060 | 4.0316 |  | 86.57% | 0.9733 |
| 16 | 71 |  |  | 0.3615 | 2.0640 |  | 73.32% | 0.8950 |
| 16 | 71 |  |  | 0.3311 | 1.8909 |  | 83.22% | 0.9129 |
| 16 | 71 |  |  | 0.3339 | 1.9066 |  | 97.01% | 0.9551 |
| 16 | 71 |  |  | 0.6238 | 3.5622 |  | 85.07% | 0.9653 |
| 16 | 71 |  |  | 0.3457 | 1.9737 |  | 80.04% | 0.9221 |
| 16 | 71 |  |  | 0.3410 | 1.9471 |  | 82.98% | 0.9156 |
| 16 | 71 |  |  | 0.6954 | 3.9708 |  | 86.65% | 0.9896 |
| 16 | 71 |  |  | 0.2719 | 1.5524 |  | 84.92% | 0.9183 |
| 16 | 71 |  |  | 0.6005 | 3.4288 |  | 88.51% | 1.0040 |
| 16 | 71 |  |  | 0.2943 | 1.6804 |  | 81.09% | 0.9057 |
| 16 | 71 |  |  | 0.5765 | 3.2916 |  | 81.02% | 0.8907 |
| 16 | 71 |  |  | 0.2980 | 1.7014 |  | 83.84% | 0.9137 |
| 16 | 71 |  |  | 0.6449 | 3.6827 |  | 87.92% | 0.9904 |
| Average |  | 0.9069 | 5.1785 | 0.5919 | 3.3799 | 83.35% | 83.73% | 0.9366 |
| Std. Dev. |  | 0.2553 | 1.4575 | 0.2651 | 1.5136 | 1.79% | 6.72% | 0.0487 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with standard dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.8803 | 5.0267 | 0.8874 | 5.0673 | 0.2856 | 1.6310 | 83.55% | 81.63% | 87.25% | 0.9319 | 1.0507 |
| 10 | 44 | 0.8873 | 5.0664 | 0.9324 | 5.3242 | 0.3327 | 1.9000 | 83.06% | 80.98% | 108.85% | 0.9969 | 1.0042 |
| 10 | 44 | 0.8859 | 5.0588 | 0.9363 | 5.3466 | 0.2737 | 1.5629 | 83.10% | 80.84% | 85.76% | 0.9163 | 0.7077 |
| 10 | 44 | 0.6348 | 3.6249 | 0.6627 | 3.7838 | 0.2855 | 1.6303 | 82.30% | 79.78% | 98.10% | 0.9638 | 1.0997 |
| 10 | 44 | 0.7280 | 4.1569 | 0.7287 | 4.1609 | 0.2765 | 1.5789 | 82.66% | 80.17% | 96.44% | 0.9511 |  |
| 10 | 44 | 0.4768 | 2.7225 | 0.4533 | 2.5882 | 0.2425 | 1.3848 | 82.24% | 79.58% | 82.36% | 0.9134 | 1.0599 |
| 10 | 44 | 0.5456 | 3.1153 | 0.4804 | 2.7431 | 0.2402 | 1.3718 | 81.40% | 80.31% | 83.81% | 0.9170 | 1.1011 |
| 10 | 44 | 0.5926 | 3.3841 | 0.5290 | 3.0205 | 0.2235 | 1.2760 | 82.17% | 81.08% | 83.47% | 0.9343 | 1.0428 |
| 10 | 44 | 0.5931 | 3.3870 | 0.5516 | 3.1498 | 0.2377 | 1.3571 | 82.35% | 79.85% | 81.33% | 0.9336 | 0.9083 |
| 10 | 44 | 0.5283 | 3.0168 | 0.5010 | 2.8608 | 0.2036 | 1.1625 | 82.57% | 80.30% | 82.94% | 0.9639 | 0.9045 |
| 10 | 44 | 0.4868 | 2.7797 | 0.4531 | 2.5876 | 0.2123 | 1.2120 | 81.48% | 80.37% | 82.51% | 0.9059 | 1.0005 |
| 10 | 44 | 0.4997 | 2.8532 | 0.4534 | 2.5889 | 0.2158 | 1.2321 | 82.52% | 78.69% | 81.26% | 0.9073 | 0.9717 |
| 10 | 44 | 0.4963 | 2.8338 | 0.4406 | 2.5157 | 0.2151 | 1.2281 | 80.51% | 78.99% | 81.66% | 0.9069 | 0.9791 |
| 10 | 44 | 0.4664 | 2.6631 | 0.4313 | 2.4631 | 0.2053 | 1.1722 | 80.78% | 79.46% | 80.67% | 0.8808 | 0.9394 |
| 10 | 44 | 0.4470 | 2.5525 | 0.4052 | 2.3138 | 0.2227 | 1.2717 | 82.66% | 79.47% | 84.42% | 0.9190 |  |
| 10 | 44 | 0.4922 | 2.8107 | 0.4558 | 2.6024 | 0.2604 | 1.4870 | 82.90% | 81.59% | 84.64% | 0.9344 | 0.9765 |
| 10 | 44 | 0.4831 | 2.7588 | 0.4451 | 2.5413 | 0.2572 | 1.4687 | 83.70% | 81.19% | 83.36% | 0.9167 | 0.9799 |
| 10 | 44 | 0.4733 | 2.7027 | 0.4361 | 2.4901 | 0.2572 | 1.4687 | 83.14% | 80.30% | 83.76% | 0.9212 |  |
| Average | 0.5888 | 3.3619 | 0.5657 | 3.2305 | 0.2471 | 1.4109 | 82.39% | 80.25% | 86.26% | 0.9286 | 0.9817 |
| Std. Dev. | 0.1530 | 0.8735 | 0.1823 | 1.0411 | 0.0347 | 0.1979 | 0.88% | 0.85% | 7.40% | 0.0269 | 0.0971 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with standard dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.8541 | 4.8768 | 0.8711 | 4.9741 | 0.2954 | 1.6869 | 83.52% | 81.19% | 86.72% | 0.9423 | 1.0455 |
| 13 | 58 | 0.8295 | 4.7364 | 0.9107 | 5.2004 | 0.3378 | 1.9286 | 82.54% | 80.31% | 108.04% | 1.0023 | 0.9976 |
| 13 | 58 | 0.8731 | 4.9855 | 0.9086 | 5.1882 | 0.2806 | 1.6023 | 82.96% | 80.38% | 84.75% | 0.9222 | 0.7261 |
| 13 | 58 | 0.6546 | 3.7381 | 0.6597 | 3.7670 | 0.2913 | 1.6633 | 82.55% | 79.83% | 97.75% | 0.9625 | 1.0840 |
| 13 | 58 | 0.7052 | 4.0267 | 0.7151 | 4.0835 | 0.2756 | 1.5736 | 82.83% | 80.37% | 93.87% | 0.9545 |  |
| 13 | 58 | 0.4789 | 2.7346 | 0.4518 | 2.5796 | 0.2473 | 1.4120 | 82.18% | 80.03% | 81.55% | 0.9016 | 1.0744 |
| 13 | 58 | 0.5426 | 3.0981 | 0.4854 | 2.7717 | 0.2410 | 1.3761 | 81.37% | 79.19% | 83.12% | 0.9088 | 1.0973 |
| 13 | 58 | 0.5808 | 3.3167 | 0.5326 | 3.0414 | 0.2326 | 1.3284 | 81.36% | 79.23% | 86.05% | 0.9161 | 1.0258 |
| 13 | 58 | 0.5846 | 3.3379 | 0.5464 | 3.1200 | 0.2505 | 1.4306 | 82.57% | 79.51% | 82.26% | 0.8969 | 0.9287 |
| 13 | 58 | 0.5328 | 3.0422 | 0.5074 | 2.8976 | 0.2220 | 1.2678 | 81.39% | 78.57% | 83.16% | 0.9081 | 0.9179 |
| 13 | 58 | 0.4902 | 2.7992 | 0.4658 | 2.6596 | 0.2144 | 1.2242 | 80.45% | 78.95% | 81.77% | 0.9048 | 0.9871 |
| 13 | 58 | 0.4977 | 2.8417 | 0.4598 | 2.6254 | 0.2203 | 1.2579 | 82.32% | 78.97% | 81.61% | 0.8964 | 0.9956 |
| 13 | 58 | 0.4972 | 2.8390 | 0.4578 | 2.6139 | 0.2222 | 1.2688 | 79.87% | 78.47% | 82.03% | 0.8972 | 0.9389 |
| 13 | 58 | 0.4666 | 2.6642 | 0.4298 | 2.4541 | 0.2112 | 1.2062 | 81.22% | 80.59% | 81.10% | 0.8885 | 0.9392 |
| 13 | 58 | 0.4523 | 2.5825 | 0.4036 | 2.3049 | 0.2289 | 1.3069 | 81.75% | 80.40% | 84.62% | 0.9063 |  |
| 13 | 58 | 0.4937 | 2.8190 | 0.4563 | 2.6054 | 0.2589 | 1.4786 | 82.64% | 81.28% | 84.19% | 0.9329 | 0.9849 |
| 13 | 58 | 0.4745 | 2.7092 | 0.4494 | 2.5660 | 0.2596 | 1.4826 | 83.67% | 81.55% | 83.18% | 0.9141 | 0.9840 |
| 13 | 58 | 0.4679 | 2.6717 | 0.4422 | 2.5250 | 0.2516 | 1.4368 | 82.65% | 82.05% | 83.45% | 0.9373 |  |
| Average | 0.5820 | 3.3233 | 0.5641 | 3.2210 | 0.2523 | 1.4406 | 82.10% | 80.05% | 86.07% | 0.9218 | 0.9818 |
| Std. Dev. | 0.1415 | 0.8079 | 0.1721 | 0.9829 | 0.0336 | 0.1918 | 1.00% | 1.04% | 7.01% | 0.0291 | 0.0906 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with standard dowel bar configuration under nominal load of 71 kN (16 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 16 | 71 | 0.8138 | 4.6468 | 0.8340 | 4.7625 | 0.2960 | 1.6899 | 83.04% | 81.01% | 86.77% | 0.9310 | 1.0354 |
| 16 | 71 | 0.8212 | 4.6893 | 0.8635 | 4.9308 | 0.3376 | 1.9277 | 82.68% | 80.56% | 107.76% | 0.9929 | 1.0012 |
| 16 | 71 | 0.8292 | 4.7350 | 0.8645 | 4.9366 | 0.2799 | 1.5981 | 82.54% | 80.57% | 84.73% | 0.9147 | 0.7539 |
| 16 | 71 | 0.6380 | 3.6429 | 0.6518 | 3.7216 | 0.2880 | 1.6447 | 82.08% | 80.04% | 96.79% | 0.9564 | 1.0689 |
| 16 | 71 | 0.6955 | 3.9711 | 0.6966 | 3.9778 | 0.2783 | 1.5894 | 82.35% | 80.14% | 93.63% | 0.9438 |  |
| 16 | 71 | 0.4737 | 2.7047 | 0.4563 | 2.6053 | 0.2517 | 1.4370 | 81.96% | 79.37% | 81.69% | 0.8998 | 1.0589 |
| 16 | 71 | 0.5295 | 3.0234 | 0.4831 | 2.7587 | 0.2435 | 1.3906 | 81.29% | 79.60% | 83.61% | 0.9044 | 1.0860 |
| 16 | 71 | 0.5588 | 3.1908 | 0.5247 | 2.9959 | 0.2316 | 1.3223 | 82.08% | 79.27% | 85.93% | 0.9203 | 1.0104 |
| 16 | 71 | 0.5701 | 3.2552 | 0.5301 | 3.0272 | 0.2494 | 1.4241 | 81.98% | 79.98% | 81.94% | 0.9048 | 0.9446 |
| 16 | 71 | 0.5218 | 2.9795 | 0.5008 | 2.8595 | 0.2254 | 1.2872 | 82.04% | 79.17% | 83.11% | 0.9101 | 0.9250 |
| 16 | 71 | 0.4838 | 2.7626 | 0.4632 | 2.6450 | 0.2181 | 1.2455 | 81.22% | 79.22% | 82.42% | 0.9068 | 0.9828 |
| 16 | 71 | 0.4959 | 2.8319 | 0.4553 | 2.5996 | 0.2194 | 1.2526 | 81.60% | 79.74% | 81.78% | 0.8997 | 1.0028 |
| 16 | 71 | 0.4928 | 2.8141 | 0.4565 | 2.6069 | 0.2259 | 1.2902 | 79.88% | 79.08% | 81.55% | 0.8997 | 0.9433 |
| 16 | 71 | 0.4634 | 2.6463 | 0.4307 | 2.4592 | 0.2141 | 1.2227 | 80.36% | 80.14% | 80.92% | 0.8788 | 0.9535 |
| 16 | 71 | 0.4507 | 2.5737 | 0.4107 | 2.3449 | 0.2277 | 1.3000 | 82.12% | 79.17% | 83.58% | 0.9013 |  |
| 16 | 71 | 0.4846 | 2.7674 | 0.4530 | 2.5868 | 0.2604 | 1.4867 | 82.24% | 80.85% | 84.89% | 0.9271 | 0.9856 |
| 16 | 71 | 0.4643 | 2.6511 | 0.4465 | 2.5496 | 0.2591 | 1.4793 | 82.86% | 81.59% | 83.28% | 0.9192 | 0.9857 |
| 16 | 71 | 0.4619 | 2.6374 | 0.4401 | 2.5130 | 0.2568 | 1.4664 | 82.22% | 81.30% | 84.11% | 0.9238 |  |
| Average | 0.5694 | 3.2513 | 0.5534 | 3.1601 | 0.2535 | 1.4475 | 81.92% | 80.04% | 86.03% | 0.9186 | 0.9825 |
| Std. Dev. | 0.1324 | 0.7561 | 0.1567 | 0.8947 | 0.0328 | 0.1871 | 0.81% | 0.79% | 6.83% | 0.0259 | 0.0792 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with E1 dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.7261 | 4.1460 | 0.7162 | 4.0894 | 0.2776 | 1.5853 | 82.34% | 80.38% | 86.57% | 0.9363 | 0.9930 |
| 10 | 44 | 0.7443 | 4.2503 | 0.7112 | 4.0608 | 0.2464 | 1.4070 | 82.10% | 80.82% | 93.08% | 0.9574 | 0.3465 |
| 10 | 44 | 0.6328 | 3.6136 | 0.7275 | 4.1539 | 0.2564 | 1.4643 | 83.19% | 81.12% | 89.29% | 0.9472 | 0.9262 |
| 10 | 44 | 0.6882 | 3.9298 | 0.6738 | 3.8474 | 0.2667 | 1.5229 | 82.77% | 79.78% | 87.51% | 0.9333 | 1.0560 |
| 10 | 44 | 0.7055 | 4.0283 | 0.7115 | 4.0628 | 0.2924 | 1.6694 | 83.38% | 80.33% | 86.31% | 0.9065 | 1.0327 |
| 10 | 44 | 0.7301 | 4.1690 | 0.7348 | 4.1957 | 0.2950 | 1.6846 | 83.31% | 80.98% | 86.31% | 0.9359 | 1.0556 |
| 10 | 44 | 0.7792 | 4.4495 | 0.7757 | 4.4291 | 0.2972 | 1.6973 | 82.63% | 80.08% | 85.74% | 0.9364 | 0.9937 |
| 10 | 44 | 0.7694 | 4.3934 | 0.7708 | 4.4013 | 0.3074 | 1.7552 | 82.60% | 80.08% | 79.60% | 0.9147 | 1.0148 |
| 10 | 44 | 0.7231 | 4.1289 | 0.7822 | 4.4663 | 0.2729 | 1.5584 | 81.94% | 80.00% | 84.11% | 0.9035 | 0.8824 |
| 10 | 44 | 0.5069 | 2.8947 | 0.6902 | 3.9410 | 0.2560 | 1.4620 | 81.26% | 80.92% | 85.19% | 0.9375 |  |
| 10 | 44 | 0.4769 | 2.7232 | 0.4883 | 2.7880 | 0.2466 | 1.4083 | 81.98% | 76.60% | 85.17% | 0.9351 | 0.9248 |
| 10 | 44 | 0.5020 | 2.8667 | 0.4515 | 2.5782 | 0.2546 | 1.4540 | 82.77% | 80.71% | 85.05% | 0.9289 | 1.0488 |
| 10 | 44 | 0.5485 | 3.1322 | 0.4735 | 2.7040 | 0.2563 | 1.4637 | 83.20% | 80.77% | 82.64% | 0.9378 | 1.0683 |
| 10 | 44 | 0.4639 | 2.6491 | 0.5059 | 2.8886 | 0.2506 | 1.4307 | 82.72% | 81.43% | 83.05% | 0.9444 | 0.9085 |
| 10 | 44 | 0.4789 | 2.7345 | 0.4596 | 2.6243 | 0.2551 | 1.4565 | 83.04% | 80.74% | 83.36% | 0.9247 | 0.9873 |
| 10 | 44 | 0.4679 | 2.6719 | 0.4538 | 2.5911 | 0.2450 | 1.3992 | 83.14% | 80.47% | 84.41% | 0.9391 | 1.0205 |
| 10 | 44 | 0.4628 | 2.6428 | 0.4631 | 2.6443 | 0.2506 | 1.4309 | 82.64% | 80.05% | 83.02% | 0.9319 | 0.9522 |
| 10 | 44 | 0.4431 | 2.5299 | 0.4410 | 2.5179 | 0.2455 | 1.4016 | 82.77% | 80.63% | 83.74% | 0.9130 | 0.9899 |
| 10 | 44 | 0.4657 | 2.6593 | 0.4365 | 2.4925 | 0.2391 | 1.3651 | 82.80% | 80.88% | 82.38% | 0.9241 | 0.9813 |
| 10 | 44 | 0.4627 | 2.6421 | 0.4283 | 2.4458 | 0.2300 | 1.3134 | 80.14% | 80.80% | 82.83% | 0.9116 |  |
| 10 | 44 | 0.4219 | 2.4092 | 0.4420 | 2.5240 | 0.2125 | 1.2134 | 80.76% | 78.74% | 81.02% | 0.8990 | 0.9067 |
| 10 | 44 | 0.4702 | 2.6849 | 0.4008 | 2.2884 | 0.2094 | 1.1960 | 81.46% | 80.05% | 79.43% | 0.9031 | 1.1002 |
| 10 | 44 | 0.4510 | 2.5751 | 0.4409 | 2.5176 | 0.2070 | 1.1817 | 79.95% | 78.54% | 78.81% | 0.9021 | 0.9691 |
| 10 | 44 | 0.4283 | 2.4458 | 0.4273 | 2.4398 | 0.2089 | 1.1930 | 80.30% | 78.89% | 83.53% | 0.9239 | 0.9194 |
| 10 | 44 |  |  | 0.3928 | 2.2432 |  |  |  | 77.66% |  |  |  |
| Average | 0.5646 | 3.2238 | 0.5600 | 3.1974 | 0.2533 | 1.4464 | 82.22% | 80.06% | 84.26% | 0.9261 | 0.9581 |
| Std. Dev. | 0.1297 | 0.5523 | 0.1197 | 0.6833 | 0.0256 | 0.1462 | 1.11% | 1.29% | 1.99% | 0.0148 | 0.0641 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with E1 dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.7094 | 4.0506 | 0.7032 | 4.0156 | 0.2871 | 1.6396 | 82.63% | 80.02% | 87.32% | 0.9264 | 0.9828 |
| 13 | 58 | 0.7191 | 4.1060 | 0.6911 | 3.9464 | 0.2495 | 1.4246 | 82.24% | 81.16% | 89.77% | 0.9375 | 0.3610 |
| 13 | 58 | 0.6197 | 3.5387 | 0.7052 | 4.0269 | 0.2590 | 1.4792 | 83.31% | 81.12% | 88.63% | 0.9396 | 0.9453 |
| 13 | 58 | 0.6702 | 3.8272 | 0.6667 | 3.8068 | 0.2696 | 1.5394 | 82.92% | 79.57% | 86.82% | 0.9333 | 1.0373 |
| 13 | 58 | 0.6840 | 3.9058 | 0.6916 | 3.9489 | 0.2949 | 1.6839 | 83.12% | 80.48% | 86.10% | 0.9122 | 1.0062 |
| 13 | 58 | 0.7097 | 4.0522 | 0.6959 | 3.9735 | 0.2995 | 1.7103 | 83.74% | 80.62% | 85.56% | 0.9319 | 1.0815 |
| 13 | 58 | 0.7541 | 4.3058 | 0.7526 | 4.2974 | 0.3020 | 1.7242 | 82.59% | 80.32% | 85.89% | 0.9377 | 0.9937 |
| 13 | 58 | 0.7475 | 4.2685 | 0.7478 | 4.2703 | 0.3096 | 1.7679 | 82.29% | 80.19% | 79.06% | 0.9137 | 1.0117 |
| 13 | 58 | 0.7043 | 4.0215 | 0.7566 | 4.3202 | 0.2718 | 1.5523 | 82.34% | 80.57% | 83.00% | 0.9159 | 0.8935 |
| 13 | 58 | 0.5105 | 2.9153 | 0.6760 | 3.8599 | 0.2621 | 1.4965 | 81.38% | 81.01% | 83.75% | 0.9154 |  |
| 13 | 58 | 0.4795 | 2.7381 | 0.4925 | 2.8121 | 0.2523 | 1.4404 | 80.93% | 76.26% | 84.83% | 0.9279 | 0.9276 |
| 13 | 58 | 0.5038 | 2.8770 | 0.4568 | 2.6086 | 0.2607 | 1.4884 | 82.08% | 80.63% | 84.80% | 0.9184 | 1.0440 |
| 13 | 58 | 0.5471 | 3.1243 | 0.4769 | 2.7234 | 0.2623 | 1.4977 | 82.90% | 81.00% | 83.44% | 0.9311 | 1.0624 |
| 13 | 58 | 0.4720 | 2.6952 | 0.5067 | 2.8933 | 0.2526 | 1.4425 | 82.55% | 81.53% | 82.44% | 0.9346 | 0.9064 |
| 13 | 58 | 0.4737 | 2.7049 | 0.4593 | 2.6224 | 0.2569 | 1.4668 | 82.24% | 80.55% | 83.56% | 0.9202 | 0.9961 |
| 13 | 58 | 0.4724 | 2.6973 | 0.4575 | 2.6122 | 0.2469 | 1.4097 | 82.52% | 81.31% | 84.53% | 0.9361 | 1.0060 |
| 13 | 58 | 0.4617 | 2.6366 | 0.4602 | 2.6279 | 0.2493 | 1.4233 | 82.79% | 80.69% | 83.07% | 0.9274 | 0.9767 |
| 13 | 58 | 0.4476 | 2.5558 | 0.4495 | 2.5665 | 0.2466 | 1.4082 | 81.59% | 80.25% | 82.38% | 0.9199 | 0.9734 |
| 13 | 58 | 0.4637 | 2.6480 | 0.4375 | 2.4984 | 0.2446 | 1.3966 | 81.37% | 80.69% | 82.90% | 0.9129 | 0.9917 |
| 13 | 58 | 0.4650 | 2.6554 | 0.4339 | 2.4776 | 0.2357 | 1.3459 | 81.20% | 80.66% | 81.74% | 0.8993 |  |
| 13 | 58 | 0.4277 | 2.4420 | 0.4444 | 2.5373 | 0.2201 | 1.2569 | 80.11% | 79.43% | 80.82% | 0.8925 | 0.9039 |
| 13 | 58 | 0.4666 | 2.6641 | 0.4017 | 2.2935 | 0.2186 | 1.2484 | 81.29% | 79.76% | 79.74% | 0.8881 | 1.0937 |
| 13 | 58 | 0.4559 | 2.6031 | 0.4393 | 2.5084 | 0.2131 | 1.2168 | 80.31% | 78.77% | 79.35% | 0.9037 | 0.9838 |
| 13 | 58 | 0.4289 | 2.4488 | 0.4322 | 2.4677 | 0.2057 | 1.1748 | 80.04% | 78.68% | 81.79% | 0.9119 | 0.9205 |
| 13 | 58 |  |  | 0.3978 | 2.2716 |  |  |  | 79.28% |  |  |  |
| Average | 0.5581 | 3.1868 | 0.5533 | 3.1595 | 0.2571 | 1.4681 | 82.02% | 80.18% | 83.80% | 0.9203 | 0.9591 |
| Std. Dev. | 0.1188 | 0.5109 | 0.1106 | 0.6313 | 0.0248 | 0.1417 | 0.92% | 1.25% | 1.81% | 0.0139 | 0.0603 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with E1 dowel bar configuration under nominal load of 71 kN (16 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 16 | 71 | 0.6838 | 3.9047 | 0.6760 | 3.8599 | 0.2847 | 1.6254 | 82.07% | 80.25% | 87.69% | 0.9389 | 0.9897 |
| 16 | 71 | 0.6851 | 3.9121 | 0.6690 | 3.8200 | 0.2474 | 1.4125 | 82.08% | 80.91% | 89.48% | 0.9424 | 0.3698 |
| 16 | 71 | 0.6029 | 3.4428 | 0.6723 | 3.8388 | 0.2601 | 1.4854 | 82.82% | 80.71% | 88.10% | 0.9379 | 0.9578 |
| 16 | 71 | 0.6418 | 3.6651 | 0.6439 | 3.6769 | 0.2719 | 1.5525 | 82.79% | 79.55% | 86.79% | 0.9300 | 1.0349 |
| 16 | 71 | 0.6466 | 3.6923 | 0.6664 | 3.8052 | 0.2963 | 1.6920 | 83.15% | 80.22% | 85.91% | 0.9116 | 1.0053 |
| 16 | 71 | 0.6810 | 3.8888 | 0.6699 | 3.8252 |  | 1.7005 | 83.30% | 80.29% | 85.52% | 0.9337 | 1.0747 |
| 16 | 71 | 0.7186 | 4.1035 | 0.7199 | 4.1108 | 0.3003 | 1.7150 | 82.33% | 80.15% | 85.18% | 0.9343 | 1.0000 |
| 16 | 71 | 0.7134 | 4.0738 | 0.7199 | 4.1106 | 0.3089 | 1.7638 | 82.03% | 79.90% | 80.01% | 0.9130 | 1.0139 |
| 16 | 71 | 0.6747 | 3.8527 | 0.7299 | 4.1676 | 0.2747 | 1.5687 | 82.13% | 80.16% | 83.75% | 0.9091 | 0.8990 |
| 16 | 71 | 0.5061 | 2.8898 | 0.6561 | 3.7467 | 0.2613 | 1.4923 | 80.98% | 80.88% | 83.46% | 0.9226 |  |
| 16 | 71 | 0.4764 | 2.7203 | 0.4908 | 2.8027 | 0.2556 | 1.4593 | 81.14% | 76.57% | 84.80% | 0.9306 | 0.9294 |
| 16 | 71 | 0.4947 | 2.8247 | 0.4562 | 2.6049 | 0.2599 | 1.4838 | 82.59% | 79.92% | 85.15% | 0.9222 | 1.0437 |
| 16 | 71 | 0.5398 | 3.0826 | 0.4761 | 2.7186 | 0.2638 | 1.5063 | 82.91% | 81.38% | 83.10% | 0.9371 | 1.0594 |
| 16 | 71 | 0.4667 | 2.6648 | 0.5044 | 2.8800 | 0.2568 | 1.4661 | 82.18% | 81.59% | 83.02% | 0.9352 | 0.9108 |
| 16 | 71 | 0.4690 | 2.6778 | 0.4594 | 2.6230 | 0.2566 | 1.4650 | 82.40% | 80.44% | 82.84% | 0.9145 | 1.0019 |
| 16 | 71 | 0.4712 | 2.6908 | 0.4602 | 2.6279 | 0.2371 | 1.3540 | 82.74% | 80.83% | 81.74% | 0.9325 | 0.9981 |
| 16 | 71 | 0.4567 | 2.6079 | 0.4593 | 2.6229 | 0.2501 | 1.4284 | 82.48% | 80.57% | 83.15% | 0.9335 | 0.9597 |
| 16 | 71 | 0.4426 | 2.5271 | 0.4408 | 2.5172 | 0.2468 | 1.4091 | 81.67% | 80.30% | 82.76% | 0.9181 | 0.9910 |
| 16 | 71 | 0.4571 | 2.6099 | 0.4369 | 2.4946 | 0.2403 | 1.3721 | 81.05% | 80.79% | 81.71% | 0.9163 | 0.9884 |
| 16 | 71 | 0.4634 | 2.6463 | 0.4318 | 2.4658 | 0.2392 | 1.3656 | 80.18% | 80.25% | 82.32% | 0.9104 |  |
| 16 | 71 | 0.4245 | 2.4240 | 0.4431 | 2.5300 | 0.2220 | 1.2678 | 80.59% | 79.16% | 79.88% | 0.9037 | 0.9192 |
| 16 | 71 | 0.4609 | 2.6317 | 0.4073 | 2.3256 | 0.2187 | 1.2489 | 81.06% | 79.79% | 79.16% | 0.9027 | 1.0857 |
| 16 | 71 | 0.4480 | 2.5583 | 0.4422 | 2.5249 | 0.2162 | 1.2344 | 80.59% | 79.27% | 79.65% | 0.9096 | 0.9747 |
| 16 | 71 | 0.4315 | 2.4637 | 0.4310 | 2.4611 | 0.2117 | 1.2087 | 80.19% | 79.14% | 82.54% | 0.9050 | 0.9311 |
| 16 | 71 |  |  | 0.4013 | 2.2916 |  |  |  | 79.17% |  |  |  |
| Average | 0.5440 | 3.1065 | 0.5426 | 3.0981 | 0.2574 | 1.4699 | 81.89% | 80.09% | 83.65% | 0.9227 | 0.9608 |
| Std. Dev. | 0.1060 | 0.4593 | 0.1010 | 0.5770 | 0.0241 | 0.1378 | 0.92% | 1.13% | 1.75% | 0.0116 | 0.0561 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with E2 dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.6848 | 3.9101 | 0.7024 | 4.0111 | 0.2400 | 1.3707 | 82.20% | 78.97% | 88.35% | 0.9083 | 1.0120 |
| 10 | 44 | 0.7125 | 4.0687 | 0.7109 | 4.0593 | 0.2486 | 1.4198 | 82.47% | 80.21% | 83.74% | 0.9202 | 0.8417 |
| 10 | 44 | 0.6524 | 3.7251 | 0.5983 | 3.4166 | 0.2393 | 1.3663 | 81.85% | 79.79% | 83.04% | 0.8991 | 0.9215 |
| 10 | 44 | 0.5380 | 3.0720 | 0.5514 | 3.1484 | 0.2276 | 1.2997 | 81.34% | 78.03% | 82.03% | 0.9074 | 0.8689 |
| 10 | 44 | 0.5170 | 2.9523 | 0.4791 | 2.7355 | 0.2314 | 1.3211 | 82.21% | 79.30% | 80.84% | 0.9091 | 0.9388 |
| 10 | 44 | 0.4557 | 2.6024 | 0.4497 | 2.5681 | 0.2287 | 1.3059 | 83.37% | 80.47% | 85.77% | 0.9220 | 1.0106 |
| 10 | 44 | 0.4613 | 2.6343 | 0.4545 | 2.5952 | 0.2227 | 1.2717 | 81.84% | 79.30% | 82.41% | 0.9143 | 1.0398 |
| 10 | 44 | 0.4618 | 2.6368 | 0.4726 | 2.6985 | 0.2348 | 1.3410 | 82.34% | 78.56% | 86.70% | 0.9099 | 0.8770 |
| 10 | 44 | 0.4548 | 2.5972 | 0.4145 | 2.3666 | 0.2378 | 1.3577 | 82.24% | 81.54% | 84.59% | 0.9248 | 1.0879 |
| 10 | 44 | 0.4437 | 2.5336 | 0.4509 | 2.5745 | 0.2405 | 1.3734 | 82.86% | 79.20% | 84.06% | 0.9127 |  |
| 10 | 44 | 0.4672 | 2.6680 | 0.4425 | 2.5270 | 0.2362 | 1.3486 | 81.84% | 78.99% | 85.82% | 0.9273 | 1.0613 |
| 10 | 44 | 0.4932 | 2.8165 | 0.4697 | 2.6819 | 0.2487 | 1.4199 | 82.61% | 80.73% | 83.93% | 0.9227 | 0.9381 |
| 10 | 44 | 0.4652 | 2.6566 | 0.4406 | 2.5158 | 0.2366 | 1.3508 | 82.22% | 80.68% | 83.12% | 0.9186 | 0.9557 |
| 10 | 44 | 0.4507 | 2.5738 | 0.4211 | 2.4043 | 0.2315 | 1.3218 | 82.38% | 80.87% | 84.77% | 0.9309 | 1.0037 |
| 10 | 44 | 0.4508 | 2.5741 | 0.4226 | 2.4132 | 0.2396 | 1.3684 | 82.90% | 81.22% | 82.96% | 0.9241 | 1.0942 |
| 10 | 44 | 0.4752 | 2.7133 | 0.4624 | 2.6405 | 0.2539 | 1.4498 | 82.58% | 80.47% | 84.11% | 0.9289 | 1.0109 |
| 10 | 44 | 0.5089 | 2.9056 | 0.4674 | 2.6691 | 0.2467 | 1.4087 | 81.97% | 80.91% | 84.14% | 0.9145 | 0.9561 |
| 10 | 44 | 0.4692 | 2.6791 | 0.4469 | 2.5521 | 0.2489 | 1.4212 | 82.05% | 79.86% | 84.29% | 0.9407 | 1.0096 |
| 10 | 44 | 0.4729 | 2.7003 | 0.4512 | 2.5767 | 0.2544 | 1.4527 | 83.37% | 81.32% | 83.78% | 0.9417 | 1.0517 |
| 10 | 44 | 0.5238 | 2.9910 | 0.4746 | 2.7099 | 0.2575 | 1.4703 | 83.23% | 81.96% | 82.53% | 0.9300 |  |
| 10 | 44 | 0.3776 | 2.1564 | 0.3517 | 2.0085 | 0.2156 | 1.2310 | 81.07% | 79.09% | 84.80% | 0.9208 | 0.9944 |
| 10 | 44 | 0.3923 | 2.2401 | 0.3498 | 1.9972 | 0.2310 | 1.3190 | 82.02% | 80.18% | 85.28% | 0.9217 | 1.2022 |
| 10 | 44 | 0.4532 | 2.5877 | 0.4205 | 2.4011 | 0.2663 | 1.5207 | 83.45% | 80.96% | 85.87% | 0.9398 | 1.0783 |
| 10 | 44 | 0.4699 | 2.6834 | 0.4534 | 2.5891 | 0.2565 | 1.4649 | 82.38% | 81.75% | 83.79% | 0.9253 | 0.9115 |
| 10 | 44 | 0.4319 | 2.4662 | 0.4133 | 2.3601 | 0.2521 | 1.4394 | 82.38% | 80.78% | 84.12% | 0.9364 |  |
| Average | 0.4914 | 2.8058 | 0.4709 | 2.6888 | 0.2411 | 1.3766 | 82.37% | 80.21% | 84.19% | 0.9220 | 0.9939 |
| Std. Dev. | 0.0809 | 0.2001 | 0.0366 | 0.2088 | 0.0123 | 0.0701 | 0.59% | 1.00% | 1.06% | 0.0094 | 0.0834 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with E2 dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.6675 | 3.8113 | 0.6864 | 3.9193 | 0.2620 | 1.4960 | 82.07% | 79.40% | 85.83% | 0.9189 | 1.0127 |
| 13 | 58 | 0.6914 | 3.9479 | 0.6951 | 3.9692 | 0.2544 | 1.4529 | 82.47% | 79.61% | 83.44% | 0.9198 | 0.8385 |
| 13 | 58 | 0.6346 | 3.6234 | 0.5829 | 3.3283 | 0.2412 | 1.3775 | 81.90% | 80.03% | 82.57% | 0.9055 | 0.9443 |
| 13 | 58 | 0.5394 | 3.0800 | 0.5504 | 3.1428 | 0.2362 | 1.3485 | 81.18% | 78.21% | 81.74% | 0.8904 | 0.8676 |
| 13 | 58 | 0.5118 | 2.9223 | 0.4775 | 2.7266 | 0.2366 | 1.3508 | 82.87% | 79.50% | 81.40% | 0.9073 | 0.9506 |
| 13 | 58 | 0.4601 | 2.6272 | 0.4539 | 2.5918 | 0.2322 | 1.3256 | 82.56% | 80.31% | 85.13% | 0.9291 | 0.9878 |
| 13 | 58 | 0.4573 | 2.6113 | 0.4483 | 2.5601 | 0.2253 | 1.2865 | 82.07% | 79.44% | 82.10% | 0.9094 | 1.0460 |
| 13 | 58 | 0.4643 | 2.6512 | 0.4690 | 2.6780 | 0.2351 | 1.3423 | 82.28% | 79.05% | 85.67% | 0.9200 | 0.8849 |
| 13 | 58 | 0.4542 | 2.5937 | 0.4150 | 2.3697 | 0.2378 | 1.3580 | 80.98% | 80.04% | 84.39% | 0.9305 | 1.0834 |
| 13 | 58 | 0.4471 | 2.5528 | 0.4496 | 2.5673 | 0.2459 | 1.4039 | 82.54% | 79.82% | 82.88% | 0.9105 |  |
| 13 | 58 | 0.4680 | 2.6723 | 0.4453 | 2.5428 | 0.2396 | 1.3683 | 81.19% | 79.22% | 85.51% | 0.9211 | 1.0346 |
| 13 | 58 | 0.4865 | 2.7783 | 0.4607 | 2.6307 | 0.2466 | 1.4082 | 82.22% | 81.24% | 84.17% | 0.9295 | 0.9561 |
| 13 | 58 | 0.4601 | 2.6270 | 0.4405 | 2.5151 | 0.2380 | 1.3591 | 82.24% | 80.94% | 82.33% | 0.9236 | 0.9491 |
| 13 | 58 | 0.4572 | 2.6105 | 0.4181 | 2.3871 | 0.2359 | 1.3473 | 81.31% | 81.25% | 84.00% | 0.9200 | 1.0078 |
| 13 | 58 | 0.4492 | 2.5649 | 0.4213 | 2.4058 | 0.2436 | 1.3912 | 82.36% | 80.98% | 83.59% | 0.9159 | 1.0857 |
| 13 | 58 | 0.4740 | 2.7064 | 0.4574 | 2.6121 | 0.2619 | 1.4953 | 81.97% | 79.97% | 84.15% | 0.9157 | 1.0339 |
| 13 | 58 | 0.5121 | 2.9240 | 0.4730 | 2.7007 | 0.2492 | 1.4227 | 81.14% | 80.30% | 83.24% | 0.9180 | 0.9447 |
| 13 | 58 | 0.4759 | 2.7174 | 0.4468 | 2.5513 | 0.2588 | 1.4777 | 81.54% | 80.32% | 83.63% | 0.9116 | 1.0100 |
| 13 | 58 | 0.4752 | 2.7137 | 0.4513 | 2.5769 | 0.2541 | 1.4507 | 82.61% | 81.13% | 84.20% | 0.9346 | 1.0335 |
| 13 | 58 | 0.5199 | 2.9684 | 0.4664 | 2.6633 | 0.2583 | 1.4749 | 83.38% | 82.31% | 82.53% | 0.9207 |  |
| 13 | 58 | 0.3794 | 2.1665 | 0.3580 | 2.0440 | 0.2126 | 1.2139 | 80.83% | 79.20% | 83.36% | 0.9145 | 0.9829 |
| 13 | 58 | 0.3948 | 2.2542 | 0.3519 | 2.0091 | 0.2304 | 1.3155 | 82.53% | 80.41% | 85.19% | 0.9384 | 1.1907 |
| 13 | 58 | 0.4475 | 2.5555 | 0.4189 | 2.3923 | 0.2638 | 1.5066 | 82.95% | 82.01% | 85.06% | 0.9251 | 1.0610 |
| 13 | 58 | 0.4538 | 2.5912 | 0.4445 | 2.5382 | 0.2621 | 1.4964 | 83.07% | 81.85% | 84.84% | 0.9339 | 0.9303 |
| 13 | 58 | 0.4284 | 2.4462 | 0.4135 | 2.3613 | 0.2548 | 1.4548 | 83.43% | 82.92% | 83.50% | 0.9288 |  |
| Average | 0.4884 | 2.7887 | 0.4678 | 2.6714 | 0.2446 | 1.3970 | 82.15% | 80.38% | 83.78% | 0.9197 | 0.9926 |
| Std. Dev. | 0.0753 | 0.1957 | 0.0343 | 0.1958 | 0.0134 | 0.0765 | 0.82% | 1.10% | 0.98% | 0.0082 | 0.0764 |

FWD data for I-490 East, Monroe, Rochester on October 12, 2006 with E2 dowel bar configuration under nominal load of 71 kN (16 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 16 | 71 | 0.6409 | 3.6594 | 0.6672 | 3.8098 | 0.2623 | 1.4975 | 81.99% | 78.99% | 86.25% | 0.9176 | 0.9954 |
| 16 | 71 | 0.6652 | 3.7985 | 0.6641 | 3.7921 | 0.2570 | 1.4672 | 82.64% | 80.13% | 83.22% | 0.9227 | 0.8596 |
| 16 | 71 | 0.6102 | 3.4843 | 0.5708 | 3.2596 | 0.2422 | 1.3832 | 81.87% | 79.89% | 82.43% | 0.9064 | 0.9478 |
| 16 | 71 | 0.5268 | 3.0082 | 0.5411 | 3.0895 | 0.2351 | 1.3425 | 81.07% | 78.05% | 81.91% | 0.8995 | 0.8741 |
| 16 | 71 | 0.5052 | 2.8848 | 0.4730 | 2.7007 | 0.2384 | 1.3614 | 82.31% | 79.62% | 82.04% | 0.9030 | 0.9549 |
| 16 | 71 | 0.4542 | 2.5938 | 0.4516 | 2.5790 | 0.2338 | 1.3352 | 82.65% | 79.66% | 84.81% | 0.9192 | 0.9983 |
| 16 | 71 | 0.4519 | 2.5804 | 0.4509 | 2.5745 | 0.2263 | 1.2925 | 81.79% | 78.86% | 82.24% | 0.9031 | 1.0284 |
| 16 | 71 | 0.4534 | 2.5889 | 0.4637 | 2.6477 | 0.2308 | 1.3176 | 82.26% | 78.59% | 85.82% | 0.9128 | 0.8811 |
| 16 | 71 | 0.4499 | 2.5687 | 0.4086 | 2.3330 | 0.2396 | 1.3682 | 81.83% | 80.70% | 83.96% | 0.9204 | 1.0930 |
| 16 | 71 | 0.4456 | 2.5446 | 0.4466 | 2.5500 | 0.2482 | 1.4175 | 81.95% | 79.36% | 83.41% | 0.9137 |  |
| 16 | 71 | 0.4596 | 2.6243 | 0.4458 | 2.5453 | 0.2387 | 1.3632 | 81.14% | 78.85% | 85.54% | 0.9185 | 1.0252 |
| 16 | 71 | 0.4780 | 2.7296 | 0.4570 | 2.6094 | 0.2461 | 1.4055 | 82.44% | 80.34% | 83.72% | 0.9209 | 0.9494 |
| 16 | 71 | 0.4498 | 2.5682 | 0.4339 | 2.4775 | 0.2331 | 1.3309 | 82.14% | 80.68% | 83.20% | 0.9213 | 0.9557 |
| 16 | 71 | 0.4494 | 2.5663 | 0.4147 | 2.3678 | 0.2317 | 1.3228 | 81.76% | 80.77% | 84.36% | 0.9237 | 1.0112 |
| 16 | 71 | 0.4433 | 2.5313 | 0.4193 | 2.3943 | 0.2412 | 1.3770 | 82.10% | 80.60% | 83.87% | 0.9218 | 1.0757 |
| 16 | 71 | 0.4672 | 2.6675 | 0.4511 | 2.5756 | 0.2634 | 1.5043 | 82.25% | 79.95% | 83.28% | 0.9182 | 1.0523 |
| 16 | 71 | 0.5039 | 2.8773 | 0.4747 | 2.7103 | 0.2514 | 1.4356 | 81.94% | 80.23% | 82.92% | 0.9214 | 0.9541 |
| 16 | 71 | 0.4757 | 2.7163 | 0.4529 | 2.5859 | 0.2611 | 1.4908 | 81.87% | 79.92% | 83.91% | 0.9190 | 0.9917 |
| 16 | 71 | 0.4682 | 2.6736 | 0.4491 | 2.5643 | 0.2585 | 1.4763 | 82.56% | 80.91% | 84.09% | 0.9304 | 1.0340 |
| 16 | 71 | 0.5132 | 2.9306 | 0.4644 | 2.6515 | 0.2616 | 1.4937 | 83.14% | 82.16% | 82.42% | 0.9248 |  |
| 16 | 71 | 0.3805 | 2.1725 | 0.3655 | 2.0872 | 0.2033 | 1.1608 | 80.79% | 78.83% | 82.00% | 0.8805 | 0.9840 |
| 16 | 71 | 0.3935 | 2.2467 | 0.3597 | 2.0537 | 0.2351 | 1.3423 | 81.21% | 79.60% | 85.72% | 0.9162 | 1.1718 |
| 16 | 71 | 0.4438 | 2.5344 | 0.4214 | 2.4064 | 0.2644 | 1.5095 | 82.41% | 80.43% | 85.32% | 0.9195 | 1.0503 |
| 16 | 71 | 0.4520 | 2.5808 | 0.4427 | 2.5276 | 0.2639 | 1.5067 | 82.20% | 80.56% | 85.04% | 0.9239 | 0.9223 |
| 16 | 71 | 0.4266 | 2.4360 | 0.4082 | 2.3312 | 0.2506 | 1.4312 | 82.22% | 80.70% | 83.64% | 0.9341 |  |
| Average | 0.4803 | 2.7427 | 0.4639 | 2.6490 | 0.2447 | 1.3973 | 82.02% | 79.94% | 83.81% | 0.9165 | 0.9914 |
| Std. Dev. | 0.0684 | 0.1837 | 0.0320 | 0.1829 | 0.0159 | 0.0909 | 0.55% | 0.88% | 1.11% | 0.0109 | 0.0740 |

Appendix E:  FWD Data from I490 September 24-25, 2008

FWD data for I-490 West, Monroe, Rochester on September 24, 2008 with nominal load 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.6274 | 3.5825 | 0.5676 | 3.2412 | 0.2066 | 1.1796 | 78.48% | 80.88% | 88.34% | 0.8913 | 1.2012 |
| 10 | 44 | 0.7413 | 4.2329 | 0.6818 | 3.8934 | 0.2003 | 1.1435 | 80.18% | 80.03% | 85.50% | 0.9282 | 0.9991 |
| 10 | 44 | 0.7416 | 4.2344 | 0.6812 | 3.8899 | 0.2088 | 1.1925 | 79.43% | 79.28% | 88.95% | 0.9110 | 0.9756 |
| 10 | 44 | 0.7418 | 4.2357 | 0.6646 | 3.7951 | 0.2069 | 1.1814 | 78.88% | 81.88% | 98.91% | 0.9206 | 1.0603 |
| 10 | 44 | 0.7832 | 4.4720 | 0.7047 | 4.0240 | 0.2020 | 1.1532 | 80.06% | 79.67% | 89.16% | 0.9565 | 1.0159 |
| 10 | 44 | 0.7926 | 4.5258 | 0.7159 | 4.0878 | 0.2201 | 1.2569 | 80.70% | 83.67% | 95.31% | 0.9703 | 1.1157 |
| 10 | 44 | 0.8271 | 4.7231 | 0.7987 | 4.5607 | 0.2144 | 1.2241 | 79.97% | 83.26% | 89.76% | 0.9235 | 0.9598 |
| 10 | 44 | 0.8247 | 4.7093 | 0.7666 | 4.3776 | 0.2239 | 1.2784 | 81.36% | 82.21% | 85.51% | 0.9272 | 1.0554 |
| 10 | 44 | 0.8460 | 4.8306 | 0.8091 | 4.6201 | 0.2301 | 1.3141 | 81.41% | 84.06% | 88.26% | 0.9333 | 0.9670 |
| 10 | 44 | 0.8456 | 4.8282 | 0.7824 | 4.4676 | 0.2188 | 1.2496 | 81.08% | 83.82% | 89.72% | 0.9461 | 0.8649 |
| 10 | 44 | 0.7162 | 4.0898 | 0.6767 | 3.8642 | 0.1843 | 1.0526 | 82.44% | 82.68% | 93.10% | 0.9240 | 0.8844 |
| 10 | 44 | 0.6351 | 3.6265 | 0.5985 | 3.4175 | 0.1633 | 0.9325 | 78.72% | 83.88% | 86.11% | 0.8627 | 0.9889 |
| 10 | 44 | 0.6450 | 3.6830 | 0.5918 | 3.3794 | 0.1727 | 0.9860 | 80.94% | 82.14% | 95.13% | 0.9816 | 0.9959 |
| 10 | 44 | 0.6060 | 3.4603 | 0.5894 | 3.3655 | 0.1911 | 1.0914 | 79.18% | 83.12% | 88.62% | 0.9261 | 0.7574 |
| 10 | 44 | 0.4745 | 2.7093 | 0.4464 | 2.5490 | 0.2016 | 1.1514 | 79.45% | 80.78% | 89.95% | 0.8763 | 1.1858 |
| 10 | 44 | 0.5772 | 3.2956 | 0.5293 | 3.0226 | 0.2329 | 1.3299 | 81.02% | 82.00% | 94.91% | 0.9769 | 1.1597 |
| 10 | 44 | 0.6415 | 3.6628 | 0.6139 | 3.5052 | 0.2249 | 1.2844 | 83.79% | 83.83% | 81.59% | 0.9143 | 0.7921 |
| 10 | 44 | 0.5308 | 3.0311 | 0.4863 | 2.7766 | 0.2522 | 1.4403 | 82.04% | 85.87% | 88.74% | 0.9359 | 1.2999 |
| 10 | 44 | 0.7253 | 4.1414 | 0.6321 | 3.6094 | 0.2694 | 1.5383 | 83.99% | 84.64% | 89.49% | 0.9398 | 1.1826 |
| 10 | 44 | 0.8161 | 4.6603 | 0.7476 | 4.2686 | 0.2347 | 1.3401 | 81.72% | 85.44% | 84.24% | 0.9815 | 0.8341 |
| 10 | 44 | 0.6824 | 3.8967 | 0.6235 | 3.5605 | 0.2340 | 1.3361 | 81.48% | 84.72% | 84.29% | 0.9206 | 0.9074 |
| 10 | 44 | 0.5948 | 3.3966 | 0.5658 | 3.2308 | 0.2513 | 1.4351 | 80.59% | 84.18% | 86.07% | 0.9152 | 1.0228 |
| 10 | 44 | 0.6036 | 3.4469 | 0.5787 | 3.3046 | 0.2617 | 1.4942 | 80.22% | 83.43% | 79.15% | 0.9072 | 0.9330 |
| 10 | 44 | 0.5946 | 3.3954 | 0.5399 | 3.0830 | 0.2499 | 1.4267 | 79.85% | 83.47% | 87.24% | 0.9640 | 1.0797 |
| 10 | 44 | 0.6428 | 3.6703 | 0.5829 | 3.3286 | 0.2708 | 1.5461 | 80.92% | 84.75% | 88.69% | 0.9456 | 1.0823 |
| 10 | 44 | 0.6720 | 3.8370 | 0.6309 | 3.6027 | 0.2714 | 1.5498 | 80.37% | 83.39% | 82.47% | 0.9508 | 0.9305 |
| 10 | 44 | 0.6705 | 3.8288 | 0.5870 | 3.3521 | 0.2714 | 1.5497 | 80.54% | 85.28% | 87.06% | 0.9407 | 1.0538 |
| 10 | 44 | 0.6483 | 3.7020 | 0.6186 | 3.5324 | 0.2535 | 1.4475 | 83.85% | 82.94% | 84.22% | 0.8863 | 0.8060 |
| 10 | 44 | 0.5302 | 3.0272 | 0.4986 | 2.8470 | 0.2484 | 1.4182 | 81.46% | 83.72% | 86.22% | 0.9693 | 0.9110 |
| 10 | 44 | 0.4943 | 2.8222 | 0.4542 | 2.5938 | 0.2330 | 1.3303 | 79.87% | 84.08% | 88.83% | 0.9486 | 0.9852 |
| 10 | 44 | 0.5005 | 2.8580 | 0.4475 | 2.5552 |  |  | 80.00% | 83.42% |  |  |  |
| Average | 0.6701 | 3.8263 | 0.6198 | 3.5389 | 0.2268 | 1.2951 | 80.77% | 83.11% | 88.18% | 0.9325 | 1.0002 |
| Std. Dev. | 0.1082 | 0.6178 | 0.1013 | 0.5785 | 0.0296 | 0.1693 | 1.41% | 1.66% | 4.27% | 0.0301 | 0.1299 |

FWD data for I-490 West, Monroe, Rochester on September 24, 2008 with nominal load 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.6192 | 3.5360 | 0.5776 | 3.2984 | 0.2045 | 1.1676 | 79.00% | 79.48% | 84.23% | 0.8971 | 1.1721 |
| 13 | 58 | 0.7373 | 4.2101 | 0.6771 | 3.8661 | 0.2062 | 1.1774 | 79.75% | 80.25% | 88.59% | 0.9720 | 0.9791 |
| 13 | 58 | 0.7227 | 4.1270 | 0.6629 | 3.7855 | 0.2070 | 1.1819 | 79.53% | 80.48% | 91.26% | 0.9370 | 0.9878 |
| 13 | 58 | 0.7332 | 4.1867 | 0.6548 | 3.7393 | 0.2123 | 1.2122 | 78.64% | 81.61% | 98.49% | 0.9222 | 1.0298 |
| 13 | 58 | 0.7723 | 4.4098 | 0.6744 | 3.8507 | 0.2054 | 1.1726 | 80.68% | 81.92% | 89.72% | 0.9280 | 1.0438 |
| 13 | 58 | 0.7808 | 4.4586 | 0.7039 | 4.0193 | 0.2241 | 1.2798 | 80.28% | 81.93% | 93.60% | 0.9044 | 1.1279 |
| 13 | 58 | 0.8092 | 4.6204 | 0.7939 | 4.5335 | 0.2198 | 1.2553 | 80.37% | 82.07% | 91.37% | 0.9478 | 0.9471 |
| 13 | 58 | 0.8170 | 4.6654 | 0.7520 | 4.2939 | 0.2281 | 1.3022 | 79.65% | 82.09% | 89.91% | 0.9321 | 1.0586 |
| 13 | 58 | 0.8364 | 4.7761 | 0.7960 | 4.5453 | 0.2339 | 1.3356 | 81.33% | 83.55% | 88.89% | 0.9271 | 0.9334 |
| 13 | 58 | 0.8258 | 4.7153 | 0.7430 | 4.2427 | 0.2109 | 1.2042 | 81.14% | 83.90% | 89.91% | 0.9455 | 0.8706 |
| 13 | 58 | 0.7137 | 4.0755 | 0.6469 | 3.6939 | 0.1839 | 1.0499 | 81.59% | 83.40% | 92.47% | 0.9286 | 0.9340 |
| 13 | 58 | 0.6250 | 3.5691 | 0.6042 | 3.4500 | 0.1744 | 0.9961 | 80.50% | 83.99% | 87.85% | 0.9170 | 0.9823 |
| 13 | 58 | 0.6278 | 3.5849 | 0.5935 | 3.3888 | 0.1804 | 1.0302 | 80.74% | 82.37% | 92.76% | 0.9619 | 0.9948 |
| 13 | 58 | 0.5988 | 3.4190 | 0.5904 | 3.3712 | 0.1883 | 1.0755 | 80.85% | 82.72% | 88.84% | 0.9215 | 0.7595 |
| 13 | 58 | 0.4743 | 2.7085 | 0.4484 | 2.5605 | 0.2084 | 1.1899 | 79.64% | 82.47% | 94.70% | 0.9481 | 1.1732 |
| 13 | 58 | 0.5684 | 3.2459 | 0.5261 | 3.0039 | 0.2369 | 1.3527 | 79.81% | 82.09% | 96.82% | 0.9542 | 1.1209 |
| 13 | 58 | 0.6283 | 3.5878 | 0.5897 | 3.3670 | 0.2239 | 1.2782 | 83.85% | 84.79% | 83.53% | 0.9483 | 0.8534 |
| 13 | 58 | 0.5281 | 3.0154 | 0.5032 | 2.8734 | 0.2546 | 1.4540 | 82.45% | 83.36% | 88.57% | 0.9360 | 1.2220 |
| 13 | 58 | 0.6994 | 3.9935 | 0.6149 | 3.5114 | 0.2717 | 1.5517 | 83.71% | 84.65% | 91.40% | 0.9427 | 1.2042 |
| 13 | 58 | 0.8022 | 4.5807 | 0.7405 | 4.2282 | 0.2406 | 1.3737 | 82.09% | 83.74% | 85.19% | 0.9387 | 0.8380 |
| 13 | 58 | 0.6530 | 3.7289 | 0.6205 | 3.5434 | 0.2403 | 1.3722 | 82.29% | 84.16% | 85.19% | 0.9161 | 0.8842 |
| 13 | 58 | 0.5845 | 3.3377 | 0.5487 | 3.1332 | 0.2507 | 1.4314 | 80.11% | 84.38% | 84.14% | 0.9088 | 1.0595 |
| 13 | 58 | 0.5952 | 3.3987 | 0.5813 | 3.3195 | 0.2719 | 1.5524 | 80.75% | 83.29% | 78.37% | 0.8961 | 0.9254 |
| 13 | 58 | 0.5910 | 3.3749 | 0.5379 | 3.0717 | 0.2638 | 1.5061 | 79.17% | 83.03% | 86.83% | 0.9329 | 1.0929 |
| 13 | 58 | 0.6324 | 3.6113 | 0.5879 | 3.3570 | 0.2739 | 1.5642 | 81.34% | 84.43% | 83.86% | 0.9360 | 1.0852 |
| 13 | 58 | 0.6446 | 3.6810 | 0.6380 | 3.6429 | 0.2703 | 1.5435 | 81.78% | 83.67% | 83.97% | 0.9362 | 0.9168 |
| 13 | 58 | 0.6487 | 3.7040 | 0.5849 | 3.3399 | 0.2769 | 1.5809 | 81.65% | 82.05% | 87.91% | 0.9583 | 1.0344 |
| 13 | 58 | 0.6284 | 3.5880 | 0.6050 | 3.4547 | 0.2455 | 1.4021 | 81.58% | 83.79% | 84.72% | 0.8601 | 0.7961 |
| 13 | 58 | 0.5236 | 2.9897 | 0.4817 | 2.7504 | 0.2340 | 1.3359 | 81.36% | 83.25% | 84.29% | 0.9053 | 0.9612 |
| 13 | 58 | 0.4870 | 2.7808 | 0.4630 | 2.6437 | 0.2318 | 1.3237 | 80.17% | 83.09% | 88.59% | 0.9468 | 0.9850 |
| 13 | 58 | 0.5000 | 2.8548 | 0.4560 | 2.6039 |  |  | 82.05% | 83.80% |  |  |  |
| Average | 0.6583 | 3.7592 | 0.6128 | 3.4995 | 0.2291 | 1.3084 | 80.90% | 82.90% | 88.53% | 0.9302 | 0.9991 |
| Std. Dev. | 0.1053 | 0.6011 | 0.0943 | 0.5387 | 0.0294 | 0.1677 | 1.26% | 1.30% | 4.40% | 0.0231 | 0.1192 |

FWD data for I-490 West, Monroe, Rochester on September 24, 2008 with nominal load 71 kN (16 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 16 | 71 | 0.5953 | 3.3993 | 0.5606 | 3.2011 | 0.2053 | 1.1721 | 79.16% | 81.29% | 85.92% | 0.9080 | 1.1511 |
| 16 | 71 | 0.6975 | 3.9828 | 0.6453 | 3.6848 | 0.2047 | 1.1688 | 79.62% | 80.49% | 87.36% | 0.9069 | 0.9801 |
| 16 | 71 | 0.6871 | 3.9233 | 0.6325 | 3.6115 | 0.2046 | 1.1683 | 79.47% |  |  | 0.9313 | 0.9835 |
| 16 | 71 | 0.6924 | 3.9536 | 0.6220 | 3.5519 | 0.2060 | 1.1764 | 78.73% | 81.18% | 98.40% | 0.9760 | 1.0392 |
| 16 | 71 | 0.7384 | 4.2164 | 0.6464 | 3.6910 | 0.2027 | 1.1573 | 80.80% |  | 90.87% | 0.9367 | 1.0401 |
| 16 | 71 | 0.7412 | 4.2324 | 0.6723 | 3.8391 | 0.2189 | 1.2499 | 80.22% | 82.43% | 92.87% | 0.9440 | 1.1123 |
| 16 | 71 | 0.7766 | 4.4345 | 0.7478 | 4.2701 | 0.2128 | 1.2151 | 80.05% | 82.52% | 89.97% | 0.9456 | 0.9626 |
| 16 | 71 | 0.7690 | 4.3913 | 0.7199 | 4.1106 | 0.2239 | 1.2785 | 79.79% | 81.99% | 88.79% | 0.9342 | 1.0600 |
| 16 | 71 | 0.7913 | 4.5184 | 0.7631 | 4.3572 | 0.2271 | 1.2965 | 80.69% | 83.17% | 88.15% | 0.9519 | 0.9391 |
| 16 | 71 | 0.7789 | 4.4478 | 0.7166 | 4.0920 | 0.2158 | 1.2324 | 81.07% | 83.83% | 88.75% | 0.9266 | 0.8616 |
| 16 | 71 | 0.6811 | 3.8890 | 0.6175 | 3.5257 | 0.1840 | 1.0505 | 80.60% |  | 91.75% | 0.9399 | 0.9403 |
| 16 | 71 | 0.6062 | 3.4615 | 0.5806 | 3.3152 | 0.1704 | 0.9728 | 81.35% | 82.77% | 88.43% | 0.9122 | 0.9670 |
| 16 | 71 | 0.6035 | 3.4460 | 0.5614 | 3.2057 | 0.1747 | 0.9978 | 80.06% | 82.59% | 91.36% | 0.9272 | 0.9852 |
| 16 | 71 | 0.5672 | 3.2387 | 0.5531 | 3.1581 | 0.1864 | 1.0645 | 83.61% | 83.12% | 89.34% | 0.9404 | 0.7846 |
| 16 | 71 | 0.4604 | 2.6292 | 0.4339 | 2.4779 | 0.2035 | 1.1620 | 79.36% | 83.00% | 89.81% | 0.9402 | 1.1641 |
| 16 | 71 | 0.5470 | 3.1235 | 0.5051 | 2.8845 | 0.2322 | 1.3262 | 80.60% | 82.42% | 96.50% | 0.9726 | 1.1294 |
| 16 | 71 | 0.6019 | 3.4371 | 0.5705 | 3.2576 | 0.2245 | 1.2822 | 83.56% | 85.36% | 83.09% | 0.9301 | 0.8437 |
| 16 | 71 | 0.5092 | 2.9078 | 0.4813 | 2.7483 | 0.2497 | 1.4256 | 81.91% | 83.82% | 88.83% | 0.9581 | 1.2038 |
| 16 | 71 | 0.6568 | 3.7503 | 0.5794 | 3.3082 | 0.2617 | 1.4942 | 82.46% | 84.62% | 90.84% | 0.9603 | 1.2018 |
| 16 | 71 | 0.7419 | 4.2361 | 0.6963 | 3.9757 | 0.2373 | 1.3553 | 82.33% |  | 85.27% | 0.9462 | 0.8471 |
| 16 | 71 | 0.6295 | 3.5947 | 0.5898 | 3.3678 | 0.2338 | 1.3350 | 81.32% | 84.98% | 85.13% | 0.9231 | 0.8881 |
| 16 | 71 | 0.5597 | 3.1962 | 0.5238 | 2.9909 | 0.2480 | 1.4160 | 81.09% | 83.63% | 84.37% | 0.9234 | 1.0776 |
| 16 | 71 | 0.5662 | 3.2332 | 0.5644 | 3.2229 | 0.2609 | 1.4897 | 80.73% | 83.87% | 70.53% | 0.9301 | 0.9344 |
| 16 | 71 | 0.5742 | 3.2787 | 0.5274 | 3.0116 | 0.2557 | 1.4599 | 81.36% | 83.49% | 86.56% | 0.9478 | 1.0640 |
| 16 | 71 | 0.6036 | 3.4465 | 0.5612 | 3.2043 | 0.2666 | 1.5220 | 80.97% | 84.55% | 87.20% | 0.9346 | 1.0691 |
| 16 | 71 | 0.6139 | 3.5054 | 0.5999 | 3.4256 | 0.2611 | 1.4910 | 81.13% | 82.56% | 84.91% | 0.9311 | 0.9460 |
| 16 | 71 | 0.6216 | 3.5497 | 0.5675 | 3.2404 | 0.2700 | 1.5417 | 81.61% | 0.00% | 86.94% | 0.9289 | 1.0368 |
| 16 | 71 | 0.6039 | 3.4481 | 0.5883 | 3.3595 | 0.2377 | 1.3570 | 82.74% | 83.49% | 83.26% | 0.8349 | 0.7942 |
| 16 | 71 | 0.5008 | 2.8597 | 0.4673 | 2.6683 | 0.2325 | 1.3274 | 80.90% | 83.94% | 85.22% | 0.9316 | 0.9679 |
| 16 | 71 | 0.4720 | 2.6949 | 0.4523 | 2.5827 | 0.2206 | 1.2596 | 80.37% | 83.73% | 87.70% | 0.9389 | 0.9750 |
| 16 | 71 | 0.4810 | 2.7466 | 0.4410 | 2.5182 |  |  | 81.96% | 82.68% |  |  |  |
| Average | 0.6280 | 3.5862 | 0.5867 | 3.3503 | 0.2244 | 1.2815 | 80.96% | 83.14% | 87.87% | 0.9338 | 0.9983 |
| Std. Dev. | 0.0959 | 0.5474 | 0.0874 | 0.4988 | 0.0274 | 0.1565 | 1.20% | 1.16% | 4.86% | 0.0247 | 0.1133 |

FWD data for I-490 East, Monroe, Rochester on Sep. 25, 2008 with standard dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.7726 | 4.4119 | 0.6943 | 3.9643 | 0.2300 | 1.3133 | 79.16% | 81.70% | 88.47% | 0.9350 | 0.9942 |
| 10 | 44 | 0.6818 | 3.8934 | 0.6902 | 3.9412 | 0.2514 | 1.4356 | 79.62% | 83.28% | 87.94% | 0.9221 | 1.1580 |
| 10 | 44 | 0.8470 | 4.8367 | 0.7992 | 4.5638 | 0.2894 | 1.6524 | 79.47% | 83.64% | 99.72% | 0.9545 | 0.8895 |
| 10 | 44 | 0.7218 | 4.1216 | 0.7109 | 4.0596 | 0.2314 | 1.3212 | 78.73% | 84.35% | 100.12% | 1.0048 | 0.7861 |
| 10 | 44 | 0.8230 | 4.6992 | 0.5588 | 3.1911 | 0.2275 | 1.2990 | 80.80% | 83.18% | 93.00% | 0.9589 | 1.2053 |
| 10 | 44 | 0.6957 | 3.9723 | 0.6736 | 3.8463 | 0.2509 | 1.4327 | 80.22% | 83.12% | 96.33% | 0.9507 | 0.9422 |
| 10 | 44 | 0.6909 | 3.9453 | 0.6347 | 3.6240 | 0.2579 | 1.4727 | 80.05% | 84.37% | 88.94% | 0.9367 | 0.4290 |
| 10 | 44 | 0.5244 | 2.9941 | 0.2723 | 1.5546 | 0.1923 | 1.0982 | 79.79% | 84.30% | 91.42% | 0.9686 | 1.3275 |
| 10 | 44 | 0.3868 | 2.2087 | 0.3614 | 2.0638 | 0.1425 | 0.8139 | 80.69% | 81.19% | 91.83% | 0.9259 | 1.0733 |
| 10 | 44 | 0.4514 | 2.5774 | 0.3879 | 2.2151 | 0.1672 | 0.9548 | 81.07% | 82.92% | 91.48% | 0.9608 | 1.1365 |
| 10 | 44 | 0.1798 | 1.0268 | 0.4409 | 2.5174 | 0.1119 | 0.6389 | 80.60% | 82.52% | 68.70% | 0.9286 | 1.1415 |
| 10 | 44 | 0.2270 | 1.2963 | 0.1978 | 1.1293 | 0.1205 | 0.6883 | 81.35% | 86.18% | 72.02% | 0.9497 | 0.6815 |
| 10 | 44 | 0.1369 | 0.7815 | 0.1348 | 0.7696 | 0.0933 | 0.5327 | 80.06% | 83.21% | 66.18% | 0.8660 | 1.0409 |
| 10 | 44 | 0.2033 | 1.1607 | 0.1403 | 0.8011 | 0.0998 | 0.5701 | 83.61% | 79.34% | 51.50% | 0.9006 | 2.0748 |
| 10 | 44 | 0.2007 | 1.1458 | 0.2911 | 1.6621 | 0.0879 | 0.5021 | 79.36% | 77.93% | 60.61% | 0.8953 | 0.4699 |
| 10 | 44 | 0.1933 | 1.1036 | 0.1368 | 0.7811 | 0.2028 | 1.1579 | 80.60% | 83.07% | 62.24% | 0.7871 | 2.2571 |
| 10 | 44 | 0.3451 | 1.9708 | 0.3087 | 1.7629 | 0.2158 | 1.2320 | 83.56% | 77.99% | 71.14% | 0.9375 | 1.0312 |
| 10 | 44 | 0.3385 | 1.9330 | 0.3184 | 1.8179 | 0.2305 | 1.3159 | 81.91% | 84.75% | 70.15% | 0.9272 | 0.9371 |
| 10 | 44 | 0.3366 | 1.9218 | 0.2983 | 1.7035 | 0.2068 | 1.1808 | 82.46% | 85.87% | 68.36% | 0.8495 | 0.9787 |
| 10 | 44 | 0.3363 | 1.9201 | 0.2920 | 1.6671 | 0.2460 | 1.4048 | 82.33% | 88.97% | 89.17% | 0.9050 | 1.2170 |
| 10 | 44 | 0.2522 | 1.4400 | 0.2344 | 1.3385 | 0.2042 | 1.1658 | 81.32% | 86.31% | 82.67% | 0.9476 | 1.0649 |
| 10 | 44 | 0.2573 | 1.4695 | 0.2496 | 1.4254 | 0.2133 | 1.2181 | 81.09% | 88.19% | 79.39% | 0.9189 | 0.9059 |
| 10 | 44 | 0.2437 | 1.3913 | 0.2261 | 1.2912 | 0.2161 | 1.2342 | 80.73% | 86.32% | 84.94% | 0.9450 | 0.9778 |
| 10 | 44 | 0.2189 | 1.2500 | 0.2211 | 1.2625 | 0.2051 | 1.1712 | 81.36% | 86.25% | 78.35% | 0.8837 | 0.9882 |
| 10 | 44 | 0.2303 | 1.3152 | 0.2185 | 1.2476 | 0.2062 | 1.1772 | 80.97% | 85.84% | 78.39% | 0.9213 |  |
| Average | 0.4118 | 2.3515 | 0.3797 | 2.1680 | 0.1960 | 1.1193 | 80.84% | 83.79% | 80.52% | 0.9232 | 1.0712 |
| Std. Dev. | 0.2327 | 1.3286 | 0.2075 | 1.1849 | 0.0560 | 0.3196 | 1.25% | 2.77% | 13.16% | 0.0437 | 0.3995 |

FWD data for I-490 East, Monroe, Rochester on Sep. 25, 2008 with standard dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.7694 | 4.3936 | 0.7012 | 4.0038 | 0.2356 | 1.3454 | 79.31% | 81.48% | 88.25% | 0.9324 | 1.0084 |
| 13 | 58 | 0.6614 | 3.7765 | 0.7071 | 4.0376 | 0.2552 | 1.4573 | 79.49% | 82.73% | 89.62% | 0.9484 | 1.0988 |
| 13 | 58 | 0.8215 | 4.6910 | 0.7769 | 4.4363 | 0.2891 | 1.6508 | 80.41% | 82.88% | 94.84% | 0.9570 | 0.9064 |
| 13 | 58 | 0.7075 | 4.0400 | 0.7042 | 4.0212 | 0.2450 | 1.3993 | 80.49% | 84.36% | 95.32% | 0.9562 | 0.8189 |
| 13 | 58 | 0.8428 | 4.8125 | 0.5767 | 3.2931 | 0.2561 | 1.4625 | 81.09% | 84.24% | 96.77% | 0.9530 | 1.0800 |
| 13 | 58 | 0.6821 | 3.8949 | 0.6228 | 3.5565 | 0.2534 | 1.4468 | 81.44% | 84.17% | 91.50% | 0.9605 | 1.0263 |
| 13 | 58 | 0.6906 | 3.9432 | 0.6392 | 3.6501 | 0.2672 | 1.5259 | 80.25% | 83.68% | 88.85% | 0.9448 | 0.6127 |
| 13 | 58 | 0.4954 | 2.8288 | 0.3917 | 2.2366 | 0.2012 | 1.1491 | 80.06% | 83.29% | 88.59% | 0.9203 | 0.8722 |
| 13 | 58 | 0.3731 | 2.1305 | 0.3416 | 1.9508 | 0.1612 | 0.9207 | 81.14% | 82.66% | 91.35% | 0.9634 | 1.1635 |
| 13 | 58 | 0.4539 | 2.5919 | 0.3975 | 2.2697 | 0.1646 | 0.9397 | 81.16% | 83.91% | 92.35% | 0.9557 | 1.0808 |
| 13 | 58 | 0.1731 | 0.9885 | 0.4296 | 2.4531 | 0.1452 | 0.8291 | 83.20% | 82.84% | 63.78% | 0.8924 | 1.1303 |
| 13 | 58 | 0.2249 | 1.2845 | 0.1914 | 1.0930 | 0.1170 | 0.6680 | 80.16% | 84.48% | 62.03% | 0.9170 | 0.7886 |
| 13 | 58 | 0.1609 | 0.9188 | 0.1509 | 0.8619 | 0.0914 | 0.5220 | 75.70% | 85.44% | 92.55% | 0.9777 | 0.8770 |
| 13 | 58 | 0.1710 | 0.9762 | 0.1324 | 0.7559 | 0.1002 | 0.5724 | 79.65% | 85.85% | 58.70% | 0.8991 | 2.1701 |
| 13 | 58 | 0.1994 | 1.1386 | 0.2873 | 1.6404 | 0.0983 | 0.5610 | 78.25% | 82.98% | 53.29% | 0.9125 | 0.5125 |
| 13 | 58 | 0.2065 | 1.1790 | 0.1472 | 0.8407 | 0.2157 | 1.2319 | 81.17% | 82.30% | 72.62% | 0.9738 | 2.1243 |
| 13 | 58 | 0.3487 | 1.9909 | 0.3127 | 1.7858 | 0.2182 | 1.2458 | 79.36% | 85.71% | 70.90% | 0.9349 | 1.0189 |
| 13 | 58 | 0.3433 | 1.9604 | 0.3187 | 1.8196 | 0.2305 | 1.3161 | 79.51% | 83.42% | 63.59% | 0.9239 | 0.9981 |
| 13 | 58 | 0.3417 | 1.9513 | 0.3181 | 1.8161 | 0.2161 | 1.2338 | 80.34% | 82.77% | 67.32% | 0.8996 | 0.9151 |
| 13 | 58 | 0.3286 | 1.8766 | 0.2911 | 1.6620 | 0.2397 | 1.3688 | 77.66% | 66.29% | 80.72% | 0.9271 | 1.2319 |
| 13 | 58 | 0.2547 | 1.4545 | 0.2459 | 1.4039 | 0.2067 | 1.1803 | 82.88% | 85.43% | 83.31% | 0.9507 | 1.0252 |
| 13 | 58 | 0.2584 | 1.4757 | 0.2521 | 1.4393 | 0.2127 | 1.2145 | 85.07% | 85.83% | 78.72% | 0.9327 | 0.9276 |
| 13 | 58 | 0.2395 | 1.3678 | 0.2338 | 1.3351 | 0.2193 | 1.2522 | 84.80% | 86.53% | 77.47% | 0.9553 | 0.9382 |
| 13 | 58 | 0.2385 | 1.3620 | 0.2194 | 1.2526 | 0.2054 | 1.1727 | 85.59% | 86.94% | 80.51% | 0.9601 | 0.9953 |
| 13 | 58 | 0.2301 | 1.3137 | 0.2183 | 1.2467 | 0.2016 | 1.1509 | 85.21% | 85.85% | 82.12% | 0.9307 |  |
| Average | 0.4087 | 2.3337 | 0.3843 | 2.1945 | 0.2019 | 1.1527 | 80.94% | 83.44% | 80.20% | 0.9392 | 1.0550 |
| Std. Dev. | 0.2285 | 1.3050 | 0.2022 | 1.1547 | 0.0553 | 0.3158 | 2.42% | 3.86% | 12.85% | 0.0235 | 0.3732 |

FWD data for I-490 East, Monroe, Rochester on Sep. 25, 2008 with standard dowel bar configuration under nominal load of 71 kN (16 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 16 | 71 | 0.7162 | 4.0894 | 0.6707 | 3.8297 | 0.2281 | 1.3025 | 79.91% | 82.59% | 89.56% | 0.9397 | 0.9170 |
| 16 | 71 | 0.6165 | 3.5203 | 0.6150 | 3.5118 | 0.2478 | 1.4149 | 79.59% | 82.99% |  | 0.9624 | 1.2009 |
| 16 | 71 | 0.7605 | 4.3423 | 0.7386 | 4.2174 | 0.2690 | 1.5363 | 84.92% | 82.55% | 95.07% | 0.9752 | 0.8753 |
| 16 | 71 | 0.6336 | 3.6180 | 0.6464 | 3.6913 | 0.1657 | 0.9464 | 80.23% | 83.35% | 93.08% | 0.9706 | 1.0234 |
| 16 | 71 | 0.7951 | 4.5400 | 0.6615 | 3.7775 | 0.2388 | 1.3634 | 80.94% | 84.03% | 96.90% | 0.9848 | 0.9310 |
| 16 | 71 | 0.6724 | 3.8393 | 0.6159 | 3.5169 | 0.2517 | 1.4371 | 80.35% | 84.19% | 93.35% | 0.9348 | 0.8975 |
| 16 | 71 | 0.6431 | 3.6722 | 0.5528 | 3.1563 | 0.2585 | 1.4759 | 81.31% | 84.28% | 89.10% | 0.9491 | 0.7024 |
| 16 | 71 | 0.5255 | 3.0008 | 0.3882 | 2.2169 | 0.2014 | 1.1500 | 80.90% | 83.60% | 89.12% | 0.9330 | 0.8739 |
| 16 | 71 | 0.3674 | 2.0978 | 0.3393 | 1.9374 | 0.1568 | 0.8954 | 80.40% | 82.97% | 90.68% | 0.9373 | 1.0817 |
| 16 | 71 | 0.4343 | 2.4801 | 0.3670 | 2.0957 | 0.1652 | 0.9435 | 80.50% | 83.11% | 92.08% | 0.9526 | 1.1446 |
| 16 | 71 | 0.2152 | 1.2288 | 0.4201 | 2.3987 | 0.1506 | 0.8602 | 81.10% | 82.22% | 83.96% | 0.8932 | 1.1239 |
| 16 | 71 | 0.2207 | 1.2603 | 0.1950 | 1.1137 | 0.1308 | 0.7469 | 81.34% | 82.11% | 78.96% | 0.9130 | 0.9906 |
| 16 | 71 | 0.2124 | 1.2131 | 0.1932 | 1.1032 | 0.1414 | 0.8077 | 81.38% | 82.91% | 62.14% | 0.8617 | 1.0697 |
| 16 | 71 | 0.2173 | 1.2408 | 0.2067 | 1.1801 | 0.1257 | 0.7176 | 80.11% | 80.08% | 64.28% | 0.8835 | 1.3092 |
| 16 | 71 | 0.2292 | 1.3087 | 0.2706 | 1.5449 | 0.1268 | 0.7241 | 78.43% | 82.31% | 53.13% | 0.9263 | 0.6980 |
| 16 | 71 | 0.2158 | 1.2322 | 0.1889 | 1.0784 | 0.2066 | 1.1799 | 80.47% | 83.44% | 74.24% | 0.8581 | 1.6300 |
| 16 | 71 | 0.3406 | 1.9451 | 0.3078 | 1.7578 | 0.2138 | 1.2206 | 80.33% | 80.92% | 81.41% | 0.9238 | 1.0203 |
| 16 | 71 | 0.3347 | 1.9114 | 0.3141 | 1.7936 | 0.2201 | 1.2566 | 78.99% | 83.27% | 68.77% | 0.9211 | 0.9781 |
| 16 | 71 | 0.3278 | 1.8716 | 0.3072 | 1.7543 | 0.2139 | 1.2213 | 79.39% | 83.27% | 74.30% | 0.9184 | 0.9291 |
| 16 | 71 | 0.3180 | 1.8158 | 0.2854 | 1.6299 | 0.2274 | 1.2982 | 79.25% | 84.06% | 79.37% | 0.9208 | 1.2067 |
| 16 | 71 | 0.2497 | 1.4256 | 0.2371 | 1.3538 | 0.2025 | 1.1566 | 84.30% | 84.88% | 80.94% | 0.9404 | 1.0189 |
| 16 | 71 | 0.2465 | 1.4077 | 0.2416 | 1.3795 | 0.2053 | 1.1723 | 85.39% | 86.97% | 82.56% | 0.9212 | 0.9501 |
| 16 | 71 | 0.2395 | 1.3674 | 0.2295 | 1.3107 | 0.0000 | 0.0000 | 85.71% | 87.30% |  |  | 0.9403 |
| 16 | 71 | 0.2384 | 1.3611 | 0.2158 | 1.2324 | 0.2096 | 1.1966 | 86.62% | 88.49% | 80.22% | 0.9012 | 0.9924 |
| 16 | 71 | 0.2163 | 1.2348 | 0.2142 | 1.2231 | 0.1990 | 1.1366 | 84.62% | 85.14% | 80.20% | 0.9275 |  |
| Average | 0.3995 | 2.2810 | 0.3769 | 2.1522 | 0.1903 | 1.0864 | 81.46% | 83.64% | 81.45% | 0.9271 | 1.0210 |
| Std. Dev. | 0.2029 | 1.1587 | 0.1821 | 1.0395 | 0.0579 | 0.3308 | 2.33% | 1.86% | 11.36% | 0.0320 | 0.1933 |

FWD data for I-490 East, Monroe, Rochester on Sep. 25, 2008 with E1 dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.5459 | 3.1170 | 0.5033 | 2.8737 | 0.2186 | 1.2482 | 77.75% | 83.26% | 85.51% | 0.9158 | 1.1176 |
| 10 | 44 | 0.5330 | 3.0438 | 0.5624 | 3.2115 | 0.2223 | 1.2692 | 79.44% | 83.50% | 91.37% | 0.9592 | 0.9030 |
| 10 | 44 | 0.5867 | 3.3501 | 0.5079 | 2.9002 | 0.2145 | 1.2246 | 80.93% | 83.00% | 91.57% | 0.9583 | 1.0321 |
| 10 | 44 | 0.5107 | 2.9163 | 0.5242 | 2.9933 | 0.2081 | 1.1883 | 80.60% | 83.23% | 91.76% | 0.9794 | 0.9693 |
| 10 | 44 | 0.6742 | 3.8496 | 0.5081 | 2.9013 | 0.2488 | 1.4205 | 81.59% | 84.30% | 88.95% | 0.9437 | 0.9862 |
| 10 | 44 | 0.5412 | 3.0903 | 0.5011 | 2.8611 | 0.2334 | 1.3327 | 77.98% | 83.48% | 86.89% | 0.9577 | 0.9674 |
| 10 | 44 | 0.5557 | 3.1730 | 0.4847 | 2.7678 | 0.2404 | 1.3725 | 80.69% | 81.10% | 89.33% | 0.9775 | 0.8852 |
| 10 | 44 | 0.5071 | 2.8954 | 0.4291 | 2.4499 | 0.2258 | 1.2896 | 78.66% | 83.33% | 86.58% | 0.9623 | 0.9373 |
| 10 | 44 | 0.4343 | 2.4800 | 0.4021 | 2.2962 | 0.2131 | 1.2170 | 81.62% | 81.56% | 85.77% | 0.9303 | 1.0103 |
| 10 | 44 | 0.4417 | 2.5225 | 0.4063 | 2.3200 | 0.1849 | 1.0560 | 80.60% | 81.36% | 87.26% | 0.9429 | 0.5664 |
| 10 | 44 | 0.4133 | 2.3598 | 0.3553 | 2.0289 | 0.2740 | 1.5647 | 79.73% | 80.19% | 62.35% | 0.9231 | 0.9588 |
| 10 | 44 | 0.3513 | 2.0062 | 0.3407 | 1.9452 | 0.2801 | 1.5995 | 82.28% | 85.34% | 81.27% | 0.9170 | 1.1771 |
| 10 | 44 | 0.3914 | 2.2348 | 0.4010 | 2.2898 | 0.1411 | 0.8057 | 81.92% | 83.00% | 79.87% | 0.9195 | 0.5841 |
| 10 | 44 | 0.2601 | 1.4850 | 0.2342 | 1.3376 | 0.1781 | 1.0168 | 82.13% | 84.19% | 63.82% | 0.9444 | 1.1000 |
| 10 | 44 | 0.2730 | 1.5588 | 0.2577 | 1.4713 | 0.2120 | 1.2108 | 82.29% | 83.40% | 63.86% | 0.9296 | 0.9776 |
| 10 | 44 | 0.2768 | 1.5808 | 0.2519 | 1.4382 | 0.1721 | 0.9827 | 77.78% | 83.73% | 55.34% | 0.0000 | 0.7144 |
| 10 | 44 | 0.1859 | 1.0616 | 0.1799 | 1.0275 | 0.1269 | 0.7247 |  | 79.49% | 82.88% | 0.9041 | 0.9213 |
| 10 | 44 | 0.2415 | 1.3789 | 0.1658 | 0.9466 | 0.1359 | 0.7760 | 82.33% | 84.58% | 58.67% | 0.9159 | 0.8548 |
| 10 | 44 | 0.1534 | 0.8761 | 0.1417 | 0.8092 | 0.1257 | 0.7177 | 82.16% | 77.35% | 68.30% | 0.9163 | 1.0350 |
| 10 | 44 | 0.1470 | 0.8392 | 0.1467 | 0.8376 | 0.1260 | 0.7194 | 84.68% | 87.77% | 75.25% | 0.8718 | 0.9743 |
| 10 | 44 | 0.2312 | 1.3202 | 0.2226 | 1.2709 | 0.2010 | 1.1480 | 80.59% | 83.04% | 72.51% | 0.8792 | 0.8985 |
| 10 | 44 | 0.2117 | 1.2089 | 0.2000 | 1.1419 | 0.2085 | 1.1903 | 79.63% | 84.88% | 77.48% | 0.8952 | 1.0479 |
| 10 | 44 | 0.2254 | 1.2870 | 0.2096 | 1.1966 | 0.2448 | 1.3980 | 82.30% | 83.94% | 75.52% | 0.9224 | 1.0464 |
| 10 | 44 | 0.2258 | 1.2893 | 0.2193 | 1.2521 | 0.2175 | 1.2421 | 81.42% | 84.40% | 76.87% | 0.8904 | 0.9329 |
| 10 | 44 | 0.1962 | 1.1203 | 0.2045 | 1.1680 | 0.2188 | 1.2496 | 81.22% | 80.98% | 75.89% | 0.8773 | 1.0389 |
| 10 | 44 | 0.2242 | 1.2804 | 0.2125 | 1.2135 | 0.1832 | 1.0461 | 77.88% | 83.26% | 77.65% | 0.9135 | 0.9446 |
| 10 | 44 | 0.2170 | 1.2391 | 0.2007 | 1.1462 | 0.1719 | 0.9816 | 75.81% | 81.68% | 79.95% | 0.8973 |  |
| Average | 0.3539 | 2.0209 | 0.3249 | 1.8554 | 0.2010 | 1.1479 | 80.54% | 82.94% | 78.24% | 0.8905 | 0.9454 |
| Std. Dev. | 0.1572 | 0.8976 | 0.1393 | 0.7956 | 0.0431 | 0.2462 | 1.98% | 2.04% | 10.51% | 0.1804 | 0.1422 |

FWD data for I-490 East, Monroe, Rochester on Sep. 25, 2008 with E1 dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.5485 | 3.1318 | 0.4856 | 2.7726 | 0.2192 | 1.2514 | 82.56% | 83.33% | 87.40% | 0.9534 | 1.1159 |
| 13 | 58 | 0.5225 | 2.9837 | 0.5418 | 3.0940 | 0.2194 | 1.2529 | 80.48% | 82.97% | 89.38% | 0.9846 | 0.8810 |
| 13 | 58 | 0.5716 | 3.2640 | 0.4774 | 2.7258 | 0.2212 | 1.2633 | 79.97% | 83.65% | 91.49% | 0.9394 | 1.1054 |
| 13 | 58 | 0.5024 | 2.8689 | 0.5277 | 3.0130 | 0.2135 | 1.2190 | 81.48% | 84.35% | 93.12% | 0.9699 | 0.9425 |
| 13 | 58 | 0.6669 | 3.8079 | 0.4973 | 2.8399 | 0.2509 | 1.4327 | 80.89% | 84.21% | 88.05% | 0.9443 | 0.9766 |
| 13 | 58 | 0.5390 | 3.0777 | 0.4857 | 2.7734 | 0.2398 | 1.3693 | 80.31% | 83.03% | 85.51% | 0.9689 | 0.9898 |
| 13 | 58 | 0.5388 | 3.0768 | 0.4808 | 2.7452 | 0.2447 | 1.3971 | 80.22% | 82.00% | 88.40% | 0.9595 | 0.8461 |
| 13 | 58 | 0.4972 | 2.8388 | 0.4068 | 2.3226 | 0.2260 | 1.2908 | 80.32% | 83.24% | 88.67% | 0.9639 | 1.0608 |
| 13 | 58 | 0.4154 | 2.3722 | 0.4315 | 2.4639 | 0.2163 | 1.2353 | 81.49% | 81.47% | 87.14% | 0.9356 | 0.8730 |
| 13 | 58 | 0.4374 | 2.4975 | 0.3767 | 2.1511 | 0.2020 | 1.1537 | 80.40% | 82.15% | 87.94% | 0.9112 | 0.7846 |
| 13 | 58 | 0.4093 | 2.3372 | 0.3586 | 2.0474 | 0.2718 | 1.5519 | 78.54% | 78.69% | 63.52% | 0.9174 | 0.9732 |
| 13 | 58 | 0.3477 | 1.9851 | 0.3490 | 1.9926 | 0.2840 | 1.6220 | 81.25% | 82.25% | 80.81% | 0.9238 | 1.0979 |
| 13 | 58 | 0.3942 | 2.2510 | 0.3831 | 2.1877 | 0.1444 | 0.8247 | 81.95% | 83.15% | 79.04% | 0.9184 | 0.5343 |
| 13 | 58 | 0.2315 | 1.3217 | 0.2047 | 1.1689 | 0.2234 | 1.2758 | 81.45% | 83.05% | 76.83% | 0.9076 | 1.2591 |
| 13 | 58 | 0.2778 | 1.5865 | 0.2577 | 1.4718 | 0.2134 | 1.2187 | 80.52% | 85.43% | 61.71% | 0.9264 | 1.0220 |
| 13 | 58 | 0.2523 | 1.4404 | 0.2634 | 1.5042 | 0.0000 | 0.0000 | 81.75% | 81.55% |  |  | 0.7913 |
| 13 | 58 | 0.1803 | 1.0297 | 0.2084 | 1.1902 | 0.1279 | 0.7302 | 80.42% | 84.63% | 74.55% | 0.8852 | 0.8080 |
| 13 | 58 | 0.2389 | 1.3642 | 0.1684 | 0.9617 | 0.1294 | 0.7391 | 80.65% | 85.16% | 69.03% | 0.9262 | 0.8730 |
| 13 | 58 | 0.1533 | 0.8756 | 0.1470 | 0.8396 | 0.1265 | 0.7224 | 82.25% | 85.45% | 79.62% | 0.9247 | 1.0348 |
| 13 | 58 | 0.1610 | 0.9194 | 0.1522 | 0.8688 | 0.1249 | 0.7132 | 86.92% | 84.19% | 73.94% | 0.9025 | 0.9809 |
| 13 | 58 | 0.2401 | 1.3709 | 0.2243 | 1.2806 | 0.2118 | 1.2097 | 81.56% | 83.49% | 75.31% | 0.9112 | 0.9051 |
| 13 | 58 | 0.2152 | 1.2289 | 0.2030 | 1.1590 | 0.2076 | 1.1856 | 82.03% | 84.88% | 78.07% | 0.9082 | 1.1059 |
| 13 | 58 | 0.2347 | 1.3400 | 0.2245 | 1.2817 | 0.2464 | 1.4071 | 82.12% | 80.62% | 76.48% | 0.9246 | 1.0124 |
| 13 | 58 | 0.2316 | 1.3225 | 0.2273 | 1.2977 | 0.2181 | 1.2454 | 79.81% | 82.50% | 76.99% | 0.9032 | 0.8754 |
| 13 | 58 | 0.2026 | 1.1569 | 0.1989 | 1.1359 | 0.2160 | 1.2334 | 81.53% | 85.36% | 74.77% | 0.8944 | 1.0807 |
| 13 | 58 | 0.2297 | 1.3114 | 0.2150 | 1.2276 | 0.1818 | 1.0379 | 78.22% | 83.61% | 78.06% | 0.9151 | 0.9422 |
| 13 | 58 | 0.2250 | 1.2850 | 0.2026 | 1.1567 | 0.1708 | 0.9751 | 78.34% | 82.37% | 81.61% | 0.9186 |  |
| Average | 0.3506 | 2.0017 | 0.3222 | 1.8398 | 0.1982 | 1.1318 | 81.02% | 83.21% | 80.29% | 0.9284 | 0.9566 |
| Std. Dev. | 0.1527 | 0.8718 | 0.1319 | 0.7533 | 0.0588 | 0.3356 | 1.64% | 1.58% | 8.21% | 0.0254 | 0.1445 |

FWD data for I-490 East, Monroe, Rochester on Sep. 24, 2008 with E1 dowel bar configuration under nominal load of 71 kN (16 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 16 | 71 | 0.5023 | 2.8682 | 0.4721 | 2.6958 | 0.2192 | 1.2514 | 80.46% | 83.29% | 87.40% | 0.9534 | 1.0771 |
| 16 | 71 | 0.5236 | 2.9899 | 0.5085 | 2.9038 | 0.2194 | 1.2529 | 80.07% | 83.54% | 89.38% | 0.9846 | 0.9173 |
| 16 | 71 | 0.5414 | 3.0914 | 0.4665 | 2.6637 | 0.2212 | 1.2633 | 80.30% | 84.39% | 91.49% | 0.9394 | 1.1394 |
| 16 | 71 | 0.4839 | 2.7630 | 0.5315 | 3.0352 | 0.2135 | 1.2190 | 80.08% | 83.91% | 93.12% | 0.9699 | 0.9049 |
| 16 | 71 | 0.6169 | 3.5226 | 0.4810 | 2.7467 | 0.2509 | 1.4327 | 80.76% | 83.44% | 88.05% | 0.9443 |  |
| 16 | 71 | 0.5102 | 2.9130 | 0.0000 | 0.0000 | 0.2398 | 1.3693 | 80.59% |  | 85.51% | 0.9689 |  |
| 16 | 71 | 0.5161 | 2.9469 | 0.4566 | 2.6071 | 0.2447 | 1.3971 | 80.35% | 82.42% | 88.40% | 0.9595 | 0.8685 |
| 16 | 71 | 0.4639 | 2.6491 | 0.3965 | 2.2642 | 0.2260 | 1.2908 | 81.67% | 82.26% | 88.67% | 0.9639 | 1.0483 |
| 16 | 71 | 0.4048 | 2.3116 | 0.4157 | 2.3736 | 0.2163 | 1.2353 | 80.71% | 82.58% | 87.14% | 0.9356 | 0.9134 |
| 16 | 71 | 0.4179 | 2.3863 | 0.3797 | 2.1679 | 0.2020 | 1.1537 | 78.09% | 81.18% | 87.94% | 0.9112 | 0.7494 |
| 16 | 71 | 0.3945 | 2.2527 | 0.3445 | 1.9669 | 0.2718 | 1.5519 | 78.10% | 78.69% | 63.52% | 0.9174 | 0.9733 |
| 16 | 71 | 0.3419 | 1.9525 | 0.3353 | 1.9144 | 0.2840 | 1.6220 | 81.24% | 83.64% | 80.81% | 0.9238 | 1.0852 |
| 16 | 71 | 0.3737 | 2.1340 | 0.3638 | 2.0775 | 0.1444 | 0.8247 | 82.27% | 82.85% | 79.04% | 0.9184 | 0.6241 |
| 16 | 71 | 0.2362 | 1.3487 | 0.2271 | 1.2965 | 0.2234 | 1.2758 | 82.32% | 84.64% | 76.83% | 0.9076 | 1.1356 |
| 16 | 71 | 0.2726 | 1.5564 | 0.2578 | 1.4723 | 0.2134 | 1.2187 | 81.66% | 83.68% | 61.71% | 0.9264 | 0.9986 |
| 16 | 71 | 0.2476 | 1.4141 | 0.2575 | 1.4703 | 0.0000 | 0.0000 | 80.23% | 83.30% |  |  | 0.7624 |
| 16 | 71 | 0.2069 | 1.1814 | 0.1963 | 1.1210 | 0.1279 | 0.7302 | 84.98% | 85.65% | 74.55% | 0.8852 | 0.9376 |
| 16 | 71 | 0.2187 | 1.2487 | 0.1841 | 1.0510 | 0.1294 | 0.7391 | 82.06% | 85.68% | 69.03% | 0.9262 | 0.9681 |
| 16 | 71 | 0.1883 | 1.0753 | 0.1782 | 1.0175 | 0.1265 | 0.7224 | 82.07% | 87.64% | 79.62% | 0.9247 | 0.9912 |
| 16 | 71 | 0.1912 | 1.0921 | 0.1766 | 1.0085 | 0.1249 | 0.7132 | 81.45% | 81.99% | 73.94% | 0.9025 | 0.9920 |
| 16 | 71 | 0.2318 | 1.3235 | 0.2222 | 1.2687 | 0.2118 | 1.2097 | 81.98% | 82.65% | 75.31% | 0.9112 | 0.9055 |
| 16 | 71 | 0.2104 | 1.2013 | 0.2012 | 1.1488 | 0.2076 | 1.1856 | 83.25% | 85.79% | 78.07% | 0.9082 | 1.1287 |
| 16 | 71 | 0.2324 | 1.3271 | 0.2271 | 1.2966 | 0.2464 | 1.4071 | 83.22% | 83.33% | 76.48% | 0.9246 | 0.9886 |
| 16 | 71 | 0.2287 | 1.3061 | 0.2245 | 1.2818 | 0.2181 | 1.2454 | 80.00% | 83.10% | 76.99% | 0.9032 | 0.8956 |
| 16 | 71 | 0.2025 | 1.1566 | 0.2010 | 1.1480 | 0.2160 | 1.2334 | 82.31% | 83.94% | 74.77% | 0.8944 | 1.0577 |
| 16 | 71 | 0.2177 | 1.2432 | 0.2126 | 1.2142 | 0.1818 | 1.0379 | 77.12% | 83.21% | 78.06% | 0.9151 | 0.9466 |
| 16 | 71 | 0.2208 | 1.2608 | 0.2013 | 1.1494 | 0.1708 | 0.9751 | 76.83% | 82.12% | 81.61% | 0.9186 |  |
| Average | 0.3406 | 1.9450 | 0.3007 | 1.7171 | 0.1982 | 1.1318 | 80.90% | 83.42% | 80.29% | 0.9284 | 0.9587 |
| Std. Dev. | 0.1372 | 0.7836 | 0.1323 | 0.7556 | 0.0588 | 0.3356 | 1.85% | 1.70% | 8.21% | 0.0254 | 0.1255 |

FWD data for I-490 East, Monroe, Rochester on Sep. 25, 2008 with E2 dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.3543 | 2.0233 | 0.2301 | 1.3139 | 0.1429 | 0.8161 | 79.10% | 83.25% | 86.37% | 0.9563 | 0.7019 |
| 10 | 44 | 0.2623 | 1.4977 | 0.1615 | 0.9223 | 0.0892 | 0.5093 | 81.75% | 85.00% | 85.08% | 0.9784 | 1.0521 |
| 10 | 44 | 0.2103 | 1.2008 | 0.1699 | 0.9704 | 0.1041 | 0.5946 | 77.57% | 84.84% | 81.55% | 0.9080 | 1.4027 |
| 10 | 44 | 0.2128 | 1.2152 | 0.2384 | 1.3612 | 0.1342 | 0.7664 | 79.45% | 77.63% | 81.66% | 0.9240 | 0.5459 |
| 10 | 44 | 0.2736 | 1.5625 | 0.1301 | 0.7431 | 0.1321 | 0.7541 | 77.49% | 84.42% | 83.05% | 0.9371 | 1.2054 |
| 10 | 44 | 0.6428 | 3.6703 | 0.1569 | 0.8957 | 0.0735 | 0.4199 | 80.92% | 81.56% | 78.18% | 0.9425 | 1.3266 |
| 10 | 44 | 0.1665 | 0.9509 | 0.2081 | 1.1882 | 0.1216 | 0.6942 | 82.49% | 83.99% | 91.93% | 0.9082 | 0.9216 |
| 10 | 44 | 0.1443 | 0.8241 | 0.1918 | 1.0950 | 0.1086 | 0.6200 | 81.98% | 82.38% | 82.82% | 0.9135 | 0.9937 |
| 10 | 44 | 0.1699 | 0.9703 | 0.1906 | 1.0882 | 0.1153 | 0.6581 | 81.56% | 84.15% | 82.77% | 0.9144 | 0.8731 |
| 10 | 44 | 0.2530 | 1.4448 | 0.1664 | 0.9501 | 0.1372 | 0.7834 | 81.85% | 84.13% | 83.74% | 0.9681 | 1.1886 |
| 10 | 44 | 0.1628 | 0.9294 | 0.1429 | 0.8160 | 0.1496 | 0.8542 | 80.16% | 85.46% | 81.36% | 0.8489 | 1.1556 |
| 10 | 44 | 0.1818 | 1.0382 | 0.1652 | 0.9430 | 0.1544 | 0.8816 | 82.52% | 87.88% | 63.73% | 0.9155 | 1.0660 |
| 10 | 44 | 0.1816 | 1.0367 | 0.1761 | 1.0053 | 0.0000 | 0.0000 | 88.26% | 86.11% | 41.19% |  | 0.5606 |
| 10 | 44 | 0.1648 | 0.9408 | 0.0987 | 0.5635 | 0.1390 | 0.7935 | 85.77% | 119.31% | 57.07% | 0.9246 | 2.1925 |
| 10 | 44 | 0.2003 | 1.1437 | 0.2164 | 1.2355 | 0.1726 | 0.9855 | 81.61% | 62.10% | 78.00% | 0.9346 | 0.9130 |
| 10 | 44 | 0.1903 | 1.0868 | 0.1975 | 1.1280 | 0.1649 | 0.9417 | 85.27% | 86.64% | 71.86% | 0.9352 | 1.1355 |
| 10 | 44 | 0.2380 | 1.3592 | 0.2243 | 1.2808 | 0.1876 | 1.0713 | 81.43% | 84.35% | 62.65% | 0.8810 | 0.9103 |
| 10 | 44 | 0.2466 | 1.4082 | 0.2042 | 1.1659 | 0.1920 | 1.0964 | 84.86% | 86.50% | 73.28% | 0.8980 | 1.1577 |
| 10 | 44 | 0.2435 | 1.3907 | 0.2364 | 1.3498 | 0.1950 | 1.1133 | 81.37% | 83.95% | 73.03% | 0.9216 | 0.9858 |
| 10 | 44 | 0.2394 | 1.3671 | 0.2330 | 1.3306 | 0.1970 | 1.1248 | 84.86% | 85.48% | 78.77% | 0.9665 | 1.0059 |
| 10 | 44 | 0.1633 | 0.9327 | 0.1592 | 0.9090 | 0.1573 | 0.8980 | 82.99% | 85.79% | 81.55% | 0.9255 | 1.1768 |
| 10 | 44 | 0.1813 | 1.0354 | 0.1873 | 1.0696 | 0.2042 | 1.1660 | 79.72% | 84.04% | 79.86% | 0.9198 |  |
| 10 | 44 | 0.2090 | 1.1933 | 0.0000 | 0.0000 | 0.1849 | 1.0558 | 83.84% |  | 82.33% | 0.9439 |  |
| 10 | 44 | 0.1813 | 1.0352 | 0.2071 | 1.1825 | 0.1577 | 0.9004 | 85.49% | 87.24% | 80.57% | 0.8959 | 1.0722 |
| 10 | 44 | 0.2312 | 1.3202 | 0.2220 | 1.2679 | 0.2017 | 1.1517 | 83.21% | 83.79% | 80.97% | 0.9179 | 0.9822 |
| 10 | 44 | 0.2414 | 1.3787 | 0.2181 | 1.2454 | 0.2128 | 1.2150 | 82.68% | 86.72% | 81.69% | 0.9231 | 1.0408 |
| 10 | 44 | 0.2410 | 1.3759 | 0.2270 | 1.2961 | 0.2207 | 1.2603 | 85.20% | 87.67% | 82.26% | 0.9024 | 1.0718 |
| 10 | 44 | 0.2589 | 1.4781 | 0.2433 | 1.3892 | 0.2240 | 1.2789 | 82.85% | 86.10% | 82.70% | 0.9659 | 1.0578 |
| 10 | 44 | 0.2710 | 1.5475 | 0.2574 | 1.4696 | 0.2361 | 1.3479 | 84.74% | 83.05% | 79.63% | 0.8945 |  |
| Average | 0.2316 | 1.3227 | 0.1883 | 1.0750 | 0.1555 | 0.8880 | 82.45% | 85.13% | 77.57% | 0.9238 | 1.0652 |
| Std. Dev. | 0.0914 | 0.5218 | 0.0521 | 0.2976 | 0.0517 | 0.2952 | 2.52% | 8.21% | 10.13% | 0.0284 | 0.3037 |

FWD data for I-490 East, Monroe, Rochester on Sep. 25, 2008 with E2 dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.4059 | 2.3178 | 0.2955 | 1.6876 | 0.1715 | 0.9795 | 79.19% | 81.03% | 87.61% | 0.9286 | 0.6303 |
| 13 | 58 | 0.2394 | 1.3668 | 0.1863 | 1.0638 | 0.1027 | 0.5865 | 81.64% | 82.49% | 85.76% | 0.9683 | 0.9595 |
| 13 | 58 | 0.2135 | 1.2189 | 0.1788 | 1.0207 | 0.1094 | 0.6249 | 77.65% | 81.80% | 80.71% | 0.8884 | 1.4217 |
| 13 | 58 | 0.2025 | 1.1561 | 0.2541 | 1.4512 | 0.1396 | 0.7971 | 80.25% | 82.77% | 85.33% | 0.9637 | 0.6799 |
| 13 | 58 | 0.2693 | 1.5379 | 0.1728 | 0.9866 | 0.1250 | 0.7136 | 78.44% | 84.24% | 85.14% | 0.9221 | 1.2662 |
| 13 | 58 | 0.6324 | 3.6113 | 0.2188 | 1.2492 | 0.1016 | 0.5799 | 81.34% | 82.50% | 81.76% | 0.9036 | 1.0010 |
| 13 | 58 | 0.1942 | 1.1088 | 0.2190 | 1.2505 | 0.1127 | 0.6436 | 80.33% | 82.28% | 86.66% | 0.9016 | 0.8472 |
| 13 | 58 | 0.1592 | 0.9090 | 0.1855 | 1.0595 | 0.1109 | 0.6331 | 82.61% | 83.71% | 82.31% | 0.8884 | 1.0721 |
| 13 | 58 | 0.1722 | 0.9831 | 0.1989 | 1.1359 | 0.1179 | 0.6733 | 81.19% | 80.89% | 77.28% | 0.9356 | 0.8254 |
| 13 | 58 | 0.2389 | 1.3643 | 0.1642 | 0.9375 | 0.1216 | 0.6944 | 81.40% | 83.29% | 79.71% | 0.9237 | 1.1658 |
| 13 | 58 | 0.1620 | 0.9251 | 0.1493 | 0.8523 | 0.1447 | 0.8261 | 81.10% | 82.62% | 76.27% | 0.8808 | 1.1413 |
| 13 | 58 | 0.1850 | 1.0561 | 0.1703 | 0.9727 | 0.1480 | 0.8452 | 85.87% | 86.23% | 67.24% | 0.9273 | 1.0054 |
| 13 | 58 | 0.1783 | 1.0179 | 0.1713 | 0.9780 | 0.1317 | 0.7521 | 83.51% | 86.82% | 72.71% | 1.0337 | 1.0308 |
| 13 | 58 | 0.1735 | 0.9904 | 0.1766 | 1.0081 | 0.1381 | 0.7885 | 81.53% | 79.11% | 53.32% | 0.9431 | 1.2069 |
| 13 | 58 | 0.1987 | 1.1348 | 0.2131 | 1.2167 | 0.1672 | 0.9545 | 82.02% | 83.57% | 70.03% | 0.9734 | 0.9238 |
| 13 | 58 | 0.2071 | 1.1823 | 0.1968 | 1.1240 | 0.1598 | 0.9124 | 84.79% | 86.96% | 82.27% | 0.9136 | 1.0948 |
| 13 | 58 | 0.2361 | 1.3481 | 0.2155 | 1.2305 | 0.1862 | 1.0634 | 83.50% | 84.91% | 82.31% | 0.8624 | 1.0469 |
| 13 | 58 | 0.2503 | 1.4291 | 0.2256 | 1.2882 | 0.1996 | 1.1398 | 86.07% | 84.73% | 81.38% | 0.9306 | 1.0691 |
| 13 | 58 | 0.2349 | 1.3412 | 0.2412 | 1.3773 | 0.1945 | 1.1105 | 82.68% | 86.21% | 83.07% | 0.9193 | 1.0026 |
| 13 | 58 | 0.2432 | 1.3884 | 0.2418 | 1.3809 | 0.1933 | 1.1035 | 84.51% | 85.80% | 77.74% | 0.9175 | 1.0167 |
| 13 | 58 | 0.1621 | 0.9255 | 0.1534 | 0.8759 | 0.1545 | 0.8820 | 84.56% | 86.26% | 81.03% | 0.8846 | 1.1379 |
| 13 | 58 | 0.1822 | 1.0401 | 0.1745 | 0.9967 | 0.2002 | 1.1431 | 86.62% | 84.01% | 81.58% | 0.9299 | 1.2715 |
| 13 | 58 | 0.2040 | 1.1648 | 0.2219 | 1.2673 | 0.1831 | 1.0453 | 85.29% | 86.58% | 83.10% | 0.9404 | 0.8604 |
| 13 | 58 | 0.1761 | 1.0055 | 0.1910 | 1.0904 | 0.1527 | 0.8721 | 85.83% | 86.89% | 81.36% | 0.9052 | 1.0900 |
| 13 | 58 | 0.2291 | 1.3082 | 0.2080 | 1.1874 | 0.2042 | 1.1660 | 82.83% | 85.55% | 81.92% | 0.9459 | 1.0565 |
| 13 | 58 | 0.2435 | 1.3902 | 0.2197 | 1.2546 | 0.2166 | 1.2369 | 83.66% | 87.21% | 81.32% | 0.9424 | 1.0408 |
| 13 | 58 | 0.2495 | 1.4247 | 0.2287 | 1.3058 | 0.2143 | 1.2237 | 83.85% | 85.85% | 81.40% | 0.9137 | 1.0870 |
| 13 | 58 | 0.2645 | 1.5101 | 0.2486 | 1.4194 | 0.2288 | 1.3066 | 79.53% | 85.05% | 83.48% | 0.9150 | 1.0653 |
| 13 | 58 | 0.2743 | 1.5665 | 0.2648 | 1.5120 | 0.2416 | 1.3799 | 83.52% | 85.59% | 81.92% | 0.9140 |  |
| Average | 0.2338 | 1.3353 | 0.2064 | 1.1786 | 0.1611 | 0.9199 | 82.60% | 84.31% | 79.85% | 0.9247 | 1.0363 |
| Std. Dev. | 0.0914 | 0.5217 | 0.0354 | 0.2019 | 0.0409 | 0.2337 | 2.37% | 2.13% | 6.85% | 0.0334 | 0.1680 |

FWD data for I-490 East, Monroe, Rochester on Sep. 24, 2008 with E2 dowel bar configuration under nominal load of 71 kN (16 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 16 | 71 | 0.3769 | 2.1524 | 0.2845 | 1.6247 | 0.1822 | 1.0402 | 80.24% | 81.87% | 87.93% | 0.9381 | 0.8594 |
| 16 | 71 | 0.2973 | 1.6978 | 0.2445 | 1.3963 | 0.1394 | 0.7960 | 79.23% | 81.83% | 83.47% | 0.9006 | 0.8808 |
| 16 | 71 | 0.2681 | 1.5310 | 0.2154 | 1.2298 | 0.1321 | 0.7546 | 80.24% | 83.14% | 81.97% | 0.9167 | 1.2256 |
| 16 | 71 | 0.2219 | 1.2673 | 0.2640 | 1.5072 | 0.1424 | 0.8131 | 80.11% | 83.08% | 83.92% | 0.9335 | 1.1759 |
| 16 | 71 | 0.2613 | 1.4922 | 0.3104 | 1.7723 | 0.1349 | 0.7703 | 81.25% | 85.21% | 83.26% | 0.9303 | 0.6677 |
| 16 | 71 | 0.6036 | 3.4465 | 0.2073 | 1.1835 | 0.1440 | 0.8221 | 80.97% | 84.06% | 84.73% | 0.9235 | 1.0071 |
| 16 | 71 | 0.2205 | 1.2593 | 0.2087 | 1.1919 | 0.1341 | 0.7657 | 80.11% | 82.42% | 86.02% | 0.9058 | 0.9744 |
| 16 | 71 | 0.2093 | 1.1950 | 0.2034 | 1.1614 | 0.1354 | 0.7733 | 82.85% | 84.08% | 83.64% | 0.9307 | 1.0622 |
| 16 | 71 | 0.2060 | 1.1763 | 0.2160 | 1.2337 | 0.1405 | 0.8020 | 81.03% | 82.27% | 78.57% | 0.9188 | 0.9154 |
| 16 | 71 | 0.2348 | 1.3409 | 0.1978 | 1.1292 | 0.1416 | 0.8088 | 80.61% | 84.12% | 85.33% | 0.9020 | 0.9862 |
| 16 | 71 | 0.1934 | 1.1046 | 0.1752 | 1.0005 | 0.1611 | 0.9199 | 81.86% | 83.26% | 82.76% | 0.9089 | 1.0387 |
| 16 | 71 | 0.1922 | 1.0972 | 0.1820 | 1.0391 | 0.1582 | 0.9034 | 85.14% | 85.59% | 61.05% | 0.9249 | 1.0331 |
| 16 | 71 | 0.1967 | 1.1231 | 0.1880 | 1.0735 | 0.1769 | 1.0104 | 81.74% | 85.06% | 82.36% | 0.8249 | 0.8427 |
| 16 | 71 | 0.1825 | 1.0419 | 0.1584 | 0.9046 | 0.1529 | 0.8731 | 84.79% | 91.49% | 80.15% | 0.9173 | 1.2453 |
| 16 | 71 | 0.1933 | 1.1040 | 0.1973 | 1.1266 | 0.1644 | 0.9388 | 83.95% | 84.74% | 83.40% | 0.9293 | 1.0209 |
| 16 | 71 | 0.1919 | 1.0959 | 0.2014 | 1.1502 | 0.1717 | 0.9805 | 84.26% | 86.98% | 79.75% | 0.9032 | 1.0886 |
| 16 | 71 | 0.2313 | 1.3206 | 0.2193 | 1.2520 | 0.1852 | 1.0574 | 82.53% | 82.90% | 81.61% | 0.8974 | 1.0188 |
| 16 | 71 | 0.2520 | 1.4387 | 0.2234 | 1.2755 | 0.1932 | 1.1034 | 82.28% | 83.26% | 83.59% | 0.9229 | 1.0604 |
| 16 | 71 | 0.2326 | 1.3279 | 0.2369 | 1.3526 | 0.1876 | 1.0712 | 83.30% | 84.87% | 78.74% | 0.9216 | 0.9971 |
| 16 | 71 | 0.2416 | 1.3795 | 0.2362 | 1.3487 | 0.1903 | 1.0865 | 84.12% | 84.38% | 79.88% | 0.9346 | 1.0038 |
| 16 | 71 | 0.1627 | 0.9288 | 0.1553 | 0.8868 | 0.1591 | 0.9086 | 85.28% | 85.88% | 80.04% | 0.8974 | 1.1536 |
| 16 | 71 | 0.1802 | 1.0292 | 0.1792 | 1.0231 | 0.1894 | 1.0815 | 84.79% | 82.66% | 80.41% | 0.9265 | 1.2481 |
| 16 | 71 | 0.2029 | 1.1584 | 0.2236 | 1.2769 | 0.1881 | 1.0741 | 83.74% | 86.04% | 82.94% | 0.9218 | 0.8606 |
| 16 | 71 | 0.1946 | 1.1112 | 0.1925 | 1.0990 | 0.1685 | 0.9620 | 83.86% | 86.78% | 81.87% | 0.9233 | 1.0821 |
| 16 | 71 | 0.2333 | 1.3324 | 0.2083 | 1.1891 | 0.1876 | 1.0714 | 83.09% | 84.53% | 81.03% | 0.9351 | 1.0608 |
| 16 | 71 | 0.2388 | 1.3634 | 0.2209 | 1.2615 | 0.2109 | 1.2045 | 85.14% | 86.07% | 80.73% | 0.9215 | 1.0211 |
| 16 | 71 | 0.2383 | 1.3606 | 0.2256 | 1.2881 | 0.2097 | 1.1972 | 85.31% | 87.17% | 81.96% | 0.9462 | 1.0749 |
| 16 | 71 | 0.2519 | 1.4384 | 0.2425 | 1.3847 | 0.2197 | 1.2546 | 82.33% | 85.01% | 82.53% | 0.9510 | 1.0374 |
| 16 | 71 | 0.2644 | 1.5100 | 0.2516 | 1.4364 | 0.2328 | 1.3295 | 84.37% | 86.71% | 80.88% | 0.9130 |  |
| Average | 0.2405 | 1.3733 | 0.2162 | 1.2344 | 0.1701 | 0.9715 | 82.71% | 84.67% | 81.54% | 0.9180 | 1.0230 |
| Std. Dev. | 0.0816 | 0.4660 | 0.0346 | 0.1976 | 0.0282 | 0.1609 | 1.87% | 2.05% | 4.49% | 0.0226 | 0.1285 |

Appendix F:  FWD data from I490 East, August 19, 2009.

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with standard dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.3125 | 1.7846 | 0.3216 | 1.8365 | 0.1640 | 0.9365 | 84.62% | 91.98% | 76.38% | 0.9114 | 1.0254 |
| 10 | 44 | 0.3339 | 1.9065 | 0.3298 | 1.8832 | 0.1713 | 0.9781 | 83.18% | 91.48% | 91.99% | 0.8788 | 0.8744 |
| 10 | 44 | 0.3020 | 1.7244 | 0.2884 | 1.6467 | 0.1733 | 0.9897 | 83.39% | 70.48% | 80.12% | 0.9434 | 1.1177 |
| 10 | 44 | 0.3388 | 1.9346 | 0.3223 | 1.8405 | 0.1895 | 1.0821 | 83.13% | 76.31% | 89.97% | 0.9394 | 1.1171 |
| 10 | 44 | 0.2886 | 1.6482 | 0.3601 | 2.0560 | 0.1765 | 1.0080 | 83.28% | 74.93% | 93.46% | 0.8935 |  |
| 10 | 44 | 0.2240 | 1.2793 | 0.2837 | 1.6202 | 0.1579 | 0.9019 | 82.82% | 83.57% | 80.17% | 0.8726 | 0.7556 |
| 10 | 44 | 0.2097 | 1.1974 | 0.2144 | 1.2242 | 0.1520 | 0.8681 | 78.24% | 87.50% | 82.91% | 1.0000 | 0.9891 |
| 10 | 44 | 0.2425 | 1.3844 | 0.2120 | 1.2108 | 0.1461 | 0.8343 | 85.54% | 70.91% | 89.71% | 1.0867 | 1.2310 |
| 10 | 44 | 0.2417 | 1.3799 | 0.2610 | 1.4906 | 0.1441 | 0.8227 | 83.13% | 89.59% | 85.77% | 0.9122 | 0.9453 |
| 10 | 44 | 0.2238 | 1.2781 | 0.2468 | 1.4091 | 0.1441 | 0.8230 | 73.59% | 85.71% |  | 0.8993 | 0.8736 |
| 10 | 44 | 0.1956 | 1.1168 | 0.2156 | 1.2310 | 0.1364 | 0.7787 | 85.17% | 81.53% | 73.92% | 0.8889 | 0.9309 |
| 10 | 44 | 0.2055 | 1.1736 | 0.2007 | 1.1459 | 0.1368 | 0.7813 | 84.86% | 86.26% | 76.38% | 0.9097 | 1.0295 |
| 10 | 44 | 0.1961 | 1.1198 | 0.2066 | 1.1797 | 0.1347 | 0.7694 | 84.06% | 84.26% | 74.15% | 0.9648 | 0.9620 |
| 10 | 44 | 0.2022 | 1.1548 | 0.1988 | 1.1349 | 0.1328 | 0.7583 | 84.91% | 82.94% | 80.41% | 0.9433 | 0.9974 |
| 10 | 44 | 0.3037 | 1.7343 | 0.1982 | 1.1320 | 0.1485 | 0.8480 | 83.02% | 89.05% | 79.49% | 0.9103 |  |
| 10 | 44 |  |  | 0.2940 | 1.6787 | 0.1853 | 1.0583 |  | 84.09% | 79.57% | 0.9231 |  |
| Average | 0.2547 | 1.4545 | 0.2596 | 1.4825 | 0.1558 | 0.8899 | 82.86% | 83.16% | 82.29% | 0.9298 | 0.9884 |
| Std. Dev. | 0.0527 | 0.3007 | 0.0551 | 0.3147 | 0.0186 | 0.1063 | 3.08% | 6.78% | 6.43% | 0.0532 | 0.1230 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with standard dowel bar configuration under nominal load of 58 kN (13 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.3188 | 1.8206 | 0.3205 | 1.8301 | 0.1684 | 0.9614 | 82.82% | 89.35% | 75.38% | 0.9383 | 1.04 |
| 13 | 58 | 0.3385 | 1.9331 | 0.3337 | 1.9056 | 0.1722 | 0.9832 | 82.20% | 78.17% |  | 0.9264 | 0.87 |
| 13 | 58 | 0.3040 | 1.7358 | 0.2900 | 1.6559 | 0.1756 | 1.0029 | 83.38% | 84.11% | 94.18% | 0.9389 | 1.10 |
| 13 | 58 | 0.3338 | 1.9060 | 0.3200 | 1.8271 | 0.1926 | 1.1000 | 82.81% | 77.02% | 85.88% | 0.9781 | 1.13 |
| 13 | 58 | 0.2871 | 1.6392 | 0.3619 | 2.0664 | 0.1692 | 0.9664 | 82.96% | 83.30% | 81.33% | 0.9644 |  |
| 13 | 58 | 0.2281 | 1.3023 | 0.2830 | 1.6161 | 0.1585 | 0.9050 | 83.85% | 77.61% | 78.45% | 0.9140 | 0.76 |
| 13 | 58 | 0.2190 | 1.2503 | 0.2150 | 1.2277 | 0.1542 | 0.8804 | 83.54% | 91.39% | 84.69% | 0.9727 | 0.98 |
| 13 | 58 | 0.2762 | 1.5769 | 0.2105 | 1.2018 | 0.1562 | 0.8921 | 78.23% | 84.82% | 77.03% | 0.0000 | 1.23 |
| 13 | 58 | 0.2474 | 1.4126 | 0.2589 | 1.4784 | 0.1551 | 0.8859 | 83.52% | 84.32% | 67.24% | 0.9148 | 0.96 |
| 13 | 58 | 0.1801 | 1.0282 | 0.2487 | 1.4199 | 0.1456 | 0.8314 | 90.42% | 80.00% | 78.77% | 0.9095 | 0.79 |
| 13 | 58 | 0.1996 | 1.1398 | 0.1969 | 1.1246 | 0.1383 | 0.7895 | 85.14% | 96.84% | 77.54% | 0.8932 | 1.01 |
| 13 | 58 | 0.2099 | 1.1984 | 0.1996 | 1.1399 | 0.1372 | 0.7834 | 83.23% | 81.69% | 65.63% | 0.8971 | 1.02 |
| 13 | 58 | 0.2017 | 1.1517 | 0.2044 | 1.1669 | 0.1370 | 0.7821 | 81.61% | 81.67% | 75.47% | 0.9212 | 0.98 |
| 13 | 58 | 0.2114 | 1.2071 | 0.2009 | 1.1474 | 0.1358 | 0.7755 | 81.09% | 79.60% | 81.50% | 0.8966 | 1.01 |
| 13 | 58 | 0.2986 | 1.7048 | 0.2028 | 1.1580 | 0.1507 | 0.8607 | 82.61% | 75.08% | 81.04% | 0.9186 |  |
| 13 | 58 |  |  | 0.2938 | 1.6779 | 0.1851 | 1.0572 |  | 81.99% | 80.65% | 0.9022 |  |
| Average | 0.2569 | 1.4671 | 0.2588 | 1.4777 | 0.1582 | 0.9036 | 83.16% | 82.94% | 78.99% | 0.8679 | 0.99 |
| Std. Dev. | 0.0538 | 0.3072 | 0.0564 | 0.3220 | 0.0176 | 0.1008 | 2.54% | 5.68% | 6.96% | 0.2330 | 0.13 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with standard dowel bar configuration under nominal load of 80 kN (18 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 18 | 80 | 0.3048 | 1.7404 | 0.3124 | 1.7840 | 0.1627 | 0.9291 | 84.24% | 82.60% | 83.78% | 0.9226 | 1.0310 |
| 18 | 80 | 0.3296 | 1.8819 | 0.3221 | 1.8393 | 0.1696 | 0.9683 | 82.08% | 80.82% | 83.85% | 0.9058 | 0.8884 |
| 18 | 80 | 0.2987 | 1.7055 | 0.2862 | 1.6341 | 0.1730 | 0.9876 | 83.14% | 78.28% | 97.43% | 0.9115 | 1.0893 |
| 18 | 80 | 0.3229 | 1.8439 | 0.3117 | 1.7800 | 0.1826 | 1.0424 | 82.44% | 82.77% | 93.88% | 0.9070 | 1.0649 |
| 18 | 80 | 0.2764 | 1.5786 | 0.3320 | 1.8956 | 0.1713 | 0.9784 | 82.70% | 79.49% | 94.62% | 0.9323 |  |
| 18 | 80 | 0.2212 | 1.2633 | 0.2749 | 1.5697 | 0.1555 | 0.8879 | 83.33% | 80.92% | 80.90% | 0.9020 | 0.7770 |
| 18 | 80 | 0.2174 | 1.2415 | 0.2136 | 1.2196 | 0.1503 | 0.8584 | 82.06% | 88.94% | 83.46% | 0.8493 | 0.9593 |
| 18 | 80 | 0.2489 | 1.4212 | 0.2049 | 1.1699 | 0.1493 | 0.8527 | 83.85% | 84.83% | 79.67% | 0.9028 | 1.2274 |
| 18 | 80 | 0.2399 | 1.3697 | 0.2515 | 1.4359 | 0.1520 | 0.8678 | 82.80% | 85.42% | 85.32% | 0.9088 | 0.9400 |
| 18 | 80 | 0.1970 | 1.1247 | 0.2364 | 1.3498 | 0.1398 | 0.7982 | 83.76% | 87.66% | 81.68% | 0.9164 | 0.8898 |
| 18 | 80 | 0.1963 | 1.1207 | 0.2103 | 1.2010 | 0.1352 | 0.7719 | 85.28% | 78.74% | 81.09% | 0.8905 | 0.9761 |
| 18 | 80 | 0.2075 | 1.1848 | 0.2053 | 1.1723 | 0.1354 | 0.7734 | 84.13% | 88.11% | 78.13% | 0.9084 | 0.9897 |
| 18 | 80 | 0.2037 | 1.1632 | 0.2032 | 1.1603 | 0.1367 | 0.7805 | 80.34% | 85.47% | 82.62% | 0.9061 | 0.9925 |
| 18 | 80 | 0.2059 | 1.1760 | 0.2017 | 1.1515 | 0.1333 | 0.7609 | 83.74% | 75.86% | 78.26% | 0.9037 | 0.9981 |
| 18 | 80 | 0.2881 | 1.6451 | 0.2013 | 1.1494 | 0.1488 | 0.8500 | 83.54% | 79.01% | 83.82% | 0.9091 |  |
| 18 | 80 |  |  | 0.2831 | 1.6165 | 0.1805 | 1.0306 |  | 82.75% | 81.14% | 0.9063 |  |
| Average | 0.2506 | 1.4307 | 0.2532 | 1.4456 | 0.1547 | 0.8836 | 83.16% | 82.61% | 84.35% | 0.9052 | 0.9864 |
| Std. Dev. | 0.0484 | 0.2762 | 0.0493 | 0.2817 | 0.0167 | 0.0954 | 1.17% | 3.87% | 5.83% | 0.0175 | 0.1091 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with E1 dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.3413 | 1.9488 | 0.3289 | 1.8782 | 0.1779 | 1.0159 | 80.80% | 74.60% | 84.54% | 0.9112 | 0.8881 |
| 10 | 44 | 0.2949 | 1.6842 | 0.2921 | 1.6680 | 0.1665 | 0.9509 | 85.40% | 83.58% | 85.24% | 0.9156 | 0.8944 |
| 10 | 44 | 0.2750 | 1.5702 | 0.2613 | 1.4919 | 0.1662 | 0.9489 | 83.14% | 80.00% | 91.04% | 0.9020 | 1.3130 |
| 10 | 44 | 0.3384 | 1.9325 | 0.3430 | 1.9588 | 0.1680 | 0.9596 | 84.59% | 82.69% | 72.32% | 0.8397 | 1.3450 |
| 10 | 44 | 0.4629 | 2.6432 | 0.4614 | 2.6346 | 0.1834 | 1.0473 | 83.37% | 76.05% | 84.22% | 0.9080 | 0.7706 |
| 10 | 44 | 0.3582 | 2.0455 | 0.3555 | 2.0302 | 0.1768 | 1.0097 | 83.94% | 81.76% | 86.11% | 0.9308 | 0.9825 |
| 10 | 44 | 0.3727 | 2.1282 | 0.3493 | 1.9947 | 0.1865 | 1.0648 | 82.21% | 76.58% | 83.98% | 0.9042 | 0.9469 |
| 10 | 44 | 0.3307 | 1.8886 | 0.3308 | 1.8889 | 0.1958 | 1.1180 | 82.78% |  | 88.10% | 0.8977 | 1.0509 |
| 10 | 44 | 0.3483 | 1.9888 | 0.3476 | 1.9850 | 0.1905 | 1.0878 | 83.54% | 69.97% | 80.92% | 0.9048 | 1.0254 |
| 10 | 44 | 0.3514 | 2.0067 | 0.3565 | 2.0355 | 0.1781 | 1.0170 | 82.37% | 90.60% | 85.56% | 0.8889 |  |
| 10 | 44 | 0.2198 | 1.2553 | 0.2284 | 1.3042 | 0.1793 | 1.0238 | 83.12% | 81.25% | 90.68% | 0.9282 | 1.3837 |
| 10 | 44 | 0.3038 | 1.7350 | 0.3160 | 1.8046 | 0.1928 | 1.1009 | 82.57% | 81.65% | 75.78% | 0.9048 | 0.8799 |
| 10 | 44 | 0.2743 | 1.5663 | 0.2781 | 1.5878 | 0.1913 | 1.0924 | 81.51% |  | 83.49% | 0.8794 | 0.9014 |
| 10 | 44 | 0.2630 | 1.5015 | 0.2507 | 1.4313 | 0.1738 | 0.9922 | 77.49% | 86.00% | 86.74% | 0.9448 | 0.9436 |
| 10 | 44 | 0.2322 | 1.3260 | 0.2365 | 1.3505 | 0.1830 | 1.0451 | 80.42% | 85.71% | 85.49% | 0.9053 | 0.9040 |
| 10 | 44 | 0.2429 | 1.3869 | 0.2138 | 1.2208 | 0.1875 | 1.0704 | 77.78% | 68.33% | 85.49% | 0.8316 | 1.2226 |
| 10 | 44 | 0.2185 | 1.2478 | 0.2614 | 1.4926 | 0.1707 | 0.9747 | 88.74% | 67.16% | 82.32% | 0.9310 | 0.8365 |
| 10 | 44 | 0.2244 | 1.2815 | 0.2187 | 1.2485 | 0.1625 | 0.9279 | 84.07% | 77.03% | 79.86% | 0.9818 | 0.9310 |
| 10 | 44 | 0.1881 | 1.0743 | 0.2036 | 1.1623 | 0.1646 | 0.9400 | 88.54% | 83.50% | 81.99% | 0.8916 | 0.9419 |
| 10 | 44 | 0.2044 | 1.1669 | 0.1917 | 1.0948 |  |  | 84.13% | 80.00% |  |  |  |
| Average | 0.2923 | 1.6689 | 0.2913 | 1.6632 | 0.1787 | 1.0204 | 83.03% | 79.25% | 83.89% | 0.9053 | 1.0090 |
| Std. Dev. | 0.0704 | 0.4019 | 0.0687 | 0.3921 | 0.0104 | 0.0593 | 2.79% | 6.31% | 4.53% | 0.0336 | 0.1825 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with E1 dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.3346 | 1.9107 | 0.3234 | 1.8466 | 0.1765 | 1.0078 | 83.33% | 76.40% | 80.42% | 0.9353 | 0.8957 |
| 13 | 58 | 0.2925 | 1.6704 | 0.2897 | 1.6540 | 0.1650 | 0.9422 | 85.19% | 89.39% | 96.92% | 0.9019 | 0.9141 |
| 13 | 58 | 0.2757 | 1.5742 | 0.2648 | 1.5120 | 0.1763 | 1.0067 | 84.83% | 79.71% | 98.09% | 0.8839 | 1.3073 |
| 13 | 58 | 0.3401 | 1.9419 | 0.3462 | 1.9766 | 0.1679 | 0.9585 | 84.07% | 86.11% | 89.79% | 0.9630 | 1.3564 |
| 13 | 58 | 0.4640 | 2.6495 | 0.4695 | 2.6810 | 0.1821 | 1.0400 | 81.14% | 82.16% | 77.10% | 0.8839 | 0.7664 |
| 13 | 58 | 0.3630 | 2.0727 | 0.3599 | 2.0548 | 0.1834 | 1.0474 | 82.44% | 79.78% |  | 0.9298 | 1.0143 |
| 13 | 58 | 0.3783 | 2.1603 | 0.3650 | 2.0841 | 0.1891 | 1.0797 | 84.06% | 74.43% | 93.37% | 0.9447 | 0.8907 |
| 13 | 58 | 0.3301 | 1.8850 | 0.3251 | 1.8562 | 0.1989 | 1.1356 | 84.03% | 88.47% | 72.41% | 0.9157 | 1.0303 |
| 13 | 58 | 0.3593 | 2.0515 | 0.3349 | 1.9125 | 0.1977 | 1.1286 | 83.37% | 81.11% | 92.03% | 0.9461 | 1.0433 |
| 13 | 58 | 0.3517 | 2.0082 | 0.3494 | 1.9953 | 0.1759 | 1.0045 | 82.94% | 92.22% | 79.50% | 0.9269 |  |
| 13 | 58 | 0.2231 | 1.2737 | 0.2333 | 1.3323 | 0.1841 | 1.0512 | 84.24% | 84.35% | 75.76% | 0.9692 | 1.3213 |
| 13 | 58 | 0.3063 | 1.7491 | 0.3083 | 1.7605 | 0.1884 | 1.0758 | 80.65% | 80.79% | 79.61% | 0.9423 | 0.9242 |
| 13 | 58 | 0.2763 | 1.5779 | 0.2849 | 1.6271 | 0.1835 | 1.0476 | 84.43% | 86.48% | 88.75% | 0.9213 | 0.9192 |
| 13 | 58 | 0.2340 | 1.3360 | 0.2619 | 1.4957 | 0.1762 | 1.0060 | 88.76% | 80.55% | 79.52% | 0.9027 | 0.9190 |
| 13 | 58 | 0.2374 | 1.3555 | 0.2407 | 1.3746 | 0.1801 | 1.0282 | 87.43% | 87.68% | 92.91% | 0.9234 | 0.8931 |
| 13 | 58 | 0.2409 | 1.3757 | 0.2150 | 1.2276 | 0.1677 | 0.9576 | 78.22% | 65.38% | 82.24% | 0.9333 | 1.1036 |
| 13 | 58 | 0.2659 | 1.5186 | 0.2373 | 1.3547 | 0.1874 | 1.0701 | 79.16% | 88.86% | 72.41% | 0.8773 | 0.9436 |
| 13 | 58 | 0.2311 | 1.3197 | 0.2239 | 1.2783 | 0.1721 | 0.9826 | 82.26% | 81.70% | 73.27% | 0.9139 | 0.8721 |
| 13 | 58 | 0.1997 | 1.1402 | 0.1952 | 1.1148 | 0.1598 | 0.9126 | 85.16% | 76.17% | 83.75% | 0.9091 | 1.0679 |
| 13 | 58 | 0.2062 | 1.1773 | 0.2085 | 1.1905 |  |  | 84.25% | 85.47% |  |  |  |
| Average | 0.2955 | 1.6874 | 0.2918 | 1.6665 | 0.1796 | 1.0254 | 83.50% | 82.36% | 83.77% | 0.9223 | 1.0101 |
| Std. Dev. | 0.0689 | 0.3934 | 0.0686 | 0.3920 | 0.0105 | 0.0597 | 2.48% | 6.26% | 8.50% | 0.0255 | 0.1673 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with E1 dowel bar configuration under nominal load of 80 kN (18 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 18 | 80 | 0.3261 | 1.8623 | 0.3147 | 1.7968 | 0.1745 | 0.9964 | 81.87% | 88.33% |  | 0.9167 | 0.8801 |
| 18 | 80 | 0.2829 | 1.6157 | 0.2769 | 1.5813 | 0.1628 | 0.9296 | 84.10% | 83.10% | 80.72% | 0.9201 | 0.9309 |
| 18 | 80 | 0.2681 | 1.5310 | 0.2578 | 1.4720 | 0.1654 | 0.9443 | 83.69% | 81.40% | 86.30% | 0.9414 | 1.2656 |
| 18 | 80 | 0.3284 | 1.8750 | 0.3263 | 1.8630 | 0.1659 | 0.9473 | 83.04% | 85.01% | 79.24% | 0.9132 | 1.3408 |
| 18 | 80 | 0.4413 | 2.5198 | 0.4374 | 2.4979 | 0.1746 | 0.9969 | 83.33% | 79.22% | 89.19% | 0.9155 | 0.7873 |
| 18 | 80 | 0.3486 | 1.9905 | 0.3444 | 1.9667 | 0.1744 | 0.9956 | 84.24% | 81.63% | 86.48% | 0.9195 | 1.0224 |
| 18 | 80 | 0.3638 | 2.0776 | 0.3521 | 2.0107 | 0.1852 | 1.0577 | 82.30% | 89.90% | 85.35% | 0.9333 | 0.8727 |
| 18 | 80 | 0.3247 | 1.8540 | 0.3073 | 1.7547 | 0.1913 | 1.0924 | 84.87% | 83.07% | 79.15% | 0.9352 | 1.0789 |
| 18 | 80 | 0.3385 | 1.9330 | 0.3315 | 1.8931 | 0.1935 | 1.1051 | 83.39% | 92.04% |  | 0.9441 | 1.0123 |
| 18 | 80 | 0.3384 | 1.9320 | 0.3356 | 1.9163 | 0.1745 | 0.9962 | 82.74% | 89.86% | 77.08% | 0.9088 |  |
| 18 | 80 | 0.2186 | 1.2483 | 0.2288 | 1.3067 | 0.1807 | 1.0320 | 82.42% | 76.75% | 82.91% | 0.9566 | 1.3016 |
| 18 | 80 | 0.2934 | 1.6754 | 0.2978 | 1.7007 | 0.1768 | 1.0095 | 82.68% | 84.04% | 79.03% | 0.9396 | 0.9141 |
| 18 | 80 | 0.2682 | 1.5317 | 0.2723 | 1.5547 | 0.1773 | 1.0126 | 84.00% | 84.25% |  | 0.9312 | 0.9371 |
| 18 | 80 | 0.2484 | 1.4184 | 0.2551 | 1.4569 | 0.1743 | 0.9952 | 83.30% | 88.52% | 76.87% | 0.9275 | 0.9253 |
| 18 | 80 | 0.2345 | 1.3390 | 0.2361 | 1.3481 | 0.1777 | 1.0147 | 84.45% | 88.10% | 83.41% | 0.9167 | 0.9292 |
| 18 | 80 | 0.2283 | 1.3037 | 0.2194 | 1.2527 | 0.1865 | 1.0651 | 84.56% | 76.85% | 77.30% | 0.8670 | 1.1687 |
| 18 | 80 | 0.2537 | 1.4486 | 0.2564 | 1.4640 | 0.1770 | 1.0110 | 79.63% | 80.93% | 74.65% | 0.8824 | 0.8416 |
| 18 | 80 | 0.2183 | 1.2463 | 0.2158 | 1.2321 | 0.1799 | 1.0272 | 86.05% | 71.81% | 96.59% | 0.8876 | 0.9467 |
| 18 | 80 | 0.1940 | 1.1080 | 0.2043 | 1.1664 | 0.1631 | 0.9312 | 85.83% | 93.11% | 80.80% | 0.9151 | 0.9477 |
| 18 | 80 | 0.2021 | 1.1543 | 0.1936 | 1.1055 |  |  | 84.40% | 81.77% |  |  |  |
| Average | 0.2860 | 1.6332 | 0.2832 | 1.6170 | 0.1766 | 1.0084 | 83.54% | 83.98% | 82.19% | 0.9196 | 1.0057 |
| Std. Dev. | 0.0642 | 0.3665 | 0.0613 | 0.3500 | 0.0086 | 0.0493 | 1.44% | 5.51% | 5.60% | 0.0222 | 0.1619 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with E2 dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.3935 | 2.2469 | 0.3941 | 2.2501 | 0.1857 | 1.0606 | 84.27% | 80.45% | 97.55% | 0.9231 | 1.0775 |
| 10 | 44 | 0.4216 | 2.4071 | 0.4246 | 2.4245 | 0.1841 | 1.0515 | 82.15% | 71.76% | 87.60% | 0.9337 | 0.6965 |
| 10 | 44 | 0.3010 | 1.7185 | 0.2957 | 1.6886 | 0.1696 | 0.9685 | 87.55% | 75.82% |  | 0.9231 | 0.7850 |
| 10 | 44 | 0.2444 | 1.3958 | 0.2321 | 1.3255 | 0.1647 | 0.9402 | 79.09% | 73.83% | 88.89% | 0.8693 | 1.1366 |
| 10 | 44 | 0.2708 | 1.5461 | 0.2638 | 1.5066 | 0.1611 | 0.9199 | 85.04% | 90.20% | 79.72% | 0.9281 | 0.9439 |
| 10 | 44 | 0.2417 | 1.3803 | 0.2490 | 1.4221 | 0.1543 | 0.8810 | 83.69% | 70.42% | 101.68% | 0.8993 | 1.1930 |
| 10 | 44 | 0.3136 | 1.7910 | 0.2971 | 1.6965 | 0.1573 | 0.8982 | 82.41% | 73.94% |  | 0.8846 | 0.8962 |
| 10 | 44 | 0.2716 | 1.5509 | 0.2662 | 1.5203 | 0.1661 | 0.9484 | 84.47% | 86.31% | 82.15% | 0.9576 | 1.0597 |
| 10 | 44 | 0.2696 | 1.5393 | 0.2822 | 1.6111 | 0.1709 | 0.9759 | 83.27% | 70.65% | 88.33% | 0.8750 | 0.7768 |
| 10 | 44 | 0.2186 | 1.2483 | 0.2192 | 1.2515 | 0.1538 | 0.8781 | 87.61% | 84.72% | 79.59% | 0.9675 |  |
| 10 | 44 | 0.1996 | 1.1396 | 0.2080 | 1.1878 | 0.1743 | 0.9954 | 83.33% | 82.95% | 70.46% | 0.8610 | 0.9366 |
| 10 | 44 | 0.2065 | 1.1793 | 0.1948 | 1.1125 | 0.1696 | 0.9685 | 84.55% | 98.07% | 84.48% | 0.9337 | 1.1421 |
| 10 | 44 | 0.2216 | 1.2656 | 0.2225 | 1.2706 | 0.1735 | 0.9905 | 81.86% | 92.02% | 85.89% | 0.9121 | 0.9540 |
| 10 | 44 | 0.2294 | 1.3100 | 0.2123 | 1.2121 | 0.1872 | 1.0687 | 83.19% | 74.31% | 79.99% | 0.8804 | 0.9899 |
| 10 | 44 | 0.2163 | 1.2353 | 0.2101 | 1.1998 | 0.2002 | 1.1429 | 86.89% | 63.11% | 73.16% | 0.8925 | 1.1771 |
| 10 | 44 | 0.2437 | 1.3915 | 0.2473 | 1.4123 | 0.2246 | 1.2824 | 85.02% | 86.03% | 75.54% | 0.8632 | 0.9932 |
| 10 | 44 | 0.2522 | 1.4403 | 0.2457 | 1.4027 | 0.1844 | 1.0527 | 85.12% | 86.27% | 83.14% | 0.8956 | 0.9869 |
| 10 | 44 | 0.2379 | 1.3586 | 0.2424 | 1.3844 | 0.1803 | 1.0295 | 84.65% | 83.54% | 73.27% | 0.9076 | 1.1860 |
| 10 | 44 | 0.2853 | 1.6293 | 0.2875 | 1.6418 | 0.1706 | 0.9739 | 84.01% | 77.89% | 86.32% | 0.9438 | 0.8290 |
| 10 | 44 | 0.2437 | 1.3918 | 0.2384 | 1.3612 | 0.1801 | 1.0285 | 85.20% | 88.84% | 82.86% | 0.9149 |  |
| Average | 0.2641 | 1.5083 | 0.2617 | 1.4941 | 0.1756 | 1.0028 | 84.17% | 80.56% | 83.37% | 0.9083 | 0.9867 |
| Std. Dev. | 0.0577 | 0.3296 | 0.0588 | 0.3360 | 0.0166 | 0.0948 | 2.00% | 8.79% | 8.05% | 0.0309 | 0.1507 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with E2 dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.3966 | 2.2647 | 0.3906 | 2.2303 | 0.1895 | 1.0819 | 84.73% | 85.71% | 80.14% | 0.9322 | 1.0777 |
| 13 | 58 | 0.4272 | 2.4391 | 0.4209 | 2.4035 | 0.1863 | 1.0636 | 83.49% | 77.63% | 74.62% | 0.9174 | 0.7087 |
| 13 | 58 | 0.3060 | 1.7474 | 0.2983 | 1.7033 | 0.1688 | 0.9637 | 82.14% | 79.43% | 84.41% | 0.9078 | 0.8118 |
| 13 | 58 | 0.2442 | 1.3946 | 0.2421 | 1.3827 | 0.1637 | 0.9345 | 85.03% | 76.04% | 97.71% | 0.8990 | 1.1289 |
| 13 | 58 | 0.2732 | 1.5600 | 0.2734 | 1.5609 | 0.1638 | 0.9353 | 86.03% | 81.79% | 73.19% | 0.9091 | 0.8915 |
| 13 | 58 | 0.2470 | 1.4103 | 0.2437 | 1.3915 | 0.1560 | 0.8906 | 83.83% | 87.31% | 109.04% | 0.9296 | 1.2251 |
| 13 | 58 | 0.3106 | 1.7738 | 0.2985 | 1.7046 | 0.1611 | 0.9198 | 81.69% | 88.24% | 91.36% | 0.9234 | 0.8852 |
| 13 | 58 | 0.2750 | 1.5705 | 0.2643 | 1.5090 | 0.1713 | 0.9779 | 84.76% | 77.90% | 80.60% | 0.8903 | 1.0684 |
| 13 | 58 | 0.2785 | 1.5905 | 0.2824 | 1.6123 | 0.1731 | 0.9883 | 83.77% | 78.81% | 81.15% | 0.8992 | 0.8067 |
| 13 | 58 | 0.2299 | 1.3127 | 0.2278 | 1.3007 | 0.1738 | 0.9922 | 85.17% | 82.86% | 83.53% | 0.9295 |  |
| 13 | 58 | 0.2027 | 1.1577 | 0.2122 | 1.2115 | 0.1738 | 0.9925 | 84.56% | 83.06% | 90.69% | 0.8769 | 0.9779 |
| 13 | 58 | 0.2013 | 1.1495 | 0.2075 | 1.1847 | 0.1724 | 0.9843 | 85.67% | 88.03% | 77.30% | 0.9261 | 1.0773 |
| 13 | 58 | 0.2181 | 1.2456 | 0.2235 | 1.2763 | 0.1768 | 1.0097 | 83.28% | 75.83% | 80.63% | 0.9049 | 0.9489 |
| 13 | 58 | 0.2226 | 1.2710 | 0.2121 | 1.2110 | 0.1810 | 1.0337 | 85.39% | 84.59% | 70.77% | 0.9027 | 0.9119 |
| 13 | 58 | 0.2209 | 1.2615 | 0.1934 | 1.1044 | 0.2000 | 1.1420 | 85.62% | 95.26% | 74.90% | 0.9122 | 1.2259 |
| 13 | 58 | 0.2408 | 1.3752 | 0.2371 | 1.3538 | 0.2100 | 1.1993 | 87.38% | 93.53% | 79.05% | 0.9418 | 1.0689 |
| 13 | 58 | 0.2562 | 1.4632 | 0.2534 | 1.4471 | 0.1825 | 1.0421 | 84.10% | 79.82% | 72.41% | 0.9102 | 0.9376 |
| 13 | 58 | 0.2344 | 1.3383 | 0.2376 | 1.3568 | 0.1838 | 1.0494 | 85.33% | 86.53% | 79.81% | 0.9198 | 1.2160 |
| 13 | 58 | 0.2838 | 1.6203 | 0.2889 | 1.6498 | 0.1802 | 1.0290 | 84.60% | 82.65% | 77.74% | 0.9011 | 0.8445 |
| 13 | 58 | 0.2415 | 1.3793 | 0.2440 | 1.3932 | 0.1814 | 1.0357 | 85.43% | 82.81% | 88.18% | 0.9211 |  |
| Average | 0.2655 | 1.5163 | 0.2626 | 1.4994 | 0.1775 | 1.0133 | 84.60% | 83.39% | 82.36% | 0.9127 | 0.9896 |
| Std. Dev. | 0.0590 | 0.3368 | 0.0577 | 0.3297 | 0.0129 | 0.0739 | 1.33% | 5.37% | 9.31% | 0.0158 | 0.1545 |

FWD data for I-490 East, Monroe, Rochester on Aug. 19, 2009 with E2 dowel bar configuration under nominal load of 80 kN (18 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/DO M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 18 | 80 | 0.3607 | 2.0599 | 0.3766 | 2.1507 | 0.1868 | 1.0669 | 94.61% | 78.55% | 91.92% | 0.9241 | 1.0745 |
| 18 | 80 | 0.4086 | 2.3332 | 0.4047 | 2.3109 | 0.1803 | 1.0293 | 82.87% | 86.88% | 84.18% | 0.9156 | 0.7184 |
| 18 | 80 | 0.2940 | 1.6790 | 0.2907 | 1.6601 | 0.1682 | 0.9606 | 82.94% | 80.31% | 82.22% | 0.9252 | 0.8093 |
| 18 | 80 | 0.2434 | 1.3898 | 0.2353 | 1.3435 | 0.1646 | 0.9397 | 83.88% | 80.00% | 77.29% | 0.9414 | 1.1247 |
| 18 | 80 | 0.2655 | 1.5163 | 0.2646 | 1.5110 | 0.1575 | 0.8995 | 84.30% | 85.56% | 88.39% | 0.9336 | 0.9136 |
| 18 | 80 | 0.2414 | 1.3786 | 0.2418 | 1.3804 | 0.1548 | 0.8841 | 83.52% | 88.96% | 95.14% | 0.9271 | 1.2060 |
| 18 | 80 | 0.2975 | 1.6987 | 0.2916 | 1.6648 | 0.1577 | 0.9003 | 83.39% | 83.74% | 78.57% | 0.9119 | 0.8955 |
| 18 | 80 | 0.2628 | 1.5005 | 0.2611 | 1.4908 | 0.1682 | 0.9605 | 84.46% | 82.02% | 92.51% | 0.8924 | 1.0577 |
| 18 | 80 | 0.2709 | 1.5469 | 0.2761 | 1.5767 | 0.1677 | 0.9575 | 84.46% | 83.88% | 86.32% | 0.8917 | 0.8143 |
| 18 | 80 | 0.2248 | 1.2837 | 0.2249 | 1.2840 | 0.1730 | 0.9879 | 85.14% | 77.30% | 82.91% | 0.8954 |  |
| 18 | 80 | 0.1983 | 1.1323 | 0.2105 | 1.2021 | 0.1597 | 0.9118 | 85.35% | 92.55% | 90.12% | 0.9536 | 0.9648 |
| 18 | 80 | 0.2038 | 1.1636 | 0.2031 | 1.1598 | 0.1648 | 0.9412 | 87.07% | 80.39% | 82.73% | 0.9192 | 1.0896 |
| 18 | 80 | 0.2227 | 1.2716 | 0.2213 | 1.2638 | 0.1705 | 0.9738 | 81.96% | 75.95% | 93.08% | 0.9206 | 0.9775 |
| 18 | 80 | 0.2143 | 1.2236 | 0.2163 | 1.2353 | 0.1749 | 0.9989 | 85.11% | 91.67% | 75.07% | 0.9080 | 0.9364 |
| 18 | 80 | 0.2112 | 1.2060 | 0.2026 | 1.1568 | 0.1889 | 1.0789 | 87.05% | 77.89% | 77.94% | 0.9184 | 1.2082 |
| 18 | 80 | 0.2343 | 1.3377 | 0.2448 | 1.3976 | 0.1989 | 1.1359 | 87.11% | 83.26% | 84.38% | 0.9022 | 1.0288 |
| 18 | 80 | 0.2504 | 1.4295 | 0.2518 | 1.4379 | 0.1804 | 1.0301 | 86.58% | 77.78% | 86.44% | 0.9193 | 0.9168 |
| 18 | 80 | 0.2294 | 1.3102 | 0.2309 | 1.3183 | 0.1787 | 1.0204 | 86.13% | 86.91% | 87.12% | 0.9429 | 1.2046 |
| 18 | 80 | 0.2698 | 1.5405 | 0.2781 | 1.5880 | 0.1733 | 0.9895 | 84.37% | 85.14% | 86.00% | 0.9193 | 0.8370 |
| 18 | 80 | 0.2315 | 1.3218 | 0.2328 | 1.3292 | 0.1742 | 0.9946 | 88.38% | 77.07% | 82.51% | 0.9060 |  |
| Average | 0.2568 | 1.4662 | 0.2580 | 1.4731 | 0.1722 | 0.9831 | 85.43% | 82.79% | 85.24% | 0.9184 | 0.9876 |
| Std. Dev. | 0.0523 | 0.2988 | 0.0530 | 0.3029 | 0.0114 | 0.0648 | 2.74% | 4.91% | 5.58% | 0.0166 | 0.1467 |

Appendix G:  I490 Eastbound FWD data collected June 21, 2011

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E1 dowel bar configuration under nominal load of 44 kN (10 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.3707 | 2.1166 | 0.3622 | 2.0684 | 0.1665 | 0.9505 | 82.97% | 80.61% | 90.59% | 0.9222 | 1.0393 |
| 10 | 44 | 0.3765 | 2.1497 | 0.3993 | 2.2802 | 0.1646 | 0.9397 | 82.93% | 78.34% | 88.66% | 0.9146 | 1.0652 |
| 10 | 44 | 0.4254 | 2.4289 | 0.3634 | 2.0751 | 0.1820 | 1.0391 | 83.81% | 82.83% | 91.62% | 0.9337 | 1.0771 |
| 10 | 44 | 0.3914 | 2.2351 | 0.3067 | 1.7511 | 0.1684 | 0.9614 | 84.24% | 80.66% | 84.52% | 0.9162 | 1.0669 |
| 10 | 44 | 0.3272 | 1.8682 | 0.3276 | 1.8704 | 0.1616 | 0.9225 | 82.30% | 79.69% | 91.60% | 0.8994 | 1.0533 |
| 10 | 44 | 0.3450 | 1.9700 | 0.3585 | 2.0472 | 0.1546 | 0.8828 | 82.30% | 80.79% | 92.05% | 0.9221 | 1.0645 |
| 10 | 44 | 0.3816 | 2.1792 | 0.3376 | 1.9279 | 0.1660 | 0.9480 | 84.00% | 76.88% | 89.11% | 0.9080 | 1.0337 |
| 10 | 44 | 0.3490 | 1.9929 | 0.3424 | 1.9552 | 0.1785 | 1.0195 | 83.92% | 79.82% | 95.66% | 0.9091 | 1.0521 |
| 10 | 44 | 0.3603 | 2.0571 | 0.3617 | 2.0653 | 0.1632 | 0.9319 | 81.74% | 78.87% | 88.89% | 0.9136 | 1.0615 |
| 10 | 44 | 0.3840 | 2.1924 | 0.3059 | 1.7470 | 0.1623 | 0.9266 | 82.06% | 78.81% | 89.76% | 0.9130 | 1.0511 |
| 10 | 44 | 0.3216 | 1.8363 | 0.4324 | 2.4691 | 0.1676 | 0.9568 | 83.17% | 78.04% | 83.44% | 0.9152 | 0.9336 |
| 10 | 44 | 0.4037 | 2.3052 | 0.3945 | 2.2524 | 0.1590 | 0.9082 | 80.86% | 81.79% | 97.63% | 0.9114 | 1.0659 |
| 10 | 44 | 0.4204 | 2.4008 | 0.3738 | 2.1346 | 0.1959 | 1.1188 | 85.23% | 80.22% | 89.41% | 0.9067 | 1.0502 |
| 10 | 44 | 0.3926 | 2.2417 | 0.3790 | 2.1642 | 0.1724 | 0.9844 | 83.38% | 82.26% | 91.76% | 0.9408 | 1.0810 |
| 10 | 44 | 0.4097 | 2.3395 | 0.3551 | 2.0280 | 0.1962 | 1.1201 | 84.00% | 82.29% | 92.45% | 0.9433 | 1.0600 |
| 10 | 44 | 0.3764 | 2.1495 | 0.2652 | 1.5146 | 0.1516 | 0.8656 | 83.60% | 79.92% | 88.05% | 0.9200 | 1.0703 |
| 10 | 44 | 0.2839 | 1.6211 | 0.4243 | 2.4230 | 0.1575 | 0.8995 | 82.56% | 81.67% | 98.30% | 0.9167 | 1.1374 |
| 10 | 44 | 0.4826 | 2.7558 | 0.5527 | 3.1558 | 0.1775 | 1.0137 | 82.98% | 77.86% | 92.26% | 0.9371 | 1.0129 |
| 10 | 44 | 0.5598 | 3.1966 | 0.3915 | 2.2355 | 0.1728 | 0.9866 | 81.60% | 79.74% | 91.37% | 0.9471 | 1.0748 |
| 10 | 44 | 0.4208 | 2.4028 | 0.3647 | 2.0825 | 0.1810 | 1.0334 | 83.25% | 81.11% | 90.52% | 0.9167 | 1.0434 |
| 10 | 44 | 0.3805 | 2.1728 | 0.3818 | 2.1799 | 0.1636 | 0.9341 | 81.60% | 78.13% | 97.26% | 0.9006 | 1.0947 |
| 10 | 44 | 0.4179 | 2.3863 | 0.3201 | 1.8276 | 0.1591 | 0.9087 | 80.79% | 78.73% | 85.57% | 0.9172 | 1.1241 |
| 10 | 44 | 0.3598 | 2.0544 | 0.2671 | 1.5250 | 0.1476 | 0.8429 | 80.00% | 82.06% | 86.15% | 0.9167 | 1.0465 |
| 10 | 44 | 0.2795 | 1.5959 | 0.3024 | 1.7266 | 0.1586 | 0.9058 | 83.88% | 81.97% | 93.65% | 0.9226 | 1.0165 |
| 10 | 44 | 0.3074 | 1.7551 | 0.3013 | 1.7207 | 0.1624 | 0.9273 | 84.62% | 79.86% | 88.19% | 0.9182 | 1.0520 |
| 10 | 44 | 0.3170 | 1.8102 |  |  |  |  | 84.14% |  |  |  |  |
| Average | 0.3786 | 2.1621 | 0.3589 | 2.0491 | 0.1676 | 0.9571 | 82.92% | 80.12% | 90.74% | 0.9193 | 1.0571 |
| Std. Dev. | 0.0597 | 0.3412 | 0.0595 | 0.3396 | 0.0122 | 0.0696 | 1.28% | 1.63% | 3.85% | 0.0124 | 0.0378 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E1 dowel bar configuration under nominal load of 58 kN (13 kip).

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.3682 | 2.1023 | 0.3658 | 2.0888 | 0.1640 | 0.9367 | 83.61% | 80.17% | 89.27% | 0.9406 | 1.0100 |
| 13 | 58 | 0.3694 | 2.1096 | 0.4057 | 2.3166 | 0.1665 | 0.9510 | 82.65% | 78.88% | 87.28% | 0.9182 | 1.0414 |
| 13 | 58 | 0.4225 | 2.4126 | 0.3676 | 2.0990 | 0.1760 | 1.0050 | 83.06% | 82.89% | 86.76% | 0.9402 | 1.0336 |
| 13 | 58 | 0.3799 | 2.1695 | 0.3056 | 1.7448 | 0.1728 | 0.9865 | 83.20% | 81.28% | 86.16% | 0.9127 | 1.0681 |
| 13 | 58 | 0.3264 | 1.8637 | 0.3273 | 1.8692 | 0.1610 | 0.9194 | 82.52% | 79.72% | 90.99% | 0.9194 | 1.0727 |
| 13 | 58 | 0.3512 | 2.0052 | 0.3588 | 2.0488 | 0.1548 | 0.8840 | 82.43% | 80.08% | 92.63% | 0.9175 | 1.0764 |
| 13 | 58 | 0.3862 | 2.2052 | 0.3310 | 1.8903 | 0.1723 | 0.9840 | 82.84% | 81.52% | 90.03% | 0.9159 | 1.0702 |
| 13 | 58 | 0.3543 | 2.0230 | 0.3437 | 1.9624 | 0.1746 | 0.9973 | 83.30% | 81.15% | 90.37% | 0.9127 | 1.0440 |
| 13 | 58 | 0.3588 | 2.0488 | 0.3645 | 2.0816 | 0.1648 | 0.9412 | 82.24% | 80.21% | 87.48% | 0.9083 | 1.0500 |
| 13 | 58 | 0.3828 | 2.1857 | 0.3050 | 1.7413 | 0.1630 | 0.9307 | 81.94% | 80.15% | 89.17% | 0.9263 | 1.0681 |
| 13 | 58 | 0.3257 | 1.8599 | 0.4341 | 2.4787 | 0.1734 | 0.9902 | 82.52% | 78.92% | 84.21% | 0.9043 | 0.9256 |
| 13 | 58 | 0.4018 | 2.2944 | 0.3899 | 2.2264 | 0.1679 | 0.9587 | 80.34% | 81.71% | 94.22% | 0.9103 | 1.0822 |
| 13 | 58 | 0.4219 | 2.4093 | 0.3743 | 2.1371 | 0.1938 | 1.1069 | 84.39% | 81.78% | 88.46% | 0.9216 | 1.0480 |
| 13 | 58 | 0.3922 | 2.2398 | 0.3785 | 2.1613 | 0.1940 | 1.1075 | 84.05% | 82.29% | 93.53% | 0.9449 | 1.0739 |
| 13 | 58 | 0.4065 | 2.3211 | 0.3504 | 2.0008 | 0.1861 | 1.0627 | 83.46% | 83.01% | 90.23% | 0.9350 | 1.0626 |
| 13 | 58 | 0.3723 | 2.1260 | 0.2674 | 1.5266 | 0.1539 | 0.8787 | 83.43% | 80.39% | 85.56% | 0.9171 | 1.0753 |
| 13 | 58 | 0.2875 | 1.6417 | 0.4189 | 2.3918 | 0.1572 | 0.8975 | 82.46% | 81.64% | 95.23% | 0.9423 | 1.1441 |
| 13 | 58 | 0.4792 | 2.7365 | 0.5412 | 3.0901 | 0.1750 | 0.9991 | 82.70% | 79.47% | 93.41% | 0.9524 | 1.0085 |
| 13 | 58 | 0.5457 | 3.1162 | 0.3842 | 2.1937 | 0.1738 | 0.9923 | 81.64% | 80.51% | 89.00% | 0.9430 | 1.0791 |
| 13 | 58 | 0.4146 | 2.3674 | 0.3615 | 2.0642 | 0.1747 | 0.9973 | 83.24% | 81.99% | 89.05% | 0.9274 | 1.0613 |
| 13 | 58 | 0.3837 | 2.1907 | 0.3758 | 2.1458 | 0.1620 | 0.9253 | 82.64% | 78.96% | 93.83% | 0.9167 | 1.0792 |
| 13 | 58 | 0.4056 | 2.3158 | 0.3227 | 1.8425 | 0.1592 | 0.9089 | 81.46% | 79.77% | 83.47% | 0.9202 | 1.0898 |
| 13 | 58 | 0.3517 | 2.0080 | 0.2657 | 1.5173 | 0.1501 | 0.8574 | 80.65% | 83.52% | 84.89% | 0.9040 | 1.0667 |
| 13 | 58 | 0.2834 | 1.6184 | 0.2967 | 1.6941 | 0.1574 | 0.8987 | 83.24% | 81.59% | 90.02% | 0.9187 | 1.0640 |
| 13 | 58 | 0.3157 | 1.8025 | 0.2956 | 1.6877 | 0.1619 | 0.9245 | 82.52% | 81.38% | 87.35% | 0.9116 | 1.0971 |
| 13 | 58 | 0.3243 | 1.8516 |  |  |  |  | 81.78% |  |  |  |  |
| Average | 0.3774 | 2.1548 | 0.3573 | 2.0400 | 0.1684 | 0.9617 | 82.63% | 80.92% | 89.30% | 0.9232 | 1.0597 |
| Std. Dev. | 0.0558 | 0.3188 | 0.0582 | 0.3324 | 0.0114 | 0.0654 | 0.94% | 1.30% | 3.25% | 0.0138 | 0.0390 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E1 dowel bar configuration under nominal load of 80 kN (18 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 18 | 80 | 0.3473 | 1.9833 | 0.3438 | 1.9631 | 0.1608 | 0.9180 | 82.66% | 80.16% | 90.61% | 0.9308 | 1.0218 |
| 18 | 80 | 0.3513 | 2.0058 | 0.3813 | 2.1772 | 0.1621 | 0.9257 | 82.01% | 78.82% | 87.17% | 0.8969 | 1.0424 |
| 18 | 80 | 0.3975 | 2.2696 | 0.3470 | 1.9812 | 0.1763 | 1.0065 | 82.50% | 82.01% | 90.01% | 0.9238 | 1.0508 |
| 18 | 80 | 0.3646 | 2.0818 | 0.2941 | 1.6795 | 0.1673 | 0.9552 | 82.82% | 80.38% | 85.54% | 0.9027 | 1.0705 |
| 18 | 80 | 0.3148 | 1.7978 | 0.3164 | 1.8067 | 0.1583 | 0.9042 | 81.15% | 78.33% | 90.46% | 0.8932 | 1.0353 |
| 18 | 80 | 0.3276 | 1.8705 | 0.3409 | 1.9463 | 0.1500 | 0.8567 | 81.00% | 80.27% | 91.65% | 0.9104 | 1.0661 |
| 18 | 80 | 0.3634 | 2.0749 | 0.3182 | 1.8168 | 0.1655 | 0.9453 | 82.84% | 80.04% | 90.67% | 0.9078 | 1.0471 |
| 18 | 80 | 0.3331 | 1.9023 | 0.3315 | 1.8928 | 0.1722 | 0.9833 | 82.91% | 80.34% | 90.82% | 0.9082 | 1.0518 |
| 18 | 80 | 0.3486 | 1.9908 | 0.3488 | 1.9917 | 0.1616 | 0.9225 | 81.30% | 79.32% | 87.51% | 0.9021 | 1.0582 |
| 18 | 80 | 0.3691 | 2.1075 | 0.2949 | 1.6839 | 0.1623 | 0.9270 | 81.38% | 79.85% | 89.06% | 0.8962 | 1.0619 |
| 18 | 80 | 0.3131 | 1.7881 | 0.4207 | 2.4020 | 0.1690 | 0.9651 | 82.15% | 78.35% | 85.08% | 0.8997 | 0.9187 |
| 18 | 80 | 0.3864 | 2.2067 | 0.3781 | 2.1588 | 0.1659 | 0.9476 | 79.91% | 80.84% | 93.83% | 0.9044 | 1.0574 |
| 18 | 80 | 0.3998 | 2.2828 | 0.3624 | 2.0692 | 0.1903 | 1.0866 | 83.95% | 81.32% | 87.90% | 0.9102 | 1.0451 |
| 18 | 80 | 0.3787 | 2.1624 | 0.3673 | 2.0975 | 0.1784 | 1.0187 | 82.78% | 81.37% | 88.58% | 0.9265 | 1.0733 |
| 18 | 80 | 0.3943 | 2.2513 | 0.3394 | 1.9378 | 0.1799 | 1.0274 | 82.53% | 82.24% | 89.50% | 0.9243 | 1.0598 |
| 18 | 80 | 0.3597 | 2.0537 | 0.2636 | 1.5055 | 0.1533 | 0.8754 | 82.52% | 80.04% | 84.85% | 0.9037 | 1.0812 |
| 18 | 80 | 0.2851 | 1.6277 | 0.4037 | 2.3054 | 0.1563 | 0.8925 | 81.40% | 81.17% | 95.74% | 0.9275 | 1.1315 |
| 18 | 80 | 0.4568 | 2.6085 | 0.5116 | 2.9214 | 0.1747 | 0.9977 | 82.34% | 79.29% | 92.98% | 0.9349 | 1.0071 |
| 18 | 80 | 0.5153 | 2.9423 | 0.3708 | 2.1174 | 0.1723 | 0.9840 | 80.97% | 80.03% | 89.01% | 0.9180 | 1.0785 |
| 18 | 80 | 0.3999 | 2.2835 | 0.3504 | 2.0007 | 0.1745 | 0.9961 | 82.45% | 81.13% | 87.37% | 0.9065 | 1.0393 |
| 18 | 80 | 0.3641 | 2.0793 | 0.3637 | 2.0768 | 0.1630 | 0.9306 | 81.85% | 78.63% | 93.55% | 0.8993 | 1.0789 |
| 18 | 80 | 0.3924 | 2.2406 | 0.3146 | 1.7966 | 0.1601 | 0.9142 | 80.20% | 78.82% | 85.97% | 0.8982 | 1.0880 |
| 18 | 80 | 0.3423 | 1.9548 | 0.2625 | 1.4987 | 0.1502 | 0.8578 | 79.53% | 81.13% | 86.31% | 0.8783 | 1.0583 |
| 18 | 80 | 0.2778 | 1.5862 | 0.2905 | 1.6588 | 0.1562 | 0.8917 | 82.38% | 79.80% | 90.31% | 0.9094 | 1.0597 |
| 18 | 80 | 0.3078 | 1.7578 | 0.2899 | 1.6556 | 0.1624 | 0.9271 | 81.99% | 80.63% | 88.15% | 0.9056 | 1.0911 |
| 18 | 80 | 0.3163 | 1.8064 |  |  |  |  | 80.72% |  |  |  |  |
| Average | 0.3618 | 2.0660 | 0.3442 | 1.9657 | 0.1657 | 0.9463 | 81.86% | 80.17% | 89.31% | 0.9088 | 1.0549 |
| Std. Dev. | 0.0510 | 0.2913 | 0.0534 | 0.3049 | 0.0098 | 0.0562 | 1.04% | 1.09% | 2.85% | 0.0134 | 0.0375 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E2 dowel bar configuration under nominal load of 44 kN (10 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.3032 | 1.7316 | 0.2959 | 1.6897 | 0.1691 | 0.9653 | 81.36% | 78.35% | 77.85% | 0.8848 | 1.0248 |
| 10 | 44 | 0.2419 | 1.3813 | 0.2329 | 1.3297 | 0.1549 | 0.8843 | 81.70% | 75.98% | 82.96% | 0.8882 | 1.0388 |
| 10 | 44 | 0.2783 | 1.5894 | 0.2539 | 1.4498 | 0.1558 | 0.8897 | 78.60% | 73.90% | 84.48% | 0.8750 | 1.0963 |
| 10 | 44 | 0.2731 | 1.5594 | 0.2425 | 1.3848 | 0.1641 | 0.9369 | 78.79% | 78.81% | 79.83% | 0.8938 | 1.1261 |
| 10 | 44 | 0.2812 | 1.6059 | 0.2755 | 1.5734 | 0.1668 | 0.9526 | 79.12% | 72.59% | 80.14% | 0.8834 | 1.0207 |
| 10 | 44 | 0.2469 | 1.4096 | 0.2256 | 1.2884 | 0.1755 | 1.0019 | 78.01% | 72.40% | 82.33% | 0.8721 | 1.0941 |
| 10 | 44 | 0.2740 | 1.5647 | 0.2516 | 1.4364 | 0.1732 | 0.9892 | 79.70% | 75.20% | 86.81% | 0.8947 | 1.0893 |
| 10 | 44 | 0.2857 | 1.6313 | 0.2558 | 1.4609 | 0.1736 | 0.9914 | 79.14% | 78.57% | 82.36% | 0.8882 | 1.1167 |
| 10 | 44 | 0.2632 | 1.5031 | 0.2465 | 1.4077 | 0.1570 | 0.8964 | 77.82% | 75.10% | 83.80% | 0.8831 | 1.0678 |
| 10 | 44 | 0.2525 | 1.4416 | 0.2348 | 1.3405 | 0.1695 | 0.9681 | 79.03% | 75.00% | 80.39% | 0.9102 | 1.0754 |
| 10 | 44 | 0.2790 | 1.5929 | 0.2637 | 1.5056 | 0.1844 | 1.0530 | 79.27% | 75.10% | 80.85% | 0.8895 | 1.0580 |
| 10 | 44 | 0.2518 | 1.4377 | 0.2464 | 1.4068 | 0.1746 | 0.9970 | 81.38% | 76.54% | 82.42% | 0.9059 | 1.0220 |
| 10 | 44 | 0.2581 | 1.4737 | 0.2499 | 1.4271 | 0.1832 | 1.0460 | 82.68% | 75.92% | 84.27% | 0.8944 | 1.0326 |
| 10 | 44 | 0.2502 | 1.4287 | 0.2364 | 1.3496 | 0.1805 | 1.0305 | 80.99% | 78.11% | 84.68% | 0.9034 | 1.0586 |
| 10 | 44 | 0.3020 | 1.7242 | 0.2866 | 1.6368 | 0.1776 | 1.0139 | 78.62% | 74.38% | 83.61% | 0.8908 | 1.0534 |
| 10 | 44 | 0.2666 | 1.5223 | 0.2681 | 1.5307 | 0.1691 | 0.9653 | 82.10% | 75.77% | 77.70% | 0.8848 | 0.9945 |
| 10 | 44 | 0.2348 | 1.3408 | 0.2272 | 1.2974 | 0.1721 | 0.9826 | 79.13% | 73.42% | 80.40% | 0.8810 | 1.0335 |
| 10 | 44 | 0.2531 | 1.4453 | 0.2395 | 1.3677 | 0.1676 | 0.9573 | 78.28% | 75.54% | 83.54% | 0.8834 | 1.0568 |
| 10 | 44 | 0.2392 | 1.3659 | 0.2307 | 1.3175 | 0.1632 | 0.9318 | 78.45% | 76.00% | 84.44% | 0.8994 | 1.0367 |
| 10 | 44 | 0.2453 | 1.4006 | 0.2413 | 1.3778 | 0.1742 | 0.9945 | 80.75% | 74.89% | 80.38% | 0.8698 | 1.0165 |
| 10 | 44 | 0.2475 | 1.4130 | 0.2506 | 1.4311 | 0.1606 | 0.9169 | 79.67% | 77.46% | 81.95% | 0.8782 | 0.9874 |
| 10 | 44 | 0.2487 | 1.4200 | 0.2413 | 1.3778 | 0.1643 | 0.9381 | 79.25% | 77.02% | 80.66% | 0.9000 | 1.0306 |
| 10 | 44 | 0.2404 | 1.3725 | 0.2388 | 1.3636 | 0.1534 | 0.8759 | 79.74% | 75.00% | 79.35% | 0.8851 | 1.0065 |
| 10 | 44 | 0.2271 | 1.2967 | 0.2161 | 1.2341 | 0.1797 | 1.0261 | 79.00% | 72.99% | 82.40% | 0.9080 | 1.0507 |
| 10 | 44 | 0.2605 | 1.4874 | 0.2503 | 1.4295 | 0.1530 | 0.8738 | 80.08% | 78.93% | 79.29% | 0.8919 | 1.0405 |
| 10 | 44 | 0.2590 | 1.4792 | 0.2475 | 1.4133 |  |  | 78.57% | 74.07% |  |  | 1.0466 |
| Average | 0.2601 | 1.4853 | 0.2481 | 1.4164 | 0.1687 | 0.9631 | 79.66% | 75.66% | 81.88% | 0.8896 | 1.0490 |
| Std. Dev. | 0.0197 | 0.1123 | 0.0183 | 0.1046 | 0.0093 | 0.0531 | 1.32% | 1.90% | 2.29% | 0.0108 | 0.0350 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E2 dowel bar configuration under nominal load of 58 kN (13 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.2985 | 1.7047 | 0.2905 | 1.6585 | 0.1708 | 0.9752 | 81.28% | 78.96% | 77.88% | 0.8978 | 1.0278 |
| 13 | 58 | 0.2441 | 1.3936 | 0.2313 | 1.3209 | 0.1558 | 0.8896 | 81.56% | 76.70% | 82.10% | 0.9034 | 1.0550 |
| 13 | 58 | 0.2748 | 1.5690 | 0.2550 | 1.4560 | 0.1567 | 0.8950 | 78.57% | 75.52% | 81.92% | 0.8750 | 1.0776 |
| 13 | 58 | 0.2765 | 1.5789 | 0.2522 | 1.4403 | 0.1691 | 0.9653 | 78.79% | 76.28% | 79.67% | 0.8750 | 1.0962 |
| 13 | 58 | 0.2850 | 1.6274 | 0.2783 | 1.5892 | 0.1698 | 0.9696 | 78.28% | 74.39% | 78.77% | 0.8850 | 1.0240 |
| 13 | 58 | 0.2502 | 1.4284 | 0.2249 | 1.2842 | 0.1768 | 1.0093 | 78.42% | 75.59% | 80.32% | 0.8809 | 1.1123 |
| 13 | 58 | 0.2742 | 1.5659 | 0.2534 | 1.4471 | 0.1760 | 1.0050 | 79.44% | 74.78% | 84.17% | 0.9103 | 1.0821 |
| 13 | 58 | 0.2855 | 1.6300 | 0.2604 | 1.4870 | 0.1740 | 0.9933 | 78.84% | 77.91% | 81.22% | 0.9048 | 1.0962 |
| 13 | 58 | 0.2691 | 1.5367 | 0.2458 | 1.4035 | 0.1573 | 0.8982 | 76.75% | 75.91% | 82.23% | 0.8900 | 1.0949 |
| 13 | 58 | 0.2533 | 1.4463 | 0.2333 | 1.3321 | 0.1738 | 0.9925 | 79.46% | 76.55% | 80.09% | 0.9091 | 1.0857 |
| 13 | 58 | 0.2794 | 1.5953 | 0.2616 | 1.4936 | 0.1730 | 0.9876 | 79.78% | 77.52% | 79.01% | 0.8922 | 1.0681 |
| 13 | 58 | 0.2568 | 1.4662 | 0.2426 | 1.3855 | 0.1770 | 1.0109 | 80.83% | 78.88% | 79.56% | 0.8889 | 1.0583 |
| 13 | 58 | 0.2734 | 1.5610 | 0.2516 | 1.4368 | 0.1847 | 1.0544 | 79.28% | 76.19% | 80.79% | 0.8984 | 1.0864 |
| 13 | 58 | 0.2562 | 1.4631 | 0.2435 | 1.3907 | 0.1829 | 1.0442 | 80.78% | 77.81% | 81.55% | 0.9091 | 1.0521 |
| 13 | 58 | 0.3010 | 1.7185 | 0.2846 | 1.6253 | 0.1755 | 1.0019 | 80.57% | 76.33% | 80.86% | 0.9095 | 1.0573 |
| 13 | 58 | 0.2842 | 1.6231 | 0.2693 | 1.5377 | 0.1719 | 0.9815 | 77.63% | 76.34% | 78.22% | 0.8855 | 1.0556 |
| 13 | 58 | 0.2417 | 1.3803 | 0.2276 | 1.2995 | 0.1725 | 0.9847 | 79.56% | 76.08% | 80.53% | 0.8908 | 1.0622 |
| 13 | 58 | 0.2553 | 1.4580 | 0.2412 | 1.3774 | 0.1766 | 1.0087 | 78.81% | 77.36% | 84.51% | 0.8932 | 1.0585 |
| 13 | 58 | 0.2436 | 1.3908 | 0.2302 | 1.3144 | 0.1690 | 0.9647 | 79.75% | 75.74% | 81.36% | 0.8834 | 1.0581 |
| 13 | 58 | 0.2492 | 1.4229 | 0.2453 | 1.4009 | 0.1756 | 1.0029 | 80.49% | 74.15% | 81.14% | 0.8913 | 1.0157 |
| 13 | 58 | 0.2506 | 1.4307 | 0.2380 | 1.3591 | 0.1595 | 0.9109 | 79.03% | 77.14% | 79.79% | 0.9009 | 1.0526 |
| 13 | 58 | 0.2527 | 1.4432 | 0.2381 | 1.3599 | 0.1687 | 0.9632 | 79.10% | 77.99% | 80.61% | 0.9018 | 1.0612 |
| 13 | 58 | 0.2441 | 1.3939 | 0.2427 | 1.3860 | 0.1604 | 0.9158 | 79.50% | 75.78% | 79.99% | 0.8915 | 1.0057 |
| 13 | 58 | 0.2276 | 1.2994 | 0.2166 | 1.2366 | 0.1807 | 1.0319 | 79.26% | 75.09% | 81.86% | 0.9198 | 1.0508 |
| 13 | 58 | 0.2599 | 1.4841 | 0.2529 | 1.4440 | 0.1568 | 0.8955 | 80.35% | 79.46% | 80.74% | 0.8986 | 1.0278 |
| 13 | 58 | 0.2580 | 1.4732 | 0.2483 | 1.4180 |  |  | 79.59% | 76.20% |  |  | 1.0389 |
| Average | 0.2633 | 1.5032 | 0.2484 | 1.4186 | 0.1706 | 0.9741 | 79.45% | 76.56% | 80.76% | 0.8954 | 1.0600 |
| Std. Dev. | 0.0186 | 0.1065 | 0.0180 | 0.1026 | 0.0084 | 0.0479 | 1.10% | 1.37% | 1.58% | 0.0115 | 0.0267 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E2 dowel bar configuration under nominal load of 80 kN (18 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 18 | 80 | 0.2939 | 1.6782 | 0.2866 | 1.6364 | 0.1728 | 0.9868 | 79.77% | 78.17% | 79.35% | 0.8808 | 1.0256 |
| 18 | 80 | 0.2422 | 1.3830 | 0.2325 | 1.3277 | 0.1594 | 0.9104 | 80.14% | 75.97% | 82.24% | 0.8790 | 1.0416 |
| 18 | 80 | 0.2717 | 1.5517 | 0.2538 | 1.4493 | 0.1579 | 0.9015 | 78.08% | 75.67% | 81.67% | 0.8741 | 1.0707 |
| 18 | 80 | 0.2758 | 1.5748 | 0.2488 | 1.4207 | 0.1713 | 0.9783 | 77.29% | 77.12% | 79.84% | 0.8775 | 1.1084 |
| 18 | 80 | 0.2845 | 1.6244 | 0.2777 | 1.5854 | 0.1722 | 0.9830 | 77.62% | 73.61% | 78.50% | 0.8651 | 1.0246 |
| 18 | 80 | 0.2519 | 1.4386 | 0.2276 | 1.2996 | 0.1803 | 1.0294 | 78.13% | 73.82% | 80.11% | 0.8675 | 1.1070 |
| 18 | 80 | 0.2723 | 1.5549 | 0.2526 | 1.4422 | 0.1807 | 1.0318 | 79.16% | 75.06% | 82.33% | 0.8959 | 1.0781 |
| 18 | 80 | 0.2828 | 1.6150 | 0.2570 | 1.4677 | 0.1781 | 1.0169 | 78.23% | 77.78% | 81.61% | 0.8885 | 1.1004 |
| 18 | 80 | 0.2645 | 1.5102 | 0.2448 | 1.3976 | 0.1606 | 0.9169 | 77.37% | 75.75% | 80.70% | 0.8768 | 1.0806 |
| 18 | 80 | 0.2553 | 1.4578 | 0.2327 | 1.3285 | 0.1770 | 1.0108 | 78.79% | 76.72% | 80.48% | 0.8939 | 1.0974 |
| 18 | 80 | 0.2772 | 1.5829 | 0.2612 | 1.4916 | 0.1753 | 1.0012 | 78.85% | 75.92% | 80.59% | 0.8814 | 1.0612 |
| 18 | 80 | 0.2527 | 1.4428 | 0.2456 | 1.4025 | 0.1796 | 1.0257 | 79.68% | 75.87% | 79.43% | 0.8857 | 1.0288 |
| 18 | 80 | 0.2705 | 1.5445 | 0.2518 | 1.4379 | 0.1882 | 1.0747 | 80.17% | 76.01% | 80.53% | 0.8855 | 1.0741 |
| 18 | 80 | 0.2564 | 1.4641 | 0.2429 | 1.3870 | 0.1835 | 1.0478 | 79.50% | 77.65% | 80.78% | 0.8913 | 1.0556 |
| 18 | 80 | 0.2944 | 1.6810 | 0.2836 | 1.6191 | 0.1803 | 1.0294 | 79.17% | 75.96% | 81.12% | 0.8921 | 1.0382 |
| 18 | 80 | 0.2762 | 1.5772 | 0.2687 | 1.5343 | 0.1723 | 0.9841 | 79.17% | 75.80% | 78.11% | 0.8841 | 1.0280 |
| 18 | 80 | 0.2448 | 1.3979 | 0.2298 | 1.3123 | 0.1726 | 0.9853 | 78.40% | 75.87% | 81.00% | 0.8820 | 1.0652 |
| 18 | 80 | 0.2547 | 1.4543 | 0.2391 | 1.3654 | 0.1721 | 0.9827 | 77.48% | 76.56% | 82.09% | 0.8808 | 1.0651 |
| 18 | 80 | 0.2438 | 1.3922 | 0.2331 | 1.3310 | 0.1720 | 0.9823 | 78.40% | 76.16% | 81.28% | 0.8738 | 1.0459 |
| 18 | 80 | 0.2494 | 1.4239 | 0.2442 | 1.3942 | 0.1783 | 1.0181 | 79.54% | 74.07% | 80.95% | 0.8803 | 1.0213 |
| 18 | 80 | 0.2504 | 1.4301 | 0.2394 | 1.3670 | 0.1637 | 0.9345 | 78.72% | 76.67% | 79.59% | 0.8789 | 1.0461 |
| 18 | 80 | 0.2506 | 1.4308 | 0.2406 | 1.3739 | 0.1702 | 0.9720 | 78.78% | 75.99% | 80.94% | 0.8937 | 1.0414 |
| 18 | 80 | 0.2449 | 1.3985 | 0.2462 | 1.4061 | 0.1603 | 0.9152 | 78.55% | 74.83% | 79.24% | 0.8754 | 0.9946 |
| 18 | 80 | 0.2284 | 1.3042 | 0.2174 | 1.2415 | 0.1836 | 1.0483 | 79.15% | 75.39% | 82.36% | 0.9088 | 1.0506 |
| 18 | 80 | 0.2610 | 1.4906 | 0.2560 | 1.4618 | 0.1590 | 0.9077 | 78.95% | 77.43% | 81.68% | 0.8853 | 1.0197 |
| 18 | 80 | 0.2556 | 1.4596 | 0.2473 | 1.4124 |  |  | 78.76% | 76.24% |  |  | 1.0334 |
| Average | 0.2618 | 1.4947 | 0.2485 | 1.4190 | 0.1728 | 0.9870 | 78.76% | 76.00% | 80.66% | 0.8831 | 1.0540 |
| Std. Dev. | 0.0169 | 0.0964 | 0.0168 | 0.0962 | 0.0086 | 0.0490 | 0.80% | 1.14% | 1.17% | 0.0095 | 0.0296 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E1 dowel bar configuration under nominal load of 44 kN (10 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 10 | 44 | 0.2529 | 1.4440 | 0.2555 | 1.4591 | 0.1883 | 1.0751 | 87.90% | 86.06% | 81.44% | 0.9149 | 0.9897 |
| 10 | 44 | 0.2008 | 1.1467 | 0.2132 | 1.2173 | 0.1891 | 1.0800 | 91.88% | 86.73% | 95.82% | 0.9355 | 0.9420 |
| 10 | 44 |  |  |  |  | 0.1923 | 1.0983 |  |  | 83.46% | 0.9110 |  |
| 10 | 44 |  |  |  |  | 0.1851 | 1.0572 |  |  | 91.72% | 0.9076 |  |
| 10 | 44 |  |  |  |  | 0.1869 | 1.0673 |  |  | 90.88% | 0.9081 |  |
| 10 | 44 |  |  |  |  | 0.1704 | 0.9729 |  |  | 78.29% | 0.8935 |  |
| 10 | 44 |  |  |  |  | 0.1700 | 0.9706 |  |  | 83.02% | 0.8817 |  |
| Average | 0.2268 | 1.2953 | 0.2343 | 1.3382 | 0.1832 | 1.0459 | 89.89% | 86.39% | 86.37% | 0.9075 | 0.9658 |
| Std. Dev. | 0.0368 | 0.2102 | 0.0299 | 0.1710 | 0.0091 | 0.0522 | 2.81% | 0.48% | 6.42% | 0.0169 | 0.0337 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E1 dowel bar configuration under nominal load of 58 kN (13 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 13 | 58 | 0.2572 | 1.4689 | 0.2578 | 1.4722 | 0.1950 | 1.1135 | 88.89% | 86.18% | 79.75% | 0.9027 | 0.9977 |
| 13 | 58 | 0.2044 | 1.1670 | 0.2139 | 1.2214 | 0.1880 | 1.0735 | 91.76% | 89.05% | 94.87% | 0.9474 | 0.9555 |
| 13 | 58 |  |  |  |  | 0.2002 | 1.1430 |  |  | 83.22% | 0.9163 |  |
| 13 | 58 |  |  |  |  | 0.1867 | 1.0661 |  |  | 88.78% | 0.9184 |  |
| 13 | 58 |  |  |  |  | 0.1881 | 1.0743 |  |  | 88.89% | 0.9190 |  |
| 13 | 58 |  |  |  |  | 0.1692 | 0.9659 |  |  | 78.75% | 0.9058 |  |
| 13 | 58 |  |  |  |  | 0.1692 | 0.9662 |  |  | 81.71% | 0.9013 |  |
| Average | 0.2308 | 1.3180 | 0.2359 | 1.3468 | 0.1852 | 1.0575 | 90.32% | 87.61% | 85.14% | 0.9159 | 0.9766 |
| Std. Dev. | 0.0374 | 0.2134 | 0.0311 | 0.1774 | 0.0119 | 0.0680 | 2.03% | 2.03% | 5.88% | 0.0158 | 0.0298 |

FWD data for I-490 East, Monroe, Rochester on June 21, 2011 with E1 dowel bar configuration under nominal load of 80 kN (18 kip)

| Load | DO L | DO A | DO M | LTE L | LTE A | SPR | D3/D0 M | JSR |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| (kip) | (kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) | (mil/kip) | (µm/kN) |  |  |  |  |  |
| 18 | 80 | 0.2459 | 1.4038 | 0.2456 | 1.4023 | 0.1878 | 1.0724 | 87.19% | 86.14% | 79.68% | 0.1878 | 1.0011 |
| 18 | 80 | 0.1942 | 1.1088 | 0.2081 | 1.1885 | 0.1835 | 1.0476 | 92.13% | 87.19% | 94.68% | 0.1835 | 0.9329 |
| 18 | 80 |  |  |  |  | 0.1951 | 1.1139 |  |  | 83.62% | 0.1951 |  |
| 18 | 80 |  |  |  |  | 0.1821 | 1.0398 |  |  | 87.92% | 0.1821 |  |
| 18 | 80 |  |  |  |  | 0.1820 | 1.0391 |  |  | 87.90% | 0.1820 |  |
| 18 | 80 |  |  |  |  | 0.1695 | 0.9679 |  |  | 78.02% | 0.1695 |  |
| 18 | 80 |  |  |  |  | 0.1700 | 0.9709 |  |  | 81.82% | 0.1700 |  |
| Average | 0.2200 | 1.2563 | 0.2269 | 1.2954 | 0.1814 | 1.0359 | 89.66% | 86.67% | 84.81% | 0.1814 | 0.9670 |
| Std. Dev. | 0.0365 | 0.2086 | 0.0265 | 0.1511 | 0.0092 | 0.0523 | 3.50% | 0.74% | 5.76% | 0.0092 | 0.0482 |

Appendix H: Supplemental falling weight testing data from I86 Hinsdale

Summarized FWD Test Data Averages (1 μm/kN = 0.175 mil/kip).

| Date | Drop 1 | Drop 2 | Drop 3 |
| --- | --- | --- | --- |
|  | NDf-0 | LTE | JSR | MidSlab SPR | NDf-0 | LTE | JSR | MidSlab SPR | NDf-0 | LTE | JSR | MidSlab SPR |
|  | (μm/kN) | (%) |  |  | (μm/kN) |  |  |  | (μm/kN) |  |  |  |
|  | Approach | Leave | MidSlab | Approach | Leave |  | (%) | Approach | Leave | MidSlab | Approach | Leave |  | (%) | Approach | Leave | MidSlab | Approach | Leave |  | (%) |
| Section 1: Crack & Seated |
| Jun-2006 | 1.631 | 1.769 |  | 80.0 | 79.9 | 1.076 |  | 1.663 | 1.779 |  | 86.3 | 81.2 | 1.069 |  | 1.671 | 1.772 |  | 84.3 | 82.0 | 1.054 |  |
| Nov-2006 | 1.493 | 1.545 | 1.363 | 78.1 | 74.3 | 1.038 | 62.3 | 1.402 | 1.458 | 1.147 | 87.6 | 82.8 | 1.050 | 75.6 | 1.518 | 1.613 | 1.348 | 84.5 | 78.3 | 1.066 | 66.9 |
| Mar-2007 | 2.113 | 2.195 | 4.623 | 76.8 | 72.9 | 1.043 | 74.1 | 2.174 | 2.250 | 4.720 | 77.4 | 73.8 | 1.040 | 74.2 | 2.219 | 2.291 | 4.768 | 77.9 | 74.4 | 1.038 | 74.4 |
| Oct-2007 | 1.494 | 1.545 | 3.097 | 76.6 | 72.3 | 1.034 | 69.4 | 1.556 | 1.601 | 3.114 | 76.8 | 73.8 | 1.030 | 69.8 | 1.607 | 1.648 | 3.120 | 77.0 | 74.3 | 1.027 | 69.9 |
| May-2008 (1) | 1.609 | 1.683 | 3.805 | 87.9 | 84.7 | 1.027 | 70.0 | 1.750 | 1.808 | 3.785 | 87.0 | 84.4 | 1.028 | 70.1 | 1.709 | 1.764 | 3.622 | 86.2 | 84.8 | 1.019 | 70.5 |
| May-2008 (2) | 1.609 | 1.683 |  | 67.9 | 67.3 | 1.031 |  | 1.657 | 1.741 |  | 67.1 | 68.4 | 1.064 |  | 1.662 | 1.726 |  | 69.0 | 71.2 | 1.048 |  |
| Oct-2008 | 2.146 | 2.277 | 1.156 | 65.7 | 66.2 | 1.065 | 70.8 | 2.163 | 2.281 | 1.188 | 67.0 | 68.1 | 1.060 | 70.5 | 2.128 | 2.231 | 1.213 | 68.4 | 70.5 | 1.051 | 70.5 |
| May-2009 | 1.750 | 1.797 | 3.394 | 72.4 | 72.2 | 1.023 | 62.0 | 1.773 | 1.824 | 3.387 | 74.5 | 73.2 | 1.025 | 62.2 | 1.760 | 1.803 | 3.294 | 75.3 | 74.5 | 1.017 | 62.4 |
| Section 2: Rubblized |
| Jun-2006 | 2.090 | 2.220 | - | 85.1 | 84.7 | 1.056 | - | 2.151 | 2.234 | - | 84.8 | 86.6 | 1.023 | - | 2.148 | 2.244 | - | 84.7 | 87.1 | 1.038 | - |
| Nov-2006 | 1.571 | 1.635 | 1.595 | 76.6 | 72.3 | 1.041 | 62.8 | 1.632 | 1.687 | 1.606 | 77.3 | 73.8 | 1.036 | 63.3 | 1.703 | 1.756 | 1.637 | 78.7 | 74.6 | 1.036 | 63.7 |
| Mar-2007 | 2.270 | 2.279 | 2.918 | 74.6 | 73.3 | 1.012 | 70.3 | 2.315 | 2.302 | 2.968 | 75.3 | 74.2 | 1.005 | 70.5 | 2.340 | 2.309 | 2.979 | 75.8 | 74.7 | 0.999 | 70.7 |
| Oct-2007 | 1.604 | 1.626 | 2.403 | 65.5 | 64.2 | 1.014 | 66.5 | 1.673 | 1.686 | 2.400 | 67.1 | 62.8 | 1.011 | 66.8 | 1.731 | 1.737 | 2.412 | 68.5 | 64.7 | 1.012 | 66.9 |
| May-2008 (1) | 1.831 | 1.873 | 3.482 | 77.9 | 78.0 | 1.017 | 68.0 | 1.863 | 1.896 | 3.481 | 79.8 | 79.3 | 1.012 | 68.8 | 1.808 | 1.849 | 3.361 | 80.4 | 80.4 | 1.001 | 68.5 |
| May-2008 (2) | 1.917 | 1.946 | - | 61.4 | 67.9 | 1.020 | - | 1.937 | 1.968 | - | 64.1 | 71.1 | 1.020 | - | 1.904 | 1.927 | - | 66.7 | 73.4 | 1.014 | - |
| Oct-2008 | 2.023 | 2.114 | 1.075 | 65.5 | 65.8 | 1.049 | 64.1 | 2.042 | 2.120 | 1.109 | 66.8 | 67.5 | 1.043 | 64.9 | 2.009 | 2.079 | 1.117 | 68.8 | 69.4 | 1.039 | 65.5 |
| May-2009 | 1.972 | 1.990 | 3.853 | 65.9 | 65.7 | 1.001 | 62.7 | 1.991 | 2.012 | 3.868 | 66.3 | 67.5 | 1.005 | 62.3 | 1.974 | 1.981 | 3.768 | 68.4 | 69.7 | 0.996 | 63.3 |
| Section 3: Untreated |
| Jun-2006 | 0.876 | 0.920 | - | 73.4 | 81.1 | 1.032 | - | 0.883 | 0.932 | - | 96.2 | 82.3 | 1.045 | - | 0.886 | 0.918 | - | 101.2 | 84.7 | 1.021 | - |
| Nov-2006 | 1.226 | 1.215 | 1.027 | 74.6 | 73.3 | 0.995 | 64.4 | 1.275 | 1.261 | 1.071 | 75.1 | 73.8 | 0.995 | 64.4 | 1.306 | 1.297 | 1.106 | 76.6 | 77.1 | 0.995 | 64.9 |
| Mar-2007 | 1.335 | 1.360 | 2.600 | 73.4 | 69.8 | 1.029 | 66.9 | 1.366 | 1.387 | 2.545 | 74.5 | 71.2 | 1.026 | 67.2 | 1.389 | 1.415 | 2.566 | 75.1 | 71.8 | 1.026 | 67.4 |
| Oct-2007 | 1.942 | 1.809 | 1.021 | 57.7 | 63.1 | 0.939 | 68.0 | 1.969 | 1.828 | 1.080 | 59.6 | 63.8 | 0.936 | 67.8 | 1.962 | 1.833 | 1.109 | 60.5 | 63.8 | 0.938 | 68.0 |
| May-2008 (1) | 1.325 | 1.362 | 2.652 | 71.2 | 70.4 | 1.028 | 63.0 | 1.345 | 1.379 | 2.616 | 72.3 | 71.5 | 1.024 | 63.3 | 1.335 | 1.363 | 2.503 | 73.3 | 73.1 | 1.017 | 63.6 |
| May-2008 (2) | 1.446 | 1.406 | - | 67.1 | 76.3 | 0.986 | - | 1.469 | 1.402 | - | 67.9 | 78.5 | 0.972 | - | 1.457 | 1.395 | - | 70.2 | 79.7 | 0.973 | - |
| Oct-2008 | 2.065 | 2.146 | 0.940 | 64.4 | 64.6 | 1.051 | 71.8 | 2.050 | 2.139 | 0.973 | 66.2 | 66.3 | 1.053 | 71.1 | 1.990 | 2.080 | 0.980 | 68.0 | 68.6 | 1.050 | 71.8 |
| May-2009 | 1.307 | 1.332 | 2.439 | 68.6 | 67.5 | 1.031 | 61.2 | 1.326 | 1.361 | 2.417 | 69.8 | 68.2 | 1.039 | 61.0 | 1.331 | 1.360 | 2.297 | 70.2 | 69.9 | 1.027 | 61.7 |

FWD Test Data (20-June-2006) (1 μm/kN = 0.175 mil/kip).

| 20-June-2006 |
| --- |
| Joint | NDf-0 | LTE | JSR |
|  | (mils/kip) | (%) |  |
|  | Approach | Leave | Approach | Leave |  |
| N | Type | Drop 1 | Drop 2 | Drop 3 | Drop 1 | Drop 2 | Drop 3 | Drop 1 | Drop 2 | Drop 3 | Drop 1 | Drop 2 | Drop 3 | Drop 1 | Drop 2 | Drop 3 |
| Section 3: Untreated |
| 1 | RJ | 0.147 | 0.147 | 0.150 | 0.156 | 0.163 | 0.157 | 52.5 | 102.3 | 107.0 | 88.8 | 86.3 | 89.3 | 1.019 | 1.090 | 1.023 |
| 2 | RJ | 0.157 | 0.154 | 0.150 | 0.149 | 0.148 | 0.148 | 73.0 | 84.6 | 85.9 | 83.8 | 87.6 | 89.7 | 0.945 | 0.952 | 0.983 |
| 3 | RJ | 0.167 | 0.172 | 0.176 | 0.184 | 0.190 | 0.196 | 72.6 | 81.2 | 81.3 | 71.3 | 72.1 | 70.9 | 1.074 | 1.088 | 1.090 |
| 4 | RJ | 0.142 | 0.146 | 0.144 | 0.149 | 0.149 | 0.147 | 88.2 | 99.5 | 113.1 | 81.8 | 84.4 | 85.7 | 1.028 | 1.024 | 1.018 |
| 5 | RJ | 0.153 | 0.154 | 0.155 | 0.167 | 0.166 | 0.156 | 80.5 | 113.3 | 118.5 | 79.8 | 81.3 | 88.0 | 1.094 | 1.071 | 0.990 |
| 6 | SJ | 0.201 | 0.207 | 0.207 | 0.198 | 0.194 | 0.190 | 119.9 | 87.3 | 107.8 | 80.0 | 71.2 | 73.0 | 0.941 | 0.907 | 0.914 |
| 7 | SJ | 0.175 | 0.180 | 0.172 | 0.172 | 0.179 | 0.175 | 82.6 | 91.3 | 88.5 | 83.3 | 80.6 | 83.1 | 1.006 | 1.025 | 1.054 |
| 8 | SJ | 0.155 | 0.144 | 0.151 | 0.144 | 0.146 | 0.146 | 108.3 | 75.0 | 110.1 | 84.4 | 82.2 | 81.5 | 0.987 | 1.033 | 1.000 |
| 9 | SJ | 0.156 | 0.204 | 0.203 | 0.191 | 0.204 | 0.203 | 88.3 | 115.9 | 111.8 | 83.5 | 85.3 | 82.4 | 0.903 | 1.018 | 1.034 |
| 10 | SJ | 0.201 | 0.203 | 0.203 | 0.189 | 0.193 | 0.196 | 90.9 | 84.3 | 86.3 | 84.0 | 84.5 | 83.0 | 0.988 | 0.983 | 1.352 |
| Section 2: Rubblized |
| 1 | SJ | 0.413 | 0.418 | 0.411 | 0.420 | 0.437 | 0.422 | 94.1 | 89.8 | 94.7 | 90.4 | 87.3 | 88.5 | 0.995 | 1.031 | 1.038 |
| 2 | SJ | 0.481 | 0.479 | 0.475 | 0.531 | 0.534 | 0.521 | 87.9 | 85.0 | 90.0 | 93.1 | 94.5 | 94.4 | 1.116 | 1.099 | 1.084 |
| 3 | SJ | 0.444 | 0.446 | 0.442 | 0.459 | 0.461 | 0.451 | 98.3 | 106.9 | 105.8 | 88.5 | 88.9 | 90.6 | 1.020 | 1.020 | 1.023 |
| 4 | SJ | 0.406 | 0.425 | 0.418 | 0.452 | 0.468 | 0.453 | 89.5 | 92.0 | 94.3 | 93.3 | 93.3 | 93.0 | 1.084 | 1.082 | 1.088 |
| 5 | SJ | 0.380 | 0.391 | 0.382 | 0.399 | 0.410 | 0.406 | 90.7 | 89.0 | 89.5 | 85.2 | 85.0 | 85.6 | 1.044 | 1.038 | 1.076 |
| 6 | RJ | 0.400 | 0.404 | 0.413 | 0.417 | 0.428 | 0.422 | 81.6 | 83.8 | 78.6 | 76.8 | 80.0 | 81.5 | 1.005 | 1.055 | 1.012 |
| 7 | RJ | 0.347 | 0.369 | 0.364 | 0.366 | 0.366 | 0.377 | 90.3 | 87.8 | 93.2 | 90.1 | 91.3 | 90.2 | 1.071 | 0.986 | 1.027 |
| 8 | RJ | 0.367 | 0.379 | 0.373 | 0.434 | 0.400 | 0.398 | 81.3 | 78.4 | 81.4 | 74.0 | 80.7 | 82.5 | 1.172 | 1.015 | 1.057 |
| 9 | RJ | 0.341 | 0.354 | 0.353 | 0.359 | 0.371 | 0.379 | 85.7 | 84.4 | 82.3 | 88.9 | 89.2 | 87.4 | 1.052 | 1.050 | 1.060 |
| 10 | RJ | 0.375 | 0.377 | 0.378 | 0.369 | 0.391 | 0.389 | 86.7 | 89.7 | 88.0 | 94.0 | 91.8 | 93.9 | 0.979 | 1.011 | 1.033 |
| Section 1: Crack & Seated |
| 1 | RJ | 0.281 | 0.297 | 0.298 | 0.302 | 0.306 | 0.306 | 90.2 | 83.5 | 86.8 | 90.0 | 91.0 | 92.0 | 1.063 | 1.022 | 1.023 |
| 2 | RJ | 0.292 | 0.274 | 0.279 | 0.310 | 0.320 | 0.313 | 94.3 | 97.3 | 88.4 | 72.7 | 73.7 | 75.2 | 1.053 | 1.164 | 1.118 |
| 3 | RJ | 0.279 | 0.287 | 0.285 | 0.317 | 0.302 | 0.308 | 71.7 | 87.5 | 83.9 | 77.4 | 83.7 | 83.3 | 1.114 | 1.049 | 1.072 |
| 4 | RJ | 0.282 | 0.278 | 0.289 | 0.295 | 0.291 | 0.291 | 80.2 | 87.6 | 83.2 | 86.4 | 86.2 | 86.9 | 1.052 | 1.055 | 1.015 |
| 5 | RJ | 0.346 | 0.353 | 0.358 | 0.380 | 0.385 | 0.387 | 58.9 | 78.4 | 77.1 | 72.2 | 74.2 | 76.2 | 1.094 | 1.086 | 1.052 |
| 6 | SJ | 0.273 | 0.277 | 0.274 | 0.261 | 0.271 | 0.265 | 83.9 | 85.5 | 86.8 | 84.6 | 85.8 | 86.2 | 0.944 | 0.961 | 0.968 |
| 7 | SJ | 0.268 | 0.267 | 0.263 | 0.270 | 0.274 | 0.275 | 70.9 | 85.1 | 92.9 | 85.7 | 86.7 | 86.0 | 1.000 | 1.028 | 1.038 |
| 8 | SJ | 0.334 | 0.337 | 0.337 | 0.365 | 0.379 | 0.376 | 75.7 | 72.3 | 72.2 | 73.7 | 73.3 | 74.0 | 1.090 | 1.119 | 1.119 |
| 9 | RJ | 0.272 | 0.282 | 0.276 | 0.280 | 0.290 | 0.284 | 76.3 | 86.7 | 88.2 | 81.6 | 79.5 | 80.5 | 1.020 | 1.024 | 1.041 |
| 10 | RJ | 0.248 | 0.268 | 0.265 | 0.284 | 0.288 | 0.283 | 88.8 | 83.2 | 82.5 | 79.1 | 80.1 | 79.9 | 1.139 | 1.081 | 1.057 |

FWD Test Data (C&S Section, 28-Novemeber-2006) (1 μm/kN = 0.175 mil/kip).

| Section 1: Cracked & Seated |
| --- |
| 28-November-2006 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.263 | 0.298 | 0.296 | 0.301 | 0.261 | 0.308 | 0.232 | 0.192 | 0.221 | 91.4 | 83.4 | 85.9 | 80.4 | 92.5 | 78.9 | 1.141 | 0.876 | 1.045 | 66.2 | 81.4 | 73.3 |
| 2 | RJ | 0.299 | 0.276 | 0.293 | 0.301 | 0.292 | 0.307 | 0.244 | 0.176 | 0.225 | 76.4 | 85.9 | 82.1 | 75.6 | 80.4 | 77.6 | 1.010 | 1.057 | 1.039 | 63.0 | 86.3 | 70.0 |
| 3 | RJ | 0.269 | 0.246 | 0.266 | 0.288 | 0.288 | 0.304 | 0.227 | 0.211 | 0.230 | 86.4 | 97.4 | 92.0 | 78.9 | 80.7 | 78.3 | 1.070 | 1.175 | 1.149 | 65.6 | 72.2 | 68.8 |
| 4 | RJ | 0.284 | 0.249 | 0.292 | 0.303 | 0.251 | 0.289 | 0.228 | 0.174 | 0.227 | 82.0 | 96.2 | 84.3 | 72.9 | 91.8 | 81.5 | 1.070 | 1.006 | 0.996 | 61.5 | 80.4 | 64.9 |
| 5 | RJ | 0.294 | 0.251 | 0.299 | 0.301 | 0.287 | 0.307 | 0.223 | 0.189 | 0.222 | 70.8 | 85.6 | 74.3 | 67.9 | 73.8 | 71.0 | 1.021 | 1.138 | 1.024 | 61.7 | 73.1 | 65.6 |
| 6 | RJ | 0.239 | 0.210 | 0.251 | 0.269 | 0.253 | 0.275 | 0.192 | 0.192 | 0.203 | 84.6 | 98.9 | 85.3 | 72.0 | 80.2 | 75.9 | 1.127 | 1.204 | 1.097 | 67.6 | 70.1 | 69.4 |
| 7 | RJ | 0.261 | 0.254 | 0.274 | 0.278 | 0.268 | 0.280 | 0.214 | 0.190 | 0.224 | 79.7 | 84.6 | 81.6 | 73.1 | 78.0 | 77.8 | 1.052 | 1.052 | 1.024 | 61.8 | 70.3 | 63.6 |
| 8 | RJ | 0.266 | 0.297 | 0.292 | 0.324 | 0.316 | 0.353 | 0.249 | 0.232 | 0.267 | 86.9 | 80.7 | 85.7 | 68.0 | 73.1 | 68.0 | 1.226 | 1.061 | 1.215 | 64.3 | 69.9 | 64.4 |
| 9 | RJ | 0.294 | 0.308 | 0.331 | 0.344 | 0.329 | 0.369 | 0.273 | 0.250 | 0.279 | 82.9 | 83.1 | 81.2 | 69.4 | 76.5 | 70.8 | 1.168 | 1.069 | 1.121 | 63.5 | 70.1 | 65.7 |
| 10 | RJ | 0.316 | 0.308 | 0.335 | 0.306 | 0.315 | 0.335 | 0.249 | 0.206 | 0.275 | 80.7 | 85.7 | 82.0 | 82.0 | 82.5 | 79.8 | 0.963 | 1.023 | 1.005 | 64.6 | 77.4 | 63.0 |
| 11 | RJ | 0.298 | 0.256 | 0.311 | 0.236 | 0.277 | 0.316 | 0.239 | 0.174 | 0.269 | 79.6 | 97.5 | 83.9 | 97.3 | 86.6 | 79.8 | 0.789 | 1.087 | 1.014 | 60.3 | 82.1 | 60.1 |
| 12 | RJ | 0.253 | 0.293 | 0.301 | 0.284 | 0.324 | 0.331 | 0.240 | 0.180 | 0.246 | 73.6 | 66.7 | 68.5 | 67.8 | 63.8 | 66.2 | 1.130 | 1.108 | 1.106 | 57.7 | 76.3 | 61.5 |
| 13 | RJ | 0.292 | 0.240 | 0.294 | 0.283 | 0.232 | 0.316 | 0.202 | 0.187 | 0.235 | 75.6 | 95.1 | 81.6 | 77.4 | 98.3 | 74.9 | 0.967 | 0.964 | 1.071 | 66.4 | 73.9 | 63.2 |
| 14 | RJ | 0.260 | 0.213 | 0.286 | 0.255 | 0.266 | 0.258 | 0.210 | 0.184 | 0.237 | 76.8 | 98.5 | 77.8 | 75.1 | 78.0 | 83.8 | 0.980 | 1.244 | 0.904 | 65.8 | 76.2 | 64.2 |
| 15 | RJ | 0.280 | 0.225 | 0.261 | 0.278 | 0.280 | 0.289 | 0.225 | 0.190 | 0.202 | 73.6 | 95.4 | 87.0 | 72.5 | 75.9 | 77.7 | 0.989 | 1.244 | 1.104 | 61.0 | 73.1 | 71.6 |
| 16 | RJ | 0.230 | 0.259 | 0.261 | 0.237 | 0.241 | 0.256 | 0.238 | 0.182 | 0.231 | 87.6 | 81.4 | 84.7 | 83.5 | 85.0 | 84.7 | 1.032 | 0.933 | 0.984 | 59.5 | 77.4 | 65.5 |
| 17 | RJ | 0.302 | 0.216 | 0.278 | 0.263 | 0.271 | 0.310 | 0.287 | 0.108 | 0.280 | 59.6 | 89.7 | 75.7 | 68.3 | 70.6 | 67.1 | 0.874 | 1.250 | 1.107 | 53.2 | 129.7 | 59.4 |
| 18 | RJ | 0.216 | 0.234 | 0.257 | 0.212 | 0.280 | 0.281 | 0.179 | 0.161 | 0.194 | 95.1 | 89.8 | 89.2 | 94.0 | 75.4 | 79.4 | 0.980 | 1.197 | 1.094 | 68.0 | 76.9 | 68.6 |
| 19 | RJ | 0.248 | 0.215 | 0.247 | 0.238 | 0.239 | 0.267 | 0.194 | 0.174 | 0.202 | 77.8 | 94.8 | 87.4 | 79.0 | 82.8 | 78.2 | 0.957 | 1.118 | 1.090 | 64.2 | 72.9 | 66.9 |
| 20 | RJ | 0.262 | 0.247 | 0.275 | 0.247 | 0.294 | 0.299 | 0.219 | 0.188 | 0.221 | 78.6 | 87.3 | 82.5 | 83.6 | 74.1 | 75.7 | 0.935 | 1.191 | 1.093 | 65.0 | 76.1 | 68.2 |
| 21 | RJ | 0.297 | 0.237 | 0.254 | 0.303 | 0.249 | 0.282 | 0.226 | 0.192 | 0.209 | 69.4 | 91.0 | 89.1 | 65.3 | 85.4 | 78.8 | 1.025 | 1.047 | 1.107 | 63.3 | 75.1 | 72.0 |
| 22 | RJ | 0.248 | 0.218 | 0.260 | 0.244 | 0.212 | 0.276 | 0.236 | 0.217 | 0.233 | 82.0 | 98.6 | 86.7 | 83.0 | 99.6 | 80.6 | 0.987 | 0.971 | 1.064 | 61.4 | 67.9 | 65.6 |
| 23 | RJ | 0.249 | 0.235 | 0.270 | 0.267 | 0.241 | 0.250 | 0.204 | 0.194 | 0.197 | 76.8 | 86.5 | 79.5 | 71.9 | 84.0 | 86.5 | 1.069 | 1.034 | 0.927 | 65.0 | 70.6 | 72.5 |
| 24 | RJ | 0.270 | 0.243 | 0.250 | 0.288 | 0.218 | 0.252 | 0.238 | 0.160 | 0.238 | 76.0 | 89.8 | 91.5 | 69.4 | 98.9 | 88.7 | 1.067 | 0.898 | 1.007 | 61.7 | 89.3 | 65.8 |
| 25 | RJ | 0.235 | 0.232 | 0.238 | 0.282 | 0.239 | 0.266 | 0.219 | 0.251 | 0.226 | 89.6 | 94.9 | 97.0 | 73.4 | 90.1 | 84.9 | 1.203 | 1.031 | 1.121 | 70.8 | 64.4 | 72.0 |
| 26 | RJ | 0.257 | 0.222 | 0.237 | 0.244 | 0.253 | 0.260 | 0.228 | 0.198 | 0.193 | 74.4 | 90.7 | 89.2 | 77.0 | 78.1 | 80.3 | 0.950 | 1.143 | 1.101 | 62.3 | 71.9 | 75.4 |
| 27 | RJ | 0.209 | 0.181 | 0.205 | 0.254 | 0.219 | 0.211 | 0.233 | 0.124 | 0.242 | 91.4 | 110.9 | 102.3 | 74.1 | 88.8 | 97.2 | 1.207 | 1.210 | 1.023 | 57.1 | 101.7 | 60.7 |
| 28 | RJ | 0.270 | 0.232 | 0.261 | 0.306 | 0.229 | 0.287 | 0.285 | 0.261 | 0.230 | 75.0 | 92.5 | 87.8 | 65.6 | 94.8 | 80.0 | 1.125 | 0.983 | 1.097 | 54.4 | 60.7 | 69.8 |
| 29 | RJ | 0.239 | 0.269 | 0.272 | 0.245 | 0.255 | 0.271 |  |  |  | 77.0 | 73.4 | 76.8 | 75.1 | 77.0 | 75.6 | 1.032 | 0.946 | 0.998 |  |  |  |
| 30 | SJ | 0.288 | 0.220 | 0.258 | 0.275 | 0.219 | 0.253 | 0.249 | 0.202 | 0.210 | 71.6 | 97.8 | 87.0 | 72.8 | 95.6 | 85.6 | 0.959 | 0.996 | 0.988 | 61.0 | 74.0 | 73.3 |
| 31 | SJ | 0.263 | 0.223 | 0.263 | 0.292 | 0.221 | 0.223 | 0.227 | 0.198 | 0.213 | 74.6 | 92.5 | 82.6 | 64.9 | 90.6 | 94.1 | 1.113 | 0.989 | 0.851 | 61.2 | 73.3 | 71.1 |
| 32 | SJ | 0.308 | 0.250 | 0.290 | 0.295 | 0.235 | 0.287 | 0.205 | 0.229 | 0.237 | 68.4 | 88.3 | 80.2 | 69.8 | 91.6 | 79.7 | 0.966 | 0.943 | 0.985 | 69.0 | 64.1 | 64.7 |
| 33 | SJ | 0.260 | 0.249 | 0.288 | 0.284 | 0.231 | 0.245 | 0.255 | 0.229 | 0.252 | 77.6 | 85.1 | 77.4 | 67.9 | 86.5 | 88.5 | 1.094 | 0.935 | 0.851 | 58.5 | 65.8 | 63.0 |
| 34 | RJ | 0.265 | 0.217 | 0.227 | 0.231 | 0.250 | 0.249 | 0.230 | 0.185 | 0.211 | 58.8 | 76.8 | 78.8 | 65.8 | 64.1 | 69.7 | 0.876 | 1.158 | 1.107 | 56.8 | 69.6 | 64.6 |
| 35 | RJ | 0.294 | 0.258 | 0.254 | 0.316 | 0.270 | 0.286 | 0.185 | 0.116 | 0.168 | 66.4 | 78.6 | 83.0 | 61.1 | 74.3 | 72.9 | 1.076 | 1.046 | 1.116 | 55.4 | 85.8 | 66.2 |
| 36 | RJ | 0.252 | 0.216 | 0.215 | 0.285 | 0.246 | 0.268 |  |  |  | 74.5 | 89.8 | 95.5 | 69.5 | 82.6 | 79.5 | 1.126 | 1.135 | 1.248 |  |  |  |
| 37 | RJ | 0.231 | 0.194 | 0.211 | 0.235 | 0.187 | 0.221 | 0.306 | 0.247 | 0.265 | 73.6 | 90.7 | 87.6 | 71.3 | 93.7 | 83.2 | 1.014 | 0.967 | 1.042 | 56.2 | 67.9 | 65.6 |
| 38 | RJ | 0.252 | 0.224 | 0.244 | 0.233 | 0.227 | 0.257 | 0.213 | 0.226 | 0.211 | 69.5 | 82.8 | 80.5 | 75.0 | 79.6 | 74.5 | 0.921 | 1.014 | 1.051 | 69.3 | 66.9 | 74.1 |
| 39 | RJ | 0.262 | 0.197 | 0.247 | 0.234 | 0.206 | 0.246 | 0.266 | 0.211 | 0.265 | 73.0 | 101.2 | 84.8 | 78.7 | 93.5 | 82.1 | 0.891 | 1.044 | 1.002 | 60.2 | 75.7 | 65.3 |
| 40 | RJ | 0.212 | 0.216 | 0.209 | 0.220 | 0.181 | 0.231 | 0.284 | 0.216 | 0.225 | 76.6 | 80.7 | 88.5 | 74.2 | 94.3 | 78.8 | 1.040 | 0.839 | 1.109 | 59.3 | 78.1 | 77.3 |
| 41 | RJ | 0.271 | 0.224 | 0.271 | 0.250 | 0.265 | 0.254 | 0.251 | 0.180 | 0.250 | 72.3 | 91.5 | 79.3 | 77.5 | 76.1 | 82.7 | 0.922 | 1.184 | 0.940 | 61.6 | 83.9 | 65.3 |
| 42 | RJ | 0.259 | 0.242 | 0.250 | 0.257 | 0.223 | 0.250 | 0.249 | 0.217 | 0.249 | 74.8 | 84.0 | 86.2 | 73.8 | 88.7 | 84.6 | 0.992 | 0.925 | 1.005 | 60.9 | 69.8 | 64.3 |
| 43 | RJ | 0.249 | 0.244 | 0.263 | 0.302 | 0.244 | 0.315 | 0.233 | 0.257 | 0.283 | 83.0 | 88.0 | 87.6 | 68.3 | 89.6 | 73.8 | 1.221 | 0.994 | 1.196 | 68.7 | 65.8 | 63.0 |
| 44 | RJ | 0.260 | 0.236 | 0.258 | 0.322 | 0.265 | 0.261 | 0.281 | 0.243 | 0.255 | 78.9 | 91.6 | 90.0 | 63.6 | 81.3 | 88.9 | 1.240 | 1.114 | 1.000 | 59.7 | 69.6 | 69.9 |
| 45 | RJ | 0.212 | 0.408 | 0.288 | 0.264 | 0.266 | 0.306 | 0.297 | 0.279 | 0.301 | 97.0 | 53.6 | 81.2 | 74.7 | 80.2 | 74.4 | 1.245 | 0.658 | 1.062 | 64.1 | 68.8 | 66.6 |
| 46 | RJ | 0.328 | 0.297 | 0.322 | 0.305 | 0.279 | 0.306 | 0.260 | 0.247 | 0.260 | 63.0 | 72.3 | 71.7 | 66.6 | 76.7 | 75.2 | 0.923 | 0.936 | 0.946 | 63.4 | 66.3 | 65.2 |
| 47 | RJ | 0.237 | 0.229 | 0.239 | 0.251 | 0.251 | 0.251 | 0.300 | 0.270 | 0.277 | 80.8 | 87.2 | 88.6 | 75.1 | 80.4 | 85.1 | 1.058 | 1.093 | 1.048 | 59.6 | 65.2 | 64.8 |
| 48 | RJ | 0.220 | 0.239 | 0.249 | 0.219 | 0.198 | 0.322 |  |  |  | 82.1 | 78.7 | 80.5 | 80.2 | 93.2 | 60.3 | 1.000 | 0.833 | 1.307 |  |  |  |

FWD Test Data (Rubblized Section, 28-Novemeber-2006) (1 μm/kN = 0.175 mil/kip).

| Section 2: Rubblized |
| --- |
| 28-November-2006 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.267 | 0.276 | 0.292 | 0.275 | 0.288 | 0.304 | 0.312 | 0.311 | 0.316 | 76.9 | 78.2 | 79.1 | 72.6 | 73.4 | 74.3 | 1.031 | 1.046 | 1.037 | 65.5 | 65.7 | 65.8 |
| 2 | RJ | 0.294 | 0.307 | 0.323 | 0.306 | 0.320 | 0.332 | 0.320 | 0.319 | 0.322 | 81.9 | 82.5 | 83.5 | 77.7 | 79.0 | 79.1 | 1.035 | 1.041 | 1.040 | 62.4 | 62.9 | 63.8 |
| 3 | RJ | 0.316 | 0.331 | 0.348 | 0.324 | 0.335 | 0.346 | 0.285 | 0.285 | 0.291 | 67.3 | 66.9 | 69.0 | 69.3 | 72.0 | 73.2 | 1.020 | 1.012 | 0.995 | 62.0 | 62.9 | 63.4 |
| 4 | SJ | 0.303 | 0.313 | 0.325 | 0.307 | 0.317 | 0.328 | 0.314 | 0.317 | 0.319 | 81.2 | 81.7 | 82.7 | 76.6 | 78.0 | 78.7 | 1.014 | 1.015 | 1.011 | 62.7 | 63.1 | 63.7 |
| 5 | SJ | 0.290 | 0.301 | 0.314 | 0.283 | 0.294 | 0.306 | 0.284 | 0.288 | 0.297 | 76.4 | 77.8 | 79.0 | 75.6 | 76.7 | 78.4 | 0.982 | 0.977 | 0.964 | 64.9 | 65.4 | 65.6 |
| 6 | SJ | 0.306 | 0.313 | 0.328 | 0.301 | 0.314 | 0.328 | 0.233 | 0.239 | 0.248 | 74.3 | 76.5 | 76.9 | 72.6 | 73.5 | 75.0 | 0.976 | 0.995 | 0.998 | 62.2 | 63.0 | 63.4 |
| 7 | SJ | 0.267 | 0.281 | 0.291 | 0.288 | 0.297 | 0.312 | 0.242 | 0.247 | 0.258 | 82.1 | 79.9 | 81.9 | 72.3 | 74.5 | 75.7 | 1.075 | 1.051 | 1.054 | 61.4 | 62.0 | 62.4 |
| 8 | SJ | 0.302 | 0.316 | 0.330 | 0.285 | 0.297 | 0.308 | 0.258 | 0.266 | 0.272 | 70.1 | 69.8 | 72.5 | 72.1 | 73.0 | 74.8 | 0.947 | 0.940 | 0.945 | 61.5 | 61.7 | 62.7 |
| 9 | RJ | 0.267 | 0.280 | 0.294 | 0.276 | 0.285 | 0.296 | 0.281 | 0.280 | 0.282 | 73.9 | 74.1 | 76.1 | 69.6 | 71.4 | 72.1 | 1.028 | 1.014 | 1.010 | 65.0 | 65.6 | 65.5 |
| 10 | RJ | 0.248 | 0.260 | 0.267 | 0.262 | 0.268 | 0.282 | 0.282 | 0.282 | 0.284 | 82.0 | 81.2 | 83.2 | 75.2 | 77.1 | 77.1 | 1.073 | 1.033 | 1.056 | 61.0 | 60.8 | 61.6 |
| 11 | RJ | 0.252 | 0.261 | 0.269 | 0.270 | 0.279 | 0.288 | 0.243 | 0.239 | 0.251 | 77.6 | 77.6 | 78.9 | 70.9 | 72.4 | 73.6 | 1.072 | 1.063 | 1.057 | 60.9 | 63.3 | 62.6 |
| 12 | RJ | 0.237 | 0.244 | 0.255 | 0.259 | 0.265 | 0.275 | 0.252 | 0.258 | 0.265 | 79.4 | 80.3 | 81.5 | 71.6 | 73.2 | 74.2 | 1.090 | 1.087 | 1.082 | 60.0 | 60.5 | 61.1 |
| 13 | RJ | 0.269 | 0.278 | 0.291 | 0.282 | 0.288 | 0.301 | 0.263 | 0.270 | 0.276 | 76.7 | 78.1 | 79.5 | 71.3 | 74.1 | 75.0 | 1.047 | 1.031 | 1.041 | 62.5 | 62.7 | 63.7 |
| 14 | RJ | 0.315 | 0.323 | 0.335 | 0.322 | 0.331 | 0.341 | 0.322 | 0.321 | 0.323 | 69.3 | 71.7 | 73.9 | 64.0 | 65.7 | 67.5 | 1.024 | 1.027 | 1.027 | 64.1 | 64.8 | 65.0 |
| 15 | RJ | 0.304 | 0.314 | 0.327 | 0.323 | 0.331 | 0.339 | 0.251 | 0.260 | 0.269 | 76.3 | 77.3 | 78.4 | 72.0 | 73.1 | 74.5 | 1.059 | 1.053 | 1.044 | 65.4 | 64.6 | 65.3 |
| 16 | RJ | 0.277 | 0.288 | 0.300 | 0.280 | 0.290 | 0.302 | 0.300 | 0.305 | 0.306 | 79.6 | 78.8 | 79.8 | 76.0 | 76.2 | 76.8 | 1.012 | 1.008 | 1.010 | 64.4 | 64.2 | 64.6 |
| 17 | RJ | 0.278 | 0.287 | 0.299 | 0.273 | 0.284 | 0.300 | 0.245 | 0.248 | 0.255 | 75.1 | 77.2 | 78.7 | 74.1 | 75.1 | 75.9 | 0.992 | 0.994 | 1.006 | 61.1 | 62.0 | 62.6 |
| 18 | RJ | 0.253 | 0.265 | 0.278 | 0.268 | 0.278 | 0.292 | 0.276 | 0.279 | 0.285 | 80.3 | 80.8 | 81.8 | 75.8 | 76.3 | 76.1 | 1.054 | 1.051 | 1.061 | 61.9 | 62.1 | 62.7 |

FWD Test Data (Untreated Section, 28-Novemeber-2006) (1 μm/kN = 0.175 mil/kip).

| Section 3: Untreated |
| --- |
| 28-November-2006 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.283 | 0.296 | 0.283 | 0.274 | 0.283 | 0.279 | 0.188 | 0.202 | 0.204 | 83.8 | 85.8 | 85.1 | 84.8 | 84.4 | 84.9 | 0.966 | 0.964 | 0.973 | 66.9 | 66.2 | 66.4 |
| 2 | RJ | 0.249 | 0.255 | 0.251 | 0.246 | 0.254 | 0.248 | 0.169 | 0.176 | 0.185 | 84.4 | 84.7 | 85.5 | 83.0 | 83.5 | 84.4 | 0.996 | 1.003 | 0.991 | 68.2 | 68.6 | 68.2 |
| 3 | RJ | 0.245 | 0.250 | 0.247 | 0.232 | 0.241 | 0.240 | 0.176 | 0.185 | 0.189 | 80.2 | 82.1 | 83.1 | 82.4 | 83.3 | 84.4 | 0.952 | 0.974 | 0.976 | 67.3 | 67.0 | 66.6 |
| 4 | RJ | 0.252 | 0.258 | 0.254 | 0.258 | 0.264 | 0.264 | 0.191 | 0.200 | 0.201 | 78.7 | 79.9 | 81.3 | 73.3 | 75.8 | 76.4 | 1.021 | 1.022 | 1.028 | 65.5 | 64.9 | 65.2 |
| 5 | RJ | 0.254 | 0.259 | 0.257 | 0.246 | 0.253 | 0.254 | 0.186 | 0.192 | 0.198 | 81.7 | 81.1 | 82.4 | 80.5 | 81.1 | 81.6 | 0.983 | 0.984 | 0.981 | 65.6 | 65.6 | 66.2 |
| 6 | RJ | 0.227 | 0.231 | 0.237 | 0.233 | 0.240 | 0.242 | 0.163 | 0.175 | 0.183 | 76.3 | 77.2 | 78.6 | 73.6 | 73.9 | 75.9 | 1.024 | 1.035 | 1.023 | 69.1 | 68.6 | 69.1 |
| 7 | RJ | 0.248 | 0.253 | 0.252 | 0.259 | 0.266 | 0.268 | 0.179 | 0.186 | 0.193 | 81.0 | 82.7 | 82.5 | 75.4 | 75.0 | 76.8 | 1.056 | 1.064 | 1.047 | 68.0 | 68.2 | 68.1 |
| 8 | RJ | 0.221 | 0.230 | 0.235 | 0.228 | 0.235 | 0.242 | 0.166 | 0.172 | 0.181 | 77.0 | 76.8 | 78.4 | 74.5 | 75.1 | 76.3 | 1.033 | 1.028 | 1.031 | 69.8 | 68.9 | 68.0 |
| 9 | RJ | 0.247 | 0.253 | 0.257 | 0.241 | 0.249 | 0.253 | 0.169 | 0.178 | 0.186 | 75.5 | 76.4 | 78.2 | 74.9 | 75.4 | 76.8 | 0.991 | 0.997 | 0.991 | 67.6 | 67.9 | 68.2 |
| 10 | RJ | 0.221 | 0.228 | 0.237 | 0.239 | 0.245 | 0.252 | 0.163 | 0.171 | 0.180 | 84.0 | 84.5 | 85.8 | 78.9 | 79.1 | 80.4 | 1.071 | 1.072 | 1.063 | 68.4 | 68.3 | 68.4 |
| 11 | RJ | 0.225 | 0.232 | 0.238 | 0.227 | 0.235 | 0.240 | 0.162 | 0.170 | 0.178 | 76.1 | 77.0 | 78.4 | 72.9 | 74.1 | 74.2 | 1.005 | 1.007 | 1.008 | 69.0 | 67.9 | 67.6 |
| 12 | RJ | 0.214 | 0.223 | 0.228 | 0.214 | 0.221 | 0.225 | 0.174 | 0.179 | 0.185 | 75.0 | 74.6 | 75.9 | 75.9 | 75.1 | 77.2 | 0.995 | 0.993 | 0.990 | 66.5 | 66.7 | 66.4 |
| 13 | RJ | 0.234 | 0.253 | 0.246 | 0.233 | 0.240 | 0.245 | 0.193 | 0.201 | 0.207 | 73.4 | 71.2 | 75.7 | 71.6 | 72.8 | 74.9 | 1.000 | 0.955 | 0.988 | 62.1 | 62.8 | 63.3 |
| 14 | RJ | 0.276 | 0.282 | 0.288 | 0.256 | 0.269 | 0.270 | 0.168 | 0.180 | 0.185 | 74.8 | 74.9 | 76.5 | 77.3 | 75.7 | 79.1 | 0.922 | 0.949 | 0.939 | 63.9 | 63.8 | 64.8 |
| 15 | RJ | 0.218 | 0.227 | 0.235 | 0.230 | 0.240 | 0.244 | 0.183 | 0.191 | 0.197 | 74.4 | 75.2 | 76.5 | 71.2 | 71.0 | 73.5 | 1.058 | 1.049 | 1.034 | 64.4 | 64.4 | 66.0 |
| 16 | RJ | 0.228 | 0.241 | 0.240 | 0.219 | 0.233 | 0.239 | 0.162 | 0.166 | 0.175 | 72.6 | 70.9 | 74.0 | 70.8 | 70.3 | 72.0 | 0.986 | 0.990 | 1.000 | 63.1 | 64.7 | 64.4 |
| 17 | RJ | 0.187 | 0.193 | 0.200 | 0.203 | 0.208 | 0.213 | 0.168 | 0.181 | 0.186 | 82.6 | 82.9 | 83.6 | 75.6 | 75.5 | 77.2 | 1.084 | 1.077 | 1.075 | 64.6 | 63.7 | 65.1 |
| 18 | RJ | 0.236 | 0.244 | 0.251 | 0.215 | 0.223 | 0.231 | 0.175 | 0.197 | 0.202 | 62.1 | 63.7 | 66.2 | 63.7 | 64.4 | 66.9 | 0.911 | 0.918 | 0.927 | 67.9 | 64.9 | 66.3 |
| 19 | RJ | 0.237 | 0.250 | 0.248 | 0.221 | 0.231 | 0.232 | 0.195 | 0.215 | 0.213 | 69.4 | 69.6 | 72.4 | 73.4 | 74.2 | 75.3 | 0.932 | 0.925 | 0.937 | 63.9 | 61.5 | 65.5 |
| 20 | RJ | 0.228 | 0.239 | 0.243 | 0.223 | 0.238 | 0.238 | 0.196 | 0.207 | 0.219 | 75.6 | 75.3 | 77.6 | 75.6 | 74.7 | 77.7 | 0.981 | 1.000 | 0.982 | 64.0 | 63.9 | 64.4 |
| 21 | RJ | 0.259 | 0.272 | 0.279 | 0.256 | 0.266 | 0.275 | 0.196 | 0.208 | 0.216 | 70.0 | 70.9 | 74.7 | 69.7 | 71.6 | 73.8 | 0.992 | 0.982 | 0.991 | 66.2 | 65.9 | 66.9 |
| 22 | RJ | 0.256 | 0.265 | 0.268 | 0.242 | 0.253 | 0.256 | 0.176 | 0.188 | 0.198 | 70.1 | 70.9 | 72.7 | 74.6 | 74.9 | 77.1 | 0.946 | 0.955 | 0.955 | 64.6 | 64.8 | 65.1 |
| 23 | RJ | 0.219 | 0.230 | 0.241 | 0.215 | 0.224 | 0.231 | 0.174 | 0.183 | 0.190 | 70.5 | 70.8 | 71.5 | 74.3 | 74.4 | 76.3 | 0.976 | 0.976 | 0.955 | 66.1 | 66.3 | 66.5 |
| 24 | RJ | 0.232 | 0.241 | 0.247 | 0.217 | 0.227 | 0.235 | 0.178 | 0.193 | 0.197 | 72.9 | 72.2 | 74.6 | 76.0 | 77.1 | 77.9 | 0.936 | 0.940 | 0.948 | 64.0 | 62.1 | 63.8 |
| 25 | RJ | 0.222 | 0.231 | 0.237 | 0.205 | 0.213 | 0.221 | 0.185 | 0.192 | 0.199 | 76.2 | 75.6 | 77.9 | 80.9 | 81.6 | 82.3 | 0.924 | 0.918 | 0.931 | 63.0 | 63.5 | 63.6 |
| 26 | RJ | 0.207 | 0.216 | 0.225 | 0.213 | 0.224 | 0.233 | 0.168 | 0.182 | 0.183 | 75.9 | 76.6 | 77.4 | 72.6 | 73.1 | 74.2 | 1.031 | 1.037 | 1.033 | 65.2 | 63.3 | 66.3 |
| 27 | RJ | 0.209 | 0.218 | 0.227 | 0.216 | 0.220 | 0.230 | 0.175 | 0.189 | 0.197 | 79.3 | 79.9 | 80.9 | 77.2 | 79.1 | 78.8 | 1.020 | 1.000 | 1.013 | 65.7 | 63.2 | 64.5 |
| 28 | RJ | 0.219 | 0.228 | 0.240 | 0.217 | 0.231 | 0.243 | 0.191 | 0.200 | 0.204 | 69.1 | 69.3 | 71.0 | 67.2 | 65.9 | 67.6 | 0.986 | 1.010 | 1.013 | 60.9 | 61.4 | 62.8 |
| 29 | RJ | 0.216 | 0.226 | 0.226 | 0.220 | 0.228 | 0.234 | 0.169 | 0.181 | 0.188 | 78.7 | 79.1 | 82.0 | 75.5 | 76.3 | 77.7 | 1.030 | 1.018 | 1.027 | 62.9 | 61.8 | 63.2 |
| 30 | RJ | 0.207 | 0.220 | 0.224 | 0.212 | 0.219 | 0.224 | 0.162 | 0.167 | 0.173 | 68.6 | 68.2 | 71.5 | 65.0 | 65.0 | 66.8 | 1.031 | 1.000 | 1.008 | 62.3 | 63.7 | 63.9 |
| 31 | RJ | 0.205 | 0.214 | 0.224 | 0.202 | 0.210 | 0.221 | 0.167 | 0.175 | 0.183 | 74.6 | 75.2 | 77.4 | 73.3 | 74.6 | 76.2 | 0.990 | 0.978 | 0.992 | 63.4 | 63.4 | 64.1 |
| 32 | RJ | 0.224 | 0.229 | 0.239 | 0.197 | 0.208 | 0.215 | 0.169 | 0.178 | 0.188 | 62.2 | 64.4 | 66.7 | 66.8 | 67.2 | 69.3 | 0.880 | 0.912 | 0.903 | 64.9 | 64.9 | 65.4 |
| 33 | RJ | 0.189 | 0.201 | 0.208 | 0.194 | 0.203 | 0.213 | 0.162 | 0.174 | 0.178 | 78.7 | 77.6 | 79.8 | 74.2 | 75.4 | 76.1 | 1.022 | 1.008 | 1.018 | 62.3 | 62.1 | 63.2 |
| 34 | RJ | 0.184 | 0.194 | 0.197 | 0.192 | 0.196 | 0.207 | 0.153 | 0.158 | 0.171 | 76.7 | 76.2 | 79.0 | 71.8 | 73.3 | 73.9 | 1.052 | 1.033 | 1.052 | 66.4 | 67.5 | 67.0 |
| 35 | RJ | 0.181 | 0.188 | 0.196 | 0.187 | 0.192 | 0.199 | 0.150 | 0.159 | 0.163 | 78.4 | 79.5 | 80.8 | 72.7 | 74.1 | 76.0 | 1.029 | 1.017 | 1.012 | 62.7 | 63.4 | 63.6 |
| 36 | RJ | 0.190 | 0.196 | 0.203 | 0.191 | 0.198 | 0.205 | 0.160 | 0.165 | 0.171 | 71.9 | 72.6 | 74.5 | 68.7 | 69.6 | 71.5 | 1.006 | 1.008 | 1.009 | 63.8 | 64.4 | 65.5 |
| 37 | RJ | 0.193 | 0.200 | 0.207 | 0.203 | 0.203 | 0.212 | 0.162 | 0.174 | 0.180 | 72.9 | 73.5 | 75.1 | 66.8 | 69.4 | 156.9 | 1.050 | 1.012 | 1.027 | 66.5 | 65.6 | 67.5 |
| 38 | RJ | 0.199 | 0.210 | 0.217 | 0.192 | 0.198 | 0.203 | 0.183 | 0.188 | 0.195 | 71.9 | 71.0 | 73.2 | 71.9 | 72.1 | 74.6 | 0.962 | 0.942 | 0.932 | 62.5 | 62.0 | 61.8 |
| 39 | RJ | 0.191 | 0.201 | 0.204 | 0.192 | 0.199 | 0.206 | 0.187 | 0.196 | 0.207 | 78.0 | 77.7 | 78.7 | 75.8 | 75.6 | 76.7 | 1.006 | 0.996 | 1.003 | 64.4 | 64.1 | 64.6 |
| 40 | RJ | 0.201 | 0.208 | 0.218 | 0.197 | 0.203 | 0.212 | 0.198 | 0.204 | 0.211 | 75.0 | 74.7 | 76.0 | 73.0 | 73.7 | 75.1 | 0.984 | 0.977 | 0.972 | 60.5 | 61.5 | 62.3 |
| 41 | RJ | 0.184 | 0.190 | 0.200 | 0.196 | 0.204 | 0.210 | 0.204 | 0.203 | 0.213 | 75.4 | 75.9 | 77.8 | 70.3 | 69.9 | 71.0 | 1.057 | 1.075 | 1.057 | 68.4 | 69.6 | 69.0 |
| 42 | RJ | 0.205 | 0.210 | 0.219 | 0.196 | 0.203 | 0.212 | 0.165 | 0.166 | 0.174 | 74.4 | 76.3 | 77.8 | 77.4 | 77.8 | 79.2 | 0.954 | 0.966 | 0.975 | 61.7 | 62.7 | 62.9 |
| 43 | RJ | 0.202 | 0.211 | 0.216 | 0.207 | 0.212 | 0.217 | 0.197 | 0.201 | 0.206 | 71.2 | 70.9 | 73.2 | 67.5 | 68.0 | 69.3 | 1.016 | 1.004 | 1.008 | 64.8 | 66.0 | 66.3 |
| 44 | RJ | 0.194 | 0.202 | 0.211 | 0.194 | 0.200 | 0.207 | 0.191 | 0.194 | 0.197 | 76.9 | 76.7 | 79.1 | 75.3 | 76.3 | 78.5 | 1.000 | 1.000 | 1.000 | 63.3 | 63.0 | 64.0 |
| 45 | RJ | 0.182 | 0.176 | 0.186 | 0.184 | 0.191 | 0.194 | 0.198 | 0.193 | 0.193 | 73.7 | 76.8 | 76.5 | 68.8 | 69.9 | 71.9 | 1.012 | 1.086 | 1.042 | 60.3 | 61.7 | 62.6 |
| 46 | RJ | 0.185 | 0.194 | 0.203 | 0.175 | 0.179 | 0.189 | 0.186 | 0.188 | 0.192 | 69.1 | 70.0 | 71.6 | 73.3 | 74.2 | 74.4 | 0.943 | 0.926 | 0.937 | 60.9 | 61.7 | 62.0 |
| 47 | RJ | 0.173 | 0.182 | 0.189 | 0.181 | 0.188 | 0.194 | 0.202 | 0.202 | 0.206 | 72.6 | 73.0 | 73.8 | 66.5 | 66.8 | 69.0 | 1.037 | 1.022 | 1.019 | 61.1 | 62.6 | 62.6 |
| 48 | RJ | 0.182 | 0.187 | 0.194 | 0.191 | 0.194 | 0.205 | 0.211 | 0.216 | 0.212 | 75.4 | 75.8 | 76.5 | 70.6 | 71.6 | 100.3 | 1.035 | 1.030 | 1.043 | 58.5 | 58.4 | 60.0 |
| 49 | RJ | 0.177 | 0.189 | 0.193 | 0.164 | 0.177 | 0.184 | 0.210 | 0.213 | 0.214 | 71.1 | 70.0 | 72.2 | 72.9 | 71.9 | 73.8 | 0.934 | 0.933 | 0.954 | 61.8 | 60.8 | 61.6 |
| 50 | RJ | 0.200 | 0.203 | 0.212 | 0.204 | 0.211 | 0.216 | 0.185 | 0.188 | 0.192 | 72.7 | 74.6 | 74.4 | 69.3 | 70.7 | 72.3 | 1.027 | 1.039 | 1.025 | 63.3 | 63.6 | 63.9 |
| 51 | RJ | 0.193 | 0.200 | 0.210 | 0.192 | 0.199 | 0.207 | 0.204 | 0.209 | 0.215 | 76.0 | 76.1 | 76.8 | 74.2 | 75.1 | 76.9 | 0.995 | 0.992 | 0.977 | 65.6 | 65.2 | 65.2 |
| 52 | RJ | 0.261 | 0.270 | 0.275 | 0.213 | 0.223 | 0.231 | 0.178 | 0.185 | 0.191 | 59.5 | 60.1 | 61.7 | 68.2 | 68.5 | 69.2 | 0.818 | 0.834 | 0.840 | 62.9 | 62.7 | 63.2 |
| 53 | RJ | 0.199 | 0.207 | 0.215 | 0.190 | 0.206 | 0.209 | 0.182 | 0.186 | 0.199 | 79.9 | 80.7 | 82.0 | 79.0 | 78.3 | 79.8 | 0.957 | 0.996 | 0.977 | 63.8 | 65.5 | 65.5 |
| 54 | RJ | 0.207 | 0.217 | 0.227 | 0.207 | 0.213 | 0.222 | 0.179 | 0.176 | 0.182 | 70.1 | 69.6 | 71.1 | 64.4 | 64.9 | 65.2 | 1.000 | 0.981 | 0.978 | 61.9 | 63.6 | 63.7 |
| 55 | RJ | 0.175 | 0.177 | 0.188 | 0.190 | 0.197 | 0.205 | 0.185 | 0.189 | 0.198 | 80.5 | 82.8 | 82.7 | 73.0 | 72.5 | 73.9 | 1.085 | 1.104 | 1.088 | 63.6 | 64.6 | 64.7 |
| 56 | RJ | 0.171 | 0.176 | 0.185 | 0.175 | 0.177 | 0.186 | 0.182 | 0.186 | 0.193 | 77.4 | 78.5 | 80.1 | 76.1 | 77.6 | 76.9 | 1.025 | 1.000 | 1.003 | 64.6 | 64.6 | 64.6 |
| 57 | RJ | 0.203 | 0.215 | 0.223 | 0.210 | 0.215 | 0.226 | 0.169 | 0.178 | 0.187 | 77.2 | 77.0 | 78.5 | 73.3 | 75.2 | 76.3 | 1.032 | 1.004 | 1.014 | 64.5 | 64.7 | 64.8 |
| 58 | RJ | 0.185 | 0.193 | 0.202 | 0.193 | 0.204 | 0.216 | 0.200 | 0.217 | 0.227 | 83.9 | 85.8 | 86.7 | 77.3 | 76.8 | 77.4 | 1.040 | 1.063 | 1.057 | 58.9 | 58.1 | 59.2 |
| 59 | RJ | 0.273 | 0.294 | 0.306 | 0.249 | 0.268 | 0.283 | 0.186 | 0.194 | 0.203 | 49.6 | 48.9 | 48.5 | 63.8 | 63.8 | 63.3 | 0.913 | 0.912 | 0.928 | 63.9 | 65.0 | 65.3 |
| 60 | RJ | 0.201 | 0.210 | 0.219 | 0.202 | 0.209 | 0.220 |  |  |  | 80.2 | 81.5 | 82.6 | 77.9 | 79.6 | 79.9 | 1.016 | 1.004 | 1.006 |  |  |  |
| 61 | SJ | 0.202 | 0.211 | 0.217 | 0.192 | 0.199 | 0.207 | 0.201 | 0.199 | 0.208 | 71.4 | 70.8 | 72.6 | 75.4 | 72.4 | 72.6 | 0.947 | 0.946 | 0.958 | 60.0 | 61.1 | 60.5 |
| 62 | SJ | 0.186 | 0.189 | 0.197 | 0.194 | 0.200 | 0.202 | 0.159 | 0.167 | 0.168 | 76.4 | 79.6 | 79.8 | 71.3 | 74.0 | 75.8 | 1.040 | 1.047 | 1.028 | 63.4 | 62.6 | 63.6 |
| 63 | SJ | 0.190 | 0.198 | 0.198 | 0.189 | 0.193 | 0.198 | 0.177 | 0.181 | 0.187 | 73.9 | 74.1 | 75.2 | 73.4 | 72.4 | 73.4 | 1.006 | 0.984 | 0.991 | 65.0 | 64.7 | 64.1 |
| 64 | SJ | 0.183 | 0.187 | 0.193 | 0.176 | 0.182 | 0.188 | 0.197 | 0.201 | 0.209 | 73.7 | 73.0 | 75.2 | 72.1 | 73.5 | 73.5 | 0.965 | 0.983 | 0.981 | 60.6 | 60.4 | 60.3 |
| 65 | SJ | 0.169 | 0.177 | 0.183 | 0.159 | 0.168 | 0.174 | 0.189 | 0.192 | 0.194 | 79.0 | 78.3 | 78.3 | 79.1 | 78.6 | 78.4 | 0.943 | 0.949 | 0.943 | 60.3 | 59.9 | 59.7 |

FWD Test Data (C&S Section, 20-March-2007) (1 μm/kN = 0.175 mil/kip).

| Section 1: Cracked & Seated |
| --- |
| 20-March-2007 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.306 | 0.319 | 0.326 | 0.361 | 0.373 | 0.378 | 0.782 | 0.799 | 0.803 | 80.5 | 81.8 | 82.3 | 69.6 | 71.5 | 72.9 | 1.169 | 1.151 | 1.147 | 76.1 | 76.3 | 76.6 |
| 2 | RJ | 0.392 | 0.399 | 0.404 | 0.390 | 0.400 | 0.406 | 0.594 | 0.607 | 0.614 | 70.3 | 72.0 | 73.1 | 66.3 | 67.6 | 68.5 | 0.990 | 1.002 | 1.002 | 65.8 | 66.0 | 66.3 |
| 3 | RJ | 0.289 | 0.299 | 0.308 | 0.336 | 0.345 | 0.351 | 0.520 | 0.524 | 0.518 | 84.3 | 85.6 | 86.1 | 74.4 | 75.5 | 75.7 | 1.157 | 1.151 | 1.141 | 67.4 | 67.2 | 67.4 |
| 4 | RJ | 0.364 | 0.372 | 0.379 | 0.385 | 0.395 | 0.403 | 0.725 | 0.733 | 0.736 | 72.8 | 74.2 | 74.7 | 69.0 | 71.0 | 71.8 | 1.058 | 1.062 | 1.058 | 68.3 | 68.4 | 68.4 |
| 5 | RJ | 0.380 | 0.392 | 0.399 | 0.408 | 0.416 | 0.422 | 0.737 | 0.745 | 0.748 | 75.5 | 77.0 | 77.6 | 72.4 | 73.8 | 74.3 | 1.070 | 1.060 | 1.058 | 69.7 | 69.9 | 69.9 |
| 6 | RJ | 0.264 | 0.279 | 0.290 | 0.288 | 0.297 | 0.302 | 0.354 | 0.365 | 0.371 | 77.9 | 78.2 | 79.0 | 71.0 | 72.5 | 73.4 | 1.080 | 1.063 | 1.048 | 66.6 | 66.8 | 66.8 |
| 7 | RJ | 0.260 | 0.268 | 0.273 | 0.293 | 0.299 | 0.303 | 0.571 | 0.573 | 0.576 | 82.6 | 83.4 | 83.8 | 73.0 | 74.9 | 75.2 | 1.120 | 1.109 | 1.102 | 69.8 | 69.7 | 69.8 |
| 8 | RJ | 0.364 | 0.374 | 0.382 | 0.384 | 0.396 | 0.404 | 0.723 | 0.737 | 0.742 | 71.1 | 73.0 | 73.6 | 67.0 | 67.6 | 68.2 | 1.053 | 1.062 | 1.061 | 75.8 | 76.0 | 76.2 |
| 9 | RJ | 0.352 | 0.364 | 0.369 | 0.361 | 0.369 | 0.374 | 0.737 | 0.752 | 0.755 | 85.6 | 85.4 | 85.8 | 82.6 | 82.5 | 82.8 | 1.023 | 1.013 | 1.011 | 74.7 | 74.8 | 75.1 |
| 10 | RJ | 0.319 | 0.333 | 0.342 | 0.301 | 0.316 | 0.326 | 0.625 | 0.643 | 0.653 | 76.4 | 76.7 | 76.9 | 76.6 | 76.2 | 76.7 | 0.942 | 0.949 | 0.951 | 77.4 | 77.7 | 78.0 |
| 11 | RJ | 0.349 | 0.363 | 0.371 | 0.408 | 0.418 | 0.421 | 0.803 | 0.820 | 0.832 | 80.5 | 81.2 | 81.6 | 72.4 | 73.2 | 74.4 | 1.160 | 1.146 | 1.135 | 74.6 | 74.4 | 74.4 |
| 12 | RJ | 0.383 | 0.392 | 0.397 | 0.440 | 0.448 | 0.453 | 0.778 | 0.795 | 0.805 | 83.4 | 83.2 | 83.6 | 73.8 | 74.4 | 74.9 | 1.155 | 1.148 | 1.140 | 75.7 | 75.8 | 75.9 |
| 13 | RJ | 0.338 | 0.357 | 0.365 | 0.335 | 0.352 | 0.362 | 0.695 | 0.710 | 0.719 | 77.3 | 77.7 | 78.6 | 77.7 | 77.6 | 78.6 | 0.988 | 0.987 | 0.989 | 76.7 | 77.1 | 77.2 |
| 14 | RJ | 0.339 | 0.352 | 0.359 | 0.378 | 0.387 | 0.391 | 0.685 | 0.705 | 0.711 | 84.1 | 82.9 | 82.9 | 73.7 | 74.6 | 75.0 | 1.108 | 1.096 | 1.091 | 69.7 | 69.9 | 70.0 |
| 15 | RJ | 0.375 | 0.389 | 0.399 | 0.384 | 0.398 | 0.407 | 0.767 | 0.779 | 0.789 | 77.8 | 78.3 | 79.0 | 74.3 | 75.0 | 75.6 | 1.025 | 1.020 | 1.025 | 74.5 | 74.9 | 75.2 |
| 16 | RJ | 0.339 | 0.346 | 0.356 | 0.336 | 0.343 | 0.351 | 0.881 | 0.902 | 0.915 | 78.0 | 80.2 | 79.8 | 74.7 | 76.6 | 77.8 | 0.988 | 0.993 | 0.983 | 77.3 | 77.7 | 78.1 |
| 17 | RJ | 0.412 | 0.432 | 0.448 | 0.376 | 0.393 | 0.409 | 0.771 | 0.791 | 0.793 | 71.5 | 72.7 | 73.9 | 72.7 | 72.4 | 72.7 | 0.912 | 0.917 | 0.926 | 78.6 | 78.3 | 78.8 |
| 18 | SJ | 0.348 | 0.360 | 0.372 | 0.318 | 0.333 | 0.339 | 0.860 | 0.875 | 0.878 | 80.8 | 81.0 | 81.0 | 84.4 | 84.0 | 84.5 | 0.922 | 0.932 | 0.926 | 72.6 | 72.6 | 72.8 |
| 19 | SJ | 0.351 | 0.361 | 0.368 | 0.358 | 0.370 | 0.378 | 0.812 | 0.819 | 0.823 | 79.4 | 79.8 | 80.3 | 77.7 | 77.7 | 78.1 | 1.018 | 1.022 | 1.021 | 85.9 | 86.1 | 86.3 |
| 20 | SJ | 0.405 | 0.416 | 0.422 | 0.423 | 0.433 | 0.440 | 0.949 | 0.954 | 0.957 | 79.9 | 80.9 | 80.8 | 77.0 | 77.1 | 77.7 | 1.038 | 1.037 | 1.039 | 77.1 | 77.2 | 77.4 |
| 21 | SJ | 0.460 | 0.468 | 0.475 | 0.406 | 0.411 | 0.415 | 0.863 | 0.865 | 0.879 | 75.5 | 75.7 | 76.3 | 85.2 | 86.0 | 86.1 | 0.885 | 0.880 | 0.880 | 67.3 | 67.1 | 67.1 |
| 22 | SJ | 0.347 | 0.363 | 0.377 | 0.344 | 0.356 | 0.369 | 0.931 | 0.954 | 0.966 | 77.9 | 78.6 | 78.8 | 77.2 | 77.9 | 78.5 | 0.997 | 0.987 | 0.984 | 75.4 | 75.5 | 75.9 |
| 23 | RJ | 0.367 | 0.375 | 0.381 | 0.386 | 0.396 | 0.404 | 0.966 | 0.985 | 0.994 | 72.3 | 73.3 | 73.9 | 70.0 | 70.1 | 70.4 | 1.054 | 1.060 | 1.062 | 75.8 | 76.0 | 76.1 |
| 24 | RJ | 0.381 | 0.394 | 0.399 | 0.383 | 0.393 | 0.398 | 1.005 | 1.027 | 1.042 | 70.3 | 69.9 | 70.7 | 67.5 | 67.7 | 68.2 | 1.005 | 0.998 | 0.992 | 77.0 | 77.1 | 77.3 |
| 25 | RJ | 0.335 | 0.351 | 0.361 | 0.385 | 0.398 | 0.407 | 1.006 | 1.026 | 1.042 | 79.8 | 79.6 | 80.1 | 69.6 | 70.9 | 71.8 | 1.141 | 1.131 | 1.126 | 77.3 | 77.7 | 78.0 |
| 26 | RJ | 0.380 | 0.389 | 0.397 | 0.385 | 0.390 | 0.396 | 0.999 | 1.021 | 1.036 | 77.8 | 77.7 | 78.3 | 76.5 | 77.0 | 77.3 | 1.005 | 1.002 | 1.002 | 72.9 | 73.0 | 73.1 |
| 27 | RJ | 0.345 | 0.353 | 0.359 | 0.394 | 0.400 | 0.403 | 1.068 | 1.083 | 1.092 | 70.9 | 70.2 | 70.1 | 63.9 | 66.0 | 67.0 | 1.128 | 1.127 | 1.128 | 76.4 | 76.5 | 76.8 |
| 28 | RJ | 0.393 | 0.398 | 0.407 | 0.365 | 0.370 | 0.379 | 1.002 | 1.033 | 1.050 | 76.1 | 77.0 | 76.9 | 79.9 | 81.0 | 81.3 | 0.932 | 0.926 | 0.922 | 78.8 | 79.1 | 79.4 |
| 29 | RJ | 0.501 | 0.509 | 0.515 | 0.516 | 0.523 | 0.528 | 1.054 | 1.080 | 1.101 | 74.3 | 74.1 | 74.1 | 70.3 | 70.7 | 71.3 | 1.025 | 1.026 | 1.034 | 76.4 | 76.2 | 76.5 |
| 30 | RJ | 0.344 | 0.357 | 0.367 | 0.371 | 0.380 | 0.389 | 0.998 | 1.023 | 1.015 | 80.2 | 80.0 | 80.3 | 73.7 | 74.4 | 75.2 | 1.072 | 1.064 | 1.054 | 72.8 | 72.3 | 71.5 |
| 31 | RJ | 0.551 | 0.551 | 0.557 | 0.539 | 0.541 | 0.549 | 0.842 | 0.861 | 0.877 | 73.6 | 74.3 | 74.9 | 73.1 | 74.0 | 74.7 | 0.979 | 0.981 | 0.978 | 75.3 | 75.2 | 75.5 |
| 32 | RJ | 0.512 | 0.515 | 0.523 | 0.464 | 0.475 | 0.482 | 1.047 | 1.071 | 1.084 | 71.0 | 72.8 | 73.7 | 78.3 | 78.6 | 78.9 | 0.917 | 0.923 | 0.926 | 77.1 | 77.2 | 77.6 |
| 33 | RJ | 0.428 | 0.439 | 0.447 | 0.408 | 0.423 | 0.435 | 0.936 | 0.955 | 0.967 | 74.5 | 74.9 | 75.4 | 77.7 | 77.7 | 77.9 | 0.959 | 0.961 | 0.966 | 76.5 | 76.5 | 76.8 |

FWD Test Data (Rubblized Section, 20-March-2007) (1 μm/kN = 0.175 mil/kip).

| Section 2: Rubblized |
| --- |
| 20-March-2007 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.401 | 0.403 | 0.396 | 0.441 | 0.440 | 0.435 | 0.290 | 0.298 | 0.299 | 70.8 | 72.3 | 74.4 | 69.2 | 73.2 | 74.6 | 1.106 | 1.091 | 1.096 | 61.0 | 61.8 | 61.9 |
| 2 | RJ | 0.490 | 0.501 | 0.505 | 0.550 | 0.547 | 0.539 | 0.254 | 0.258 | 0.261 | 84.9 | 83.4 | 82.8 | 70.4 | 71.9 | 71.6 | 1.121 | 1.094 | 1.077 | 64.7 | 66.5 | 66.7 |
| 3 | SJ | 0.334 | 0.347 | 0.351 | 0.321 | 0.328 | 0.332 | 0.284 | 0.290 | 0.291 | 81.9 | 81.7 | 81.8 | 82.8 | 84.2 | 84.2 | 0.961 | 0.947 | 0.945 | 62.8 | 63.6 | 63.9 |
| 4 | SJ | 0.340 | 0.350 | 0.354 | 0.320 | 0.328 | 0.331 | 0.329 | 0.332 | 0.332 | 79.6 | 80.0 | 80.2 | 83.0 | 83.3 | 83.2 | 0.938 | 0.937 | 0.932 | 66.0 | 67.0 | 67.5 |
| 5 | SJ | 0.617 | 0.614 | 0.604 | 0.628 | 0.609 | 0.590 | 0.240 | 0.250 | 0.254 | 71.1 | 71.2 | 71.2 | 56.7 | 60.0 | 61.1 | 1.022 | 0.995 | 0.982 | 66.6 | 66.6 | 67.3 |
| 6 | SJ | 0.392 | 0.398 | 0.398 | 0.356 | 0.362 | 0.362 | 0.232 | 0.239 | 0.242 | 79.5 | 79.6 | 79.9 | 86.6 | 86.4 | 86.3 | 0.909 | 0.917 | 0.907 | 62.8 | 63.6 | 63.9 |
| 7 | SJ | 0.410 | 0.417 | 0.421 | 0.353 | 0.361 | 0.364 | 0.234 | 0.241 | 0.245 | 67.1 | 68.1 | 68.1 | 78.6 | 79.2 | 79.0 | 0.869 | 0.871 | 0.867 | 64.0 | 64.3 | 64.7 |
| 8 | RJ | 0.401 | 0.407 | 0.413 | 0.384 | 0.388 | 0.389 | 0.280 | 0.282 | 0.284 | 67.7 | 69.2 | 70.2 | 69.9 | 69.9 | 70.7 | 0.957 | 0.955 | 0.948 | 69.9 | 70.3 | 70.3 |
| 9* | RJ | 0.405 | 0.412 | 0.413 | 0.400 | 0.397 | 0.396 | 0.323 | 0.323 | 0.325 | 79.9 | 80.4 | 80.5 | 79.7 | 80.4 | 80.2 | 0.980 | 0.972 | 0.969 | 61.8 | 62.5 | 62.7 |
| 10* | RJ | 0.363 | 0.370 | 0.376 | 0.359 | 0.363 | 0.364 | 0.294 | 0.294 | 0.294 | 71.6 | 71.9 | 71.7 | 71.5 | 72.3 | 72.9 | 0.986 | 0.977 | 0.966 | 61.0 | 61.4 | 61.3 |
| 11* | RJ | 0.420 | 0.427 | 0.436 | 0.437 | 0.434 | 0.431 | 0.276 | 0.285 | 0.288 | 80.5 | 79.9 | 79.9 | 72.3 | 73.1 | 74.2 | 1.034 | 1.018 | 0.997 | 61.8 | 62.8 | 63.1 |
| 12* | RJ | 0.573 | 0.568 | 0.569 | 0.443 | 0.451 | 0.456 | 0.428 | 0.418 | 0.410 | 57.1 | 60.1 | 61.7 | 80.3 | 80.8 | 81.0 | 0.772 | 0.795 | 0.806 | 67.3 | 67.6 | 67.6 |
| 13 | RJ | 0.395 | 0.402 | 0.411 | 0.421 | 0.428 | 0.429 | 1.024 | 1.038 | 1.033 | 73.4 | 74.4 | 74.2 | 62.4 | 64.6 | 65.7 | 1.072 | 1.069 | 1.059 | 79.2 | 79.2 | 79.3 |
| 14 | RJ | 0.542 | 0.548 | 0.551 | 0.392 | 0.410 | 0.407 | 0.191 | 0.196 | 0.196 | 65.6 | 66.4 | 66.7 | 88.4 | 87.7 | 86.3 | 0.731 | 0.762 | 0.748 | 64.7 | 64.9 | 65.3 |
| 15 | RJ | 0.436 | 0.449 | 0.453 | 0.491 | 0.488 | 0.489 | 0.717 | 0.721 | 0.705 | 86.2 | 85.8 | 85.6 | 73.1 | 74.3 | 74.4 | 1.131 | 1.110 | 1.097 | 71.8 | 71.0 | 70.9 |
| 16 | RJ | 0.388 | 0.399 | 0.407 | 0.370 | 0.377 | 0.379 | 0.290 | 0.293 | 0.294 | 73.3 | 73.4 | 73.6 | 72.5 | 72.9 | 73.4 | 0.953 | 0.948 | 0.939 | 66.9 | 67.7 | 67.4 |
| 17 | RJ | 0.312 | 0.329 | 0.336 | 0.306 | 0.312 | 0.317 | 0.619 | 0.619 | 0.611 | 72.5 | 72.9 | 73.0 | 70.9 | 72.4 | 73.7 | 0.977 | 0.965 | 0.959 | 69.9 | 69.5 | 69.5 |
| 18 | RJ | 0.370 | 0.380 | 0.381 | 0.379 | 0.385 | 0.386 | 0.486 | 0.494 | 0.495 | 57.4 | 59.4 | 61.1 | 57.1 | 60.6 | 62.4 | 1.025 | 1.006 | 1.008 | 70.7 | 70.8 | 70.8 |
| 19 | RJ | 0.414 | 0.420 | 0.419 | 0.422 | 0.420 | 0.419 | 0.421 | 0.422 | 0.420 | 77.5 | 78.0 | 78.4 | 77.1 | 77.0 | 77.7 | 1.015 | 0.998 | 0.997 | 65.1 | 65.2 | 65.3 |
| 20 | RJ | 0.417 | 0.427 | 0.434 | 0.477 | 0.478 | 0.472 | 0.604 | 0.619 | 0.623 | 81.6 | 81.7 | 81.9 | 76.2 | 77.3 | 77.6 | 1.131 | 1.113 | 1.088 | 70.6 | 71.0 | 71.2 |
| 21 | RJ | 0.313 | 0.323 | 0.325 | 0.322 | 0.333 | 0.337 | 0.714 | 0.729 | 0.735 | 78.8 | 79.2 | 80.0 | 74.3 | 74.5 | 75.5 | 1.029 | 1.029 | 1.028 | 76.0 | 75.9 | 76.0 |
| 22 | RJ | 0.438 | 0.442 | 0.437 | 0.411 | 0.416 | 0.419 | 0.561 | 0.561 | 0.564 | 64.8 | 66.0 | 68.6 | 69.3 | 70.4 | 70.5 | 0.941 | 0.935 | 0.952 | 70.5 | 70.8 | 70.8 |
| 23 | RJ | 0.274 | 0.288 | 0.295 | 0.279 | 0.290 | 0.298 | 0.516 | 0.530 | 0.536 | 77.7 | 77.6 | 78.2 | 73.7 | 75.9 | 76.9 | 1.019 | 1.008 | 1.009 | 68.5 | 68.3 | 68.3 |
| 24 | RJ | 0.378 | 0.390 | 0.402 | 0.437 | 0.444 | 0.447 | 0.612 | 0.629 | 0.637 | 83.4 | 83.3 | 83.3 | 74.4 | 74.6 | 74.4 | 1.155 | 1.137 | 1.115 | 74.1 | 74.1 | 74.3 |
| 25 | RJ | 0.287 | 0.301 | 0.309 | 0.324 | 0.333 | 0.340 | 0.622 | 0.642 | 0.651 | 86.5 | 86.8 | 87.2 | 77.6 | 78.4 | 78.2 | 1.124 | 1.114 | 1.111 | 76.3 | 76.3 | 76.5 |
| 26 | RJ | 0.298 | 0.309 | 0.316 | 0.299 | 0.309 | 0.317 | 0.614 | 0.634 | 0.639 | 66.9 | 69.0 | 70.1 | 67.7 | 69.7 | 69.8 | 1.003 | 1.008 | 1.004 | 75.5 | 75.3 | 75.5 |
| 27 | RJ | 0.359 | 0.366 | 0.367 | 0.349 | 0.353 | 0.355 | 0.507 | 0.507 | 0.509 | 70.9 | 72.4 | 72.8 | 71.1 | 71.3 | 72.0 | 0.977 | 0.978 | 0.977 | 69.0 | 69.0 | 69.1 |
| 28 | RJ | 0.275 | 0.281 | 0.293 | 0.298 | 0.307 | 0.314 | 0.650 | 0.671 | 0.680 | 78.4 | 80.8 | 81.0 | 72.1 | 73.0 | 74.4 | 1.078 | 1.092 | 1.077 | 78.8 | 78.7 | 79.2 |
| 29 | RJ | 0.400 | 0.408 | 0.414 | 0.389 | 0.390 | 0.396 | 0.669 | 0.688 | 0.698 | 74.7 | 75.3 | 76.1 | 75.5 | 76.4 | 76.6 | 0.969 | 0.960 | 0.960 | 79.9 | 80.0 | 80.4 |
| 30 | RJ | 0.550 | 0.550 | 0.556 | 0.549 | 0.538 | 0.530 | 0.702 | 0.724 | 0.729 | 76.6 | 76.7 | 76.9 | 78.2 | 78.0 | 78.1 | 0.989 | 0.980 | 0.963 | 77.7 | 77.7 | 78.0 |
| 31 | RJ | 0.436 | 0.442 | 0.445 | 0.452 | 0.453 | 0.453 | 0.623 | 0.638 | 0.649 | 81.4 | 81.0 | 81.8 | 80.6 | 79.6 | 79.5 | 1.035 | 1.027 | 1.019 | 75.3 | 75.4 | 75.6 |

FWD Test Data (Untreated Section, 20-March-2007) (1 μm/kN = 0.175 mil/kip).

| Section 3: Untreated |
| --- |
| 20-March-2007 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.268 | 0.264 | 0.265 | 0.266 | 0.267 | 0.268 | 0.172 | 0.178 | 0.182 | 50.5 | 54.2 | 56.7 | 53.6 | 56.9 | 58.6 | 0.999 | 1.012 | 1.014 | 65.4 | 65.7 | 65.8 |
| 2 | RJ | 0.199 | 0.204 | 0.207 | 0.222 | 0.227 | 0.230 | 0.184 | 0.193 | 0.199 | 76.5 | 75.8 | 76.1 | 73.1 | 74.5 | 75.2 | 1.117 | 1.110 | 1.110 | 68.3 | 68.4 | 68.7 |
| 3 | RJ | 0.251 | 0.257 | 0.262 | 0.243 | 0.248 | 0.253 | 0.158 | 0.167 | 0.173 | 52.8 | 51.1 | 50.9 | 65.5 | 67.2 | 68.4 | 0.963 | 0.968 | 0.971 | 67.8 | 67.7 | 67.5 |
| 4 | RJ | 0.225 | 0.230 | 0.235 | 0.239 | 0.239 | 0.242 | 0.176 | 0.182 | 0.187 | 74.7 | 75.8 | 76.4 | 69.1 | 70.6 | 71.6 | 1.059 | 1.039 | 1.034 | 66.9 | 67.4 | 67.7 |
| 5 | RJ | 0.233 | 0.240 | 0.246 | 0.237 | 0.241 | 0.245 | 0.203 | 0.206 | 0.208 | 60.9 | 61.2 | 61.8 | 57.8 | 60.9 | 62.5 | 1.018 | 1.001 | 0.992 | 59.7 | 60.9 | 61.5 |
| 6 | RJ | 0.193 | 0.199 | 0.203 | 0.248 | 0.255 | 0.259 | 0.216 | 0.219 | 0.222 | 82.5 | 82.1 | 82.4 | 65.0 | 66.4 | 67.1 | 1.284 | 1.274 | 1.274 | 61.4 | 62.3 | 62.6 |
| 7 | RJ | 0.191 | 0.193 | 0.193 | 0.208 | 0.212 | 0.215 | 0.182 | 0.184 | 0.186 | 68.4 | 69.4 | 70.7 | 63.0 | 65.1 | 65.1 | 1.090 | 1.098 | 1.119 | 63.9 | 65.0 | 65.4 |
| 8 | RJ | 0.175 | 0.178 | 0.180 | 0.181 | 0.184 | 0.186 | 0.196 | 0.197 | 0.198 | 80.8 | 81.2 | 81.6 | 77.7 | 77.9 | 79.0 | 1.032 | 1.036 | 1.032 | 59.2 | 60.1 | 61.0 |
| 9 | RJ | 0.178 | 0.184 | 0.188 | 0.203 | 0.210 | 0.215 | 0.176 | 0.178 | 0.180 | 82.2 | 81.8 | 82.1 | 70.1 | 71.7 | 71.7 | 1.141 | 1.136 | 1.134 | 63.3 | 64.4 | 65.1 |
| 10 | RJ | 0.181 | 0.185 | 0.190 | 0.190 | 0.195 | 0.197 | 0.223 | 0.224 | 0.223 | 78.9 | 80.0 | 79.6 | 75.5 | 76.1 | 77.1 | 1.050 | 1.056 | 1.038 | 63.0 | 64.1 | 64.9 |
| 11 | RJ | 0.209 | 0.210 | 0.214 | 0.232 | 0.235 | 0.240 | 0.186 | 0.189 | 0.192 | 93.0 | 95.3 | 95.5 | 66.4 | 67.2 | 67.9 | 1.114 | 1.125 | 1.123 | 61.8 | 62.3 | 62.8 |
| 12 | RJ | 0.168 | 0.174 | 0.180 | 0.181 | 0.185 | 0.186 | 0.179 | 0.182 | 0.187 | 83.2 | 82.1 | 81.1 | 72.4 | 74.0 | 74.9 | 1.075 | 1.063 | 1.037 | 67.0 | 68.2 | 68.1 |
| 13 | RJ | 0.242 | 0.247 | 0.251 | 0.222 | 0.229 | 0.235 | 0.198 | 0.200 | 0.201 | 59.8 | 61.2 | 62.8 | 63.1 | 63.1 | 64.0 | 0.920 | 0.925 | 0.935 | 61.1 | 61.5 | 61.8 |
| 14 | RJ | 0.200 | 0.205 | 0.211 | 0.215 | 0.220 | 0.224 | 0.211 | 0.218 | 0.223 | 68.3 | 69.6 | 70.8 | 64.1 | 65.8 | 67.0 | 1.071 | 1.067 | 1.061 | 68.2 | 68.0 | 67.9 |
| 15 | RJ | 0.178 | 0.184 | 0.189 | 0.179 | 0.186 | 0.191 | 0.207 | 0.211 | 0.210 | 77.3 | 78.2 | 79.0 | 74.9 | 75.2 | 75.4 | 1.006 | 1.008 | 1.013 | 63.8 | 64.1 | 65.2 |
| 16 | RJ | 0.290 | 0.297 | 0.286 | 0.262 | 0.267 | 0.265 | 0.819 | 0.775 | 0.744 | 71.5 | 73.6 | 73.7 | 76.0 | 77.3 | 76.6 | 0.902 | 0.912 | 0.917 | 77.6 | 77.8 | 77.8 |
| 17 | RJ | 0.339 | 0.343 | 0.331 | 0.285 | 0.291 | 0.290 | 1.090 | 1.114 | 1.116 | 72.8 | 74.8 | 75.9 | 76.2 | 77.4 | 77.5 | 0.844 | 0.857 | 0.872 | 76.4 | 76.4 | 76.5 |
| 18 | RJ | 0.322 | 0.329 | 0.329 | 0.289 | 0.297 | 0.303 | 0.998 | 0.924 | 0.895 | 64.2 | 66.2 | 67.8 | 69.1 | 70.5 | 71.6 | 0.903 | 0.911 | 0.919 | 72.7 | 71.5 | 71.6 |
| 19 | RJ | 0.264 | 0.275 | 0.281 | 0.288 | 0.290 | 0.299 | 0.916 | 0.860 | 0.852 | 73.3 | 74.1 | 75.0 | 65.4 | 67.9 | 68.4 | 1.090 | 1.058 | 1.062 | 69.7 | 69.7 | 69.9 |
| 20 | RJ | 0.270 | 0.278 | 0.282 | 0.275 | 0.276 | 0.284 | 0.940 | 0.893 | 0.884 | 73.8 | 75.3 | 75.9 | 70.9 | 73.0 | 72.9 | 1.013 | 0.993 | 0.998 | 66.5 | 65.8 | 65.9 |
| 21* | RJ | 0.273 | 0.277 | 0.284 | 0.266 | 0.269 | 0.277 | 0.497 | 0.477 | 0.485 | 72.5 | 73.6 | 74.1 | 72.4 | 73.3 | 73.0 | 0.971 | 0.972 | 0.979 | 63.7 | 63.8 | 63.5 |
| 22* | RJ | 0.222 | 0.224 | 0.230 | 0.235 | 0.237 | 0.241 | 0.900 | 0.880 | 0.891 | 73.0 | 74.6 | 75.1 | 69.6 | 70.6 | 71.4 | 1.063 | 1.055 | 1.043 | 71.2 | 70.4 | 70.3 |
| 23* | RJ | 0.268 | 0.274 | 0.282 | 0.288 | 0.293 | 0.302 | 0.591 | 0.576 | 0.598 | 77.7 | 78.9 | 79.2 | 70.2 | 71.0 | 71.8 | 1.072 | 1.070 | 1.065 | 67.1 | 67.0 | 67.1 |
| 24* | RJ | 0.239 | 0.240 | 0.244 | 0.236 | 0.238 | 0.244 | 0.769 | 0.725 | 0.728 | 73.2 | 74.9 | 75.8 | 71.8 | 73.5 | 73.5 | 0.990 | 0.993 | 1.002 | 65.8 | 65.7 | 65.7 |
| 25 | RJ | 0.226 | 0.232 | 0.240 | 0.227 | 0.228 | 0.237 | 0.723 | 0.687 | 0.695 | 78.0 | 78.7 | 78.9 | 74.3 | 76.1 | 76.7 | 1.006 | 0.985 | 0.982 | 77.1 | 76.8 | 76.9 |
| 26 | SJ | 0.323 | 0.325 | 0.329 | 0.271 | 0.275 | 0.286 | 0.493 | 0.484 | 0.495 | 63.9 | 66.1 | 67.9 | 76.0 | 76.9 | 76.5 | 0.843 | 0.848 | 0.868 | 65.1 | 65.4 | 65.4 |
| 27 | SJ | 0.286 | 0.285 | 0.290 | 0.299 | 0.302 | 0.312 | 0.431 | 0.431 | 0.445 | 81.2 | 83.1 | 83.5 | 78.9 | 79.7 | 78.4 | 1.042 | 1.059 | 1.069 | 64.0 | 64.4 | 64.9 |
| 28 | SJ | 0.242 | 0.249 | 0.257 | 0.251 | 0.253 | 0.259 | 0.544 | 0.532 | 0.533 | 80.5 | 80.0 | 80.8 | 75.3 | 76.7 | 76.5 | 1.036 | 1.020 | 1.025 | 68.4 | 68.3 | 68.1 |
| 29 | SJ | 0.224 | 0.229 | 0.235 | 0.204 | 0.213 | 0.220 | 0.535 | 0.520 | 0.516 | 75.4 | 76.9 | 76.8 | 80.0 | 80.1 | 79.4 | 0.913 | 0.936 | 0.941 | 70.3 | 70.1 | 70.1 |
| 30 | SJ | 0.245 | 0.249 | 0.257 | 0.235 | 0.238 | 0.245 | 0.413 | 0.410 | 0.425 | 77.5 | 77.7 | 77.5 | 77.7 | 78.3 | 78.1 | 0.955 | 0.959 | 0.963 | 59.7 | 60.5 | 60.5 |
| 31 | RJ | 0.235 | 0.241 | 0.249 | 0.240 | 0.244 | 0.252 | 0.561 | 0.564 | 0.590 | 76.5 | 77.8 | 78.3 | 74.9 | 75.3 | 75.7 | 1.018 | 1.013 | 1.012 | 70.3 | 70.6 | 70.8 |
| 32 | RJ | 0.221 | 0.229 | 0.236 | 0.212 | 0.219 | 0.226 | 0.569 | 0.561 | 0.582 | 78.0 | 78.3 | 79.0 | 78.7 | 79.2 | 79.7 | 0.962 | 0.958 | 0.959 | 68.1 | 68.5 | 69.0 |
| 33 | RJ | 0.248 | 0.259 | 0.267 | 0.233 | 0.243 | 0.251 | 0.549 | 0.536 | 0.543 | 79.5 | 80.0 | 80.5 | 82.8 | 83.7 | 83.0 | 0.940 | 0.939 | 0.940 | 68.0 | 67.9 | 68.0 |
| 34 | RJ | 0.292 | 0.299 | 0.312 | 0.299 | 0.308 | 0.319 | 0.369 | 0.370 | 0.382 | 65.9 | 68.8 | 69.8 | 57.2 | 59.5 | 60.3 | 1.018 | 1.033 | 1.035 | 63.8 | 64.2 | 64.5 |
| 35 | RJ | 0.216 | 0.225 | 0.233 | 0.245 | 0.252 | 0.259 | 0.502 | 0.502 | 0.523 | 83.8 | 85.0 | 86.3 | 71.7 | 74.0 | 75.3 | 1.136 | 1.121 | 1.115 | 68.4 | 68.6 | 68.7 |

FWD Test Data (C&S and Rubblized Sections, 31-October-2007) (1 μm/kN = 0.175 mil/kip).

| 31-October-2007 |
| --- |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| Section 1: Cracked & Seated |
| 1 | RJ | 0.293 | 0.302 | 0.313 | 0.286 | 0.295 | 0.309 | 0.537 | 0.545 | 0.560 | 72.6 | 74.4 | 74.7 | 69.8 | 72.6 | 72.1 | 0.975 | 0.974 | 0.981 | 68.0 | 68.7 | 68.3 |
| 2 | RJ | 0.234 | 0.246 | 0.254 | 0.259 | 0.273 | 0.281 | 0.486 | 0.489 | 0.487 | 79.1 | 80.3 | 81.2 | 70.4 | 71.9 | 72.4 | 1.111 | 1.108 | 1.101 | 68.3 | 68.4 | 68.4 |
| 3 | RJ | 0.261 | 0.272 | 0.283 | 0.272 | 0.284 | 0.290 | 0.591 | 0.590 | 0.584 | 71.3 | 72.2 | 72.5 | 70.4 | 70.5 | 71.2 | 1.036 | 1.040 | 1.028 | 69.4 | 70.0 | 69.7 |
| 4 | RJ | 0.274 | 0.289 | 0.297 | 0.281 | 0.294 | 0.303 | 0.528 | 0.520 | 0.509 | 71.9 | 71.5 | 72.4 | 70.4 | 71.3 | 71.9 | 1.027 | 1.022 | 1.022 | 67.2 | 66.8 | 67.0 |
| 5 | RJ | 0.218 | 0.228 | 0.236 | 0.227 | 0.236 | 0.241 | 0.393 | 0.395 | 0.396 | 76.3 | 77.1 | 77.7 | 72.0 | 75.2 | 77.6 | 1.033 | 1.034 | 1.019 | 68.2 | 68.3 | 68.2 |
| 6 | RJ | 0.223 | 0.226 | 0.232 | 0.226 | 0.231 | 0.235 | 0.400 | 0.391 | 0.386 | 82.3 | 84.5 | 84.2 | 77.3 | 79.0 | 80.0 | 1.005 | 1.017 | 1.017 | 64.9 | 65.4 | 65.5 |
| 7 | RJ | 0.277 | 0.287 | 0.296 | 0.290 | 0.300 | 0.309 | 0.622 | 0.626 | 0.636 | 68.3 | 68.9 | 69.7 | 65.2 | 67.1 | 68.0 | 1.042 | 1.046 | 1.045 | 75.0 | 76.2 | 76.5 |
| 8 | RJ | 0.282 | 0.290 | 0.295 | 0.278 | 0.282 | 0.291 | 0.634 | 0.647 | 0.660 | 77.4 | 77.8 | 77.4 | 75.9 | 77.4 | 77.4 | 0.985 | 0.973 | 0.991 | 72.0 | 72.8 | 73.0 |
| 9 | RJ | 0.273 | 0.285 | 0.294 | 0.257 | 0.269 | 0.278 | 0.588 | 0.608 | 0.619 | 74.5 | 73.3 | 73.0 | 75.4 | 75.1 | 74.8 | 0.943 | 0.940 | 0.940 | 67.2 | 67.5 | 67.8 |
| 10 | RJ | 0.269 | 0.281 | 0.293 | 0.299 | 0.309 | 0.316 | 0.633 | 0.643 | 0.644 | 82.1 | 80.7 | 80.4 | 70.6 | 73.7 | 74.3 | 1.125 | 1.103 | 1.090 | 68.3 | 69.0 | 69.0 |
| 11 | RJ | 0.264 | 0.277 | 0.288 | 0.295 | 0.303 | 0.311 | 0.556 | 0.540 | 0.522 | 80.6 | 80.8 | 80.8 | 73.3 | 73.6 | 74.9 | 1.115 | 1.093 | 1.082 | 73.0 | 73.8 | 73.7 |
| 12 | RJ | 0.271 | 0.286 | 0.296 | 0.276 | 0.289 | 0.300 | 0.540 | 0.549 | 0.554 | 82.2 | 80.0 | 80.5 | 76.8 | 77.7 | 77.5 | 1.015 | 1.008 | 1.013 | 70.7 | 71.3 | 71.6 |
| 13 | SJ | 0.316 | 0.321 | 0.331 | 0.279 | 0.293 | 0.301 | 0.679 | 0.692 | 0.698 | 80.7 | 81.6 | 81.8 | 78.9 | 75.0 | 76.9 | 0.880 | 0.914 | 0.908 | 75.0 | 74.8 | 74.9 |
| 14 | SJ | 0.256 | 0.264 | 0.271 | 0.271 | 0.281 | 0.288 | 0.687 | 0.662 | 0.632 | 77.0 | 76.9 | 77.1 | 70.0 | 69.5 | 69.6 | 1.058 | 1.059 | 1.055 | 69.0 | 68.3 | 68.2 |
| 15 | SJ | 0.287 | 0.301 | 0.310 | 0.317 | 0.323 | 0.330 | 0.681 | 0.637 | 0.598 | 74.3 | 73.5 | 73.2 | 71.1 | 64.4 | 66.3 | 1.107 | 1.065 | 1.061 | 70.5 | 69.9 | 69.7 |
| 16 | SJ | 0.311 | 0.317 | 0.322 | 0.296 | 0.299 | 0.306 | 0.680 | 0.685 | 0.693 | 71.1 | 72.2 | 73.1 | 74.5 | 76.4 | 77.1 | 0.959 | 0.945 | 0.951 | 68.6 | 68.9 | 68.6 |
| 17 | SJ | 0.271 | 0.281 | 0.290 | 0.275 | 0.286 | 0.297 | 0.605 | 0.588 | 0.576 | 73.3 | 73.6 | 74.1 | 70.5 | 70.6 | 71.1 | 1.023 | 1.022 | 1.023 | 70.7 | 70.2 | 70.0 |
| Section 2: Rubblized |
| 1 | RJ | 0.286 | 0.299 | 0.311 | 0.287 | 0.302 | 0.311 | 0.342 | 0.346 | 0.352 | 62.1 | 64.1 | 66.2 | 63.0 | 60.7 | 60.5 | 1.004 | 1.013 | 1.002 | 64.2 | 65.5 | 65.4 |
| 2 | RJ | 0.286 | 0.308 | 0.317 | 0.293 | 0.310 | 0.318 | 0.309 | 0.316 | 0.320 | 76.4 | 77.0 | 78.5 | 72.8 | 75.6 | 75.4 | 1.025 | 1.008 | 1.004 | 61.0 | 61.3 | 62.0 |
| 3 | RJ | 0.319 | 0.335 | 0.348 | 0.320 | 0.329 | 0.337 | 0.286 | 0.290 | 0.296 | 53.4 | 54.4 | 55.2 | 56.7 | 61.0 | 63.5 | 1.010 | 0.988 | 0.981 | 61.5 | 62.4 | 62.9 |
| 4 | SJ | 0.331 | 0.344 | 0.359 | 0.337 | 0.344 | 0.357 | 0.336 | 0.342 | 0.346 | 59.1 | 60.9 | 61.8 | 56.5 | 59.7 | 61.1 | 1.013 | 1.000 | 0.996 | 64.8 | 65.3 | 65.7 |
| 5 | SJ | 0.302 | 0.318 | 0.324 | 0.330 | 0.339 | 0.348 | 0.355 | 0.360 | 0.363 | 68.3 | 68.3 | 69.5 | 59.0 | 59.7 | 61.2 | 1.082 | 1.059 | 1.060 | 67.6 | 67.6 | 67.6 |
| 6 | SJ | 0.352 | 0.368 | 0.380 | 0.446 | 0.456 | 0.470 | 0.287 | 0.291 | 0.294 | 104.1 | 103.8 | 104.4 | 70.6 | 73.0 | 72.4 | 1.259 | 1.232 | 1.230 | 64.3 | 64.6 | 65.0 |
| 7 | SJ | 0.340 | 0.351 | 0.360 | 0.289 | 0.297 | 0.310 | 0.262 | 0.266 | 0.273 | 54.1 | 56.7 | 57.9 | 58.6 | 60.8 | 61.9 | 0.850 | 0.848 | 0.860 | 63.4 | 63.7 | 64.2 |
| 8 | SJ | 0.371 | 0.384 | 0.396 | 0.335 | 0.341 | 0.353 | 0.351 | 0.356 | 0.357 | 35.8 | 38.4 | 40.3 | 36.9 | 41.7 | 43.2 | 0.908 | 0.895 | 0.902 | 66.8 | 66.2 | 66.0 |
| 9 | RJ | 0.262 | 0.273 | 0.283 | 0.269 | 0.276 | 0.286 | 0.417 | 0.404 | 0.403 | 64.5 | 66.9 | 68.1 | 60.2 | 61.7 | 62.4 | 1.020 | 1.014 | 1.016 | 68.8 | 69.9 | 69.5 |
| 10 | RJ | 0.267 | 0.282 | 0.291 | 0.267 | 0.278 | 0.289 | 0.449 | 0.454 | 0.458 | 75.6 | 76.3 | 77.6 | 70.2 | 71.9 | 72.5 | 1.000 | 0.994 | 1.016 | 67.2 | 67.3 | 67.3 |
| 11 | RJ | 0.266 | 0.277 | 0.285 | 0.270 | 0.277 | 0.287 | 0.506 | 0.509 | 0.512 | 67.7 | 68.3 | 69.5 | 68.6 | 66.4 | 67.0 | 1.016 | 1.003 | 1.007 | 68.3 | 67.8 | 67.7 |
| 12 | RJ | 0.248 | 0.260 | 0.268 | 0.251 | 0.263 | 0.270 | 0.349 | 0.347 | 0.351 | 63.4 | 65.0 | 66.0 | 71.4 | 55.7 | 62.1 | 1.013 | 1.006 | 1.007 | 63.9 | 64.8 | 64.8 |
| 13 | RJ | 0.282 | 0.288 | 0.297 | 0.266 | 0.276 | 0.284 | 0.310 | 0.312 | 0.316 | 58.3 | 60.9 | 63.3 | 59.6 | 61.0 | 63.0 | 0.941 | 0.962 | 0.967 | 64.6 | 64.3 | 64.5 |
| 14 | RJ | 0.283 | 0.295 | 0.305 | 0.314 | 0.325 | 0.333 | 0.645 | 0.642 | 0.639 | 68.1 | 71.1 | 71.9 | 60.1 | 53.3 | 59.3 | 1.103 | 1.110 | 1.105 | 68.8 | 68.7 | 68.4 |
| 15 | RJ | 0.314 | 0.321 | 0.336 | 0.321 | 0.329 | 0.342 | 0.529 | 0.517 | 0.510 | 63.2 | 66.3 | 67.1 | 59.9 | 63.1 | 63.6 | 1.023 | 1.034 | 1.032 | 70.1 | 70.2 | 69.9 |
| 16 | RJ | 0.271 | 0.282 | 0.291 | 0.284 | 0.289 | 0.298 | 0.517 | 0.515 | 0.517 | 69.9 | 71.0 | 72.2 | 67.0 | 61.1 | 64.5 | 1.054 | 1.031 | 1.034 | 71.3 | 71.7 | 71.5 |
| 17 | RJ | 0.286 | 0.296 | 0.304 | 0.275 | 0.288 | 0.296 | 0.391 | 0.392 | 0.396 | 63.4 | 64.5 | 65.9 | 60.8 | 62.1 | 63.0 | 0.963 | 0.973 | 0.970 | 68.2 | 67.9 | 68.4 |

FWD Test Data (Untreated Section, 31-October-2007) (1 μm/kN = 0.175 mil/kip).

| Section 3: Untreated |
| --- |
| 31-October-2007 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.402 | 0.404 | 0.398 | 0.319 | 0.323 | 0.326 | 0.200 | 0.212 | 0.215 | 47.7 | 49.8 | 51.3 | 73.3 | 75.1 | 75.8 | 0.795 | 0.804 | 0.817 | 74.0 | 74.1 | 74.3 |
| 2 | RJ | 0.585 | 0.578 | 0.558 | 0.540 | 0.528 | 0.510 | 0.193 | 0.204 | 0.208 | 28.2 | 30.8 | 32.5 | 26.1 | 27.3 | 28.6 | 0.936 | 0.920 | 0.912 | 71.4 | 70.1 | 70.0 |
| 3 | RJ | 0.322 | 0.329 | 0.325 | 0.333 | 0.336 | 0.333 | 0.176 | 0.189 | 0.193 | 77.3 | 78.2 | 79.2 | 73.9 | 74.2 | 73.6 | 1.042 | 1.022 | 1.016 | 68.5 | 68.2 | 68.6 |
| 4 | RJ | 0.275 | 0.287 | 0.291 | 0.271 | 0.279 | 0.279 | 0.165 | 0.176 | 0.180 | 62.2 | 63.5 | 63.8 | 64.3 | 62.6 | 60.9 | 0.985 | 0.970 | 0.962 | 67.5 | 66.5 | 66.1 |
| 5 | RJ | 0.326 | 0.334 | 0.335 | 0.313 | 0.316 | 0.318 | 0.162 | 0.173 | 0.179 | 60.2 | 61.0 | 61.5 | 66.0 | 66.7 | 67.6 | 0.959 | 0.946 | 0.945 | 67.2 | 66.3 | 66.9 |
| 6 | RJ | 0.263 | 0.270 | 0.273 | 0.253 | 0.259 | 0.263 | 0.160 | 0.167 | 0.173 | 73.2 | 74.7 | 74.6 | 73.7 | 74.2 | 73.7 | 0.961 | 0.959 | 0.964 | 65.7 | 66.4 | 66.4 |
| 7 | RJ | 0.300 | 0.301 | 0.302 | 0.284 | 0.287 | 0.289 | 0.165 | 0.174 | 0.180 | 63.5 | 66.0 | 67.1 | 65.0 | 66.7 | 68.2 | 0.945 | 0.951 | 0.952 | 69.9 | 69.9 | 69.9 |
| 8 | RJ | 0.364 | 0.357 | 0.351 | 0.323 | 0.328 | 0.332 | 0.185 | 0.197 | 0.203 | 53.1 | 57.9 | 59.8 | 65.3 | 67.7 | 68.8 | 0.895 | 0.927 | 0.942 | 65.7 | 66.7 | 67.1 |
| 9 | RJ | 0.394 | 0.410 | 0.418 | 0.367 | 0.374 | 0.379 | 0.181 | 0.190 | 0.196 | 32.8 | 34.0 | 34.9 | 45.9 | 46.2 | 47.3 | 0.924 | 0.910 | 0.902 | 65.3 | 65.3 | 65.5 |
| 10 | RJ | 0.250 | 0.255 | 0.254 | 0.233 | 0.235 | 0.241 | 0.201 | 0.208 | 0.215 | 71.6 | 73.9 | 74.5 | 73.5 | 73.3 | 72.5 | 0.930 | 0.932 | 0.943 | 65.3 | 65.8 | 66.2 |
| 11 | RJ | 0.259 | 0.269 | 0.273 | 0.249 | 0.256 | 0.261 | 0.179 | 0.189 | 0.194 | 64.8 | 65.7 | 66.7 | 67.4 | 67.9 | 64.7 | 0.957 | 0.959 | 0.959 | 67.2 | 66.9 | 67.0 |
| 12 | SJ | 0.254 | 0.258 | 0.264 | 0.267 | 0.276 | 0.279 | 0.182 | 0.193 | 0.194 | 57.7 | 59.6 | 59.5 | 51.7 | 51.7 | 53.2 | 1.053 | 1.064 | 1.053 | 61.2 | 61.3 | 62.1 |
| 13 | SJ | 0.231 | 0.241 | 0.249 | 0.218 | 0.232 | 0.237 | 0.168 | 0.176 | 0.178 | 71.4 | 70.8 | 70.2 | 70.4 | 70.6 | 71.1 | 0.951 | 0.961 | 0.949 | 61.8 | 62.8 | 63.7 |
| 14 | SJ | 0.260 | 0.268 | 0.273 | 0.247 | 0.249 | 0.254 | 0.176 | 0.179 | 0.185 | 55.6 | 56.8 | 57.4 | 55.4 | 56.5 | 56.4 | 0.960 | 0.926 | 0.927 | 64.2 | 66.4 | 66.1 |
| 15 | SJ | 0.213 | 0.223 | 0.226 | 0.232 | 0.237 | 0.239 | 0.192 | 0.196 | 0.201 | 63.3 | 63.8 | 64.9 | 53.7 | 56.0 | 56.0 | 1.097 | 1.071 | 1.065 | 64.6 | 65.3 | 65.7 |
| 16 | SJ | 0.185 | 0.193 | 0.199 | 0.172 | 0.183 | 0.188 | 0.197 | 0.202 | 0.205 | 76.0 | 75.8 | 76.5 | 71.9 | 76.0 | 69.6 | 0.933 | 0.955 | 0.950 | 61.8 | 62.0 | 61.9 |

FWD Test Data (C&S Section, 6-May-2008) (1 μm/kN = 0.175 mil/kip).

| Section 1: Cracked & Seated |
| --- |
| 6-May-2008 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.297 | 0.308 | 0.310 | 0.320 | 0.324 | 0.318 | 0.648 | 0.637 | 0.609 | 90.0 | 89.5 | 90.2 | 85.1 | 85.6 |  | 1.067 | 1.049 | 1.039 | 69.2 | 69.4 | 70.1 |
| 2 | R | 0.305 | 0.319 | 0.308 | 0.336 | 0.343 | 0.337 | 0.613 | 0.618 | 0.600 | 89.9 | 90.6 | 91.0 | 81.0 | 82.9 | 82.0 | 1.101 | 1.078 | 1.078 | 72.2 | 72.8 | 72.9 |
| 3 | R | 0.296 | 0.308 | 0.293 | 0.300 | 0.310 | 0.301 | 0.596 | 0.592 | 0.574 | 87.5 | 84.9 | 91.5 | 85.9 | 83.3 | 86.8 | 1.019 | 1.003 | 0.992 | 67.3 | 67.2 | 67.6 |
| 4 | R | 0.284 | 0.284 | 0.279 | 0.295 | 0.301 | 0.295 | 0.685 | 0.692 | 0.679 | 85.3 | 88.9 | 87.9 | 83.8 | 83.5 |  | 1.027 | 1.061 | 1.040 | 70.1 | 71.1 | 70.8 |
| 5 | R | 0.298 | 0.298 | 0.293 | 0.310 | 0.316 | 0.311 | 0.715 | 0.712 | 0.683 | 85.3 | 85.6 | 79.2 | 82.8 | 81.7 | 83.1 | 1.026 | 1.055 | 1.046 | 71.9 | 71.8 | 72.1 |
| 6 | R | 0.327 | 0.323 | 0.312 | 0.325 | 0.321 | 0.312 | 0.817 | 0.807 | 0.766 | 83.5 | 87.1 | 85.4 | 84.1 | 85.5 | 84.1 | 0.997 | 0.979 | 0.980 | 73.7 | 74.1 | 74.5 |
| 7 | R | 0.323 | 0.325 | 0.323 | 0.315 | 0.321 | 0.310 | 0.590 | 0.581 | 0.528 | 95.0 | 83.8 | 77.6 | 89.7 | 89.9 | 88.4 | 0.946 | 0.975 | 0.954 | 65.5 | 64.5 | 65.7 |
| 8 | S | 0.329 | 0.329 | 0.314 | 0.331 | 0.333 | 0.319 | 0.632 | 0.605 | 0.561 | 90.8 | 87.0 | 83.7 | 84.4 | 85.3 | 86.5 | 1.027 | 1.018 | 1.004 | 67.3 | 67.5 |  |
| 9 | S | 0.280 | 0.279 | 0.278 | 0.289 | 0.298 | 0.290 | 0.504 | 0.486 | 0.450 | 85.9 | 88.4 | 95.8 | 84.6 | 85.5 | 83.0 | 1.020 | 1.020 | 1.026 | 66.3 | 67.1 | 67.5 |
| 10 | S | 0.331 | 0.338 | 0.325 | 0.372 | 0.370 | 0.359 | 0.540 | 0.527 | 0.491 | 98.0 | 87.9 | 95.0 | 83.1 | 81.8 | 81.7 | 1.122 | 1.099 | 1.124 | 68.6 | 67.6 |  |
| 11 | S | 0.390 | 0.388 | 0.369 | 0.402 | 0.394 | 0.382 | 0.548 | 0.537 | 0.508 | 84.2 | 86.9 | 86.0 | 83.3 | 87.1 | 85.4 | 1.028 | 1.017 | 1.020 | 65.7 | 66.0 | 66.2 |
| 12 | S | 0.347 | 0.346 | 0.335 | 0.383 | 0.389 | 0.379 | 0.640 | 0.637 | 0.586 | 94.9 | 92.8 | 90.9 | 85.3 | 84.4 | 83.9 | 1.112 | 1.128 | 1.115 | 69.4 | 67.6 | 68.3 |
| 13 | R | 0.285 | 0.286 | 0.277 | 0.299 | 0.296 | 0.287 |  |  |  | 86.8 | 85.3 | 87.3 | 85.4 | 83.1 | 84.5 | 1.035 | 1.023 | 1.022 |  |  |  |

FWD Test Data (Rubblized Section, 6-May-2008) (1 μm/kN = 0.175 mil/kip).

| Section 2: Rubblized |
| --- |
| 6-May-2008 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.330 | 0.337 | 0.329 | 0.315 | 0.325 | 0.321 | 0.571 | 0.576 | 0.557 | 68.5 | 72.9 | 72.4 | 80.4 | 79.8 | 79.6 | 0.953 | 0.925 | 0.874 | 62.6 | 62.4 | 62.7 |
| 2 | R | 0.360 | 0.369 | 0.360 | 0.388 | 0.387 | 0.380 | 0.412 | 0.413 | 0.399 | 79.0 | 86.5 | 83.9 | 78.4 | 80.0 | 81.9 | 1.073 | 1.058 | 1.029 | 59.2 | 60.0 | 60.5 |
| 3 | R | 0.313 | 0.326 | 0.316 | 0.339 | 0.347 | 0.339 | 0.411 | 0.405 | 0.391 | 83.2 | 82.9 | 84.2 | 74.5 | 81.2 | 80.8 | 1.082 | 1.061 | 1.075 | 62.4 | 63.0 | 63.5 |
| 4 | S | 0.314 | 0.319 | 0.312 | 0.346 | 0.347 | 0.333 | 0.403 | 0.395 | 0.379 | 86.1 | 88.2 | 89.0 | 81.1 | 82.7 | 82.8 | 1.110 | 1.097 | 1.078 | 60.9 | 61.7 | 62.3 |
| 5 | S | 0.305 | 0.313 | 0.306 | 0.321 | 0.327 | 0.323 | 0.529 | 0.531 | 0.512 | 89.2 | 89.4 | 89.6 | 83.6 | 85.9 | 84.3 | 1.032 | 1.034 | 1.051 |  | 59.5 | 60.9 |
| 6 | S | 0.345 | 0.355 | 0.348 | 0.347 | 0.348 | 0.345 | 0.416 | 0.407 | 0.389 | 80.8 | 81.7 | 80.4 | 79.4 | 81.3 | 81.5 | 0.981 | 0.977 | 0.974 | 60.7 | 61.0 | 61.1 |
| 7 | S | 0.339 | 0.343 | 0.332 | 0.342 | 0.334 | 0.334 | 0.469 | 0.467 | 0.452 | 84.2 | 80.9 | 83.0 | 82.8 | 83.5 | 82.2 | 1.017 | 0.993 | 1.029 | 62.9 | 62.3 | 62.1 |
| 8 | S | 0.323 | 0.334 | 0.322 | 0.313 | 0.313 | 0.307 | 0.428 | 0.427 | 0.412 | 80.5 | 79.4 | 81.0 | 83.2 | 83.6 | 83.1 | 1.004 | 1.030 | 0.980 | 59.4 | 59.0 | 59.8 |
| 9 | R | 0.311 | 0.301 | 0.296 | 0.291 | 0.292 | 0.288 | 0.507 | 0.503 | 0.494 | 76.6 | 84.1 | 82.5 | 86.7 | 84.9 | 82.3 | 0.933 | 0.964 | 0.963 | 60.4 |  | 62.3 |
| 10 | R | 0.311 | 0.315 | 0.305 | 0.303 | 0.305 | 0.301 | 0.454 | 0.456 | 0.441 | 83.3 | 82.0 | 85.8 | 85.7 | 88.1 | 84.8 | 0.943 | 0.943 | 0.960 | 60.3 | 60.6 | 61.1 |
| 11 | R | 0.290 | 0.295 | 0.292 | 0.307 | 0.309 | 0.309 | 0.482 | 0.482 | 0.470 | 84.3 | 85.2 | 84.8 | 77.7 | 81.1 | 81.3 | 1.022 | 1.039 | 1.034 | 59.5 |  | 60.0 |
| 12 | R | 0.288 | 0.302 | 0.290 | 0.300 | 0.309 | 0.298 | 0.453 | 0.451 | 0.434 | 87.4 | 84.3 | 82.6 | 74.4 | 76.1 | 80.1 | 1.031 | 1.025 | 1.023 | 57.8 | 58.1 | 58.7 |
| 13 | R | 0.323 | 0.332 | 0.322 | 0.315 | 0.315 | 0.312 | 0.739 | 0.739 | 0.707 | 71.5 | 71.8 | 76.1 | 76.7 | 81.2 | 79.9 | 0.973 | 0.945 | 0.950 | 70.2 | 70.1 | 70.3 |
| 14 | R | 0.374 | 0.384 | 0.372 | 0.382 | 0.388 | 0.371 | 0.860 | 0.851 | 0.824 | 81.8 | 76.4 | 80.6 | 83.8 | 81.2 | 80.7 | 1.030 | 1.026 | 1.031 | 68.8 | 70.3 | 70.2 |
| 15 | R | 0.345 | 0.351 | 0.341 | 0.365 | 0.371 | 0.359 | 0.780 | 0.771 | 0.744 | 78.8 | 80.4 | 79.2 | 76.2 | 75.7 | 78.2 | 1.068 | 1.050 | 1.027 | 69.6 | 70.1 | 70.1 |
| 16 | R | 0.316 | 0.324 | 0.325 | 0.330 |  | 0.325 | 0.726 | 0.725 | 0.711 | 78.2 | 83.8 | 82.6 | 74.9 |  | 78.2 | 1.035 |  | 0.968 | 73.5 | 74.2 | 74.4 |
| 17 | R | 0.359 | 0.364 | 0.349 | 0.331 | 0.336 | 0.329 | 0.624 | 0.616 | 0.594 | 70.1 | 73.0 | 70.3 | 75.2 | 77.6 |  | 0.909 | 0.914 | 0.913 | 71.2 | 72.1 | 71.7 |
| 18 | R | 0.307 | 0.316 | 0.306 | 0.323 | 0.326 | 0.320 | 0.732 | 0.731 | 0.702 | 83.2 | 83.0 | 86.0 | 82.3 | 80.1 | 85.6 | 1.050 | 1.023 | 0.998 | 73.5 | 73.2 | 73.3 |
| 19 | R | 0.341 | 0.334 | 0.323 | 0.342 | 0.347 | 0.339 | 0.637 | 0.628 | 0.607 | 72.3 | 79.0 | 73.3 | 77.0 | 77.0 | 77.2 | 0.984 | 1.020 | 1.008 | 73.5 | 73.9 | 74.0 |
| 20 | R | 0.323 | 0.326 | 0.311 | 0.331 | 0.328 | 0.316 | 0.606 | 0.617 | 0.593 | 80.7 | 79.3 | 77.4 | 77.6 | 78.1 |  | 1.024 | 1.003 | 1.016 | 74.0 | 72.9 | 74.0 |
| 21 | R | 0.319 | 0.320 | 0.310 | 0.346 | 0.339 | 0.324 | 0.650 | 0.654 | 0.631 | 74.6 | 75.3 | 76.2 | 71.3 | 70.8 | 74.2 | 1.092 | 1.060 | 1.022 | 73.5 | 73.2 | 73.1 |
| 22 | R | 0.301 | 0.310 | 0.296 | 0.303 | 0.310 | 0.300 | 0.717 | 0.722 | 0.698 | 73.9 | 83.0 | 80.8 | 81.0 | 83.1 | 82.3 | 0.989 | 0.992 | 0.998 | 74.1 |  | 74.6 |
| 23 | R | 0.334 | 0.341 | 0.324 | 0.342 | 0.345 | 0.335 | 0.625 | 0.636 | 0.604 | 75.3 | 75.1 | 84.0 | 76.8 | 77.9 |  | 1.033 | 1.015 | 0.996 | 70.9 | 69.6 | 70.4 |
| 24 | R | 0.283 | 0.283 | 0.273 | 0.293 | 0.302 | 0.294 | 0.594 | 0.591 | 0.564 | 78.4 | 80.6 | 85.7 | 77.4 | 78.8 | 78.8 | 1.039 | 1.067 | 1.033 | 70.4 | 70.4 | 70.2 |
| 25 | R | 0.288 | 0.295 | 0.290 | 0.317 | 0.328 | 0.317 | 0.616 | 0.624 | 0.608 | 77.7 | 77.6 | 78.8 | 72.2 | 74.0 |  | 1.072 | 1.101 | 1.095 | 75.3 | 75.2 | 75.3 |

FWD Test Data (Untreated Section, 6-May-2008) (1 μm/kN = 0.175 mil/kip).

| Section 3: Untreated |
| --- |
| 6-May-2008 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.302 | 0.293 | 0.303 | 0.290 | 0.281 | 0.282 | 0.203 | 0.200 | 0.208 | 48.0 | 53.5 | 53.3 | 60.9 | 67.2 | 69.2 | 0.956 | 0.930 | 0.890 | 67.7 | 71.5 | 70.0 |
| 2 | R | 0.271 | 0.268 | 0.260 | 0.297 | 0.298 | 0.278 | 0.202 | 0.215 | 0.206 | 56.1 | 60.2 | 67.8 | 62.5 | 66.0 | 72.2 | 1.094 | 1.125 | 1.063 | 69.2 | 65.6 | 68.3 |
| 3 | R | 0.294 | 0.292 | 0.303 | 0.302 | 0.315 | 0.314 | 0.203 | 0.208 | 0.209 | 74.2 | 77.8 | 78.1 | 72.0 | 72.4 | 73.0 | 1.027 | 1.074 | 1.058 | 72.0 | 72.1 | 72.5 |
| 4 | R | 0.299 | 0.309 | 0.295 | 0.282 | 0.280 | 0.284 | 0.176 | 0.193 | 0.193 | 51.7 | 47.1 | 51.2 | 70.6 | 72.7 | 72.7 | 0.944 | 0.923 | 0.968 | 66.9 | 64.0 | 65.2 |
| 5 | R | 0.229 | 0.257 | 0.247 | 0.259 | 0.253 | 0.258 | 0.162 | 0.173 | 0.174 | 49.0 | 50.8 | 50.4 | 61.6 | 66.6 | 68.1 | 1.115 | 0.965 | 1.023 | 67.0 | 67.9 | 69.0 |
| 6 | R | 0.247 | 0.235 | 0.250 | 0.257 | 0.268 | 0.255 | 0.188 | 0.205 | 0.199 | 66.2 | 74.4 | 70.6 | 69.1 | 69.2 | 75.4 | 1.050 | 1.142 | 1.023 | 59.4 | 61.4 | 64.2 |
| 7 | R | 0.233 | 0.247 | 0.245 | 0.238 | 0.227 | 0.233 | 0.210 | 0.218 | 0.218 | 67.0 | 64.3 | 65.3 | 71.4 | 76.8 | 76.1 | 1.038 | 0.925 | 0.969 | 64.6 | 64.8 | 64.0 |
| 8 | R | 0.227 | 0.232 | 0.232 | 0.232 | 0.231 | 0.240 | 0.190 | 0.197 | 0.196 | 72.9 | 73.2 | 74.7 | 67.6 | 72.2 | 69.6 | 1.034 | 0.989 | 1.038 | 64.7 | 65.3 | 66.1 |
| 9 | R | 0.227 | 0.256 | 0.245 | 0.236 | 0.255 | 0.247 | 0.176 | 0.194 | 0.187 | 60.0 | 52.4 | 57.3 | 74.9 | 70.6 | 74.7 | 1.029 | 0.997 | 0.995 | 69.1 | 60.6 | 68.3 |
| 10 | R | 0.239 | 0.236 | 0.235 | 0.220 | 0.235 | 0.236 | 0.199 | 0.197 | 0.190 | 63.1 | 70.5 | 72.8 | 72.7 | 74.1 | 76.6 | 0.925 | 1.000 | 1.003 | 53.7 | 63.0 | 64.9 |
| 11 | R | 0.219 | 0.238 | 0.245 | 0.234 | 0.239 | 0.237 | 0.191 | 0.200 | 0.204 | 75.0 | 69.2 | 69.0 | 66.7 | 69.9 |  | 1.056 | 0.990 | 0.947 | 64.8 | 63.9 | 64.0 |
| 12 | R | 0.222 | 0.236 | 0.234 | 0.251 | 0.236 | 0.244 | 0.185 | 0.203 | 0.198 | 60.3 |  | 67.5 | 53.7 | 55.5 |  | 1.141 | 0.989 | 1.043 | 67.1 | 63.4 | 66.2 |
| 13 | R | 0.213 | 0.214 | 0.217 | 0.234 | 0.245 | 0.231 | 0.194 | 0.225 | 0.208 | 71.5 | 73.0 | 71.2 | 66.7 | 67.8 | 72.4 | 1.073 | 1.141 | 1.074 | 68.7 | 61.6 | 64.9 |
| 14 | R | 0.232 | 0.218 | 0.230 | 0.238 | 0.220 | 0.230 | 0.202 | 0.191 | 0.206 | 68.8 | 72.3 | 70.3 | 63.0 | 70.4 |  | 1.068 | 1.027 | 1.033 | 65.0 | 69.1 | 66.8 |
| 15 | R | 0.234 | 0.244 | 0.240 | 0.244 | 0.243 | 0.249 | 0.189 | 0.194 | 0.197 | 73.2 | 66.6 | 66.9 | 70.0 | 71.5 | 71.6 | 1.053 | 1.028 | 1.044 | 65.6 | 64.3 | 63.6 |
| 16 | R | 0.216 | 0.205 | 0.213 | 0.208 | 0.225 | 0.215 | 0.182 | 0.194 | 0.200 | 62.8 | 68.6 | 71.0 | 74.6 | 67.2 | 74.3 | 0.964 | 1.118 | 1.036 | 70.2 | 69.1 | 68.2 |
| 17 | R | 0.237 | 0.231 | 0.238 | 0.216 | 0.225 | 0.221 | 0.191 | 0.185 | 0.182 | 63.0 | 65.0 | 66.1 | 75.9 | 70.7 | 76.0 | 0.903 | 0.964 | 0.924 | 46.5 | 62.9 | 63.9 |
| 18 | R | 0.228 | 0.228 | 0.215 | 0.231 | 0.233 | 0.233 | 0.215 | 0.207 | 0.205 | 67.0 | 71.4 | 74.3 | 64.1 | 67.5 | 68.0 | 1.030 | 1.026 | 1.093 | 61.1 | 64.0 | 64.6 |
| 19 | R | 0.209 | 0.224 | 0.219 | 0.234 | 0.248 | 0.240 | 0.214 | 0.216 | 0.213 | 71.1 | 71.6 | 77.5 | 67.8 | 67.0 | 70.3 | 1.128 | 1.136 | 1.127 | 67.0 | 67.3 | 67.8 |
| 20 | R | 0.241 | 0.219 | 0.226 | 0.230 | 0.220 | 0.220 | 0.260 | 0.259 | 0.248 | 69.4 | 73.1 | 69.7 | 68.3 | 74.9 | 76.8 | 0.949 | 0.981 | 0.983 | 61.3 | 62.6 | 63.1 |
| 21 | R | 0.211 | 0.212 | 0.219 | 0.222 | 0.217 | 0.213 | 0.352 | 0.328 | 0.309 | 72.2 | 80.5 | 78.5 | 71.6 | 77.4 | 79.8 | 1.036 | 1.000 | 0.966 | 62.3 | 64.5 | 64.8 |
| 22 | R | 0.234 | 0.228 | 0.239 | 0.244 | 0.245 | 0.242 | 0.367 | 0.343 | 0.315 | 77.1 | 76.8 | 74.8 | 68.0 | 69.5 | 72.0 | 1.043 | 1.069 | 1.000 | 58.8 | 58.8 | 60.1 |
| 23 | R | 0.212 | 0.205 | 0.206 | 0.204 | 0.222 | 0.226 | 0.470 | 0.419 | 0.380 | 71.4 | 77.7 | 79.5 | 72.3 | 70.2 | 69.9 | 0.958 | 1.073 | 1.076 | 61.5 | 63.3 | 63.5 |
| 24 | R | 0.233 | 0.243 | 0.241 | 0.255 | 0.251 | 0.254 | 0.301 | 0.286 | 0.262 | 74.3 | 72.2 | 72.7 | 65.4 | 69.1 | 69.7 | 1.086 | 1.045 | 1.064 | 61.2 | 61.1 | 63.5 |
| 25 | R | 0.234 | 0.237 | 0.237 | 0.236 | 0.234 | 0.225 | 0.490 | 0.454 | 0.416 | 70.1 | 72.3 | 71.6 | 64.6 | 68.6 | 71.5 | 1.005 | 0.993 | 0.935 | 61.4 | 63.5 | 62.1 |
| 26 | R | 0.221 | 0.244 | 0.233 | 0.244 | 0.254 | 0.256 | 0.476 | 0.430 | 0.389 | 82.4 | 75.7 | 79.1 | 67.1 | 70.7 | 71.7 | 1.116 | 1.051 | 1.119 | 60.3 | 60.4 | 63.0 |
| 27 | R | 0.213 | 0.212 | 0.200 | 0.207 | 0.216 | 0.212 | 0.465 | 0.412 | 0.365 | 66.7 | 66.0 | 69.8 | 66.7 | 66.0 | 67.4 | 0.969 | 1.000 | 1.040 | 60.2 | 62.0 | 62.1 |
| 28 | R | 0.212 | 0.208 | 0.216 | 0.219 | 0.226 | 0.221 | 0.411 | 0.386 | 0.349 | 72.7 | 75.7 | 76.8 | 74.9 | 71.0 | 72.4 | 1.026 | 1.055 | 1.029 | 59.3 | 58.3 | 59.1 |
| 29 | R | 0.201 | 0.218 | 0.207 | 0.217 | 0.214 | 0.212 | 0.485 | 0.474 | 0.430 | 68.0 | 69.6 | 72.7 | 65.8 | 68.1 | 68.7 | 1.066 | 0.966 | 0.985 | 62.9 | 61.7 | 61.6 |
| 30 | R | 0.222 | 0.216 | 0.218 | 0.207 | 0.214 | 0.212 | 0.494 | 0.461 | 0.411 | 70.0 | 73.4 | 73.5 | 70.6 | 73.9 | 73.5 | 0.935 | 0.992 | 0.968 | 59.0 | 59.1 | 59.5 |
| 31 | R | 0.217 | 0.221 | 0.220 | 0.233 | 0.236 | 0.226 | 0.547 | 0.523 | 0.466 | 69.7 | 73.9 | 75.2 | 69.2 | 70.7 | 75.9 | 1.082 | 1.087 | 1.051 | 63.1 | 63.0 | 63.4 |
| 32 | R | 0.217 | 0.220 | 0.229 | 0.243 | 0.245 | 0.246 | 0.389 | 0.358 | 0.329 | 66.0 | 71.6 | 68.8 | 66.2 | 66.4 | 67.4 | 1.129 | 1.117 | 1.076 | 62.6 | 62.9 | 63.8 |
| 33 | R | 0.224 | 0.223 | 0.236 | 0.239 | 0.231 | 0.240 | 0.546 | 0.542 | 0.484 | 79.7 | 79.0 | 75.0 | 71.4 | 76.9 | 75.7 | 1.074 | 1.033 | 1.008 | 61.9 | 61.0 | 61.8 |
| 34 | R | 0.247 | 0.259 | 0.254 | 0.265 | 0.264 | 0.262 | 0.396 | 0.361 | 0.322 | 71.6 | 73.6 | 76.2 | 69.4 | 71.0 | 72.6 | 1.090 | 1.046 | 1.029 | 60.8 | 61.8 | 60.6 |
| 35 | R | 0.227 | 0.236 | 0.239 | 0.210 | 0.217 | 0.228 | 0.553 | 0.547 | 0.509 | 63.7 | 66.5 | 67.7 | 73.6 | 72.9 | 70.1 | 0.905 | 0.907 | 0.940 | 55.5 | 57.1 | 57.7 |
| 36 | R | 0.204 | 0.216 | 0.215 | 0.212 | 0.225 | 0.215 | 0.595 | 0.596 | 0.590 | 72.4 | 76.9 | 75.2 | 73.3 | 69.9 | 73.9 | 1.032 | 1.035 | 0.972 | 63.6 | 62.9 | 62.2 |
| 37 | R | 0.226 | 0.226 | 0.229 | 0.243 | 0.259 | 0.246 | 0.582 | 0.583 | 0.553 | 80.3 | 80.1 | 80.1 | 69.9 | 68.8 | 72.8 | 1.053 | 1.123 | 1.045 | 63.2 | 62.4 | 62.2 |
| 38 | R | 0.203 | 0.211 | 0.194 | 0.212 | 0.216 | 0.209 | 0.662 | 0.659 | 0.630 | 76.8 | 77.6 | 79.8 | 72.8 | 68.8 | 74.7 | 1.032 | 1.035 | 1.077 | 68.0 | 69.0 | 68.4 |
| 39 | R | 0.271 | 0.276 | 0.268 | 0.272 | 0.278 | 0.271 | 0.538 | 0.509 | 0.465 | 73.3 | 72.8 | 74.4 | 72.0 | 70.0 | 72.4 | 0.996 | 1.027 | 1.000 | 65.7 | 65.9 | 54.5 |
| 40 | R | 0.222 | 0.234 | 0.219 | 0.223 | 0.239 | 0.232 |  |  |  | 75.0 | 75.0 | 80.4 | 76.7 | 72.6 | 76.7 | 1.010 | 1.029 | 1.031 |  |  |  |
| 41 | R | 0.206 | 0.210 | 0.214 | 0.221 | 0.227 | 0.227 | 0.498 | 0.497 | 0.484 | 78.6 | 80.9 | 76.8 | 71.4 | 71.1 | 74.2 | 1.064 | 1.066 | 1.055 | 64.7 | 64.8 | 64.9 |
| 42 | R | 0.252 | 0.255 | 0.253 | 0.262 | 0.277 | 0.271 | 0.597 | 0.592 | 0.583 | 77.5 | 77.5 | 77.9 | 77.5 | 75.1 | 73.9 | 1.040 | 1.058 | 1.077 | 64.4 | 64.7 | 64.9 |
| 43 | R | 0.228 | 0.233 | 0.233 | 0.240 | 0.243 | 0.243 | 0.623 | 0.612 | 0.597 | 63.1 | 68.6 | 76.3 | 72.4 | 74.6 |  | 1.039 | 1.025 | 1.029 | 60.5 |  | 60.5 |
| 44 | R | 0.224 | 0.224 | 0.218 | 0.233 | 0.237 | 0.239 | 0.661 | 0.651 | 0.631 | 68.9 | 75.8 | 72.3 | 65.9 | 67.0 | 67.2 | 1.024 | 1.044 | 1.056 | 62.5 | 63.0 | 63.6 |
| 45 | R | 0.223 | 0.238 | 0.229 | 0.231 | 0.227 | 0.226 | 0.644 | 0.654 | 0.641 |  | 79.6 | 74.6 | 76.0 | 78.0 | 78.2 | 1.030 | 0.958 | 0.978 | 64.1 | 63.6 | 63.4 |
| 46 | R | 0.212 | 0.213 | 0.209 | 0.220 | 0.234 | 0.228 | 0.675 | 0.689 | 0.663 | 69.7 | 68.1 | 76.3 | 67.3 | 67.7 | 67.1 | 1.036 | 1.096 | 1.058 | 66.1 | 65.6 | 66.1 |
| 47 | R | 0.220 | 0.220 | 0.215 | 0.218 | 0.213 | 0.217 | 0.600 | 0.592 | 0.566 | 78.4 | 77.4 | 81.3 | 80.5 | 78.0 | 78.6 | 0.980 | 0.974 | 1.023 | 62.6 | 63.6 | 63.5 |
| 48 | R | 0.209 | 0.217 | 0.209 | 0.227 | 0.229 | 0.229 | 0.549 | 0.542 | 0.526 | 67.4 | 66.3 | 71.8 | 64.2 | 66.2 | 67.7 | 1.074 | 1.042 | 1.062 | 64.7 | 64.7 | 64.7 |
| 49 | R | 0.212 | 0.210 | 0.212 | 0.227 | 0.221 | 0.220 | 0.213 | 0.223 | 0.216 | 77.1 | 81.4 | 78.7 | 71.2 | 75.2 | 75.6 | 1.068 | 1.051 | 1.038 | 66.0 | 63.9 | 65.4 |
| 50 | R | 0.237 | 0.244 | 0.237 | 0.235 | 0.238 | 0.233 | 0.674 | 0.676 | 0.637 | 66.2 | 73.9 | 71.3 | 70.3 | 71.1 | 70.6 | 1.024 | 1.000 | 1.003 | 65.8 | 64.9 | 66.0 |
| 51 | R | 0.232 | 0.241 | 0.242 | 0.234 | 0.238 | 0.231 | 0.683 | 0.689 | 0.659 | 71.6 | 72.4 | 73.2 | 69.0 | 71.7 | 72.7 | 1.009 | 0.973 | 0.972 | 61.8 | 60.7 | 60.7 |
| 52 | R | 0.223 | 0.229 | 0.225 | 0.235 | 0.230 | 0.231 | 0.724 | 0.723 | 0.702 | 71.3 | 69.2 | 74.9 | 70.4 | 77.5 | 75.1 | 1.054 | 0.989 | 1.028 | 64.9 | 64.7 | 65.2 |
| 53 | R | 0.235 | 0.235 | 0.228 | 0.227 | 0.233 | 0.229 | 0.643 | 0.636 | 0.612 | 74.2 | 75.7 | 73.2 | 73.5 | 72.9 | 75.2 | 0.940 | 0.972 | 0.963 | 61.9 | 61.8 | 62.0 |
| 54 | R | 0.252 | 0.253 | 0.250 | 0.254 | 0.251 | 0.246 | 0.551 | 0.559 | 0.538 | 69.4 | 71.2 | 71.7 | 69.3 | 67.2 | 69.3 | 0.983 | 0.968 | 0.978 | 65.3 | 64.0 |  |
| 55 | R | 0.225 | 0.232 | 0.234 | 0.235 | 0.241 | 0.234 | 0.580 | 0.582 | 0.558 | 81.7 | 69.7 | 70.4 | 70.4 | 70.4 | 73.1 | 1.054 | 1.000 | 0.989 | 64.3 | 63.1 | 63.9 |
| 56 | R | 0.221 | 0.210 | 0.212 | 0.224 | 0.225 | 0.220 | 0.512 | 0.508 | 0.491 | 76.6 | 78.0 | 78.2 | 66.8 | 77.2 | 71.9 | 1.005 | 1.035 | 1.011 | 63.4 | 63.1 | 63.5 |
| 57 | R | 0.215 | 0.214 | 0.211 | 0.203 | 0.207 | 0.203 | 0.510 | 0.506 | 0.485 | 76.6 | 78.8 | 80.5 | 82.7 | 81.9 | 79.6 | 0.964 | 0.961 | 0.956 | 64.0 | 64.3 | 64.7 |
| 58 | R | 0.207 | 0.208 | 0.209 | 0.223 | 0.217 | 0.211 | 0.624 | 0.616 | 0.608 | 72.6 | 79.6 | 81.9 | 69.3 | 73.1 |  | 1.086 | 1.056 | 1.030 | 66.4 | 66.9 | 66.7 |
| 59 | R | 0.259 | 0.270 | 0.257 | 0.266 | 0.270 | 0.263 | 0.577 | 0.574 | 0.548 | 79.1 | 67.6 | 74.8 | 73.8 | 71.7 | 72.3 | 1.021 | 0.982 | 0.988 | 59.3 | 59.7 | 59.7 |
| 60 | R | 0.209 | 0.211 | 0.214 | 0.218 | 0.220 | 0.220 | 0.653 | 0.655 | 0.628 | 78.6 | 76.7 | 74.4 | 73.0 | 75.3 | 74.1 | 1.021 | 1.035 | 0.991 | 65.9 | 65.5 | 65.0 |
| 61 | R | 0.250 | 0.251 | 0.248 | 0.238 | 0.238 | 0.238 | 0.741 | 0.741 | 0.724 | 78.5 | 77.8 | 79.1 | 77.4 | 79.0 | 79.1 | 0.973 | 0.960 | 0.985 | 67.6 | 67.3 | 67.2 |
| 62 | R | 0.263 | 0.271 | 0.272 | 0.249 | 0.255 | 0.256 | 0.635 | 0.622 | 0.603 | 69.5 | 70.1 | 70.2 | 79.7 | 75.4 | 74.2 | 0.950 | 0.954 | 0.928 | 56.9 | 57.0 | 57.4 |
| 63 | R | 0.254 | 0.257 | 0.249 | 0.273 | 0.273 | 0.266 | 0.705 | 0.699 | 0.675 | 79.2 | 75.8 | 78.1 | 69.0 | 70.6 | 72.2 | 1.061 | 1.078 | 1.075 | 57.7 | 57.3 | 57.8 |
| 64 | R | 0.258 | 0.260 | 0.250 | 0.271 | 0.269 | 0.265 | 0.744 | 0.738 | 0.710 | 79.3 | 79.5 | 80.0 | 73.0 | 75.4 | 75.2 | 1.030 | 1.013 | 1.027 | 55.9 | 56.4 | 56.3 |
| 65 | R | 0.234 | 0.230 | 0.225 | 0.243 | 0.240 | 0.233 | 0.588 | 0.581 | 0.559 | 70.3 | 72.9 | 73.7 | 69.9 | 72.2 | 70.2 | 1.048 | 1.039 | 1.022 | 57.0 | 57.7 | 57.4 |
| 66 | R | 0.262 | 0.269 | 0.256 | 0.261 | 0.251 | 0.253 | 0.723 | 0.707 | 0.690 | 82.9 | 73.6 | 80.0 | 72.0 | 79.9 | 77.8 | 0.983 | 0.944 | 0.966 | 58.7 | 59.6 | 59.5 |
| 67 | R | 0.256 | 0.258 | 0.255 | 0.269 | 0.284 | 0.273 | 0.812 | 0.792 | 0.759 | 80.8 | 80.6 | 80.2 | 76.7 | 72.3 | 75.6 | 1.047 | 1.092 | 1.045 |  | 62.2 | 62.6 |
| 68 | R | 0.229 | 0.229 | 0.224 | 0.249 | 0.249 | 0.238 | 0.942 | 0.925 | 0.887 | 80.0 | 81.4 | 81.2 | 75.0 | 70.6 | 77.0 | 1.067 | 1.086 | 1.054 | 66.1 | 65.6 | 65.8 |
| 69 | R | 0.235 | 0.234 | 0.228 | 0.240 | 0.246 | 0.232 | 0.849 | 0.832 | 0.812 | 77.6 | 75.4 | 77.7 | 75.3 | 72.7 | 75.7 | 1.023 | 1.028 | 1.027 | 61.9 | 62.2 | 61.9 |
| 70 | S | 0.302 | 0.293 | 0.282 | 0.243 | 0.242 | 0.235 | 0.660 | 0.661 | 0.632 | 69.6 | 70.7 | 71.3 | 82.5 | 84.5 | 84.9 | 1.032 | 1.007 | 0.997 | 61.9 | 61.8 | 61.8 |
| 71 | S | 0.295 | 0.294 | 0.283 | 0.290 | 0.283 | 0.274 | 0.556 | 0.549 | 0.526 | 80.4 | 76.6 | 79.7 | 80.6 | 81.2 | 82.7 | 0.956 | 0.963 | 0.967 | 61.9 | 62.2 | 61.8 |
| 72 | S | 0.246 | 0.247 | 0.241 | 0.242 | 0.245 | 0.238 | 0.519 | 0.523 | 0.499 | 83.0 | 83.6 | 81.4 | 84.5 | 85.2 | 81.1 | 0.978 | 0.997 | 0.997 | 57.7 | 58.8 | 58.4 |
| 73 | S | 0.223 | 0.221 | 0.218 | 0.213 | 0.215 | 0.210 | 0.697 | 0.693 | 0.667 | 81.6 | 79.5 | 77.8 | 82.0 | 82.2 | 81.4 | 0.965 | 0.963 | 0.963 | 63.8 | 64.4 | 64.2 |
| 74 | S | 0.337 | 0.325 | 0.308 | 0.318 | 0.310 | 0.292 | 0.503 | 0.514 | 0.495 | 81.4 | 81.0 | 79.2 | 83.6 | 80.2 | 81.8 | 0.973 | 0.966 | 0.996 | 55.4 | 55.6 | 56.0 |

FWD Test Data (7-May-2008) (1 μm/kN = 0.175 mil/kip).

| 7-May-2008 |
| --- |
| Joint | NDf-0 | LTE | JSR |
|  | (mils/kip) | (%) |  |
|  | Approach | Leave | Approach | Leave |  |
| N | Type | Drop1 | Drop 2 | Drop 3 | Drop1 | Drop 2 | Drop 3 | Drop1 | Drop 2 | Drop 3 | Drop1 | Drop 2 | Drop 3 | Drop1 | Drop 2 | Drop 3 |
| Section 3: Untreated |
| 1 | R | 0.281 | 0.292 | 0.283 | 0.270 | 0.268 | 0.267 | 50.7 | 56.3 | 60.4 | 75.0 | 77.1 | 77.8 | 1.051 | 0.981 | 1.007 |
| 2 | R | 0.285 | 0.285 | 0.286 | 0.264 | 0.260 | 0.259 | 63.7 | 66.3 | 66.1 | 80.8 | 83.5 | 83.7 | 0.932 | 0.922 | 0.918 |
| 3 | R | 0.268 | 0.262 | 0.258 | 0.256 | 0.254 | 0.251 |  | 64.0 | 68.0 | 71.8 | 75.2 | 77.1 | 0.946 | 0.974 | 0.980 |
| 4 | S | 0.267 | 0.273 | 0.271 | 0.293 | 0.302 | 0.295 | 74.9 | 73.9 | 74.7 | 64.9 | 65.6 | 67.5 | 1.091 | 1.094 | 1.085 |
| 5 | S | 0.242 | 0.241 | 0.241 | 0.268 | 0.268 | 0.265 | 80.3 | 82.1 | 79.8 | 68.6 | 68.2 | 71.4 | 1.096 | 1.117 | 1.093 |
| 6 | S | 0.262 | 0.264 | 0.259 | 0.279 | 0.282 | 0.281 | 71.2 | 73.9 | 74.9 | 65.7 | 68.0 | 65.3 | 1.090 | 1.076 | 1.085 |
| 7 | S | 0.233 | 0.234 | 0.234 | 0.276 | 0.275 | 0.270 | 72.0 | 73.5 | 77.2 | 54.7 | 60.4 | 58.7 | 1.193 | 1.186 | 1.161 |
| 8 | S | 0.208 | 0.211 | 0.210 | 0.191 | 0.197 | 0.201 | 86.0 | 83.3 | 81.8 | 80.5 | 82.1 | 82.4 | 0.935 | 0.929 | 0.967 |
| 9 | R | 0.223 | 0.233 | 0.231 | 0.220 | 0.223 | 0.222 | 69.0 | 65.9 | 71.7 | 70.8 | 74.4 | 75.6 | 0.975 | 0.953 | 0.959 |
| 10 | R | 0.213 | 0.220 | 0.218 | 0.217 | 0.212 | 0.215 | 77.1 | 79.7 | 79.0 | 81.0 | 82.5 | 82.8 | 1.016 | 0.966 | 0.977 |
| 11 | R | 0.250 | 0.252 | 0.256 | 0.250 | 0.256 | 0.252 | 75.2 | 75.0 | 75.7 | 78.2 | 78.1 | 80.8 | 0.996 | 1.033 | 0.995 |
| Section 2: Rubblized |
| 1 | R | 0.351 | 0.350 | 0.345 | 0.370 | 0.367 | 0.359 | 69.5 | 66.7 | 70.9 | 60.1 | 63.3 | 63.9 | 1.051 | 1.058 | 1.051 |
| 2 | R | 0.361 | 0.364 | 0.358 | 0.358 | 0.359 | 0.349 | 53.5 | 62.0 | 63.0 | 73.1 | 76.8 | 81.3 | 0.991 | 0.995 | 0.982 |
| 3 | R | 0.384 | 0.386 | 0.389 | 0.363 | 0.366 | 0.369 | 51.5 | 51.3 | 54.3 | 71.5 | 74.5 | 77.0 | 0.965 | 0.948 | 0.959 |
| 4 | S | 0.353 | 0.358 | 0.357 | 0.367 | 0.368 | 0.367 | 66.9 | 68.6 | 69.6 | 68.2 | 70.1 | 72.9 | 1.061 | 1.043 | 1.046 |
| 5 | S | 0.350 | 0.343 | 0.351 | 0.371 | 0.379 | 0.372 | 70.3 | 72.3 | 72.5 | 69.7 | 70.9 | 72.5 | 1.050 | 1.040 | 1.039 |
| 6 | S | 0.467 | 0.479 | 0.469 | 0.495 | 0.496 | 0.488 | 21.6 | 24.6 | 23.0 | 23.9 | 24.1 | 26.6 | 1.043 | 1.035 | 1.041 |
| 7 | S | 0.332 | 0.338 | 0.333 | 0.352 | 0.353 | 0.356 | 61.8 | 62.2 | 64.4 | 64.5 | 67.3 | 67.6 | 1.023 | 1.017 | 1.031 |
| 8 | S | 0.423 | 0.426 | 0.417 | 0.419 | 0.427 | 0.415 | 34.8 | 35.6 | 40.2 | 41.2 | 42.1 | 44.5 | 0.971 | 1.008 | 1.008 |
| 9 | R | 0.309 | 0.311 | 0.303 | 0.327 | 0.337 | 0.325 | 64.7 | 66.4 | 70.1 | 57.6 | 60.5 | 64.4 | 1.068 | 1.075 | 1.053 |
| 10 | R | 0.288 | 0.295 | 0.281 | 0.296 | 0.298 | 0.295 | 73.1 | 78.0 | 79.1 | 75.8 | 79.1 | 79.9 | 1.015 | 1.011 | 1.009 |
| 11 | R | 0.321 | 0.329 | 0.324 | 0.331 | 0.341 | 0.328 | 56.1 | 59.8 | 62.8 | 69.4 | 72.1 | 74.0 | 1.028 | 1.030 | 1.027 |
| Section 1: Crack & Seated |
| 1 | R | 0.289 | 0.301 | 0.295 | 0.327 | 0.336 | 0.331 | 74.2 | 71.5 | 76.5 | 63.4 | 64.6 | 66.4 | 1.123 | 1.116 | 1.121 |
| 2 | R | 0.289 | 0.296 | 0.294 | 0.276 | 0.295 | 0.290 |  | 64.1 | 65.8 | 66.8 | 69.5 | 74.3 | 0.938 | 0.983 | 0.983 |
| 3 | R | 0.326 | 0.333 | 0.336 | 0.326 | 0.336 | 0.340 | 74.8 | 77.2 | 76.0 | 71.2 | 71.8 | 73.0 | 0.993 | 1.025 | 1.000 |
| 4 | S | 0.245 | 0.254 | 0.258 | 0.247 | 0.256 | 0.260 | 82.4 | 82.1 | 82.3 | 80.4 | 82.0 | 80.4 | 1.014 | 0.997 | 1.015 |
| 5 | S | 0.235 | 0.242 | 0.241 | 0.257 | 0.268 | 0.268 | 79.4 | 79.9 | 81.8 | 73.2 | 72.9 | 73.3 | 1.079 | 1.092 | 1.100 |
| 6 | S | 0.268 | 0.282 | 0.281 | 0.316 | 0.323 | 0.324 | 73.3 | 73.8 | 74.8 | 65.7 | 65.9 | 66.4 | 1.177 | 1.138 | 1.134 |
| 7 | S | 0.261 | 0.279 | 0.282 | 0.249 | 0.252 | 0.256 | 76.4 | 79.3 | 80.8 | 74.8 | 75.2 | 76.2 | 1.017 | 1.051 | 1.031 |
| 8 | S | 0.250 | 0.254 | 0.258 | 0.284 | 0.290 | 0.295 | 83.6 | 79.3 | 82.2 | 69.0 | 72.2 | 72.7 | 1.198 | 1.196 | 1.202 |
| 9 | R | 0.254 | 0.256 | 0.258 | 0.266 | 0.268 | 0.267 | 57.5 | 61.3 | 63.3 | 63.9 | 65.2 | 68.1 | 1.044 | 1.066 | 1.049 |
| 10 | R | 0.321 | 0.324 | 0.326 | 0.292 | 0.304 | 0.301 | 55.5 | 50.1 | 53.8 | 74.3 | 72.9 | 77.1 | 0.914 | 0.929 | 0.916 |
| 11 | R | 0.211 | 0.231 | 0.237 | 0.281 | 0.289 | 0.285 | 77.5 | 78.2 | 78.5 | 64.4 | 66.1 | 68.3 | 1.172 | 1.265 | 1.218 |

FWD Test Data (C&S Section, 21-October-2008) (1 μm/kN = 0.175 mil/kip).

| Section 1: Cracked & Seated |
| --- |
| 21-October-2008 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.295 | 0.304 | 0.302 | 0.347 | 0.344 | 0.340 | 0.197 | 0.197 | 0.204 | 80.3 | 82.6 | 81.1 | 72.7 | 74.7 | 76.1 | 1.156 | 1.131 | 1.119 |  | 71.2 | 69.7 |
| 2 | R | 0.369 | 0.374 | 0.368 | 0.390 | 0.388 | 0.383 | 0.192 | 0.199 | 0.202 | 64.8 | 63.9 | 66.0 | 64.1 | 65.9 | 68.1 | 1.057 | 1.045 | 1.029 | 70.8 | 71.8 | 71.8 |
| 3 | R | 0.352 | 0.359 | 0.356 | 0.367 | 0.368 | 0.364 | 0.192 | 0.207 | 0.210 | 68.3 | 62.6 | 66.7 | 68.0 | 71.6 | 72.4 | 1.041 | 1.023 | 1.035 | 78.9 | 76.6 | 76.7 |
| 4 | R | 0.358 | 0.370 | 0.366 | 0.368 | 0.381 | 0.377 | 0.257 | 0.267 | 0.266 | 70.6 | 69.9 | 72.8 | 77.7 | 77.5 | 79.7 | 1.015 | 1.025 | 1.012 | 78.4 | 77.5 | 77.2 |
| 5 | R | 0.378 | 0.373 | 0.371 | 0.398 | 0.396 | 0.390 | 0.228 | 0.233 | 0.240 | 72.0 | 77.0 | 74.8 | 74.7 | 75.7 | 76.7 | 1.062 | 1.076 | 1.057 | 73.3 | 74.0 | 72.6 |
| 6 | R | 0.398 | 0.405 | 0.395 | 0.418 | 0.417 | 0.407 | 0.254 | 0.258 | 0.260 | 66.3 | 68.0 | 69.2 | 68.8 | 70.0 | 71.7 | 1.062 | 1.033 | 1.029 |  | 69.8 | 69.4 |
| 7 | R | 0.350 | 0.349 | 0.352 | 0.395 | 0.403 | 0.391 | 0.204 | 0.211 | 0.216 | 70.5 | 72.7 | 74.6 | 66.1 | 66.9 | 70.0 | 1.124 | 1.151 | 1.110 | 71.7 | 73.0 | 72.4 |
| 8 | R | 0.400 | 0.406 | 0.399 | 0.433 | 0.437 | 0.426 | 0.198 | 0.208 | 0.210 | 70.5 | 71.7 | 73.1 | 67.9 | 69.1 | 71.0 | 1.084 | 1.083 | 1.069 | 71.8 | 71.2 | 72.0 |
| 9 | R | 0.398 | 0.394 | 0.385 | 0.395 | 0.391 | 0.389 | 0.199 | 0.203 | 0.207 | 60.8 | 63.5 | 66.5 | 65.1 | 67.7 | 70.5 | 1.009 | 0.998 | 1.005 | 70.1 | 69.3 | 70.5 |
| 10 | R | 0.283 | 0.290 | 0.293 | 0.308 | 0.311 | 0.314 | 0.183 | 0.186 | 0.193 | 66.4 | 67.7 | 69.3 | 64.3 | 66.8 | 68.6 | 1.082 | 1.066 | 1.072 | 68.4 | 70.2 | 70.1 |
| 11 | R | 0.356 | 0.361 | 0.364 | 0.379 | 0.388 | 0.384 | 0.209 | 0.204 | 0.210 | 67.8 | 68.4 | 68.7 | 63.6 | 64.3 | 66.0 | 1.072 | 1.079 | 1.059 |  | 72.6 | 71.6 |
| 12 | R | 0.361 | 0.368 | 0.365 | 0.366 | 0.382 | 0.373 | 0.241 | 0.248 | 0.257 | 67.4 | 68.5 | 69.2 | 69.3 | 70.0 | 73.8 | 0.982 | 1.021 | 1.010 | 71.6 | 73.2 | 72.7 |
| 13 | R | 0.479 | 0.479 | 0.470 | 0.506 | 0.504 | 0.493 | 0.252 | 0.265 | 0.267 | 67.0 | 68.9 | 71.3 | 63.4 | 66.2 | 69.0 | 1.056 | 1.054 | 1.051 | 69.4 | 68.3 | 69.2 |
| 14 | S | 0.368 | 0.372 | 0.372 | 0.383 | 0.390 | 0.385 | 0.213 | 0.221 | 0.226 | 73.1 | 72.8 | 74.9 | 70.8 | 69.9 | 69.7 | 1.036 | 1.045 | 1.034 | 66.1 | 68.2 | 67.7 |
| 15 | S | 0.349 | 0.352 | 0.352 | 0.393 | 0.395 | 0.389 | 0.203 | 0.210 | 0.212 | 68.9 | 69.4 | 69.9 | 63.1 | 62.7 | 63.8 | 1.101 | 1.123 | 1.113 |  | 66.1 | 66.9 |
| 16 | S | 0.386 | 0.393 | 0.392 | 0.420 | 0.427 | 0.418 | 0.187 | 0.195 | 0.199 | 51.7 | 53.1 | 53.8 | 52.0 | 53.6 | 54.7 | 1.071 | 1.075 | 1.067 |  | 66.7 | 67.7 |
| 17 | S | 0.341 | 0.356 | 0.351 | 0.397 | 0.400 | 0.388 | 0.201 | 0.212 | 0.216 | 67.8 | 66.9 | 67.9 | 58.8 | 59.9 | 62.0 | 1.174 | 1.124 | 1.098 | 63.4 | 63.4 | 63.9 |
| 18 | S | 0.349 | 0.356 | 0.357 | 0.365 | 0.376 | 0.375 | 0.199 | 0.204 | 0.207 | 65.8 | 66.2 | 67.5 | 66.4 | 65.9 | 65.2 | 1.054 | 1.068 | 1.047 |  | 61.7 | 62.5 |
| 19 | R | 0.352 | 0.352 | 0.349 | 0.371 | 0.369 | 0.357 | 0.169 | 0.176 | 0.180 | 54.4 | 55.9 | 58.4 | 58.5 | 61.0 | 64.6 | 1.060 | 1.047 | 1.034 | 65.7 | 66.0 | 66.8 |
| 20 | R | 0.477 | 0.480 | 0.459 | 0.448 | 0.447 | 0.434 | 0.160 | 0.158 | 0.161 | 59.9 | 60.2 | 60.7 | 74.3 | 74.6 | 77.2 | 0.942 | 0.937 | 0.947 | 66.0 | 67.5 | 69.3 |
| 21 | R | 0.354 | 0.353 | 0.344 | 0.410 | 0.403 | 0.390 | 0.187 | 0.192 | 0.197 | 61.5 | 61.6 | 63.4 | 60.1 | 61.8 | 63.9 | 1.161 | 1.143 | 1.137 |  | 68.6 | 68.3 |
| 22 | R | 0.349 | 0.344 | 0.334 | 0.378 | 0.368 | 0.352 | 0.178 | 0.182 | 0.186 | 68.2 | 69.8 | 71.9 | 59.9 | 65.7 | 68.5 | 1.090 | 1.078 | 1.054 | 64.8 | 65.2 | 64.7 |
| 23 | R | 0.394 | 0.398 | 0.391 | 0.462 | 0.454 | 0.435 | 0.173 | 0.174 | 0.181 | 58.0 | 62.8 | 61.0 | 60.2 | 61.8 | 64.5 | 1.169 | 1.139 | 1.105 |  | 69.0 | 69.1 |
| 24 | R | 0.439 | 0.438 | 0.418 | 0.440 | 0.436 | 0.424 | 0.174 | 0.187 | 0.190 | 54.2 | 57.1 | 60.6 | 60.0 | 62.7 | 66.6 | 1.010 | 1.020 | 1.026 |  | 64.9 | 65.9 |

FWD Test Data (Rubblized Section, 21-October-2008) (1 μm/kN = 0.175 mil/kip).

| Section 2: Rubblized |
| --- |
| 21-October-2008 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.394 | 0.399 | 0.387 | 0.420 | 0.417 | 0.404 | 0.215 | 0.222 | 0.222 | 59.1 | 59.4 | 64.2 | 56.4 | 59.2 | 62.4 | 1.069 | 1.046 | 1.059 | 64.7 | 65.1 | 65.7 |
| 2 | R | 0.401 | 0.404 | 0.393 | 0.399 | 0.399 | 0.391 | 0.201 | 0.207 | 0.209 | 53.9 | 57.5 | 62.1 | 65.2 | 68.7 |  | 1.003 | 0.998 | 0.997 | 62.8 | 63.7 | 64.9 |
| 3 | R | 0.435 | 0.435 | 0.429 | 0.435 | 0.434 | 0.422 | 0.196 | 0.200 | 0.204 | 50.1 | 51.0 | 53.8 | 62.6 | 65.7 | 67.6 | 0.985 | 0.973 | 0.977 | 64.7 | 65.3 | 65.3 |
| 4 | S | 0.463 | 0.457 | 0.446 | 0.480 | 0.473 | 0.462 | 0.210 | 0.212 | 0.216 | 55.2 | 56.8 | 57.9 | 62.6 | 64.2 | 65.9 | 1.041 | 1.042 | 1.040 | 69.6 | 71.0 | 70.8 |
| 5 | S | 0.481 | 0.478 | 0.470 | 0.541 | 0.534 | 0.521 | 0.216 | 0.225 | 0.229 | 64.2 | 64.7 | 65.6 | 60.3 | 61.4 | 62.3 | 1.103 | 1.108 | 1.100 | 69.2 | 69.1 | 69.5 |
| 6 | S | 0.607 | 0.602 | 0.587 | 0.653 | 0.639 | 0.614 | 0.188 | 0.196 | 0.199 | 17.1 | 19.8 | 21.7 | 18.6 | 21.1 | 23.0 | 1.087 | 1.069 | 1.044 |  | 68.2 | 68.3 |
| 7 | S | 0.487 | 0.482 | 0.469 | 0.476 | 0.471 | 0.459 | 0.176 | 0.184 | 0.189 | 51.4 | 51.6 | 52.8 | 60.6 | 63.7 | 65.3 | 0.972 | 0.971 | 0.985 | 70.7 | 69.2 | 69.7 |
| 8 | S | 0.659 | 0.646 | 0.615 | 0.694 | 0.669 | 0.637 | 0.189 | 0.188 | 0.194 | 34.0 | 37.0 | 40.0 | 30.8 | 33.7 | 36.6 | 1.061 | 1.052 | 1.054 | 63.5 | 67.5 | 66.7 |
| 9 | R | 0.396 | 0.394 | 0.383 | 0.398 | 0.403 | 0.390 | 0.185 | 0.186 | 0.189 | 62.5 | 64.2 | 66.5 | 63.0 | 63.9 | 66.2 | 1.011 | 1.021 | 1.021 | 63.5 | 64.9 | 65.1 |
| 10 | R | 0.350 | 0.353 | 0.352 | 0.354 | 0.361 | 0.358 | 0.174 | 0.181 | 0.184 | 72.5 | 74.1 | 74.9 | 72.9 | 74.4 | 74.6 | 1.003 | 1.021 | 1.016 | 63.2 | 64.1 | 64.7 |
| 11 | R | 0.422 | 0.418 | 0.410 | 0.456 | 0.452 | 0.437 | 0.165 | 0.172 | 0.175 | 69.9 | 71.7 | 72.8 | 66.2 | 68.1 | 70.3 | 1.093 | 1.088 | 1.063 | 63.6 | 65.0 | 64.7 |
| 12 | R | 0.393 | 0.394 | 0.385 | 0.407 | 0.403 | 0.390 | 0.189 | 0.193 | 0.196 | 61.9 | 61.8 | 66.0 | 61.9 | 64.6 | 67.9 | 1.017 | 1.030 | 1.013 | 58.1 | 65.1 | 66.0 |
| 13 | R | 0.457 | 0.456 | 0.445 | 0.439 | 0.439 | 0.430 | 0.195 | 0.203 | 0.203 | 52.3 | 53.5 | 56.5 | 63.7 | 66.5 | 68.3 | 0.963 | 0.967 | 0.961 | 67.2 | 66.4 | 68.4 |
| 14 | R | 0.382 | 0.385 | 0.377 | 0.405 | 0.397 | 0.392 | 0.211 | 0.216 | 0.219 | 64.8 | 66.2 | 69.1 | 62.2 | 65.5 | 67.7 | 1.061 | 1.030 | 1.045 | 65.0 |  | 65.9 |
| 15 | R | 0.461 | 0.460 | 0.444 | 0.461 | 0.459 | 0.443 | 0.192 | 0.203 | 0.203 | 48.0 | 53.3 | 56.0 | 61.2 | 64.9 | 68.6 | 1.005 | 1.000 | 1.000 | 66.7 | 67.6 | 67.5 |
| 16 | R | 0.415 | 0.407 | 0.399 | 0.474 | 0.465 | 0.447 | 0.209 | 0.214 | 0.215 | 57.8 | 61.8 | 66.1 | 53.2 | 57.3 | 61.1 | 1.148 | 1.146 | 1.121 | 63.2 | 62.7 | 66.3 |
| 17 | R | 0.357 | 0.358 | 0.356 | 0.396 | 0.391 | 0.385 | 0.189 | 0.198 | 0.199 | 65.9 | 66.7 | 69.0 | 52.9 | 54.6 | 57.7 | 1.126 | 1.096 | 1.081 | 66.2 | 65.5 | 66.5 |
| 18 | R | 0.349 | 0.351 | 0.352 | 0.334 | 0.339 | 0.338 | 0.206 | 0.209 | 0.212 | 64.5 | 65.5 | 67.9 | 71.1 | 72.3 | 74.0 | 0.962 | 0.957 | 0.963 |  | 66.8 | 66.4 |
| 19 | R | 0.274 | 0.281 | 0.281 | 0.297 | 0.302 | 0.301 | 0.194 | 0.204 | 0.207 | 81.0 | 80.5 | 81.1 | 77.7 | 77.1 | 77.0 | 1.067 | 1.071 | 1.055 | 64.6 | 63.2 | 64.5 |
| 20 | R | 0.307 | 0.316 | 0.314 | 0.334 | 0.340 | 0.342 | 0.172 | 0.181 | 0.184 | 64.8 | 67.1 | 68.2 | 64.2 | 64.1 | 64.2 | 1.084 | 1.072 | 1.090 | 63.4 | 63.5 | 64.4 |
| 21 | R | 0.261 | 0.266 | 0.267 | 0.287 | 0.289 | 0.292 | 0.164 | 0.167 | 0.169 | 78.0 | 79.8 | 80.8 | 73.5 | 74.6 | 75.4 | 1.089 | 1.091 | 1.096 |  |  | 65.2 |
| 22 | R | 0.310 | 0.324 | 0.318 | 0.310 | 0.317 | 0.313 | 0.171 | 0.180 | 0.182 | 63.6 | 62.8 | 62.5 | 66.7 | 68.2 | 70.5 | 0.996 | 0.982 | 0.984 | 62.1 | 63.3 | 63.3 |
| 23 | R | 0.253 | 0.257 | 0.256 | 0.283 | 0.290 | 0.285 |  |  | 0.179 | 75.8 | 80.8 | 79.1 | 74.5 | 74.4 | 75.3 | 1.123 | 1.134 | 1.102 |  |  | 64.5 |
| 24 | R | 0.254 | 0.265 | 0.263 | 0.268 | 0.280 | 0.277 | 0.168 | 0.175 | 0.177 | 78.6 | 77.3 | 78.3 | 75.1 | 72.0 | 75.3 | 1.076 | 1.073 | 1.075 | 64.4 | 63.8 | 65.1 |
| 25 | R | 0.291 | 0.300 | 0.292 | 0.316 | 0.316 | 0.310 | 0.184 | 0.188 | 0.192 | 70.0 | 67.9 | 68.1 | 61.3 | 63.9 | 65.7 | 1.080 | 1.050 | 1.049 | 65.8 | 66.7 | 65.9 |
| 26 | R | 0.277 | 0.285 | 0.285 | 0.299 | 0.302 | 0.301 | 0.184 | 0.185 | 0.189 | 81.4 | 80.2 | 81.3 | 75.8 | 76.9 | 78.4 | 1.063 | 1.050 | 1.057 | 63.8 | 65.5 | 65.8 |

FWD Test Data (Untreated Section, 21-October-2008) (1 μm/kN = 0.175 mil/kip).

| Section 3: Untreated |
| --- |
| 21-October-2008 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.455 | 0.448 | 0.419 | 0.430 | 0.422 | 0.400 | 0.185 | 0.190 | 0.193 | 58.6 | 63.6 | 67.8 | 64.5 | 67.9 | 71.5 | 0.953 | 0.948 | 0.939 |  |  |  |
| 2 | R | 0.387 | 0.387 | 0.374 | 0.408 | 0.425 | 0.406 | 0.164 | 0.175 | 0.173 | 51.5 | 54.8 | 57.2 | 51.1 | 55.9 | 60.2 | 1.064 | 1.100 | 1.093 | 76.3 |  | 77.5 |
| 3 | R | 0.449 | 0.438 | 0.419 | 0.462 | 0.457 | 0.441 | 0.156 | 0.159 | 0.162 | 62.2 | 65.1 | 66.0 | 62.8 | 65.1 | 67.0 | 1.017 | 1.042 | 1.049 |  | 72.2 | 71.2 |
| 4 | R | 0.357 | 0.352 | 0.339 | 0.363 | 0.358 | 0.348 | 0.158 | 0.168 | 0.170 | 60.8 | 65.4 | 68.4 | 61.7 | 65.0 | 68.9 | 1.032 | 1.024 | 1.035 | 71.4 | 69.5 | 69.7 |
| 5 | R | 0.317 | 0.316 | 0.314 | 0.345 | 0.339 | 0.335 | 0.182 | 0.192 | 0.192 | 57.4 | 57.9 | 60.0 | 54.8 | 56.0 | 60.0 | 1.113 | 1.077 | 1.070 | 75.6 | 73.1 | 72.3 |
| 6 | R | 0.330 | 0.329 | 0.328 | 0.372 | 0.372 | 0.369 | 0.153 | 0.163 | 0.165 | 71.9 | 71.9 | 72.3 | 59.2 | 59.5 | 60.6 | 1.140 | 1.133 | 1.129 |  |  |  |
| 7 | R | 0.405 | 0.401 | 0.386 | 0.424 | 0.417 | 0.401 | 0.144 | 0.152 | 0.154 | 57.9 | 59.7 | 62.0 | 61.6 | 64.0 | 65.8 | 1.055 | 1.044 | 1.041 | 72.9 | 72.4 | 72.9 |
| 8 | R | 0.382 | 0.376 | 0.362 | 0.373 | 0.362 | 0.352 | 0.160 | 0.152 | 0.158 | 59.9 | 61.3 | 63.5 | 65.8 | 69.2 | 70.9 | 0.991 | 0.971 | 0.976 | 68.9 | 71.8 | 71.3 |
| 9 | R | 0.396 | 0.389 | 0.372 | 0.395 | 0.384 | 0.368 | 0.160 | 0.170 | 0.164 | 64.2 | 61.9 | 66.7 | 64.6 | 67.9 | 70.6 | 1.011 | 0.991 | 0.995 | 67.8 | 66.1 | 68.4 |
| 10 | S | 0.565 | 0.544 | 0.519 | 0.786 | 0.723 | 0.654 | 0.163 | 0.166 | 0.166 | 35.3 | 38.1 | 40.7 | 26.0 | 29.4 | 32.8 | 1.373 | 1.320 | 1.267 | 76.7 | 76.9 | 76.7 |
| 11 | S | 0.490 | 0.484 | 0.463 | 0.497 | 0.477 | 0.451 | 0.164 | 0.168 | 0.172 | 57.8 | 60.0 | 59.9 | 59.1 | 62.0 | 63.6 | 1.021 | 0.984 | 0.972 | 75.1 | 75.8 | 75.2 |
| 12 | S | 0.829 | 0.782 | 0.702 | 0.880 | 0.806 | 0.715 | 0.207 | 0.204 | 0.205 | 57.5 | 58.8 | 60.6 | 51.7 | 53.4 | 55.2 | 1.066 | 1.042 | 1.024 |  |  |  |
| 13 | S | 0.804 | 0.755 | 0.685 | 0.763 | 0.712 | 0.652 | 0.195 | 0.205 | 0.203 | 53.7 | 54.5 | 55.3 | 68.5 | 70.0 | 71.3 | 0.957 | 0.954 | 0.961 |  |  |  |
| 14 | S | 0.368 | 0.359 | 0.346 | 0.391 | 0.390 | 0.373 | 0.186 | 0.189 | 0.189 | 68.7 | 70.3 | 71.1 | 73.3 | 72.9 | 74.1 | 1.082 | 1.096 | 1.085 |  | 73.3 | 74.1 |
| 15 | R | 0.331 | 0.331 | 0.321 | 0.325 | 0.331 | 0.322 | 0.163 | 0.170 | 0.172 | 61.5 | 64.1 | 65.3 | 67.5 | 66.5 | 69.8 | 0.986 | 1.005 | 1.008 |  | 70.2 | 69.4 |
| 16 | R | 0.293 | 0.291 | 0.286 | 0.325 | 0.326 | 0.325 | 0.156 | 0.161 | 0.158 | 75.5 | 74.4 | 76.6 | 76.8 | 76.6 | 77.7 | 1.091 | 1.135 | 1.138 | 70.8 | 70.7 | 72.6 |
| 17 | R | 0.294 | 0.303 | 0.299 | 0.337 | 0.340 | 0.334 | 0.148 | 0.153 | 0.154 | 70.7 | 71.1 | 69.8 | 63.0 | 62.3 | 63.9 | 1.128 | 1.118 | 1.108 | 70.7 | 71.6 | 72.7 |
| 18 | R | 0.334 | 0.335 | 0.328 | 0.359 | 0.361 | 0.353 | 0.192 | 0.197 | 0.200 | 80.7 | 80.3 | 80.0 | 77.1 | 78.3 | 78.5 | 1.077 | 1.085 | 1.074 | 70.5 | 71.7 | 71.2 |
| 19 | R | 0.330 | 0.332 | 0.332 | 0.344 | 0.350 | 0.346 | 0.182 | 0.183 | 0.188 | 69.4 | 75.7 | 76.2 | 74.4 | 73.5 | 74.8 | 1.061 | 1.068 | 1.042 | 72.7 | 72.7 | 72.4 |

FWD Test Data (C&S Section, 13-May-2009) (1 μm/kN = 0.175 mil/kip).

| Section 1: Cracked & Seated |
| --- |
| 13-May-2009 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.348 | 0.359 | 0.360 | 0.386 | 0.382 | 0.373 | 0.533 | 0.525 | 0.506 | 69.1 | 64.1 | 65.6 | 58.3 | 62.5 | 66.6 | 1.088 | 1.043 | 1.029 | 60.3 | 60.0 |  |
| 2 | S | 0.316 | 0.323 | 0.324 | 0.341 | 0.352 | 0.353 | 0.587 | 0.581 | 0.553 | 71.1 | 73.7 | 73.3 | 66.7 | 65.0 | 67.7 | 1.088 | 1.082 | 1.085 | 61.7 | 62.4 |  |
| 3 | S | 0.342 | 0.350 | 0.349 | 0.422 | 0.420 | 0.414 | 0.752 | 0.750 | 0.731 |  | 66.7 | 69.2 | 50.1 | 53.8 | 54.0 | 1.203 | 1.191 | 1.170 | 64.8 | 64.3 | 64.7 |
| 4 | S | 0.419 | 0.428 | 0.426 | 0.444 | 0.451 | 0.442 | 0.631 | 0.628 | 0.603 | 53.1 | 47.8 | 47.8 | 45.7 | 48.0 | 50.3 | 1.056 | 1.047 | 1.020 | 62.3 |  |  |
| 5 | S | 0.316 | 0.318 | 0.319 | 0.320 | 0.330 | 0.329 | 0.660 | 0.662 | 0.644 | 68.8 | 71.9 | 73.4 |  | 67.8 |  | 0.990 | 1.023 | 1.017 | 64.3 | 64.7 | 65.0 |
| 6 | S | 0.381 | 0.387 | 0.386 | 0.398 | 0.399 | 0.396 | 0.656 | 0.658 | 0.641 | 55.5 | 52.6 | 51.4 | 47.8 | 50.0 | 52.5 | 1.035 | 1.030 | 1.002 | 63.5 |  |  |
| 7 | R | 0.311 | 0.320 | 0.316 | 0.312 | 0.317 | 0.314 | 0.666 | 0.662 | 0.649 | 69.1 | 68.5 | 70.8 | 63.7 | 67.1 |  | 0.986 | 0.980 | 0.973 | 63.5 |  |  |
| 8 | R | 0.316 | 0.321 | 0.320 | 0.334 | 0.342 | 0.336 | 0.577 | 0.584 | 0.567 | 76.2 | 73.7 | 76.2 | 67.2 | 68.4 | 70.6 | 1.056 | 1.062 | 1.046 | 61.4 | 61.4 | 61.3 |
| 9 | R | 0.335 | 0.340 | 0.336 | 0.344 | 0.345 | 0.341 | 0.643 | 0.644 | 0.630 | 60.6 | 64.4 | 65.5 | 66.3 | 66.9 | 69.2 | 1.033 | 1.002 | 1.011 | 61.7 | 62.0 |  |
| 10 | R | 0.308 | 0.312 | 0.314 | 0.301 | 0.309 | 0.306 | 0.703 | 0.698 | 0.680 | 59.7 | 63.6 | 65.6 | 65.8 | 68.0 | 68.8 | 0.951 | 0.974 | 0.967 | 62.0 | 62.4 |  |
| 11 | R | 0.341 | 0.347 | 0.348 | 0.330 | 0.340 | 0.335 | 0.848 | 0.851 | 0.830 | 73.1 | 70.5 | 71.9 | 73.2 | 73.4 | 74.4 | 0.968 | 0.976 | 0.973 | 65.7 |  |  |
| 12 | R | 0.410 | 0.403 | 0.395 | 0.397 | 0.403 | 0.397 | 0.979 | 0.985 | 0.971 | 69.0 | 70.6 | 73.0 | 73.7 | 73.0 | 73.5 | 0.957 | 1.004 | 0.989 | 66.7 |  | 66.4 |
| 13 | R | 0.389 | 0.389 | 0.386 | 0.396 | 0.397 | 0.391 | 0.771 | 0.785 | 0.760 | 71.2 | 68.4 | 71.0 | 70.6 | 71.4 | 73.3 | 1.017 | 0.994 | 0.990 | 63.8 | 63.2 | 64.1 |
| 14 | R | 0.357 | 0.357 | 0.354 | 0.368 | 0.371 | 0.361 | 0.758 | 0.759 | 0.738 | 65.1 | 64.6 | 66.3 | 61.1 | 61.0 | 65.8 | 1.015 | 1.014 | 1.005 | 63.3 | 62.4 | 63.0 |
| 15 | R | 0.386 | 0.387 | 0.378 | 0.347 | 0.358 | 0.353 | 0.567 | 0.567 | 0.549 | 57.1 | 58.0 | 62.1 | 66.7 | 67.4 | 69.2 | 0.900 | 0.942 | 0.909 | 58.9 | 58.6 |  |
| 16 | R | 0.338 | 0.340 | 0.336 | 0.354 | 0.359 | 0.359 | 0.781 | 0.783 | 0.763 | 63.9 | 67.8 | 70.8 | 61.4 | 61.7 | 64.9 | 1.036 | 1.056 | 1.063 | 66.4 | 66.0 | 66.0 |
| 17 | R | 0.371 | 0.371 | 0.369 | 0.376 | 0.375 | 0.370 | 0.685 | 0.692 | 0.678 | 58.8 | 57.0 | 62.8 | 57.7 | 60.6 | 62.0 | 1.003 | 1.011 | 1.000 | 67.2 | 67.0 |  |
| 18 | R | 0.364 | 0.364 | 0.355 | 0.358 | 0.353 | 0.346 | 0.460 | 0.461 | 0.454 | 57.0 | 61.3 | 65.0 | 63.8 | 65.4 | 68.2 | 0.985 | 0.973 | 0.982 | 60.0 | 60.1 | 60.1 |
| 19 | R | 0.316 | 0.322 | 0.324 | 0.327 | 0.330 | 0.320 | 0.543 | 0.545 | 0.539 | 58.5 | 61.2 | 60.5 | 59.5 | 63.8 | 68.1 | 1.014 | 1.028 | 0.996 | 61.1 | 61.8 | 61.9 |
| 20 | R | 0.288 | 0.297 | 0.294 | 0.296 | 0.303 | 0.302 | 0.606 | 0.619 | 0.584 | 79.3 | 81.2 | 79.5 | 77.2 | 81.3 | 81.7 | 1.008 | 1.020 | 1.004 | 58.3 |  |  |

FWD Test Data (Rubblized Section, 13-May-2009) (1 μm/kN = 0.175 mil/kip).

| Section 2: Rubblized |
| --- |
| 13-May-2009 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | RJ | 0.286 | 0.299 | 0.311 | 0.287 | 0.302 | 0.311 | 0.342 | 0.346 | 0.352 | 62.1 | 64.1 | 66.2 | 63.0 | 60.7 | 60.5 | 1.004 | 1.013 | 1.002 | 64.2 | 65.5 | 65.4 |
| 2 | RJ | 0.286 | 0.308 | 0.317 | 0.293 | 0.310 | 0.318 | 0.309 | 0.316 | 0.320 | 76.4 | 77.0 | 78.5 | 72.8 | 75.6 | 75.4 | 1.025 | 1.008 | 1.004 | 61.0 | 61.3 | 62.0 |
| 3 | RJ | 0.319 | 0.335 | 0.348 | 0.320 | 0.329 | 0.337 | 0.286 | 0.290 | 0.296 | 53.4 | 54.4 | 55.2 | 56.7 | 61.0 | 63.5 | 1.010 | 0.988 | 0.981 | 61.5 | 62.4 | 62.9 |
| 4 | SJ | 0.331 | 0.344 | 0.359 | 0.337 | 0.344 | 0.357 | 0.336 | 0.342 | 0.346 | 59.1 | 60.9 | 61.8 | 56.5 | 59.7 | 61.1 | 1.013 | 1.000 | 0.996 | 64.8 | 65.3 | 65.7 |
| 5 | SJ | 0.302 | 0.318 | 0.324 | 0.330 | 0.339 | 0.348 | 0.355 | 0.360 | 0.363 | 68.3 | 68.3 | 69.5 | 59.0 | 59.7 | 61.2 | 1.082 | 1.059 | 1.060 | 67.6 | 67.6 | 67.6 |
| 6 | SJ | 0.352 | 0.368 | 0.380 | 0.446 | 0.456 | 0.470 | 0.287 | 0.291 | 0.294 | 104.1 | 103.8 | 104.4 | 70.6 | 73.0 | 72.4 | 1.259 | 1.232 | 1.230 | 64.3 | 64.6 | 65.0 |
| 7 | SJ | 0.340 | 0.351 | 0.360 | 0.289 | 0.297 | 0.310 | 0.262 | 0.266 | 0.273 | 54.1 | 56.7 | 57.9 | 58.6 | 60.8 | 61.9 | 0.850 | 0.848 | 0.860 | 63.4 | 63.7 | 64.2 |
| 8 | SJ | 0.371 | 0.384 | 0.396 | 0.335 | 0.341 | 0.353 | 0.351 | 0.356 | 0.357 | 35.8 | 38.4 | 40.3 | 36.9 | 41.7 | 43.2 | 0.908 | 0.895 | 0.902 | 66.8 | 66.2 | 66.0 |
| 9 | RJ | 0.262 | 0.273 | 0.283 | 0.269 | 0.276 | 0.286 | 0.417 | 0.404 | 0.403 | 64.5 | 66.9 | 68.1 | 60.2 | 61.7 | 62.4 | 1.020 | 1.014 | 1.016 | 68.8 | 69.9 | 69.5 |
| 10 | RJ | 0.267 | 0.282 | 0.291 | 0.267 | 0.278 | 0.289 | 0.449 | 0.454 | 0.458 | 75.6 | 76.3 | 77.6 | 70.2 | 71.9 | 72.5 | 1.000 | 0.994 | 1.016 | 67.2 | 67.3 | 67.3 |
| 11 | RJ | 0.266 | 0.277 | 0.285 | 0.270 | 0.277 | 0.287 | 0.506 | 0.509 | 0.512 | 67.7 | 68.3 | 69.5 | 68.6 | 66.4 | 67.0 | 1.016 | 1.003 | 1.007 | 68.3 | 67.8 | 67.7 |
| 12 | RJ | 0.248 | 0.260 | 0.268 | 0.251 | 0.263 | 0.270 | 0.349 | 0.347 | 0.351 | 63.4 | 65.0 | 66.0 | 71.4 | 55.7 | 62.1 | 1.013 | 1.006 | 1.007 | 63.9 | 64.8 | 64.8 |
| 13 | RJ | 0.282 | 0.288 | 0.297 | 0.266 | 0.276 | 0.284 | 0.310 | 0.312 | 0.316 | 58.3 | 60.9 | 63.3 | 59.6 | 61.0 | 63.0 | 0.941 | 0.962 | 0.967 | 64.6 | 64.3 | 64.5 |
| 14 | RJ | 0.283 | 0.295 | 0.305 | 0.314 | 0.325 | 0.333 | 0.645 | 0.642 | 0.639 | 68.1 | 71.1 | 71.9 | 60.1 | 53.3 | 59.3 | 1.103 | 1.110 | 1.105 | 68.8 | 68.7 | 68.4 |
| 15 | RJ | 0.314 | 0.321 | 0.336 | 0.321 | 0.329 | 0.342 | 0.529 | 0.517 | 0.510 | 63.2 | 66.3 | 67.1 | 59.9 | 63.1 | 63.6 | 1.023 | 1.034 | 1.032 | 70.1 | 70.2 | 69.9 |
| 16 | RJ | 0.271 | 0.282 | 0.291 | 0.284 | 0.289 | 0.298 | 0.517 | 0.515 | 0.517 | 69.9 | 71.0 | 72.2 | 67.0 | 61.1 | 64.5 | 1.054 | 1.031 | 1.034 | 71.3 | 71.7 | 71.5 |
| 17 | RJ | 0.286 | 0.296 | 0.304 | 0.275 | 0.288 | 0.296 | 0.391 | 0.392 | 0.396 | 63.4 | 64.5 | 65.9 | 60.8 | 62.1 | 63.0 | 0.963 | 0.973 | 0.970 | 68.2 | 67.9 | 68.4 |

FWD Test Data (Untreated Section, 13-May-2009) (1 μm/kN = 0.175 mil/kip).

| Section 3: Untreated |
| --- |
| 13-May-2009 |
| Joint | NDf-0 | LTE | JSR | Mid-Slab SPR |
|  | (mils/kip) | (%) |  |  |
|  | Approach | Leave | Mid-Slab | Approach | Leave |  | (%) |
| N | Type | Drop | Drop | Drop | Drop | Drop | Drop | Drop |
|  |  | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 | 1 | 2 | 3 |
| 1 | R | 0.210 | 0.218 | 0.219 | 0.233 | 0.240 | 0.240 | 0.216 | 0.218 | 0.217 | 61.9 | 64.4 | 66.8 | 60.6 | 61.2 | 64.2 | 1.101 | 1.096 | 1.097 | 63.7 | 64.4 | 65.3 |
| 2 | R | 0.221 | 0.230 | 0.220 | 0.199 | 0.207 | 0.213 | 0.174 | 0.169 | 0.166 | 52.4 | 51.9 | 53.1 | 69.0 | 64.7 | 68.6 | 0.962 | 0.958 | 0.917 | 64.8 | 65.2 | 65.5 |
| 3 | R | 0.240 | 0.244 | 0.244 | 0.226 | 0.231 |  | 0.205 | 0.178 | 0.179 | 65.0 | 65.2 | 67.0 | 64.0 | 67.8 |  | 1.000 | 1.011 |  | 66.4 | 65.2 | 67.1 |
| 4 | R | 0.201 | 0.204 | 0.207 | 0.209 | 0.214 | 0.211 | 0.146 | 0.147 | 0.147 | 61.7 | 64.5 | 66.1 | 55.2 | 57.6 | 58.8 | 0.939 | 1.034 | 0.916 | 63.7 | 64.4 | 65.3 |
| 5 | R | 0.157 | 0.161 | 0.167 | 0.188 | 0.191 | 0.191 | 0.153 | 0.161 | 0.159 | 61.3 | 72.3 | 69.7 | 63.5 | 63.6 | 66.3 | 1.181 | 1.165 | 1.123 | 62.5 | 63.7 | 64.6 |
| 6 | R |  | 0.190 | 0.199 | 0.212 | 0.221 | 0.219 | 0.200 | 0.204 | 0.204 |  | 69.7 | 69.4 | 61.4 | 61.3 | 63.4 |  | 1.217 | 1.168 | 65.2 | 65.3 | 66.2 |
| 7 | R | 0.223 | 0.231 | 0.233 | 0.239 | 0.232 | 0.231 | 0.423 | 0.395 | 0.366 | 66.1 | 68.9 | 70.7 | 69.5 | 68.7 | 68.3 | 1.183 | 1.096 | 1.121 | 58.0 | 58.5 | 59.1 |
| 8 | R | 0.230 | 0.238 | 0.238 | 0.260 | 0.266 | 0.265 | 0.207 | 0.210 | 0.204 | 75.5 | 73.7 | 73.9 | 64.4 | 64.8 | 67.1 | 1.197 | 1.172 | 1.160 | 63.5 | 63.2 | 64.7 |
| 9 | R | 0.231 | 0.230 | 0.232 | 0.232 | 0.233 | 0.235 | 0.338 | 0.321 | 0.304 | 68.8 | 68.8 | 69.9 | 70.0 | 72.6 | 74.4 | 1.010 | 1.033 | 1.016 | 61.6 | 62.3 | 63.0 |
| 10 | R | 0.244 | 0.248 | 0.250 | 0.239 | 0.252 | 0.252 | 0.566 | 0.491 | 0.426 | 65.4 | 65.3 | 65.9 | 64.2 | 66.7 | 65.7 | 0.991 | 1.020 | 1.015 | 65.8 | 65.7 | 65.9 |
| 11 | R | 0.267 | 0.276 | 0.275 | 0.238 | 0.246 | 0.248 | 0.384 | 0.355 | 0.330 | 73.0 | 72.7 | 73.7 | 78.3 | 77.4 | 79.1 | 0.869 | 0.889 | 0.902 | 58.9 | 59.5 | 60.3 |
| 12 | R | 0.239 | 0.247 | 0.246 | 0.223 | 0.234 | 0.233 | 0.323 |  | 0.283 | 66.5 | 63.4 | 63.9 | 62.5 | 59.8 | 57.8 | 0.917 | 0.943 | 0.939 | 59.8 |  | 61.5 |
| 13 | R | 0.227 | 0.229 | 0.226 | 0.219 | 0.222 | 0.222 | 0.490 | 0.475 | 0.441 | 66.0 | 70.3 | 68.7 | 69.7 | 71.1 | 72.5 | 0.961 | 0.964 | 0.978 | 65.3 | 65.3 | 65.4 |
| 14 | R | 0.203 | 0.206 | 0.206 | 0.197 | 0.201 | 0.201 | 0.549 | 0.554 | 0.542 | 71.3 | 70.6 | 73.4 | 70.8 | 73.6 | 74.3 | 0.983 | 0.976 | 0.988 | 62.5 | 62.9 | 62.8 |
| 15 | R | 0.219 | 0.223 | 0.228 | 0.223 | 0.226 | 0.227 | 0.535 | 0.483 | 0.422 | 73.2 | 76.8 | 74.6 | 72.0 | 71.0 | 72.9 | 1.010 | 1.019 | 0.986 | 64.8 | 65.2 | 65.5 |
| 16 | R | 0.247 | 0.255 | 0.257 | 0.257 | 0.262 | 0.260 | 0.406 | 0.402 | 0.396 | 72.4 | 72.0 | 73.4 | 70.3 | 68.7 | 70.9 | 1.031 | 1.020 | 1.022 | 54.5 | 54.8 | 55.7 |
| 17 | R | 0.256 | 0.262 | 0.260 | 0.293 | 0.297 | 0.299 | 0.384 | 0.376 | 0.361 | 67.1 | 68.4 | 69.1 | 58.8 | 60.7 | 62.5 | 1.134 | 1.127 | 1.141 | 51.0 | 52.0 | 53.1 |
| 18 | R | 0.329 | 0.334 | 0.338 | 0.333 | 0.338 | 0.339 | 0.509 | 0.510 | 0.496 | 50.2 | 50.0 | 48.6 | 57.9 | 58.3 |  | 1.014 | 1.013 | 1.009 | 57.6 | 57.0 |  |
| 19 | R | 0.224 | 0.229 | 0.228 | 0.229 | 0.236 | 0.235 | 0.688 | 0.701 | 0.682 | 72.1 | 74.4 | 75.9 | 75.1 | 71.7 | 73.1 | 1.005 | 1.022 | 1.014 | 63.8 |  |  |
| 20 | R | 0.250 | 0.254 | 0.253 | 0.248 | 0.253 | 0.251 | 0.565 | 0.562 | 0.528 | 70.4 | 68.1 | 72.2 | 68.2 | 68.4 | 70.0 | 0.987 | 0.990 | 0.976 | 64.2 | 63.9 |  |
| 21 | R | 0.233 | 0.239 | 0.240 | 0.235 | 0.241 | 0.239 | 0.560 | 0.560 | 0.533 | 76.9 | 75.8 | 77.6 | 75.0 | 77.2 | 78.6 | 1.000 | 1.000 | 0.987 | 60.0 | 60.2 |  |
| 22 | R | 0.232 | 0.235 | 0.235 | 0.245 | 0.246 | 0.244 | 0.722 | 0.723 | 0.702 | 75.6 | 77.5 | 74.9 | 70.6 | 73.0 | 73.9 | 1.057 | 1.039 | 1.032 |  | 60.2 |  |
| 23 | R | 0.199 | 0.202 | 0.205 | 0.212 | 0.216 | 0.216 | 0.537 | 0.545 | 0.537 | 71.4 | 72.4 | 72.2 | 66.1 | 70.0 | 71.6 | 1.055 | 1.057 | 1.042 | 61.9 | 61.5 | 61.7 |
| 24 | R | 0.235 | 0.235 | 0.239 | 0.231 | 0.238 | 0.235 | 0.392 | 0.390 | 0.376 | 74.6 | 78.2 | 76.0 | 77.3 | 78.1 | 77.1 | 0.972 | 1.011 | 0.990 | 58.0 | 57.9 | 58.4 |
| 25 | R | 0.227 | 0.233 | 0.232 | 0.263 | 0.267 | 0.265 | 0.464 | 0.467 | 0.454 | 74.5 | 75.9 | 74.6 | 64.9 | 64.8 | 66.5 | 1.172 | 1.155 | 1.154 | 56.7 | 57.0 | 57.1 |
| 26 | R | 0.207 | 0.213 | 0.211 | 0.217 | 0.221 | 0.219 | 0.585 | 0.588 | 0.576 | 76.8 | 77.8 | 77.9 | 69.4 | 70.4 | 70.8 | 1.059 | 1.039 | 1.038 | 57.6 |  |  |
| 27 | R | 0.205 | 0.207 | 0.208 | 0.210 | 0.216 | 0.213 | 0.615 | 0.619 | 0.620 | 72.3 | 72.1 | 74.6 | 71.3 | 73.1 | 74.1 | 1.022 | 1.036 | 1.015 | 58.7 |  | 58.3 |
| 28 | S | 0.260 | 0.264 | 0.260 | 0.233 | 0.243 | 0.241 | 0.503 | 0.502 | 0.473 | 67.8 | 74.1 | 69.7 | 73.3 | 71.8 | 72.7 | 0.890 | 0.907 | 0.919 | 60.3 | 60.1 |  |
| 29 | S | 0.225 | 0.225 | 0.229 | 0.224 | 0.228 | 0.229 | 0.443 | 0.425 | 0.397 | 78.2 | 77.6 | 77.0 | 81.2 | 77.7 | 76.7 | 1.000 | 1.007 | 0.986 | 60.2 | 60.4 |  |
| 30 | S | 0.234 | 0.239 | 0.236 | 0.232 | 0.240 | 0.243 | 0.436 | 0.428 | 0.404 | 67.3 | 73.9 | 75.0 | 69.2 | 72.0 | 70.4 | 1.000 | 1.007 | 1.024 |  | 58.0 | 58.5 |
| 31 | S | 0.211 | 0.217 | 0.218 | 0.219 | 0.221 | 0.225 | 0.619 | 0.617 | 0.603 | 75.8 | 71.8 | 72.0 | 74.7 | 69.6 | 67.7 | 1.042 | 1.004 | 1.034 | 62.8 | 63.0 |  |
| 32 | S | 0.233 | 0.232 | 0.231 | 0.200 | 0.207 | 0.206 | 0.412 | 0.411 | 0.409 | 73.0 | 69.3 | 69.3 | 74.7 | 76.4 | 76.8 | 0.863 | 0.893 | 0.888 | 54.4 | 55.7 |  |
| 33 | R | 0.225 | 0.227 | 0.231 | 0.223 | 0.227 | 0.227 | 0.624 | 0.623 | 0.608 |  | 74.8 | 73.0 | 71.1 | 74.7 | 75.8 | 1.015 | 0.996 | 0.984 | 61.3 | 49.8 | 50.4 |

Normalized Strain and Mid-Slab Spreadability at Sensor Locations (1st and 2nd Drop) (1 μm/kN = 0.175 mil/kip).

| Drop | Date | Normalized Deflection | Spreadability |
| --- | --- | --- | --- |
|  |  | ((m/kN) | (%) |
|  |  | A | B | C | D | I | J | K | L | T | U | V | W | K | T | V |
| Drop 1 | Section 1: Cracked & Seated |
|  | Jun-2006 | 1.760 | 1.671 | 1.418 | 1.458 | 1.600 | 1.550 | 1.443 | 1.574 | 1.486 | 1.597 | 1.660 | 1.696 | 55.3 | 58.4 | 55.1 |
|  | Nov-2006 |  |  | 1.350 | 1.326 |  | 1.437 | 2.332 | 3.591 | 1.427 | 1.432 | 1.414 | 1.609 | 42.8 | 63.7 | 72.5 |
|  | Mar-2007 |  |  | 2.297 | 2.021 |  | 1.878 | 3.424 | 2.005 | 3.751 | 1.920 | 4.378 | 2.416 | 72.3 | 72.2 | 76.7 |
|  | Oct-2007 |  |  | 2.018 | 1.432 |  | 1.442 | 2.703 | 1.497 | 2.746 | 1.660 | 3.278 | 1.863 | 66.4 | 68.2 | 67.4 |
|  | May-2008 |  |  |  | 1.539 |  | 1.634 | 2.994 | 1.618 | 2.605 | 1.547 | 3.029 | 1.961 | 64.1 | 69.1 | 70.6 |
|  | Oct-2008 |  |  | 1.164 | 1.430 |  | 1.555 | 1.148 | 2.158 | 1.214 | 1.842 | 1.480 | 2.528 | 72.8 | 69.1 | 71.1 |
|  | May-2009 |  |  | 1.207 | 1.530 |  | 1.650 | 1.607 | 1.820 |  |  |  |  | 57.9 |  |  |
|  | Section 2: Rubblized |
|  | Jun-2006 | 1.976 | 2.195 | 1.937 | 1.826 | 2.421 | 1.890 | 1.820 | 1.893 | 1.780 | 1.691 | 1.817 | 1.922 | 54.6 | 55.5 | 52.8 |
|  | Nov-2006 |  |  | 1.368 | 1.218 |  | 1.352 | 1.301 | 1.304 | 1.305 | 1.173 | 1.267 | 1.298 | 61.1 | 59.2 | 60.4 |
|  | Mar-2007 |  |  | 2.484 | 1.750 |  | 1.504 | 1.970 | 1.335 | 2.628 | 1.461 | 1.860 | 1.764 | 66.9 | 64.0 | 61.4 |
|  | Oct-2007 |  |  | 1.770 | 1.439 |  | 1.383 | 2.123 | 1.212 | 2.248 | 1.231 | 1.852 | 1.320 | 66.0 | 62.4 | 62.7 |
|  | May-2008 |  |  |  | 1.600 |  | 1.489 | 2.204 | 1.599 | 2.372 | 1.399 | 2.387 | 1.548 | 66.3 | 69.3 | 67.1 |
|  | Oct-2008 |  |  | 1.546 | 1.895 |  | 1.978 | 1.024 | 1.948 | 1.087 | 1.754 | 1.093 | 1.810 |  |  |  |
|  | May-2009 |  |  | 1.882 |  |  | 1.547 | 2.131 | 1.535 |  |  |  |  | 66.0 |  |  |
|  | Section 3: Untreated |
|  | Jun-2006 | 1.373 | 1.333 | 1.223 | 1.164 | 1.478 | 1.219 | 1.235 | 1.240 | 1.142 | 1.106 | 1.168 | 1.141 | 59.5 | 57.5 | 55.3 |
|  | Nov-2006 |  |  | 1.384 | 1.085 |  | 1.148 |  | 1.075 | 1.396 | 1.046 | 2.366 | 1.372 |  | 50.8 | 34.7 |
|  | Mar-2007 |  |  | 1.444 | 2.045 |  | 1.339 | 3.147 | 1.460 | 1.691 | 1.324 | 2.092 | 1.411 | 59.0 | 63.8 | 65.6 |
|  | Oct-2007 |  |  | 1.194 | 1.888 |  | 1.274 | 1.228 | 1.238 | 1.146 | 1.200 | 1.152 | 1.368 | 67.3 | 70.7 | 69.1 |
|  | May-2008 |  |  |  | 1.630 |  | 1.344 | 3.134 | 1.652 | 3.191 | 1.426 | 3.333 | 1.570 | 67.4 | 71.1 | 69.4 |
|  | Oct-2008 |  |  | 1.644 | 2.175 |  | 2.212 | 1.259 | 2.581 | 1.446 | 2.446 | 1.409 | 2.677 | 75.9 | 75.6 | 72.7 |
|  | May-2009 |  |  | 1.466 | 1.462 |  | 1.498 | 1.747 | 1.468 |  |  |  |  | 65.7 |  |  |
| Drop 2 | Section 1: Cracked & Seated |
|  | Jun-2006 | 1.762 | 1.740 | 1.399 | 1.509 | 1.650 | 1.536 | 1.461 | 1.643 | 1.509 | 1.565 | 1.707 | 1.777 | 58.8 | 55.7 | 55.7 |
|  | Nov-2006 |  |  | 1.212 | 1.465 |  | 1.263 | 2.240 | 2.783 | 1.300 | 1.270 | 1.320 | 1.648 | 45.4 | 71.5 | 79.9 |
|  | Mar-2007 |  |  | 2.371 | 2.095 |  | 1.962 | 3.538 | 2.072 | 3.799 | 1.975 | 4.490 | 2.495 | 72.1 | 72.3 | 76.9 |
|  | Oct-2007 |  |  | 2.043 | 1.486 |  | 1.486 | 2.759 | 1.527 | 2.732 | 1.721 | 3.284 | 1.855 | 66.3 | 69.0 | 67.9 |
|  | May-2008 |  |  |  | 1.544 |  | 1.679 | 2.958 | 1.657 | 2.583 | 1.563 | 3.011 | 1.899 | 64.3 | 69.1 | 71.4 |
|  | Oct-2008 |  |  | 1.195 | 1.505 |  | 1.579 | 1.205 | 2.197 | 1.235 | 1.845 | 1.511 | 2.525 | 71.5 | 70.9 | 72.1 |
|  | May-2009 |  |  | 1.237 | 1.580 |  | 1.666 | 1.585 | 1.878 |  |  |  |  | 60.0 |  |  |
|  | Section 2: Rubblized |
|  | Jun-2006 | 2.043 | 2.280 | 2.001 | 1.837 | 2.508 | 1.979 | 1.834 | 1.903 | 1.820 | 1.735 | 1.852 | 1.921 | 57.1 | 57.4 | 54.6 |
|  | Nov-2006 |  |  | 1.443 | 1.276 |  | 1.444 | 1.336 | 1.377 | 1.327 | 1.230 | 1.295 | 1.366 | 62.1 | 60.2 | 60.2 |
|  | Mar-2007 |  |  | 2.540 | 1.835 |  | 1.668 | 2.040 | 1.404 | 2.690 | 1.525 | 1.940 | 1.797 | 66.9 | 63.8 | 60.8 |
|  | Oct-2007 |  |  | 1.803 | 1.457 |  | 1.462 | 2.152 | 1.257 | 2.230 | 1.232 | 1.859 | 1.378 | 66.6 | 63.9 | 63.4 |
|  | May-2008 |  |  |  | 1.608 |  | 1.494 | 2.215 | 1.659 | 2.467 | 1.449 | 2.396 | 1.550 | 66.8 | 68.4 | 67.8 |
|  | Oct-2008 |  |  | 1.552 | 1.930 |  | 2.007 | 1.066 | 1.990 | 1.104 | 1.812 | 1.124 | 1.861 | 64.9 | 62.6 | 62.9 |
|  | May-2009 |  |  | 1.919 |  |  | 1.526 | 2.148 | 1.552 |  |  |  |  | 65.7 |  |  |
|  | Section 3: Untreated |
|  | Jun-2006 | 1.433 | 1.422 | 1.213 | 1.208 | 1.460 | 1.303 | 1.217 | 1.246 | 1.150 | 1.098 | 1.222 | 1.132 | 56.3 | 57.8 | 53.6 |
|  | Nov-2006 |  |  | 1.289 | 1.228 |  | 1.163 |  | 1.387 | 1.497 | 1.131 | 1.828 | 1.395 |  | 50.1 | 43.7 |
|  | Mar-2007 |  |  | 1.474 | 1.983 |  | 1.359 | 3.027 | 1.528 | 1.737 | 1.346 | 2.095 | 1.430 | 60.7 | 64.2 | 66.1 |
|  | Oct-2007 |  |  | 1.257 | 1.964 |  | 1.324 | 1.242 | 1.314 | 1.256 | 1.244 | 1.232 | 1.350 | 69.1 | 69.0 | 68.4 |
|  | May-2008 |  |  |  | 1.606 |  | 1.502 | 3.056 | 1.662 | 3.076 | 1.404 | 3.299 | 1.554 | 70.0 | 71.2 | 69.9 |
|  | Oct-2008 |  |  | 1.609 | 2.188 |  | 2.242 | 1.317 | 2.563 | 1.475 | 2.430 | 1.392 | 2.649 | 74.6 | 74.8 | 72.6 |
|  | May-2009 |  |  | 1.480 | 1.486 |  | 1.495 | 1.761 | 1.492 |  |  |  |  | 65.3 |  |  |

Appendix I:  Supplemental FWD Response Data from I90, Weedsport

FWD Test Results – PCC Pavement

D0 at joints – Left lane (5.714µm/kN = 1 mil/kip)

D0 at joints – Right lane (5.714µm/kN = 1 mil/kip)

D60 at mid-slab – Left lane (5.714µm/kN = 1 mil/kip)

D60 at mid-slab – Right lane (5.714µm/kN = 1 mil/kip)

D0 at mid-slab – Left lane (5.714µm/kN = 1 mil/kip)

D0 at mid-slab – Right lane (5.714µm/kN = 1 mil/kip)

Spreadability – Left lane

Spreadability – Right lane

AREA72 – Left lane (2.54cm = 1 in)

AREA72 – Right lane (2.54cm = 1 in)

Subgrade k-value – Left lane (1MPa/m = 3.70 lb/in3)

Subgrade k-value – Right lane (1MPa/m = 3.70 lb/in3)

LTE approach position – Left lane

LTE approach position – Right lane

JSR – Left lane

JSR – Right lane

# Text boxes

DRAFT

358 mm

14.1 in

430 mm

16.9 in

538 mm

21.2 in

717 mm

28.2 in

1075 mm

42.3 in

350 mm

=13.8 in

5.0 m

16.4 ft

5.0 m

16.4 ft

5.0 m

16.4 ft

5.0 m

16.4 ft

5.0 m

16.4 ft

3.6 m

11.8 ft

3.6 m

11.8 ft

3.6 m

11.8 ft

0.6 m

2.0 ft

2.4 m

7.9 ft

4.2 m

13.8 ft

1.8 m

5.9 ft

3.6 m

11.8 ft

5.0 m

16.4 ft

Project Location

Test Section Location

Failure Surface

CTPB Base

PCC Slab